Supporting Information

Delay Tumor Growth Properties of LA-PEG-G Molecule and Its' Application as Drug Carrier

Guangcheng Wei*,†, Meixiu Xin†, Hao Wang, Yehong Huo, Wei Hu, Jigang Jiang, Lei Wang, Liying Ma, Miaomiao Yan, Chunhua Wang*

Department of Pharmacy Science, Binzhou Medical University, Yantai, 264003, China

† These authors are equal to the contribution of this work.

*Correspondence authors E-mail: weiguangcheng2004@126.com;      chhuawang2018@126.com

Contents

- Synthesis and Characterization of LA-PEG-G molecules

1.1 Thin layer chromatography

1.2 FT-IR spectrum of LA-PEG-G molecules

1.3 NMR spectrum of LA-PEG-G molecules

1.4 MS spectrum of LA-PEG-G molecules

- CAC determination of LA-PEG-G aggregates

- Cell uptake assay with flow cytrometry

- Tissue Sections

- Synthesis and Characterization of LA-PEG-G molecules

1.1 Thin layer chromatography

Figure S1 Thin layer chromatography of LA-PEG-G, LA, NHS, DCC and PEG molecules.

1.2 FT-IR spectrum of LA-PEG-G molecules

Figure S2  The FT-IR spectrum of LA-PEG-Gmolecule

1.3 NMR spectrum of LA-PEG-G molecules

Figure S3  1HNMR spectra of LA-PEG-G molecule

1H NMR (500 MHz, MeOD).  δ 8.56 (s, 1H, -C=C-CO-NH-), 7.81 (s, 1H, -CO-NH-), 5.58 – 4.40 (m, 4H, -COO-CH2-, -O-CH-N-),  4.900 (q, 2H, -N=C-NH2), 3.805-3.770 (m, 4H,-O-CH2-CH2-), 3.63 (m, 6H,-CH2-CH=CH-CH2-CH=CH-CH2-), 3.37-3.334 (m, 4H,CH3-CH2-CH2-), 1.199(t, 2H, =CH-CH2-C=).

MALDI-TOF MS (m/z): 964.36 ([M+HCOOH-H]-).

1.4 MS spectrum of LA-PEG-G molecules

Figure S4 MS spectrum of LA-PEG-G molecule

2. CMC determination of LA-PEG-G molecules

Figure S5  CMC determination of LA-PEG-G molecules in aqueous solution

3. Cell uptake assay with flow cytrometry

Figure S6  Cell uptake assay with the flow cytrometry. (a) 10μg·mL-1LA-PEG-G-Dox nanomedicine was incubated with HepG2 cell for 2h; (b) 10μg·mL-1LA-PEG-G-Dox nanomedicine was incubated with HepG2 cell for 8h;(c) 10μg·mL-1LA-PEG-G-Dox nanomedicine was incubated with HepG2 cell for 24h; (d)20μg·mL-1LA-PEG-G-Dox nanomedicine was incubated with HepG2 cell for 2h; (e)20μg·mL-1LA-PEG-G-Dox nanomedicine was incubated with HepG2 cell for 8h; (f)20μg·mL-1LA-PEG-G-Dox nanomedicine was incubated with HepG2 cell for 24h; (g) Control group.

4. Tissue sections

|  | PBS | Dox | LA-PEG-G aggregate | LA-PEG-G-Dox nanomedicine |
| --- | --- | --- | --- | --- |
| Heart |  |  |  |  |
| Liver |  |  |  |  |
| Spleen |  |  |  |  |
| Lung |  |  |  |  |
| Kidney |  |  |  |  |

Figure S7 Tissue section of heart, liver, spleen and lung tissue after 19 days of injection of PBS, Dox, LA-PEG-G aggregates and LA-PEG-G-DOX nanomedicine.