SUPPLEMENTAL FIGURE 1. Experimental surgery. Iconography of the procedure used for the introduction of cylindrical constructs in athymic mice. A) Preparation of surgical area; B) incision between scapulae to create a pouch in which the construct will be inserted; C) preparation of constructs using a syringe as a template; D) subdermal administration of cylindrical constructs; E) closure of the wound with surgical staples and return to cages.

SUPPLEMENTAL FIGURE 2. Necropsy. Highlights of major findings in the complete, systematic and ordered necropsy performed to all animals of the in vivo study. Briefly, unspecific findings were seen in animals from the three experimental groups, irrespective of treatment. A small and local whitish area was detected in the dorsal part of the spleen of animal ID 4 (A) and increased mesenteric lymph nodes were observed in animal 12 (B). At the same time, increased axillary lymph nodes were found in animal ID 17 (C). These findings were not considered to have pathologic relevance and were not related to the treatments.

SUPPLEMENTAL FIGURE 3. Aspect of constructs at week 5 post-implantation. Images taken from one of the 6 animals included in each group at week 5 post-implantation of the tissue engineering products (arrows), either acellular (control), or loaded with MNC (fragmented in three pieces) or BM-MSC.

SUPPLEMENTAL TABLES

SUPPLEMENTAL TABLE 1. Histological grading score. Parameters related to bone formation were assessed under 5 different categories.

| Bone formation | SCORE |
| --- | --- |
| Obvious bone remodelling activity Some degree of bone remodelling Vascularisation Fibrosis | 3 2 1 0 |
| Tissue reaction | SCORE |
| No reaction Low fibrous reaction Intermediate fibrous reaction High fibrous reaction | 3 2 1 0 |
| Inflammatory reaction | SCORE |
| No infiltration Low (1-3 cell layers around bone particles) Intermediate (4-6 cell layers around bone particles) High (>6 cell layers around bone particles) | 3 2 1 0 |
| Inflammatory cell type | SCORE |
| Histiocytes/fibroblasts Lymphocytes Macrophages Polymorphonuclear | 3 2 1 0 |
| Vascularisation around bone particles | SCORE |
| High (>15 vases) Intermediate (5-15 vases) Low (1-5 vases) No vascularisation | 3 2 1 0 |