Characterization of Heparinized Chitosan and Hydrogel-DBM composite

Heparin conjugation was analyzed by 1H nuclear magnetic resonance spectroscopy (NMR) in D2O (Bruker ARX400 spectrometer). It was quantified by the integration of the peaks at 2.7 - 3.2 ppm (CHNHSO3-, CHOSO3-, CH2OSO3-) and compared with methacrylate peak at 5.6 - 6.1 ppm. The degree of heparin substitution was reported as 6.76%. Heparinized chitosan was also characterized by fourier transform infrared spectrophotometer (FTIR, Jasco 420) to verify the heparin conjugation. The incorporation of heparin over time was examined by toluidine blue (Sigma-Aldrich, MO) staining that the hydrogels were stained with 1% (w/v) toluidine blue in PBS and washed with PBS for 1 h.

Mechanical properties of composites were measured by compressive modulus and water content. The compressive modulus was evaluated by 1.6 mm diameter flat-ended indentation test via Instron Electro- Mechanical Testing Machines (Instron, Model 5564, Norwood, MA) using a Poisson’s ratio of 0.25[26, 43]. Water content was calculated by the following equation where Wwet and Wdry referred wet and dry weight of hydrogels respectively.

Water content %= Wwet-WdryWwet × 100