# A fast and simple protocol for synthesizing effective antimicrobial silver nanoparticles in non-specialized facilities

Supplementary material

# Notes on the AgNPs synthesis protocol.

For the proposed synthesis, the stock solutions were prepared using Milli-Q water, although distilled water can be used too. Yet, it will impact the quality of the synthesized AgNPs. Still, the AgNPs will exhibit antimicrobial activity.

We selected the PVP K-10 and the NaBH4 for the synthesis protocols. PVP is widely used in medical products and cosmetics. When used for nanoparticle synthesis, PVP grants stability (1), biocompatibility (2,3), and also acts as a dispersant (4). PVP coating confers a negative surface charge to the AgNPs and has no antimicrobial properties by itself. The charge influences the AgNPs – cell interaction (5,6). Also, the capping influences the AgNPs antimicrobial properties (7). PVP comes in different sizes, and the size and concentration of this polymer influences in the AgNPs overall size and shape, for the purposes of this work we selected the PVP K-10, which was the smallest available (M.W.=10,000 Daltons). Sodium borohydride (NaBH4) is a good reducing agent, relatively inexpensive and easily handled. NaBH4 rapidly reduces the silver ion to zero-valent silver, leading to a formation of nanostructures under the proper conditions. Yet, it loses its activity fast when diluted in water, thus it has been used as soon after it is prepared. Moreover, NaBH4 has no inhibitory activity against the microbial cells at the tested concentrations.

# Antimicrobial activity of AgNPs in the literature.

The antimicrobial activity of our synthesized PVP-AgNPs is comparable to other reported in different studies, using similar culture conditions. MIC values in the literature range from 0.8 µg mL-1 to 13.5 µg mL-1 for S. aureus (Table S1), and from 0.4 µg mL-1 to 40 µg mL-1 for C. albicans (Table S2).

| Table S1. AgNPs antimicrobial activity vs S. aureus |  |  |
| --- | --- | --- |
| AgNPs characteristics | MIC (µg ml-1) | Ref. |
| 6.18 ± 5 nm, spheroids. Stabilizer: PVP | 3 | This work |
| 13 ±3 nm, Polyhedral. Stabilizer: Tannic acid | 1.56 | (8) |
| 16-25 nm, shape not mentioned. Stabilizer: N/A | 0.8 | (9) |
| 20 nm, spherical, biosynthesis | 20 | (10) |
| 20 nm, ellipsoid. Stabilizer: PVP 7 nm, ellipsoid. Stabilizer: PEG | 10.1 13.5 | (11) |
| 1 nm, Spheroids, Uncapped | 12.5 | (12) |
| 9 nm, shape not mentioned. Stabilizer: PVA. | 1.95 | (13) |
| 8.6 nm, poly-shaped. Stabilizer: N-Cholyl L-Valine. | 3.5 | (14) |
| 18.34 nm, spheroids & polyhedrons. Stabilizer: N/A | 2 | (15) |
| 5-10 nm, shape not mentioned. Stabilizer: N/A. From Nanoparticle Biochem, Inc. | 12.5 | (16) |
| Culture conditions are based on the CLSI’s A07 protocols for S. aureus: 106 cells mL-1, Mueller Hinton broth, 24 h at 37 oC. |  |  |

| Table S2. AgNPs antimicrobial activity vs. C. albicans |  |  |
| --- | --- | --- |
| AgNPs characteristics | MIC (µg mL-1) | Ref. |
| 6.18 ± 5 nm, spheroids. Stabilizer: PVP | 1.5 | This work |
| 5 nm, shape polyhedron-like. Stabilizer: NH3. 5 nm, shape polyhedron-like. Stabilizer: PVP | 0.4 0.8 | (17) |
| 8.6 nm, poly-shaped. Stabilizer: N-Cholyl amino acids. | 1.75 | (14) |
| 21.6 nm, spherical. Stabilizer: N/A | 40 | (18) |
| Culture conditions are based on the CLSI’s M27 protocol for C. albicans, 103 cells mL-1, RPMI media, and 48 h, at 35 oC. |  |  |

# References

1. 	Tejamaya M, Römer I, Merrifield RC, Lead JR. Stability of citrate, PVP, and PEG coated silver nanoparticles in ecotoxicology media. Environ Sci Technol. 2012;46(13):7011–7.

2. 	Lyutakov O, Kalachyova Y, Solovyev A, Vytykacova S, Svanda J, Siegel J, et al. One-step preparation of antimicrobial silver nanoparticles in polymer matrix. J Nanoparticle Res [Internet]. 2015 Mar 6 [cited 2019 Jul 12];17(3):120. Available from: http://link.springer.com/10.1007/s11051-015-2935-3

3. 	Rogero SO, Malmonge SM, Lugão AB, Ikeda TI, Miyamaru L, Cruz ÁS. Biocompatibility Study of Polymeric Biomaterials. Artif Organs [Internet]. 2003 May 9 [cited 2019 Jul 12];27(5):424–7. Available from: http://doi.wiley.com/10.1046/j.1525-1594.2003.07249.x

4. 	Koczkur KM, Mourdikoudis S, Polavarapu L, Skrabalak SE. Polyvinylpyrrolidone (PVP) in nanoparticle synthesis. Dalt Trans [Internet]. 2015 Oct 13 [cited 2019 Jul 15];44(41):17883–905. Available from: http://xlink.rsc.org/?DOI=C5DT02964C

5. 	Abbaszadegan A, Ghahramani Y, Gholami A, Hemmateenejad B, Dorostkar S, Nabavizadeh M, et al. The Effect of Charge at the Surface of Silver Nanoparticles on Antimicrobial Activity against Gram-Positive and Gram-Negative Bacteria: A Preliminary Study. 2015 [cited 2019 Jul 15]; Available from: http://dx.doi.org/10.1155/2015/720654

6. 	El Badawy AM, Silva RG, Morris B, Scheckel KG, Suidan MT, Tolaymat TM. Surface Charge-Dependent Toxicity of Silver Nanoparticles. Environ Sci Technol [Internet]. 2011 Jan [cited 2019 Jul 15];45(1):283–7. Available from: https://pubs.acs.org/doi/10.1021/es1034188

7. 	Gnanadhas DP, Ben Thomas M, Thomas R, Raichur AM, Chakravortty D. Interaction of silver nanoparticles with serum proteins affects their antimicrobial activity in vivo. Antimicrob Agents Chemother [Internet]. 2013 Oct 1 [cited 2019 Mar 6];57(10):4945–55. Available from: http://www.ncbi.nlm.nih.gov/pubmed/23877702

8. 	Orlowski P, Zmigrodzka M, Tomaszewska E, Ranoszek-Soliwoda K, Czupryn M, Antos-Bielska M, et al. Tannic acid-modified silver nanoparticles for wound healing: the importance of size. Int J Nanomedicine [Internet]. 2018 [cited 2019 Apr 6];13:991–1007. Available from: http://www.ncbi.nlm.nih.gov/pubmed/29497293

9. 	Esmaeillou M, Zarrini G, Ahangarzadeh Rezaee M, Shahbazi Mojarrad J, Bahadori A. Vancomycin Capped with Silver Nanoparticles as an Antibacterial Agent against Multi-Drug Resistance Bacteria. Adv Pharm Bull [Internet]. 2017 Sep [cited 2019 Apr 6];7(3):479–83. Available from: http://www.ncbi.nlm.nih.gov/pubmed/29071232

10. 	Hoskote Anand KK, Mandal BK. Activity study of biogenic spherical silver nanoparticles towards microbes and oxidants. Spectrochim Acta - Part A Mol Biomol Spectrosc [Internet]. 2015;135:639–45. Available from: http://dx.doi.org/10.1016/j.saa.2014.07.013

11. 	Suchomel P, Kvitek L, Panacek A, Prucek R, Hrbac J, Vecerova R, et al. Comparative Study of Antimicrobial Activity of AgBr and Ag Nanoparticles (NPs). PLoS One. 2015;10(3):1–16.

12. 	Romero-Urbina DG, Lara HH, Velázquez-Salazar JJ, Arellano-Jiménez MJ, Larios E, Srinivasan A, et al. Ultrastructural changes in methicillin-resistant Staphylococcus aureus induced by positively charged silver nanoparticles. Beilstein J Nanotechnol [Internet]. 2015 [cited 2019 Apr 17];6:2396–405. Available from: http://www.ncbi.nlm.nih.gov/pubmed/26734530

13. 	Wady AF, Machado AL, Foggi CC, Zamperini CA, Zucolotto V, Moffa EB, et al. Effect of a Silver Nanoparticles Solution on Staphylococcus aureus and Candida spp. J Nanomater [Internet]. 2014 Aug 20 [cited 2019 Apr 17];2014:1–7. Available from: http://www.hindawi.com/journals/jnm/2014/545279/

14. 	Annadhasan M, SankarBabu VR, Naresh R, Umamaheswari K, Rajendiran N. A sunlight-induced rapid synthesis of silver nanoparticles using sodium salt of N-cholyl amino acids and its antimicrobial applications. Colloids Surfaces B Biointerfaces [Internet]. 2012 Aug 1 [cited 2019 Apr 6];96:14–21. Available from: https://www.sciencedirect.com/science/article/pii/S0927776512001798

15. 	Mirzajani F, Ghassempour A, Aliahmadi A, Esmaeili MA. Antibacterial effect of silver nanoparticles on Staphylococcus aureus. Res Microbiol [Internet]. 2011 Jun 1 [cited 2018 May 18];162(5):542–9. Available from: https://www.sciencedirect.com/science/article/pii/S0923250811000829?via%3Dihub

16. 	Ma A, Hm K, Aa K, Malik A, Sultan A, Shahid M, et al. Evaluation of antibacterial activity of silver nanoparticles against MSSA and MRSA on isolates from skin infections. Res Artic Biol Med. 2011;3(2):141–6.

17. 	Monteiro DR, Silva S, Negri M, Gorup LF, De Camargo ER, Oliveira R, et al. Silver nanoparticles: Influence of stabilizing agent and diameter on antifungal activity against Candida albicans and Candida glabrata biofilms. Lett Appl Microbiol. 2012;54(5):383–91.

18. 	Radhakrishnan VS, Dwivedi SP, Siddiqui MH, Prasad T. In vitro studies on oxidative stress-independent, Ag nanoparticles-induced cell toxicity of Candida albicans, an opportunistic pathogen. Int J Nanomedicine [Internet]. 2018 [cited 2019 May 6];13(T-NANO 2014 Abstracts):91–6. Available from: http://www.ncbi.nlm.nih.gov/pubmed/29593404