Table 1

Physicochemical properties of CeO2 NPs

| Physicochemical properties |  | CeO2 NPs |  |
| --- | --- | --- | --- |
| Primary shape (TEM image) |  |  |  |
| Primary size |  | 14.2 ± 5.03 nm |  |
| Purity |  | 100% |  |
| Hydrodynamic size |  | 76.3 nm |  |
| Zeta potential |  | 47.37 mV |  |