Supplementary material

Probing the beam-induced heating effect inside a transmission electron microscope by nanoparticle labels

Lei Zhang 1, Longbing He 1, 2*, Yufeng Yang 1, Hua Hong 1, Luping Tang 1, and Litao Sun 1, 2*

1. SEU-FEI Nano-Pico Center, Key Lab of MEMS of MoE, Southeast University, Nanjing 210096, P. R. China

2. Southeast University-Monash University Joint Research Institute, Suzhou 215123, P. R. China

Calibration on the decomposition temperature of Ag3N nanoparticles

The temperatures at which Ag3N nanoparticles decomposed were calibrated using an electrical chip (E-chip) with a heating holder (Protochips AduroTM). The E-chip contained hole-arrays as observation windows, and holey carbon films were overlaid on the windows to support the nano-specimens. By controlling the applied current, the heating temperature of the E-chip can be precisely programmed. As the nominal ramp rate of the E-chip is 1000 K/ms, the retardation of the temperature increase during heating can thus be neglected.

Figs.S1a-e show the sequence of Ag3N decomposition by in-situ heating when the temperature is increased to 380K. In order to double check the accuracy of the heating e-chip, Bi nanoparticles (Fig.S2) are used to make a comparison as our group has a lot of experience on dealing with material sublimation [1, 2]. It is important to note that Bi nanoparticles located on the g-C3N4 film or holey carbon film as well as Ag3N nanoparticles located on holey carbon film can remain well unchanged under the same irradiation condition described in paper. By heating up the e-chip to 515K, sublimation of Bi nanoparticles is achieved (Figs. S1f-i) and the manner is in good consistent with the expected analytic calculation as following.

Fig. S1 (a)-(e) Decomposition of Ag3N nanoparticles; (f)-(i) Sublimation of Bi nanoparticles. (scale bar: 10nm)

Fig. S2 HRTEM of bismuth nanoparticles. The two lattice planes (0 1 2) and (1 0 4) have an interplanar distance of 3.28nm and 2.37nm, respectively (scale bar: 5nm)

The sublimation process of particle at nanoscale is supposed to follow the Kelvin’s law with an exponential form written as:

where Pr is the equilibrium vapor pressure over the curved surface, is the surface energy (490mJ/m2 for Bi), Mr is the molecular weight, r is the curvature radius, T is the thermodynamic temperature,  is the density, R is the gas constant and P∞ is the equilibrium vapor pressure over a flat surface which, for a bulk bismuth, follow the established vapor pressure equation

where A, B, C, D and E are the fitting constants. With a certain temperature, the equilibrium vapor pressure over a flat surface is a constant. The increase of the vapor pressure over the curved surface will lead to more atoms breaking away from the curved particle surface to the background and accelerate the sublimation rate.

Taking a perfect and unsupported spherical particle with a radius rp into consideration, its sublimation volume per second dV/dt and the number of atoms lost from the particle per second dN/dt can be calculated, respectively, through kinetic theory as

where N is the number of sublimated atoms, Va is the molecular volume of Bi crystal,  is the mean speed of the vapor atoms which can be calculated by , ninside and noutside is the number of vapor atoms per unit of volume inside and outside the particle surface area S, respectively. Assuming the vapor behaves as a monatomic perfect gas, the vapor pressures can be expressed as  and. The k is the Boltzmann constant. Through combining these equations, the change rate of particle radius drp/dt can be finally calculated by:

Fig.S3 shows the calculated sublimation rate with the temperature for Bi nanoparticles having radius of 2nm, 5nm, 10nm, 20nm and 50nm. The sublimation process is size-dependent and under a certain temperature, the smaller the particle radius is, the easier or faster it sublimates. In the experiment, Bi nanoparticle is not perfectly spherical whose curvature all over the particle surface is different and this gives rise to the anisotropic volume reduction. Furthermore, there are also several defects on the particle and under a tiny thermal disturbance, these defects may break. The curvature of the breaking area is very small and this is the reason why the sublimation of Bi particle always starts at its frail part. It is difficult to exactly characterize the actual decrease rate as the multi-direction sublimation happens, but the experimental result that a particle having a radius of around 10nm disappears within 70s (the red marked particle in Fig.S1) is apparently in agreement with the theoretical predictions where the sublimation rate is around 0.2nm/s at 515K. Hence, the temperature from the heating e-chip is credible. Ag3N nanoparticles decompose at 380K and an obvious sublimation of prepared bismuth nanoparticle happens at a temperature around 515K.

Fig. S3 Calculated sublimation rates of Bi nanoparticle with radius of 2nm, 5nm, 10nm, 20nm and 50nm under various temperatures.

References

[1] Lian R, Yu H, He L, Zhang L, Zhou Y, Bu X, Xu T, Sun, L (2016) Sublimation of Ag nanocrystals and their wetting behaviors with graphene and carbon nanotubes. Carbon 101:368-376

[2] He LB, Zhang L, Tan XD, Tang LP, Xu T, Zhou YL, Ren ZY, Wang Y, Teng CY, Sun LT, Nie JF (2017) Surface Energy and Surface Stability of Ag Nanocrystals at Elevated Temperatures and Their Dominance in Sublimation-Induced Shape Evolution. small 13:1700743.