Supplementary Information

Bioinspired Lotus Fiber-Based Graphene Electronic Textile for Gas Sensing

Da Yeon Cheonga,b,†, Sang Won Leec,†, Hyo Gi Jungc,d, Seokbeom Roha,b, Dongtak Leec, Taeha Leea,b, Saebomeena Leea, Wonseok Leee, Dae Sung Yoonc,d,*, Gyudo Leea,b,*

aDepartment of Biotechnology and Bioinformatics, Korea University, Sejong 30019, South Korea

bInterdisciplinary Graduate Program for Artificial Intelligence Smart Convergence Technology, Korea University, Sejong 30019, South Korea

cSchool of Biomedical Engineering, Korea University, Seoul 02841, South Korea

dInterdisciplinary Program in Precision Public Health, Korea University, Seoul 02841, South Korea

eDepartment of Electrical Engineering, Korea National University of Transportation, Chungju 27469, South Korea

†These authors contributed equally to this work.

*Corresponding author: G.L. (E-mail: lkd0807@korea.ac.kr); D.S.Y. (dsyoon@korea.ac.kr)

Figure S1. High resolution XPS C 1s spectra of (a) the GOLF, and (b) the RGOLF

Table S1. Analysis of deconvoluted C 1s peaks obtained from the XPS spectra of GOLF and RGOLF

| Sample |  | C=C & C-C | C-O | C=O | O-C=O |
| --- | --- | --- | --- | --- | --- |
| GO-coated CF (i.e., the GOLF) | Area | 46827.89 | 30940.57 | 4672.53 | 6060.09 |
|  | Area (%) | 52.92 | 34.96 | 5.28 | 6.85 |
| rGO-coated CF (i.e., the RGOLF) | Area | 42144.42 | 24732.25 | 54479.97 | 473.26 |
|  | Area (%) | 57.87 | 33.95 | 7.52 | 0.65 |

Table S2. Electrical properties of RGOLFs fabricated with 1 g/L of graphene and various dimeters (150 – 300 μm). (Electrical current measured at 2 V applied voltage)

| Diameter | Electric current | Electrical conductance |
| --- | --- | --- |
| 150 μm | 1.76 ± 0.10 μA | 0.87 ± 0.06 μS |
| 200 μm | 3.05 ± 0.32 μA | 1.49 ± 0.20 μS |
| 250 μm | 4.70 ± 0.24 μA | 2.33 ± 0.11 μS |
| 300 μm | 9.31 ± 0.40 μA | 4.63 ± 0.22 μS |