Supplementary information

For

Well dispersed heteropolyacids on clay supports catalysed glycolysis and aminolysis of PET polymer wastes

Gopal Jeya,1 Elumalai Ganesan2, Aimi Asilah Haji Tajuddin2, Yoshikazu Ito2, Ravikumar Dhanalakshmi1 and Vajiravelu Sivamurugan1*

1PG and Research Department of Chemistry, Pachaiyappa’s College, Chennai-600030, Tamilnadu, India.

2Institute of Applied Physics, Graduate School of Pure and Applied Sciences, University of Tsukuba, 1-1-1 Tennodai, Tsukuba 305-8571, Japan

Figure S1. Pore size distribution of (a) Supported Kaolin Catalysts, (b) Supported Bentonite Catalysts

Figure S2. FTIR spectrum of pure and impregnated kaolin catalysts

Figure S3. FTIR spectrum of pure and impregnated bentonite catalysts

(a)

(b)

(c)

Figure S4. SEM images, element mapping and EDX analysis for (a) Zn-kaolin, (b) PWA-Kaolin and (c) PMA-Kaolin

Figure S5. SEM images, element mapping and EDX analysis for (a) Zn-Bentonite (b) PWA-Bentonite and (c) PMA-Bentonite

Table S1. SEM- EDX mapping Mass percentage and atomic percentage of Kaolin catalysts

| Elements | 5wt% Zn-Kaolin |  | 5wt% PWA-Kaolin |  | 5wt% PMA-Kaolin |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Mass % | Atomic % | Mass% | Atomic % | Mass% | Atomic % |
| O | 59.43±0.15 | 71.81±0.19 | 54.40±0.20 | 69.52±0.26 | 53.93±0.18 | 67.11±0.23 |
| Na | 0.11±0.01 | 0.09±0.01 | 0.31±0.01 | 0.28±0.01 | - | - |
| Al | 13.65±0.06 | 9.78±0.04 | 16.85±0.08 | 12.77±0.06 | 15.15±0.07 | 11.18±0.05 |
| Si | 26.39±0.09 | 18.16±0.06 | 19.55±0.09 | 14.23±0.07 | 30.33±0.11 | 21.50±0.08 |
| K | 0.13±0.01 | 0.07±0.00 | 5.26±0.06 | 2.75±0.03 | 0.19±0.01 | 0.09±0.01 |
| Fe | 0.14±0.01 | 0.05±0.01 | 0.21±0.02 | 0.08±0.01 | 0.23±0.02 | 0.08±0.01 |
| M* | 0.16±0.03 (Zn) | 0.05±0.01 (Zn) | 3.43±0.10 (W) | 0.38±0.01 (W) | 0.18±0.02 (Mo) | 0.04±0.00 (Mo) |

Figure S6. SEM images of (a) pure kaolin

Figure S7. SEM images of (a) pure Bentonite and (b) Al-Bentonite

Figure S8. XPS Spectra of Zn2+ loaded kaolin

Figure S9. XPS Spectra of PWA loaded kaolin

Figure S10. XPS Spectra of PMA loaded kaolin

Figure S11. XPS Spectra of Al3+ loaded kaolin

Figure S12. XPS Spectra of pure kaolin

(a)

(b)

(c)

(d)

(e)

(f)

Figure S13. XPS spectra of (a) Zn-Kaolin, (b) Al3+ in Zn-Kaolin, (c) W6+ in PWA-Kaolin, (d) Mo6+ in PMA-Kaolin, (e) Al3+ in Al-Kaolin and (f) Al3+ in pure Kaolin

Figure S14. XPS Spectra of Zn2+ loaded bentonite

Figure S15. XPS Spectra of PWA loaded bentonite

Figure S16. XPS Spectra of PMA loaded bentonite

Figure S17. XPS Spectra of Al3+ loaded bentonite

Figure S18. XPS Spectra of pure bentonite

(a)

(b)

(c)

(d)

(e)

(f)

Figure S19. XPS spectra of (a) Zn-Bentonite, (b) Al3+ in Zn-Bentonite, (c) W6+ in PWA-Bentonite, (d) Mo6+ in PMA-Bentonite, (e) Al3+ in Al-Bentonite and (f) Al3+ in pure Bentonite

Table S2. Binding energies values (eV) for Zn2+, W6+ of PWA, Mo6+ of PMA  and Al-Kaolin spectra and surface M/Al compositions of samples and reference ZnO, PWA and PMA.

| Catalysts | Metals | Binding energy (eV) | M/Al ratio (surface) | Atomic (%) |
| --- | --- | --- | --- | --- |
| Zn-Kaolin | Zn2p3/2 Zn2p1/2 | 1022.12 1045.16 | 0.1854 0.0618 | 2.07 0.69 |
|  | Al 2p B | 75.75 | - | 7.02 |
|  | Al 2p A | 74.72 | - | 4.14 |
| PWA-Kaolin | W 4f7/2 | 36.06 | 0.0055 | 0.07 |
|  | W 4f5/2 | 38.19 | 0.0039 | 0.05 |
|  | Al 2p B | 75.51 | - | 7.93 |
|  | Al 2p A | 74.63 | - | 4.65 |
| PMA-Kaolin | Mo 3d5/2 | 232.74 | 0.0033 | 0.04 |
|  | Mo 3d3/2 | 235.73 | 0.0016 | 0.02 |
|  | Al 2p B | 75.62 | - | 7.69 |
|  | Al 2p A | 74.79 | - | 4.36 |
| Al-Kaolin | Al 2p B | 75.42 | 0.2553 | 3.09 |
|  | Al 2p A | 74.52 | 0.1264 | 1.53 |
| Pure Kaolin | Al 2p B | 75.64 | - | 9.19 |
|  | Al 2p A | 74.65 | - | 2.91 |

Table S3. Binding energies values (eV) for Zn2+, W6+ of PWA, Mo6+ of PMA and Al-Bentonite spectra and surface M/Al compositions of samples

| Catalysts | Metals | Binding energy (eV) | M/Al ratio (surface) | Atomic (%) |
| --- | --- | --- | --- | --- |
| Zn-Bentonite | Zn2p3/2 Zn2p1/2 | 1022.99 1045.10 | 0.3161 0.1053 | 2.07 0.69 |
|  | Al 2p A | 74.69 | - | 8.73 |
| PWA-Bentonite | W 4f7/2 | 35.62 | 0.0129 | 0.11 |
|  | W 4f5/2 | 37.82 | 0.0094 | 0.08 |
|  | Al 2p B | 75.15 | - | 6.99 |
|  | Al 2p A | 74.54 | - | 1.52 |
| PMA-Bentonite | Mo 3d5/2 | 231.97 | 0.0156 | 0.13 |
|  | Mo 3d3/2 | 235.08 | 0.0016 | 0.09 |
|  | Al 2p A | 74.59 | - | 8.3 |
| Al-Bentonite | Al 2p B | 75.31 | 1.19 | 9 |
| Pure Kaolin | Al 2p A | 74.65 | - | 7.55 |

Figure S20. 1H NMR spectra of depolymerized PET using ethylene glycol

Figure S21. 1H NMR spectra of depolymerized PET using Ethanolamine

Figure S22. 13C NMR spectra of depolymerized PET using ethylene glycol

Figure S23. 13C NMR spectra of depolymerized PET using Ethanolamine

Figure S24. FT-IR spectra of depolymerized PET using ethylene glycol (BHET)

Figure S25. FT-IR spectra of depolymerized PET using Ethanolamine (BHETA)

Figure S26. Mass spectrum of depolymerized PET using Ethanolamine (BHETA)