Rheology of concentrated CNF suspensions following PEG and NaOH modification

Shadi G. Mehmandoust Olya a,*, Thomas Rainey a

a Queensland University of Technology (QUT), School of Mechanical, Medical and Process Engineering, Gardens Point Campus, 2 George St, Brisbane 4000, Queensland, Australia

* Corresponding author's E-mail address: s.ghaebi@qut.edu.au

Supplementary Data

Derivation of Equation (3)

Equation (3) derived from the fundamental oscillatory shear relation (τA=G*γA), where τA is the shear-stress amplitude (Pa), γA is the strain amplitude, and G* is the complex shear modulus (pa) (G*=(G')2+(G")2) (Malvern, 2016).

Derivation of strain-energy density in shear (Equation 4)

Consider a rectangular elastic element of volume V=Ah subjected to a tangential (shear) force F applied to the top face (area A), producing a lateral displacement Δx. The corresponding shear stress (τ) and shear strain (γ) are:

| τ=FA | (S1) |
| --- | --- |
| γ=Δxh | (S2) |

Within the linear elastic regime, the force–displacement relation is linear, so the work done, and hence the strain energy (U) stored, during loading from 0 to Δx equals the area under the force–displacement curve:

| U=0ΔxF dx=12F Δx | (S3) |
| --- | --- |

The strain-energy density (u) (energy per unit volume) is therefore:

| u=UV=12F ΔxAh=12(FA)(Δxh)=12τ γ | (S4) |
| --- | --- |

Using Hooke’s law in shear, τ=Gγ, with G be the shear modulus, the same result can be written in equivalent forms:

| u=12Gγ2=12τ2G | (S5) |
| --- | --- |

This expression is the classical linear-elastic strain-energy density for simple shear and underpins our use of Uc*=12G0'(γf*)2 as a recoverable energy measure at the onset of flow in oscillatory tests, with G0' the plateau storage modulus in the LVER and γf* the flow strain identified at G'=G''.

Ostwald-de Waele power-law model

| η=kγ̇-n | (S6) |
| --- | --- |

where η is the apparent viscosity (mPa·s), γ̇ is the shear rate (s-1), k is the consistency index (mPa.sn), and n is the flow behaviour index (Yadav et al., 2021).

Derivation of κ

From Fig. S2 and S3(a), the two oscillatory-yield fits are τf*=6×10-6N2.6418 and τf*=0.5944C2.6418, considering N=κC, the κ will be derived as:

| κ=2/3(ρl/ρc)(L/d)2/100 | (S7) |
| --- | --- |
| κ=(0.59446×10-6)1/2.6418=77.8229 | (S8) |

Supplementary Figures

Fig. S1 Sedimentation analysis of CNF suspensions: initial solid concentration (C0) vs. the sediment height ratio (hs/h0). The linear coefficient from the quadratic fit was used to estimate the critical gel point and fibril aspect ratio

Fig. S2 Steady and oscillatory yield stress of pure CNF suspension as a function of calculated crowding factor on log-log axes, showing a power-law dependence with exponent m≈2.5m

Fig. S3 Yield stress from oscillatory tests (τf*) of pure CNF suspensions (a) as a function of CNF concentration plotted on log–log axes. The fitted power-law relationship (τf* ∝Cm) yields m = 2.64 (R2 = 0.99), consistent with percolation theory for fibrillar gels, where yield stress scales with the square or cube of concentration, (b) as a function of steady yield stress, the fitted linear relationship yields a slope of 1.38.

Supplementary Tables

Table S1. Comparison of steady shear and oscillatory rheological tests (Mezger, 2014)

| Test Feature | Steady Shear (Rotational) Tests | Oscillatory Tests |
| --- | --- | --- |
| Imposed shear force | Constant, unidirectional rotation | Small/Large amplitude, oscillating rotation |
| Test results | Shear stress; Viscosity | Viscoelastic behaviour: Storage modulus (G') and loss modulus (G") |
| Purpose | Measures viscosity (flow resistance); identifies flow behaviour | Measures elastic and viscous components (viscoelasticity); identifies gel point |
| Deformation | Large deformations and structural changes can occur | Small deformations within the linear viscoelastic region (LVR) with structure being preserved |
| Typical use-case | Predicting material behaviour during processing (e.g. pumping, mixing, and spreading) | Analysing material structure, stability, curing or gelation processes (e.g. paints, gels) |

Table S2. Viscosity at 0.1, 1, 10 and 100 s-1. Values are mean ± standard deviation, for a minimum of three replicates.

| Studied Parameter | Sample Code | Viscosity (0.1 s-1) (Pa.s) | Viscosity (1 s-1) (Pa.s) | Viscosity (10 s-1) (Pa.s) | Viscosity (100 s-1) (Pa.s) |
| --- | --- | --- | --- | --- | --- |
| CNF Concentration | C2P0N0 | 28.22 ± 5.50 | 4.03 ± 0.45 | 0.52 ± 0.03 | 0.11 ± 0.01 |
|  | C4P0N0 | 239.72 ± 39.44 | 31.51 ± 4.38 | 3.99 ± 0.69 | 0.72 ± 0.15 |
|  | C6P0N0 | 622.15 ± 55.21 | 85.29 ± 8.29 | 10.77 ± 0.96 | 1.81 ± 0.13 |
|  | C7P0N0 | 906.58 ± 64.82 | 125.69 ± 11.06 | 17.06 ± 1.06 | 2.74 ± 0.10 |
| One-way ANOVA P-Value |  | 2.1×10-15 (*) | 1.1×10-14 (*) | 3.8×10-16 (*) | 3.1×10-17 (*) |
| PEG Concentration | C6P1N0 | 497.35 ± 29.42 | 69.52 ± 6.86 | 9.87 ± 0.54 | 1.75 ± 0.17 |
|  | C6P3N0 | 375.39 ± 64.49 | 52.40 ± 6.47 | 8.04 ± 1.61 | 1.44 ± 0.33 |
|  | C6P5N0 | 374.51 ± 21.37 | 52.22 ± 2.50 | 7.98 ± 1.27 | 1.48 ± 0.30 |
|  | C6P10N0 | 373.27 ± 43.57 | 59.11 ± 7.43 | 7.42 ± 0.72 | 1.27 ± 0.10 |
| One-way ANOVA P-Value |  | 0.0029 (*) | 0.0041 (*) | 0.0420 (*) | 0.1025 |
| NaOH Concentration | C6P0N1 | 443.30 ± 31.40 | 43.93 ± 4.63 | 5.68 ± 0.50 | 0.91 ± 0.07 |
|  | C6P0N5 | 269.52 ± 50.91 | 32.38 ± 5.92 | 4.64 ± 0.61 | 0.76 ± 0.10 |
|  | C6P0N9 | 111.58 ±14.62 | 13.80 ± 2.92 | 2.38 ± 0.59 | 0.41 ± 0.08 |
|  | C6P0N10 | 95.95 ± 10.16 | 11.48 ± 0.47 | 1.75 ± 0.13 | 0.32 ± 0.03 |
| One-way ANOVA P-Value |  | 1.0×10-9 (*) | 4.9×10-8 (*) | 1.0×10-7 (*) | 1.0×10-7 (*) |
| pH | C6pH3 | 765.74 ± 58.50 | 78.53 ± 14.10 | 8.70 ± 1.59 | 1.32 ± 0.22 |
|  | C6pH5 | 416.34 ± 99.43 | 51.88 ± 10.32 | 6.15 ± 0.46 | 1.08 ± 0.03 |
|  | C6pH8 | 371.77 ± 90.69 | 48.99 ± 15.67 | 7.82 ± 1.13 | 1.30 ± 0.11 |
|  | C6pH10 | 303.03 ± 24.43 | 36.55 ± 5.36 | 5.79 ± 0.73 | 1.04 ± 0.08 |
| One-way ANOVA P-Value |  | 4.9×10-5 (*) | 0.0073 (*) | 0.0138 (*) | 0.0254 (*) |
| Combined PEG NaOH | C6P1N9 | 113.01 ± 21.43 | 15.18 ± 2.48 | 2.57 ± 0.55 | 0.43 ± 0.08 |
| One-way ANOVA P-Value |  | NA | NA | NA | NA |

NA: Not Applicable.

P<0.05 denotes for significant result and is shown by *.

Table S3. HB model fit values for yield stress, consistency and flow indices. P-value < 0.05 is considered as significant, as noted by (*).

| Studied Parameter | Sample Code | Yield Stress (τy) (Pa) | Consistency Index (k) (Pa.sn) | Flow Index (n) | R2 |
| --- | --- | --- | --- | --- | --- |
| CNF Concentration | C2P0N0 | 3.05 ± 0.54 | 0.71 ± 0.23 | 0.52 ± 0.04 | 0.9975 |
|  | C4P0N0 | 22.16 ± 2.69 | 8.48 ± 3.50 | 0.39 ± 0.03 | 0.9985 |
|  | C6P0N0 | 54.41 ± 7.46 | 26.75 ± 4.30 | 0.34 ± 0.02 | 0.9973 |
|  | C7P0N0 | 70.96 ± 10.92 | 51.15 ± 6.03 | 0.30 ± 0.01 | 0.9975 |
| One-way ANOVA P-Value |  | 1.1×10-10 (*) | 6.44×10-12 (*) | 1×10-8 (*) | - |
| PEG Concentration | C6P1N0 | 38.21 ± 8.15 | 29.19 ± 6.07 | 0.33 ± 0.02 | 0.9983 |
|  | C6P3N0 | 26.19 ± 2.63 | 25.77 ± 8.28 | 0.33 ± 0.01 | 0.9985 |
|  | C6P5N0 | 23.72 ± 8.42 | 28.34 ± 11.19 | 0.33 ± 0.03 | 0.9985 |
|  | C6P10N0 | 35.44 ± 5.07 | 17.77 ± 0.99 | 0.36 ± 0.00 | 0.9963 |
| One-way ANOVA P-Value |  | 0.019 (*) | 0.024 (*) | 0.13 | - |
| NaOH Concentration | C6P0N1 | 39.38 ± 5.15 | 5.84 ± 1.33 | 0.46 ± 0.03 | 0.9864 |
|  | C6P0N5 | 23.57 ± 4.79 | 8.88 ± 1.10 | 0.39 ± 0.01 | 0.9985 |
|  | C6P0N9 | 9.09 ± 2.30 | 5.15 ± 2.91 | 0.42 ± 0.06 | 0.9946 |
|  | C6P0N10 | 8.74 ± 1.38 | 2.57 ± 0.87 | 0.42 ± 0.05 | 0.9975 |
| One-way ANOVA P-Value |  | 1.09×10-7 (*) | 3.4×10-3 (*) | 1.5×10-2 (*) | - |
| pH | C6pH3 | 73.43 ± 0.70 | 6.31 ± 5.37 | 0.51 ± 0.09 | 0.9827 |
|  | C6pH5 | 38.85 ± 13.10 | 10.85 ±5.68 | 0.41 ± 0.06 | 0.9985 |
|  | C6pH8 | 28.04 ± 13.28 | 20.83 ± 2.15 | 0.34 ± 0.01 | 0.9976 |
|  | C6pH10 | 21.59 ± 1.93 | 15.74 ± 3.55 | 0.36 ± 0.02 | 0.9982 |
| One-way ANOVA P-Value |  | 1.03×10-3 (*) | 0.02 (*) | 0.02 (*) | - |
| Combined PEG NaOH | C6P1N9 | 10.08 ± 3.02 | 5.62 ± 2.98 | 0.42 ± 0.08 | 0.9934 |

Table S4. Storage modulus (G') at 0.1, 1.17, 13.6 and 85.8 rad.s-1. Values are mean ± standard deviation, for a minimum of three replicates.

| Studied Parameter | Sample Code | G’ (Pa) (0.1 rad.s-1) | G’ (Pa) (1.17 rad.s-1) | G’ (Pa) (13.6 rad.s-1) | G’ (Pa) (85.8 s-1) |
| --- | --- | --- | --- | --- | --- |
| CNF Concentration | C2P0N0 | 49.69±3.99 | 55.27±4.55 | 66.83±5.12 | 138.93±42.63 |
|  | C4P0N0 | 530.40±17.49 | 592.28±17.35 | 695.97±19.05 | 859.56±26.97 |
|  | C6P0N0 | 1700.32±60.32 | 1904.2±69.26 | 2245.72±86.23 | 2685.8±96.89 |
|  | C7P0N0 | 2141.17±339.09 | 2532.22±418.13 | 3176.45±403.80 | 3827.52±386.28 |
| PEG Concentration | C6P1N0 | 1490.87±184.08 | 1679.05±187.18 | 1984.45±214.23 | 2305±255.74 |
|  | C6P3N0 | 1456.92±115.76 | 1646.65±113.00 | 1955.55±127.97 | 2405.72±226.01 |
|  | C6P5N0 | 1232.98±348.82 | 1391.45±386.24 | 1648.7±464.89 | 2037.62±561.31 |
|  | C6P10N0 | 914.95±75.12 | 1033.27±82.05 | 1231.8±95.69 | 1550.5±95.69 |
| NaOH Concentration | C6P0N1 | 623.39±81.60 | 680.06± 87.45 | 788.72± 99.65 | 920.09± 128.16 |
|  | C6P0N5 | 532.19±89.33 | 544.41±113.16 | 596.28±131.77 | 741.13±146.35 |
|  | C6P0N9 | 204.18±110.50 | 194.79±109.63 | 206.86±116.95 | 309.83±178.70 |
|  | C6P0N10 | 118.89±22.27 | 114.28±19.89 | 125.43±20.93 | 287.5±48.99 |
| pH | C6pH3 | 1087.47±134.94 | 1217.53±146.64 | 1430.47±173.82 | 1751.37±249.23 |
|  | C6pH5 | 944.56±49.17 | 1087.93±35.19 | 1277.37±40.40 | 1637.87±21.59 |
|  | C6pH8 | 1229.90±50.30 | 1382.07±61.58 | 1629.77±74.72 | 1930.63±151.30 |
|  | C6pH10 | 887.47±46.85 | 1030.13±15.32 | 1221.20±13.71 | 1517.37±91.35 |
| Combined PEG NaOH | C6P1N9 | 321.72±4.50 | 300.50±3.97 | 317.41±4.43 | 424.95±63.03 |

Table S5. Loss modulus (G") at 0.1, 1.17, 13.6 and 85.8 rad.s-1. Values are mean ± standard deviation, for a minimum of three replicates.

| Studied Parameter | Sample Code | G" (Pa) (0.1 rad.s-1) | G" (Pa) (1.17 rad.s-1) | G" (Pa) (13.6 rad.s-1) | G" (Pa) (85.8 s-1) |
| --- | --- | --- | --- | --- | --- |
| CNF Concentration | C2P0N0 | 9.81±0.90 | 11.23±1.08 | 15.56±1.49 | 63.24±3.21 |
|  | C4P0N0 | 119.71± 3.50 | 136.08±4.98 | 172.26±6.43 | 270.8±8.66 |
|  | C6P0N0 | 433.02±50.29 | 487.42±52.22 | 600.79±57.70 | 816.22±61.11 |
|  | C7P0N0 | 918.43±61.79 | 958.13±63.81 | 1038.02±26.41 | 1267.47±79.31 |
| PEG Concentration | C6P1N0 | 376.62±33.96 | 408.47±39.35 | 507.95±50.53 | 713.02±68.56 |
|  | C6P3N0 | 507.53±291.80 | 579.18±341.40 | 708.86±389.90 | 946.93±442.69 |
|  | C6P5N0 | 300.85±84.71 | 338.11±99.74 | 431.75±127.45 | 623.57±172.90 |
|  | C6P10N0 | 222.50±10.59 | 252.71±16.30 | 330.88±23.12 | 501.27±31.00 |
| NaOH Concentration | C6P0N1 | 129.67±21.87 | 144.18±23.08 | 183.11± 26.22 | 291.51± 32.19 |
|  | C6P0N5 | 77.92±16.58 | 84.52±20.01 | 111.57±27.13 | 203.61±41.16 |
|  | C6P0N9 | 19.51±12.15 | 21.22±12.92 | 31.82±17.15 | 94.89±25.42 |
|  | C6P0N10 | 10.82±2.16 | 12.21±2.58 | 19.83±3.71 | 75.78±6.34 |
| pH | C6pH3 | 265.11±35.91 | 292.93±36.34 | 356.44±43.47 | 502.61±53.62 |
|  | C6pH5 | 293.12±11.56 | 311.46±31.26 | 386.91±44.22 | 526.32±53.34 |
|  | C6pH8 | 305.62±25.07 | 334.94±24.39 | 410.67±26.31 | 578.40±33.19 |
|  | C6pH10 | 248.41±32.66 | 266.09±19.90 | 320.78±13.41 | 454.93±9.67 |
| Combined PEG NaOH | C6P1N9 | 30.94±0.39 | 33.55±0.78 | 50.90±1.10 | 122.89±2.21 |

Table S6. One-way ANOVA results for parameters derived from frequency sweep

| Studied Parameter | Parameter | p-value | Significance |
| --- | --- | --- | --- |
| CNF Concentration | GLF' (Pa) | 1.9×10-7 | Significant |
|  | ωc (rad/s) | 1.31×10-2 | Significant |
|  | tanδLF | 4.08×10-4 | Significant |
|  | a exponent | 3.24×10-8 | Significant |
|  | b exponent | 2.01×10-4 | Significant |
| PEG Concentration | GLF' (Pa) | 3.29×10-2 | Significant |
|  | ωc (rad/s) | 3.48×10-1 | Non-significant |
|  | tanδLF | 4.73×10-1 | Non-significant |
|  | a exponent | 7.91×10-1 | Non-significant |
|  | b exponent | 3.69×10-1 | Non-significant |
| NaOH Concentration | GLF' (Pa) | 2.70×10-6 | Significant |
|  | ωc (rad/s) | 1.13×10-2 | Significant |
|  | tanδLF | 2.12×10-11 | Significant |
|  | a exponent | 5.61×10-6 | Significant |
|  | b exponent | 3.63×10-5 | Significant |
| pH | GLF' (Pa) | 3.12×10-3 | Significant |
|  | ωc (rad/s) | 3.62×10-1 | Non-significant |
|  | tanδLF | 5.82×10-2 | Non-significant |
|  | a exponent | 2.18×10-1 | Non-significant |
|  | b exponent | 6.59×10-1 | Non-significant |
| Combined PEG-NaOH | - | NA | NA |

P-value < 0.05 is considered as significant.

Table S7. One-way ANOVA results for parameters derived from amplitude sweep

| Studied Parameter | Parameter | p-value | Significance |
| --- | --- | --- | --- |
| CNF Concentration | G0' (Pa) | 7.6×10-11 | Significant |
|  | γLVE* (%) | 0.99 | Non-significant |
|  | S' | 0.049 | Significant |
|  | γf* (%) | 7.4×10-4 | Significant |
|  | τf* (Pa) | 5.4×10-8 | Significant |
|  | UC* (mJ/m3) | 8.4×10-7 | Significant |
|  | Wd (mJ/m3) | 1×10-4 | Significant |
| PEG Concentration | G0' (Pa) | 2×10-3 | Significant |
|  | γLVE* (%) | 0.94 | Non-significant |
|  | S' | 0.70 | Non-significant |
|  | γf* (%) | 3.5×10-4 | Significant |
|  | τf* (Pa) | 3.5×10-4 | Significant |
|  | UC* (mJ/m3) | 0.08 | Non-significant |
|  | Wd (mJ/m3) | 1.4×10-4 | Significant |
| NaOH Concentration | G0' (Pa) | 9.2×10-12 | Significant |
|  | γLVE* (%) | 1.3×10-6 | Significant |
|  | S' | 0.047 | Significant |
|  | γf* (%) | 2.3×10-6 | Significant |
|  | τf* (Pa) | 1.5×10-6 | Significant |
|  | UC* (mJ/m3) | 1.6×10-4 | Significant |
|  | Wd (mJ/m3) | 0.14 | Non-significant |
| pH | G0' (Pa) | 1.5×10-4 | Significant |
|  | γLVE* (%) | 2.9×10-2 | Significant |
|  | S' | 1.6×10-4 | Significant |
|  | γf* (%) | 3.8×10-2 | Significant |
|  | τf* (Pa) | 5.1×10-3 | Significant |
|  | UC* (mJ/m3) | 2.4×10-2 | Significant |
|  | Wd (mJ/m3) | 3.8×10-2 | Significant |
| Combined PEG-NaOH | - | NA | NA |

P-value < 0.05 is considered as significant.

Malvern (2016) A basic introduction to rheology Malvern Instruments Worldwide. https://cdn.technologynetworks.com/tn/resources/pdf/wp160620basicintrorheology.pdf

Mezger TG (2014) The Rheology Handbook for users of rotational and oscillatory rheometers (4 ed.). Vincentz Network. https://books.google.com.au/books?id=iO8-swEACAAJ

Yadav C, Saini A, Zhang W, You X, Chauhan I, Mohanty P,  Li X (2021) Plant-based nanocellulose: A review of routine and recent preparation methods with current progress in its applications as rheology modifier and 3D bioprinting. Int J Biol Macromol 166: 1586-1616. https://doi.org/10.1016/j.ijbiomac.2020.11.038