|  | Donor age | Samples (n) | Mean BMP-7 (ng/g) | Standard deviation (ng/g) | P-value |
| --- | --- | --- | --- | --- | --- |
| Group 1 | 29-33 years | 72 | 201.705 | 12.941 | <0.001 |
| Group 2 | 55-60 years | 72 | 135.522 | 10.974 |  |

Table 1. Comparison of mean BMP-7 levels of DFDBA samples based on donor age