Supporting Information

Tuning Local Proton Flux in Yolk-Shell Cu@Cu2Se Nanoreactors to Enable Efficient Electrochemical Nitrate-Ammonia Conversion

He et al.,

Experimental section

Synthesis of Cu2O nanocubes

Cu2O nanocubes were synthesized through a method of solution reduction[1].In a typical process, Cu(NO3)2•3H2O (0.3624 g) was dissolved into 3 mL anhydrous ethanol to generate a clear solution, which was then slowly added into 60 mL of NaOH aqueous solution (5.0 M) to get a dark blue [Cu(OH)4]2-solution under stirring. Afterwards, the [Cu(OH)4]2-solution was added into 400 mL of ascorbic acid aqueous solution (20 mM) under stirring for 20 minutes at room temperature. Finally, the orange precipitate was obtained through centrifugation, washed with deionized water for several times, and dried at 60 oC for overnight. The resulting product was denoted Cu2O-NB.

Synthesis of yolk-shell structured Cu2Se@Cu nanoreactors

A NaHSe solution was prepared in advance: Se powder (0.036 g) was added into 50 ml NaBH4 aqueous solution (0.13 M) under vigorously stirring until the solution was transparent. Then, the above synthesized Cu2O-NB (0.1 g) was well dispersed into 30 ml deionized water under ultrasonic bath. The NaHSe solution (4 mL) was added into the obtained Cu2O-NB dispersion solution for 20 minutes under stirring at room temperature. Due to reaction of NaHSe and CuO2, a Cu2Se shell would be generated outside the Cu2O. The resulting core-shell structured Cu2Se@Cu2O (denoted CS- Cu2Se@Cu2O) was obtained through centrifugation, washed with deionized water several times, and dried at 60 oC for overnight. The CS-Cu2Se@Cu2O was then treated with an ammonia (6-7%) aqueous solution for partially etching the Cu2O core and thus generating yolk-shell structured Cu2Se@Cu2O (denoted YS-Cu2Se@Cu2O). The YS-Cu2Se@Cu2O nanoreactors with void sizes (i.e., 40, 60, and 80 nm) were obtained by using different ammonia treatment time such as 0.5, 1, and 1.5 h. Finally, an electrochemical reduction was performed on the YS-Cu2Se@Cu2O at the potential of -0.4 V vs RHE for 1 h for the reduction of Cu2O to Cu and yet remaining the crystal phase of Cu2Se. The resulting product was denoted YS-Cu2Se@Cu. For comparison, we also completely removed the Cu2O core of YS-Cu2Se@Cu2O by extending the ammonia treatment time to 8 h, and the resulting product was denoted hollow structured Cu2Se (denoted H-Cu2Se).

Material characterizations

SEM images were obtained on a field emission scanning electron microscopy (FESEM, FEI JEOL-7800F). TEM and HRTEM images were taken on transmission electron microscopy of JEM-2100F and JEOL F200, respectively. XPS measurements were performed on X-ray photoelectron spectrometer (Thermo VG Scientific ESCALAB 250, Thermo Electron, U.K.). XRD patterns were recorded by using an X-ray diffractometer (Rigaku Mini Flex 600) with Cu Kα radiation (λ = 0.15418 nm). UV-Vis was measured on Ultraviolet–Visible Spectrophotometer (UV-2550). 1H NMR were measured by H-nuclear magnetic resonance (H-NMR) technic (AVANCE Ⅲ 500MHz). Operando Raman spectra were conducted on Raman microscope (Jobin Yvon Horiba HR800) using a HeNe laser (632.8 nm).

Electrochemical Measurements

NO3-RR performance was measured on a CHI 760E electrochemical workstation (Chenhua, Shanghai) using an H-type electrochemical cell separated by FAB-PK-130 anion exchange membrane. A piece of carbon paper (0.25 cm2) with electrocatalysts (mass loading of 2 mg cm-2), Hg/HgO (in 1 M KOH) and Pt foil were employed as the working electrode, reference electrode and counter electrode, respectively. The electrocatalyst inks were prepared by uniformly dispersing electrocatalysts (2 mg) in 400 µL mixture solution (Vethanol∶VNafion = 92∶8) under ultrasonic bath. To avoid the interfere of air, argon is continuously pumped into the cathode side of H-type cell during tests. Prior to the NO3-RR test, an electrochemical reduction was performed on all the samples at the potential of -0.4 V vs RHE in 1 M KOH without NO3- for ensuring that the Cu2O core was completely reduced to the metallic Cu. The tested potentials were recorded against the reversible hydrogen electrode (RHE) based on the Nernst equation: ERHE = EHg/HgO + 0.098 +0.0591pH (pH =14). All Linear sweep voltammetry (LSV) curves were recorded after 60%iR compensation if not specifically stated, where R stands for the solution resistance. The ECSA values were determined using a method of double layer capacitance (Cdl).[2] The apparent energy barrier was determined by recording LSV curves of NO3-RR at different temperatures according to the Arrhenius equation.

Product detection and efficiency calculations

Ammonia content in liquid products was quantified using an indophenol blue method[3].To ensure the concentration of NH3 in liquid products well situated at the linear range of this method, the electrolytes electrolyzed for 3600 s electrolysis at different potentials were firstly diluted by KOH aqueous solution (1.0 M). The mixed solution of salicylic acid (0.36 M), potassium sodium tartrate tetrahydrate (0.18 M), and NaOH (0. 36 M) was used as coloring agents. Afterwards, 500 μL of coloring agents, 50 μL of NaOH aqueous solution (0.75 M), 50 μL of sodium nitroprusside (0.034 M) and 50 μL of NaClO (available chlorine 6-14%) were added into 4 ml of diluted electrolyte. After standing in the dark at room temperature for 1 h, the UV-Vis absorption spectrum was measured, and the concentration of NH3 was determined by the absorbance peak at a wavelength ~655 nm. Likewise, the nitrite (NO2-) and hydrazine hydrate (N2H4) were also quantified by using UV-Vis spectra according to the Griess50 and Watt & Chrisp50 method, respectively.[4]

To further confirm the amount of produced ammonia, we also carried out 1H NMR experiments. In the experiments, maleic acid (MA) was used as internal standard to quantify NH3. Detailly, 20 ml of the treated electrolyte was mixed with 5 ml of H2SO4 aqueous solution (4.0 M) and 10 mg of maleic acid. Then, 50 μL of D2O was added to 0.5 ml of the above solution for 1H NMR (500 MHz) measurement. Finally, the concentration of NH3 in products were calculated based on the standard curves measured for AreaNH4+/AreaMA. As for the 15N isotope labeling experiments, the K14NO3 was changed to K15NO3 as nitrogen resources for performing the electrolysis experiments, and the liquid products containing 15NH4+ were analyzed by 1H NMR.

The Faraday efficiency of ammonia is calculated according to the following equation.

Faradaic efficiency =nVcatholyteCNH3FQ

where n stands for the number of transferred electrons for the formation of 1 mol of ammonia, here is 8; Vcatholyte is the volume of liquid product (L), and the value is 0.030 L; CNH3 is the detected concentration of ammonia (M) detected; F is the Faraday constant (96485 C∙mol-1); Q represents the total consumed charge (Q = it).

Computational Details

All density functional theory (DFT) calculations were performed by using the Vienna ab initio Simulation Program (VASP) package.[5] Perdew–Burke–Ernzerhof (PBE) functional within the generalized gradient approximation (GGA) was employed to describ the exchange-correlation energy.[6] The cutoff energy of plane wave basis set was set to 450 eV, which was used to represent the valence electrons with the projector-augmented wave (PAW). Brillouin-zone integration was performed via the Monkhorst-Pack scheme with a 3 ×3 × 1 k-mesh. The convergence criterion for the electronic relaxation and ionic optimizations were set to 10–4 eV and 0.02 eV/Å, respectively. In addition, we have set a vacuum width of of 15 Å along the Z axis, which is used to ensure negligible interaction. Cu(111) and Cu2Se (220) surface were selected as structural models for calculating water dissociation energy. The water dissociation energy was calculated according to the following equation

Edissociation = EH2O* – EH*+OH*

where EH2O* represent the energy of adsorption H2O, and EH*+OH* is the energy of simultaneous adsorption H and OH.

The free Gibbs adsorption energy of NO3- (∆GNO3*). The ∆GNO3* values on different surfaces can be calculated according to the following equation[7]:

∆Gads(NO3*) = GNO3* + ½ GH2 – Esur – Ggas(HNO3)

where GNO3*, GH2 and Ggas(HNO3) represent free Gibbs adsorption energy of nitrate, H2 and HNO3, respectively. Esur was the DFT-computed electronic energies of the bare surface.

The free energy of hydrogen adsorption (ΔGH*) was calculated by the following equation[8]:

ΔGH*=ΔEH +0.24 eV

where ΔEH is the difference of H adsorption energy on the catalyst surface, 0.24 eV is the correction of zero-point energy and entropy difference.

Figure S1 (a) Calculated energies of NO3- adsorption on the surface of Cu and Cu2Se. Optimized surface configurations of NO3- adsorbed on the Cu and Cu2Se.

Figure S2 Optimized surface configurations of hydrogen adsorbed on the Cu and Cu2Se.

Figure S3 SEM images of Cu2O nanocubes (Cu2O-NB).

Figure S4 XRD patterns of Cu2O-NB and the standard XRD card of Cu2O (JCPDS no. 05-0667)

.

Figure S5 HRTEM images of core-shell structured Cu2O@Cu2Se (CS-Cu2O@Cu2Se).

Figure S6 SEM images of CS-Cu2O@Cu2Se (before the treatment of NH3·H2O) and YS-Cu2O@Cu2Se-60 (after the treatment of NH3·H2O).

Figure S7 LSV of YS-Cu@Cu2Se-40, YS-Cu@Cu2Se-60, and YS-Cu@Cu2Se-80 for the NO3-RR in 1 M KOH with 0.1 M NO3- (40, 60, and 80 stands for the void size of nanoreactors). The YS-Cu@Cu2Se-40, YS-Cu@Cu2Se-60, and YS-Cu@Cu2Se-80 were prepared by the electrochemical reduction of YS-Cu2O@Cu2Se-40, YS-Cu@ Cu2O-60, and YS-Cu@Cu2O-80 at the potential of -0.4 V vs RHE for 1 h.

Figure S8 TEM images of hollow-structured Cu2Se nanoboxes (H-Cu2Se).

Figure S9 XRD patterns of H-Cu2Se and the standard XRD card of Cu2Se (JCPDS no. 06-0680).

Figure S10 XRD patterns of YS-Cu2O@Cu2Se-60 and the standard XRD card of Cu2O (JCPDS no. 05-0667).

Figure S11 XRD patterns of Cu2O-NB before and after the reduction at the potential of -0.4 V vs RHE for 1 h, and the standard XRD cards of Cu (JCPDS no. 05-0836) and Cu2O (JCPDS no. 05-0667). The XRD peak of carbon paper is orginated from the substrate of electrodes.

Figure S12 Raman spectra of the Cu2O-NB before and after the reduction at the potential of -0.4 V vs RHE for 1 h.

Figure S13 XPS spectra of (a) Cu 2p and Cu LMM for the Cu2O-NB before and after the reduction at the potential of -0.4 V vs RHE for 1 h.

Figure S14 XRD patterns of H-Cu2Se before and after the reduction at the potential of -0.4 V vs RHE for 1 h, and the standard XRD cards of Cu2Se (JCPDS no. 06-0680). The XRD peak of carbon paper is orginated from the substrate of electrodes.

Figure S15 Raman spectra of H-Cu2Se before and after the the reduction at the potential of -0.4 V vs RHE for 1 h.

Figure S16 XPS spetra of (a) Cu 2p, (b) Cu LMM, and (c) Se 3d for the H-Cu2Se before and after the reduction at the potential of -0.4 V vs RHE for 1 h.

Figure S17 XRD patterns of YS-Cu2O@Cu2Se-60 before and after the reduction at the potential of -0.4 V vs RHE for 1 h, and the standard XRD cards of Cu (JCPDS no. 04-0836) and Cu2O (JCPDS no. 05-0667). The XRD peak of carbon paper is orginated from the substrate of electrodes.

Figure S18 HRTEM images of YS-Cu2O@Cu2Se-60 after the reduction at the potential of -0.4 V vs RHE for 1 h.

Figure S19 HADDF-STEM images of YS-Cu2O@Cu2Se-60 after the reduction at the potential of -0.4 V vs RHE for 1 h, and corresponding elemental mapping of (f) Cu and (g) Se.

Figure 20 LSV of YS-Cu@Cu2Se-60 with different mass loadings for the NO3-RR in 1 M KOH with 0.1 M NO3-.

Figure S21 Quantifying ammonia in the liquid products via the indophenol blue method: (a) Optical photographs of liquid products on the catalyst of YS-Cu@Cu2Se-60 at different potentials after adding he coloring agent, and (b) corresponding UV-Vis adsorption spectra.

Figure S22 Quantifying (NO2-) in the liquid products via the Griess method: (a) Optical photographs of liquid products on the catalyst of YS-Cu@Cu2Se-60 at the potential of -0.15 V vs RHE after adding he coloring agent, and (b) corresponding UV-Vis adsorption spectra. Quantifying of hydrazine hydrate (N2H4) in the electrolyte via the Watt & Chrisp method: (c) Optical photographs of liquid products on the catalyst of YS-Cu@Cu2Se-60 at the potential of -0.15 V vs RHE after adding he coloring agent, and (d) corresponding UV-Vis adsorption spectra.

Figure S23 1H NMR spectra of liquid products obtained on the YS-Cu@Cu2Se-60 from NO3-RR at the potential of -0.15 V vs RHE for 1 h.

Figure S24 Comparing FENH3 values calculated via the UV-Vis and 1H NMR spectra on the YS-Cu@Cu2Se-60 at different potentials.

Figure S25 Representative gas-chromatography of gas products obtained on the YS-Cu@Cu2Se-60 at the potential of -0.20 V vs RHE. The absence of peak for the N2 indicates that the no presence of N2 in gas products.

Figure S26 CV of (a) Cu-NB, (b) CS-Cu@Cu2Se, and (c) YS-Cu@Cu2Se-60 over a potential range without Faradic current densities at different scan rates. (d) Curves of capacitance Δj (|jcharge−jdischarge|) as a function of different scan rates.

Figure S27  LSV of Cu-NB, CS-Cu@Cu2Se, and YS-Cu@Cu2Se-60 normalized by Cdl for NO3-RR in 1 M KOH with 0.1 M NO3-.

Figure S28 FENH3 values of YS-Cu@Cu2Se-60 at the potential of -0.15 V vs RHE before and after the 20-h stability test.

Figure S29 TEM images of YS-Cu@Cu2Se-60 after the 20-h stability test.

Figure S30 FENH3 of (a) Cu-NB, and (b) YS-Cu@Cu2Se-60 at the potential of -0.15 V vs RHE in 1 M NaOH/H2O and 1 M NaOD/D2O with 0.1 M NO3-.

Figure S31 Tafel slope of Cu-NB, CS-Cu@Cu2Se, and YS-Cu@Cu2Se-60.

Figure S32 LSV of (a) Cu-NB and (b) YS-Cu@Cu2Se-60 for NO3-RR in 1 M with 0.1 M NO3- at different temperatures.

Figure S33 LSV of (a) Cu-NB, (b) YS-Cu@Cu2Se-40, (c) YS-Cu@Cu2Se-60, (d) YS-Cu@Cu2Se-80 for NO3-RR in 1 M KOH with 0.1 M NO3- at different scan rates.

Figure S34 Faradic effeciency towards H2 (FEH2) of Cu-NB, YS-Cu@Cu2Se-40, YS-Cu@Cu2Se-60, and YS-Cu@Cu2Se-80 for NO3-RR at the potenital -0.2 V vs RHE in 1 M KOH containing 0.1 M NO3-.

Table S1 FEH2 and FENH3 values of Cu-NB, CS-Cu@Cu2Se, and YS-Cu@Cu2Se-60 for the NO3-RR at the potential of -0.15 V vs RHE.

| Electrocatalyst | FEH2 (%) | FENH3 (%) |
| --- | --- | --- |
| Cu-NB | 6.0 | 93.5 |
| CS-Cu@Cu2Se | 3.2 | 96.4 |
| YS-Cu@Cu2Se-60 | N.A. | 99.6 |

Table S2 Comparing the NO3-RR performance of our YS-Cu@Cu2Se-60 with other reported electrocatalysts.

| Electrocatalyst | Electrolyte | Potential (V vs RHE) | NH3 partial current density (mA cm-2) | NH3 Selectivity | NH3 yield rate | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| YS-Cu@Cu2Se-60 | 0.1 M KNO3+1 M KOH | -0.15 V | 202 | 99.5% | 471 mmol gcat.−1 h−1 (0.94 mmol cm-2 h−1) | This work |
| Fe-PPy single-atom | 0.1 M KNO3+0.1M KOH | -0.7 V | ~36 | ~100% | 168.75 mmol gcat.−1 h−1 (0.16 mmol cm-2 h-1) | Energy Environ. Sci., 2021, DOI: 10.1039/D1EE00545F |
| Cu50Ni50 alloys | 0.1 M KNO3+1 M KOH | -0.15 V | ~53 | ~100% | ~0.79 mmol cm-2 h−1 | J. Am. Chem. Soc. 2020, 142, 5702–5708 |
| Fe single-atom | 0.5 M KNO3+0.1 M K2SO4 | -0.66 V | 35.3 | ~75% | 308.53 mmol gcat.−1 h−1 (0.062 mmol cm-2 h-1) | Nat. Commun., 2021, 12, 2870-2870 |
| Strained Ru Nanoclusters | 1 M KNO3+1 M KOH | -0.2 V | 223.3 | 96 % | 5560 mmol gcat.−1 h−1 (1.17 mmol cm-2 h−1 ) | J. Am. Chem. Soc., 2020, 142, 7036-7046 |
| Cu nanosheets | 10 mM KNO3+0.1 M KOH | -0.15 V | ~7.5 | 99.7% | 22.95 mmol gcat.−1 h−1 (0.023 mmol cm-2 h−1 ) | Appl. Mater. Today 2020, 19, 100620 |
| Porous Cu70Ni30 | 0.1 M NaNO3 +1 M NaOH | -0.276 V | ~0.17 | 85.4 % | ~4.121 mmol gcat.−1 h−1 (~0.0026 mmol cm-2 h−1 ) | Electrochim. Acta., 2014, 140, 337-344 |
| Copper powders (Cu 6h, Air) | 0.1 M NaNO3+1 M NaOH | -0.376 V | ~60 | 85 % | ~0.27 mmol cm-2 h−1 | J. Electroanal. Chem., 2006, 596, 13-24 |

References

[1] Y. Sun, Z. Hu, J. Zhang, L. Wang, C. Wu, J. Xu, A top-down strategy to synthesize wurtzite Cu2ZnSnS4 nanocrystals by green chemistry, Chem. Commun., 52 (2016) 9821-9824.

[2] Q. Hu, G. Li, Z. Han, Z. Wang, X. Huang, X. Chai, Q. Zhang, J. Liu, C. He, General Synthesis of Ultrathin Metal Borate Nanomeshes Enabled by 3D Bark-Like N-Doped Carbon for Electrocatalysis, Adv. Energy Mater., 9 (2019) 1901130.

[3] D. Zhu, L. Zhang, R.E. Ruther, R.J. Hamers, Photo-illuminated diamond as a solid-state source of solvated electrons in water for nitrogen reduction, Nat. Mater., 12 (2013) 836-841.

[4] L.C. Green, D.A. Wagner, J. Glogowski, P.L. Skipper, J.S. Wishnok, S.R. Tannenbaum, Analysis of nitrate, nitrite, and [15N]nitrate in biological fluids, Anal. Biochem., 126 (1982) 131-138.

[5] G. Kresse, J. Furthmüller, Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set, Phy. Rev. B, 54 (1996) 11169-11186.

[6] G. Kresse, D. Joubert, From ultrasoft pseudopotentials to the projector augmented-wave method, Phy. Rev. B, 59 (1999) 1758-1775.

[7] S. Guo, K. Heck, S. Kasiraju, H. Qian, Z. Zhao, L.C. Grabow, J.T. Miller, M.S. Wong, Insights into Nitrate Reduction over Indium-Decorated Palladium Nanoparticle Catalysts, ACS Catal., 8 (2018) 503-515.

[8] W. Zhong, B. Xiao, Z. Lin, Z. Wang, L. Huang, S. Shen, Q. Zhang, L. Gu, RhSe2: A Superior 3D Electrocatalyst with Multiple Active Facets for Hydrogen Evolution Reaction in Both Acid and Alkaline Solutions, Adv. Mater., 33 (2021) 2007894.