Visible light active Nitrogen and Cobalt co-doped TiO2 Nanoparticles: Synthesis, Characterization and Photocatalytic activity

Aroosa Javed* a, Memoona Qammara, b, Rooha Khurramc, Zaib-un-Nisaa and Habib Nasira

Department of chemistry, National University of Sciences and Technology (NUST), Sector H-12 Islamabad 44000, Pakistan

Department of Chemistry, Hong Kong University of Science and Technology (HKUST), Clear Water Bay Road, Kowloon, 999077, Hong Kong SAR

Beijing Key laboratory for green catalysis and separation, Department of Chemistry and Chemical engineering Beijing university of technology Beijing 100124, China

*Corresponding author.

Aroosa Javed

Email: aroosa.899@gmail.com

Contact number: +92-302-5276422

__________________________________________________________________________________

Figure S1.  EDX Spectra of (a) TiO2 (b) CoN-TiO2-1 (c) CoN-TiO2-2 (d) CoN-TiO2-3 (e CoN-TiO2-4) (f) CoN-TiO2-5

a

b

d

e

c

f

(b)

(a)

(d)

(c)

(f)

(e)

Figure S2. Degradation graphs of methyl orange by using (a) undoped TiO2 (b) CoN-TiO2-1 (c) CoN-TiO2-2 (d) CoN-TiO2-3 (e) CoN-TiO2-4 (f) CoN-TiO2-5

| Catalyst | Time (hr.) | Absorbance | Ct | Co | Ct/Co | ln Ct/Co | Negative of ln Ct/Co |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TiO2 nanoparticles | 1 | 0.64 | 1.64 | 1.68 | 0.98 | - 0.02 | 0.02 |
|  | 2 | 0.58 | 1.53 |  | 0.91 | - 0.09 | 0.09 |
|  | 3 | 0.53 | 1.43 |  | 0.85 | - 0.16 | 0.16 |
|  | 4 | 0.49 | 1.36 |  | 0.81 | - 0.21 | 0.21 |
|  | 5 | 0.45 | 1.23 |  | 0.73 | - 0.31 | 0.31 |
| CoN-TiO2-1 | 1 | 0.59 | 1.54 | 1.62 | 0.95 | - 0.05 | 0.05 |
|  | 2 | 0.49 | 1.36 |  | 0.84 | - 0.13 | 0.13 |
|  | 3 | 0.42 | 1.22 |  | 0.75 | - 0.24 | 0.24 |
|  | 4 | 0.36 | 1.10 |  | 0.68 | - 0.38 | 0.38 |
|  | 5 | 0.26 | 0.91 |  | 0.56 | - 0.58 | 0.58 |
| CoN-TiO2-2 | 1 | 0.57 | 1.51 | 1.62 | 0.93 | - 0.08 | 0.08 |
|  | 2 | 0.46 | 1.30 |  | 0.80 | - 0.22 | 0.22 |
|  | 3 | 0.37 | 1.13 |  | 0.70 | - 0.42 | 0.42 |
|  | 4 | 0.32 | 1.02 |  | 0.63 | - 0.56 | 0.56 |
|  | 5 | 0.22 | 0.84 |  | 0.52 | - 0.65 | 0.65 |
| CoN-TiO2-3 | 1 | 0.54 | 1.45 | 1.60 | 0.91 | - 0.07 | 0.07 |
|  | 2 | 0.44 | 1.25 |  | 0.78 | - 0.25 | 0.25 |
|  | 3 | 0.35 | 1.08 |  | 0.68 | - 0.38 | 0.38 |
|  | 4 | 0.28 | 0.95 |  | 0.60 | - 0.51 | 0.51 |
|  | 5 | 0.19 | 0.78 |  | 0.49 | - 0.71 | 0.71 |
| CoN-TiO2-4 | 1 | 0.53 | 1.43 | 1.56 | 0.87 | - 0.10 | 0.10 |
|  | 2 | 0.39 | 1.17 |  | 0.75 | - 0.28 | 0.28 |
|  | 3 | 0.32 | 1.02 |  | 0.65 | - 0.43 | 0.43 |
|  | 4 | 0.23 | 0.86 |  | 0.55 | - 0.60 | 0.60 |
|  | 5 | 0.15 | 0.70 |  | 0.45 | - 0.80 | 0.80 |
| CoN-TiO2-5 | 1 | 0.45 | 1.28 | 1.49 | 0.86 | - 0.15 | 0.15 |
|  | 2 | 0.31 | 1.01 |  | 0.68 | - 0.38 | 0.38 |
|  | 3 | 0.26 | 0.91 |  | 0.61 | - 0.49 | 0.49 |
|  | 4 | 0.17 | 0.74 |  | 0.50 | - 0.7 | 0.7 |
|  | 5 | 0.11 | 0.63 |  | 0.42 | - 0.87 | 0.87 |

Table S1.  Degradation rate calculation for MO degradation under visible light