Table S5. Performance by fabrication method.

| Fabrication Method | Studies (n) | Avg. Max Pressure (kPa) | Avg. Max Force (N) | Avg. Max Payload (kg) | Key Strength |
| --- | --- | --- | --- | --- | --- |
| 3D-Printed (TPU/NinjaFlex/PLA) | 14 | 185 | 42.1 | 3.8 | Rapid prototyping & complex geometry |
| Silicone Casting (Ecoflex/Dragon Skin) | 18 | 98 | 29.3 | 1.9 | Superior compliance & biocompatibility |
| Fabric-Reinforced | 2 | 85 | >150 | >7 | Extreme load-to-weight ratio |
| Hybrid (rigid inserts/jamming) | 9 | 92 | 71.4 | 11.2 | Highest absolute performance |
| Emerging (origami/pump/solar) | 4 | 44 | 13.3 | 0.5 | Low-energy / untethered operation |