Supporting Information

Direct valorization of real acid mine drainage into MgAlFe-LDHs: structural evolution, sulfate fixation, and anionic pollutant removal

Jierong Wang a#, Junyu Ren a#, Dong Zhangb, Meng Zhang a, Ruijie Guo a,c, Peide Han a, Hong Yan a,c

a College of Materials Science and Engineering, Taiyuan University of Technology, Taiyuan, P.R. 030024, China

b Taiyuan Bilan Hydralic Engineering Design Co., LTD., Taiyuan, Shanxi 030024, P.R. China

c Key Laboratory of Interface Science and Engineering in Advanced Materials (Taiyuan University of Technology), Ministry of Education, Taiyuan 030024, P.R. China

Figure S1 Calibration curve for SO2− 4 concentration determination

Figure S2 Possible atomic arrangements in the single-layer structure of LDHs at M2+/M3+=1 (a), 1.5 (b), 2 (c), and 2.5 (d)

Figure S3 Calculated energies corresponding to the possible single-layer atomic arrangements of LDHs at M2+/M3+=1 (a), 1.5 (b), 2 (c), and 2.5 (d)

Figure S4 Potential adsorption sites of SO2− 4within the interlayer region of LDHs

Table S1 Removal ratio of metal ions from AMD during LDH formation at different M2+/M3+ ratios

| pH | M2+/M3+ | Removal ratio (%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Fe3+ | Al3+ | Zn2+ | Mn2+ | Ca2+ |
| 8.5 | 1 | 99.96 | 99.89 | 97.76 | 98.45 | 21.68 |
| 8.5 | 2.5 | 99.97 | 99.96 | 98.54 | 98.78 | 22.31 |
| 9 | 1 | 99.96 | 99.34 | 98.76 | 99.77 | 22.75 |
| 9 | 2.5 | 99.97 | 99.96 | 99.19 | 99.80 | 26.01 |
| 9.5 | 1 | 99.97 | 98.51 | 99.52 | 99.86 | 26.71 |
| 9.5 | 2.5 | 99.99 | 99.99 | 99.83 | 99.92 | 31.91 |
| 10 | 1 | 99.78 | 98.96 | 99.74 | 99.98 | 22.53 |
| 10 | 2.5 | 99.98 | 99.94 | 99.87 | 99.99 | 31.47 |

Table S2 Experimental factors and levels for response surface optimization of MO adsorption

| Factor | Unit | Code | Code level |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | −1 | 0 | 1 |
| LDHs dosage | g | A | 0.1 | 0.2 | 0.3 |
| pH |  | B | 6 | 7 | 8 |
| adsorption time | min | C | 30 | 135 | 240 |

Table S3 Box–Behnken design and results

| Standard order | Run order | Factor level |  |  | Removal ratio (%) |
| --- | --- | --- | --- | --- | --- |
|  |  | A | B | C |  |
| 1 | 15 | 0.1 | 6 | 135 | 72.2 |
| 2 | 5 | 0.3 | 6 | 135 | 81 |
| 3 | 2 | 0.1 | 8 | 135 | 70.3 |
| 4 | 12 | 0.3 | 8 | 135 | 81 |
| 5 | 13 | 0.1 | 7 | 30 | 68.8 |
| 6 | 6 | 0.3 | 7 | 30 | 77.6 |
| 7 | 4 | 0.1 | 7 | 240 | 83 |
| 8 | 9 | 0.3 | 7 | 240 | 92.4 |
| 9 | 10 | 0.2 | 6 | 30 | 74.1 |
| 10 | 3 | 0.2 | 8 | 30 | 77.5 |
| 11 | 8 | 0.2 | 6 | 240 | 88 |
| 12 | 7 | 0.2 | 8 | 240 | 87.2 |
| 13 | 11 | 0.2 | 7 | 135 | 85.3 |
| 14 | 14 | 0.2 | 7 | 135 | 84.9 |
| 15 | 1 | 0.2 | 7 | 135 | 83.8 |

Table S4 ANOVA for the response surface model of MO adsorption

| Source | Sum of squares | df | Mean square | F-value | P-value |
| --- | --- | --- | --- | --- | --- |
| Model | 663.38 | 9 | 73.71 | 48.53 | 0.0002 |
| A-LDHs dosage | 177.66 | 1 | 177.66 | 116.97 | 0.0001 |
| B-pH | 0.0612 | 1 | 0.0612 | 0.0403 | 0.8488 |
| C-adsorption time | 345.85 | 1 | 345.85 | 227.70 | <0.0001 |
| AB | 0.9025 | 1 | 0.9025 | 0.5942 | 0.4756 |
| AC | 0.0900 | 1 | 0.0900 | 0.0593 | 0.8173 |
| BC | 4.41 | 1 | 4.41 | 2.90 | 0.1491 |
| A2 | 88.50 | 1 | 88.50 | 58.27 | 0.0006 |
| B2 | 49.08 | 1 | 49.08 | 32.31 | 0.0023 |
| C2 | 1.70 | 1 | 1.70 | 1.12 | 0.3381 |
| Residual | 7.59 | 5 | 1.52 |  |  |
| Lack of fit | 6.39 | 3 | 2.13 | 3.53 | 0.2286 |
| Pure error | 1.21 | 2 | 0.6033 |  |  |
| Total | 670.97 | 14 |  |  |  |

Figure S5 Comparison between the predicted and actual values of MO removal

Figure S6 Three-dimensional surface plots and contour plots for the interactive effects of LDHs dosage and pH (a, a1), LDHs dosage and adsorption time (b, b1), and adsorption time and pH (c, c1) on MO removal

Table S5 Experimental factors and levels for response surface optimization of Cr(VI) adsorption

| Factor | Unit | Code | Code level |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | −1 | 0 | 1 |
| LDHs dosage | g | A | 0.1 | 0.15 | 0.2 |
| pH |  | B | 5 | 6 | 7 |
| adsorption time | min | C | 30 | 45 | 60 |

Table S6 Box–Behnken design and experimental results for Cr(VI) removal

| Standard order | Run order | Factor level |  |  | Removal ratio (%) |
| --- | --- | --- | --- | --- | --- |
|  |  | A | B | C |  |
| 1 | 15 | 0.1 | 5 | 45 | 83.6 |
| 2 | 8 | 0.2 | 5 | 45 | 89.8 |
| 3 | 7 | 0.1 | 7 | 45 | 81.3 |
| 4 | 10 | 0.2 | 7 | 45 | 87 |
| 5 | 13 | 0.1 | 6 | 30 | 79.1 |
| 6 | 4 | 0.2 | 6 | 30 | 85.4 |
| 7 | 5 | 0.1 | 6 | 60 | 83.1 |
| 8 | 14 | 0.2 | 6 | 60 | 90.7 |
| 9 | 9 | 0.15 | 5 | 30 | 85.1 |
| 10 | 2 | 0.15 | 7 | 30 | 79.9 |
| 11 | 6 | 0.15 | 5 | 60 | 88.6 |
| 12 | 3 | 0.15 | 7 | 60 | 86.3 |
| 13 | 12 | 0.15 | 6 | 45 | 87.7 |
| 14 | 1 | 0.15 | 6 | 45 | 86.9 |
| 15 | 11 | 0.15 | 6 | 45 | 87.8 |

Table S7 ANOVA for the response surface model of Cr(VI) adsorption

| Source | Sum of squares | df | Mean square | F-value | P-value |
| --- | --- | --- | --- | --- | --- |
| Model | 200.05 | 9 | 22.23 | 45.38 | 0.0003 |
| A-LDHs dosage | 105.85 | 1 | 105.85 | 216.10 | <0.0001 |
| B-pH | 19.53 | 1 | 19.53 | 39.87 | 0.0015 |
| C-adsorption time | 59.40 | 1 | 59.40 | 121.28 | 0.0001 |
| AB | 0.3600 | 1 | 0.3600 | 0.7349 | 0.4304 |
| AC | 2.72 | 1 | 2.72 | 5.56 | 0.0649 |
| BC | 1.56 | 1 | 1.56 | 3.19 | 0.1342 |
| A2 | 0.6933 | 1 | 0.6933 | 1.42 | 0.2876 |
| B2 | 3.22 | 1 | 3.22 | 6.57 | 0.0505 |
| C2 | 7.85 | 1 | 7.85 | 16.03 | 0.0103 |
| Residual | 2.45 | 5 | 0.4898 |  |  |
| Lack of fit | 1.00 | 3 | 0.3342 | 0.4620 | 0.7381 |
| Pure error | 1.45 | 2 | 0.7233 |  |  |
| Total | 202.50 | 14 |  |  |  |

Figure S7 Comparison between the predicted and actual values of Cr(VI) removal

Figure S8 Three-dimensional surface plots and contour plots for the interactive effects of LDHs dosage and pH (a, a1), LDHs dosage and adsorption time (b, b1), and adsorption time and pH (c, c1) on Cr(VI) removal

# # These authors contributed equally to this work and should be considered co-first authors.

# Corresponding author. College of Materials Science and Engineering, Taiyuan University of Technology, Taiyuan 030024, P.R. China

E-mail address: yanhong@tyut.edu.cn (H. Yan).