Table 1: Comparison of the data obtained from Debye-Scherrer's relation and W-H plot

	Parameters
	Debye-Scherrer's relation
	W-H plot

	Crystallite Size  (D)
	29.6 (nm)
	45.26 (nm)

	Microstrain (ε) 
	4.7601 × 10-3
	3.97 × 10-3

	Dislocation density(δ) 
	11.41×1014/m2
	4.8816×1014/m2



