Table 1: Comparison of the data obtained from Debye-Scherrer's relation and W-H plot

| Parameters | Debye-Scherrer's relation | W-H plot |
| --- | --- | --- |
| Crystallite Size (D) | 29.6 (nm) | 45.26 (nm) |
| Microstrain (ε) | 4.7601 × 10-3 | 3.97 × 10-3 |
| Dislocation density(δ) | 11.41×1014/m2 | 4.8816×1014/m2 |