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Dataset Name	1-zno
File name	C:\Users\alzahra\Desktop\03-08-01\03-08-01-Dr hosseinzade\1-zno\1-zno.raw
Raw Data Origin	Rigaku-binary (.RAW)
Scan Axis	Gonio
Start Position [°2Th.]	6.0000
End Position [°2Th.]	80.0000
Step Size [°2Th.]	0.0400
Scan Step Time [s]	1.0000
Scan Type	Pre-set time
Offset [°2Th.]	0.0000
Divergence Slit Type	Fixed
Divergence Slit Size [°]	1.0000
Specimen Length [mm]	10.00
Receiving Slit Size [mm]	0.1000
Measurement Temperature [°C]	25.00
Anode Material	Cu
K-Alpha1 [?]	1.54060
K-Alpha2 [?]	1.54443
K-Beta [?]	1.39225
K-A2 / K-A1 Ratio	0.50000
Generator Settings	0 mA, 0 kV
Diffractometer Number	0
Goniometer Radius [mm]	240.00
Dist. Focus-Diverg. Slit [mm]	91.00
Incident Beam Monochromator	No
Spinning	No
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	Pos. [°2Th.]
	Height [cts]
	FWHM Left [°2Th.]
	d-spacing [?]
	Rel. Int. [%]
	Tip Width
	Matched by

	20.7432
	326.74
	0.2755
	4.28224
	4.15
	0.3306
	

	21.2463
	423.36
	0.2362
	4.18195
	5.38
	0.2834
	

	23.6746
	19.63
	0.4723
	3.75823
	0.25
	0.5668
	

	25.3605
	18.04
	0.4723
	3.51208
	0.23
	0.5668
	

	30.3232
	285.87
	0.1574
	2.94765
	3.63
	0.1889
	

	31.8988
	4357.21
	0.4330
	2.80557
	55.36
	0.5196
	

	33.1323
	82.67
	0.3542
	2.70388
	1.05
	0.4251
	

	34.5489
	3559.75
	0.2755
	2.59619
	45.23
	0.3306
	

	34.7354
	2816.78
	0.1181
	2.58268
	35.79
	0.1417
	

	36.4081
	7870.12
	0.4330
	2.46777
	100.00
	0.5196
	

	40.4692
	25.48
	0.3149
	2.22901
	0.32
	0.3779
	

	41.8575
	9.37
	1.2595
	2.15824
	0.12
	1.5114
	

	45.5848
	30.61
	0.3936
	1.99006
	0.39
	0.4723
	

	46.4410
	71.69
	0.3936
	1.95535
	0.91
	0.4723
	

	47.6930
	1738.49
	0.4330
	1.90690
	22.09
	0.5196
	

	52.0945
	92.82
	0.4723
	1.75567
	1.18
	0.5668
	

	55.3594
	84.66
	0.3149
	1.65961
	1.08
	0.3779
	

	56.7369
	2673.19
	0.4330
	1.62255
	33.97
	0.5196
	

	61.6721
	137.76
	0.3542
	1.50402
	1.75
	0.4251
	

	62.9951
	2206.03
	0.4330
	1.47558
	28.03
	0.5196
	

	66.4438
	185.39
	0.1574
	1.40712
	2.36
	0.1889
	

	68.0454
	1798.38
	0.4330
	1.37785
	22.85
	0.5196
	

	69.1735
	815.85
	0.4330
	1.35811
	10.37
	0.5196
	

	72.6445
	127.37
	0.3936
	1.30154
	1.62
	0.4723
	

	77.0137
	264.53
	0.1968
	1.23824
	3.36
	0.2362
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Insert Measurement:
- File name = 1-zno.raw
- Modification time = "10/22/2024 12:56:06 ب.ظ"
- Modification editor = "alzahra"

Determine Background:
- Add to net scan = "User defined intensity"
- User defined intensity = "100"
- Correction method = "Automatic"
- Bending factor = "4"
- Minimum significance = "1"
- Minimum tip width = "0.97"
- Maximum tip width = "5"
- Peak base width = "2"
- Use smoothed input data = "Yes"
- Granularity = "2"
- Modification time = "08/20/2024 02:26:32 ب.ظ"
- Modification editor = "alzahra"

Search Peaks:
- Minimum significance = "2"
- Minimum tip width = "0.01"
- Maximum tip width = "9"
- Peak base width = "19"
- Method = "Top of smoothed peak"
- Modification time = "03/02/2024 12:01:48 ب.ظ"
- Modification editor = "alzahra"
[bookmark: _GoBack]
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