Fantastic report on

1-zno.DOC

Distribution:

| Name | Function | 0.1 | 0.5 | 1.0 |
| --- | --- | --- | --- | --- |
| N.N.-999 | Masterking Group Manager (MGM) |  |  |  |
| N.N.-998 | Product Ontwikkelt Manager (POM) |  |  |  |
| N.N.-1 | (AS) |  |  |  |
| N.N.-2 | (DS) |  |  |  |
| N.N.-3 | (BS) |  |  |  |
| T.P. | Supervisor All Coding |  |  |  |

# Table of Contents:

Table of Contents:	2

Anchor Scan Parameters: (Bookmark1)	3

Graphics: (Bookmark2)	4

Peak List: (Bookmark 3)	5

Identified Patterns List: (Bookmark4)	6

Plot of Identified Phases: (Bookmark 5)	6

Document History: (Bookmark 6)	7

# Anchor Scan Parameters: (Bookmark1)

Dataset Name	1-zno

File name	C:\Users\alzahra\Desktop\03-08-01\03-08-01-Dr hosseinzade\1-zno\1-zno.raw

Raw Data Origin	Rigaku-binary (.RAW)

Scan Axis	Gonio

Start Position [°2Th.]	6.0000

End Position [°2Th.]	80.0000

Step Size [°2Th.]	0.0400

Scan Step Time [s]	1.0000

Scan Type	Pre-set time

Offset [°2Th.]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	1.0000

Specimen Length [mm]	10.00

Receiving Slit Size [mm]	0.1000

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [?]	1.54060

K-Alpha2 [?]	1.54443

K-Beta [?]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	0 mA, 0 kV

Diffractometer Number	0

Goniometer Radius [mm]	240.00

Dist. Focus-Diverg. Slit [mm]	91.00

Incident Beam Monochromator	No

Spinning	No

# Graphics: (Bookmark2)

# Peak List: (Bookmark 3)

| Pos. [°2Th.] | Height [cts] | FWHM Left [°2Th.] | d-spacing [?] | Rel. Int. [%] | Tip Width | Matched by |
| --- | --- | --- | --- | --- | --- | --- |
| 20.7432 | 326.74 | 0.2755 | 4.28224 | 4.15 | 0.3306 |  |
| 21.2463 | 423.36 | 0.2362 | 4.18195 | 5.38 | 0.2834 |  |
| 23.6746 | 19.63 | 0.4723 | 3.75823 | 0.25 | 0.5668 |  |
| 25.3605 | 18.04 | 0.4723 | 3.51208 | 0.23 | 0.5668 |  |
| 30.3232 | 285.87 | 0.1574 | 2.94765 | 3.63 | 0.1889 |  |
| 31.8988 | 4357.21 | 0.4330 | 2.80557 | 55.36 | 0.5196 |  |
| 33.1323 | 82.67 | 0.3542 | 2.70388 | 1.05 | 0.4251 |  |
| 34.5489 | 3559.75 | 0.2755 | 2.59619 | 45.23 | 0.3306 |  |
| 34.7354 | 2816.78 | 0.1181 | 2.58268 | 35.79 | 0.1417 |  |
| 36.4081 | 7870.12 | 0.4330 | 2.46777 | 100.00 | 0.5196 |  |
| 40.4692 | 25.48 | 0.3149 | 2.22901 | 0.32 | 0.3779 |  |
| 41.8575 | 9.37 | 1.2595 | 2.15824 | 0.12 | 1.5114 |  |
| 45.5848 | 30.61 | 0.3936 | 1.99006 | 0.39 | 0.4723 |  |
| 46.4410 | 71.69 | 0.3936 | 1.95535 | 0.91 | 0.4723 |  |
| 47.6930 | 1738.49 | 0.4330 | 1.90690 | 22.09 | 0.5196 |  |
| 52.0945 | 92.82 | 0.4723 | 1.75567 | 1.18 | 0.5668 |  |
| 55.3594 | 84.66 | 0.3149 | 1.65961 | 1.08 | 0.3779 |  |
| 56.7369 | 2673.19 | 0.4330 | 1.62255 | 33.97 | 0.5196 |  |
| 61.6721 | 137.76 | 0.3542 | 1.50402 | 1.75 | 0.4251 |  |
| 62.9951 | 2206.03 | 0.4330 | 1.47558 | 28.03 | 0.5196 |  |
| 66.4438 | 185.39 | 0.1574 | 1.40712 | 2.36 | 0.1889 |  |
| 68.0454 | 1798.38 | 0.4330 | 1.37785 | 22.85 | 0.5196 |  |
| 69.1735 | 815.85 | 0.4330 | 1.35811 | 10.37 | 0.5196 |  |
| 72.6445 | 127.37 | 0.3936 | 1.30154 | 1.62 | 0.4723 |  |
| 77.0137 | 264.53 | 0.1968 | 1.23824 | 3.36 | 0.2362 |  |

# Identified Patterns List: (Bookmark4)

# Plot of Identified Phases: (Bookmark 5)

# Document History: (Bookmark 6)

Insert Measurement:

- File name = 1-zno.raw

- Modification time = "10/22/2024 12:56:06 ب.ظ"

- Modification editor = "alzahra"

Determine Background:

- Add to net scan = "User defined intensity"

- User defined intensity = "100"

- Correction method = "Automatic"

- Bending factor = "4"

- Minimum significance = "1"

- Minimum tip width = "0.97"

- Maximum tip width = "5"

- Peak base width = "2"

- Use smoothed input data = "Yes"

- Granularity = "2"

- Modification time = "08/20/2024 02:26:32 ب.ظ"

- Modification editor = "alzahra"

Search Peaks:

- Minimum significance = "2"

- Minimum tip width = "0.01"

- Maximum tip width = "9"

- Peak base width = "19"

- Method = "Top of smoothed peak"

- Modification time = "03/02/2024 12:01:48 ب.ظ"

- Modification editor = "alzahra"