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Dataset Name	2-Zn Mg
File name	C:\Users\alzahra\Desktop\03-08-01\03-08-01-Dr hosseinzade\2-Zn Mg\2-Zn Mg.raw
Raw Data Origin	Rigaku-binary (.RAW)
Scan Axis	Gonio
Start Position [°2Th.]	6.0000
End Position [°2Th.]	80.0000
Step Size [°2Th.]	0.0400
Scan Step Time [s]	1.0000
Scan Type	Pre-set time
Offset [°2Th.]	0.0000
Divergence Slit Type	Fixed
Divergence Slit Size [°]	1.0000
Specimen Length [mm]	10.00
Receiving Slit Size [mm]	0.1000
Measurement Temperature [°C]	25.00
Anode Material	Cu
K-Alpha1 [?]	1.54060
K-Alpha2 [?]	1.54443
K-Beta [?]	1.39225
K-A2 / K-A1 Ratio	0.50000
Generator Settings	0 mA, 0 kV
Diffractometer Number	0
Goniometer Radius [mm]	240.00
Dist. Focus-Diverg. Slit [mm]	91.00
Incident Beam Monochromator	No
Spinning	No
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	Pos. [°2Th.]
	Height [cts]
	FWHM Left [°2Th.]
	d-spacing [?]
	Rel. Int. [%]
	Tip Width
	Matched by

	20.6888
	244.13
	0.3149
	4.29336
	5.90
	0.3779
	

	21.0645
	374.48
	0.3149
	4.21764
	9.05
	0.3779
	

	30.3269
	435.28
	0.1968
	2.94731
	10.52
	0.2362
	

	31.8755
	2524.34
	0.3936
	2.80757
	60.99
	0.4723
	

	33.1077
	82.75
	0.4723
	2.70583
	2.00
	0.5668
	

	34.7098
	2084.56
	0.3542
	2.58452
	50.37
	0.4251
	

	36.3889
	4138.62
	0.4330
	2.46903
	100.00
	0.5196
	

	36.9654
	580.40
	0.2362
	2.43184
	14.02
	0.2834
	

	39.6053
	6.64
	0.3936
	2.27562
	0.16
	0.4723
	

	41.5976
	21.34
	0.6298
	2.17112
	0.52
	0.7557
	

	42.9393
	3380.51
	0.4723
	2.10634
	81.68
	0.5668
	

	45.5091
	13.42
	0.3149
	1.99320
	0.32
	0.3779
	

	46.2988
	83.71
	0.3936
	1.96102
	2.02
	0.4723
	

	47.7222
	927.22
	0.4330
	1.90580
	22.40
	0.5196
	

	51.9642
	63.97
	0.7085
	1.75977
	1.55
	0.8502
	

	56.6689
	1534.19
	0.4330
	1.62433
	37.07
	0.5196
	

	62.2544
	1641.63
	0.4330
	1.49135
	39.67
	0.5196
	

	63.0284
	1263.42
	0.3936
	1.47489
	30.53
	0.4723
	

	66.4192
	83.35
	0.3936
	1.40758
	2.01
	0.4723
	

	68.0349
	1001.03
	0.4723
	1.37804
	24.19
	0.5668
	

	69.0999
	471.38
	0.3149
	1.35938
	11.39
	0.3779
	

	72.8083
	33.54
	0.4723
	1.29902
	0.81
	0.5668
	

	74.4809
	247.38
	0.2755
	1.27394
	5.98
	0.3306
	

	76.9720
	121.46
	0.4723
	1.23881
	2.93
	0.5668
	

	78.3752
	407.81
	0.1574
	1.22010
	9.85
	0.1889
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Insert Measurement:
- File name = 2-Zn Mg.raw
- Modification time = "10/22/2024 02:22:46 ب.ظ"
- Modification editor = "alzahra"

Determine Background:
- Add to net scan = "User defined intensity"
- User defined intensity = "100"
- Correction method = "Automatic"
- Bending factor = "4"
- Minimum significance = "1"
- Minimum tip width = "0.97"
- Maximum tip width = "5"
- Peak base width = "2"
- Use smoothed input data = "Yes"
- Granularity = "2"
- Modification time = "08/20/2024 02:26:32 ب.ظ"
- Modification editor = "alzahra"

Search Peaks:
- Minimum significance = "2"
- Minimum tip width = "0.01"
- Maximum tip width = "9"
- Peak base width = "19"
- Method = "Top of smoothed peak"
- Modification time = "03/02/2024 12:01:48 ب.ظ"
- Modification editor = "alzahra"

Search & Match:
- Allow pattern shift = "No"
- Auto residue = "Yes"
- Data source = "Profile and peak list"
- Demote unmatched strong = "Yes"
- Multi phase = "Yes"
- Restriction set = "Untitled"
- Restriction = "Restriction set"
- Subset name = ""
- Match intensity = "No"
- Two theta shift = "0"
- Identify = "No"
- Max. no. of accepted patterns = "5"
- Minimum score = "50"
- Min. new lines / total lines = "60"
- Search depth = "10"
- Minimum new lines = "5"
- Minimum scale factor = "0.1"
- Intensity threshold = "0"
- Use line clustering = "Yes"
- Line cluster range = "1.5"
- Search sensitivity = "1.8"
- Use adaptive smoothing = "Yes"
- Smoothing range = "1.5"
- Threshold factor = "3"
- Modification time = "10/22/2024 02:22:56 ب.ظ"
- Modification editor = "alzahra"
[bookmark: _GoBack]
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