Supplementary Information for:

Physics-Informed Machine Learning for Strength Prediction in High-Strength Steels: Microstructural Descriptor Completion versus TS-to-YS Cascade Transfer

Hong Li1, Wanlin Wang1, Kun Dou1*, Artem Okulov2

- School of Metallurgy and Environment, Central South University, Changsha 410083, China.

- M.N. Mikheev Institute of Metal Physics, Ural Branch of the Russian Academy of Sciences, Ekaterinburg 620108, Russia.

Email: Kun.Dou@csu.edu.cn

Supplementary overview

This Supplementary Information provides additional details supporting the conclusions of the main text. It includes dataset definitions, qualitative descriptor encoding rules, model settings, evaluation protocols, benchmark results, and supplementary analyses on model interpretability and robustness. Methodological procedures for dataset construction, descriptor reconstruction, leakage-controlled learning, and performance evaluation are covered in Section 4 of the main text and are only further clarified here where necessary.

Supplementary Note 1. Dataset details and auxiliary descriptor definitions

Two datasets were used in this study: a high-strength steel (HSS) dataset structured under the composition–process–microstructure–property (CPM) framework and an aluminium-alloy dataset under the composition–process–property (CP) framework. Each dataset consisted of 73 samples derived from systematic literature curation, screening, and consolidation.

HSS dataset

The HSS dataset incorporates chemical composition, heat-treatment parameters, microstructural descriptors, and mechanical-property targets (TS and YS). Microstructural descriptors include both quantitative variables (e.g., phase fractions, grain size, dislocation density) and qualitative descriptors (e.g., high-angle grain-boundary ratio, second-phase distribution). Detailed definitions, units, and numerical ranges for all variables are summarized in Supplementary Table S1, while encoding rules for qualitative descriptors are presented in Supplementary Table S3.

Because this dataset originates from heterogeneous sources, microstructural reporting varies across samples. Fig. 1 of the main text outlines descriptor availability and missingness patterns. Reconstruction rules for missing descriptors are described in Section 2.2 of the main text and were implemented strictly within training data to prevent information leakage.

Aluminium-alloy dataset

The aluminium-alloy dataset includes chemical composition, heat-treatment parameters, and mechanical properties (TS and YS), but lacks explicit microstructural descriptors. The variable definitions, units, and ranges are detailed in Supplementary Table S2. This dataset represents a descriptor-limited regime for strength prediction, allowing comparative evaluation of cascade prediction strategies.

Naming convention

All variable names reported in the Supplementary Information follow the same machine-readable format used in the modeling pipeline, ensuring transparency and traceability between raw data, feature selection, and model configurations.

Table S1. Variable definitions, units, and numerical ranges for the HSS dataset.

| Feature group | Content | Description | Min | Max |
| --- | --- | --- | --- | --- |
| Chemical feature | Fe | wt.% | 93.69 | 99.017 |
|  | C |  | 0.025 | 0.62 |
|  | Si |  | 0 | 1.79 |
|  | Mn |  | 0.601 | 4.37 |
|  | Cr |  | 0 | 1.5 |
|  | Ni |  | 0 | 1.68 |
|  | Mo |  | 0 | 0.49 |
|  | Cu |  | 0 | 0.33 |
|  | V |  | 0 | 0.19 |
|  | P |  | 0 | 0.024 |
|  | S |  | 0 | 0.025 |
|  | N |  | 0 | 0.004 |
|  | Al |  | 0 | 1.4 |
|  | Ti |  | 0 | 0.208 |
|  | Nb |  | 0 | 0.05 |
| Heat treatment feature | quenching_tem1 | ℃ | 0 | 1100 |
|  | quenching_tem2 |  | 0 | 900 |
|  | quenching_tem3 |  | 0 | 900 |
|  | tempering_tem1 |  | 0 | 600 |
|  | tempering_tem2 |  | 0 | 300 |
|  | annealing_tem1 |  | 0 | 1250 |
|  | annealing_tem2 |  | 0 | 815 |
|  | quenching_time1 | h | 0 | 3 |
|  | quenching_time2 |  | 0 | 0.05 |
|  | quenching_time3 |  | 0 | 0.05 |
|  | tempering_time1 |  | 0 | 2 |
|  | tempering_time2 |  | 0 | 2 |
|  | annealing_time1 |  | 0 | 3 |
|  | annealing_time2 |  | 0 | 6 |
|  | quenching_cooling1 | 1.Water cooling, 2.Air cooling, 3.Oil cooling, 4.Furnace cooling | 0 | 3 |
|  | quenching_cooling2 |  | 0 | 3 |
|  | quenching_cooling3 |  | 0 | 3 |
|  | tempering_cooling1 |  | 0 | 2 |
|  | tempering_cooling2 |  | 0 | 2 |
|  | annealing_cooling1 |  | 0 | 4 |
|  | annealing_cooling2 |  | 0 | 4 |
|  | forging_ratio | / | 0 | 3 |
| Structural feature | M_volume_fraction | vol.% | 0 | 100 |
|  | F_volume_fraction |  | 0 | 100 |
|  | B_volume_fraction |  | 0 | 66.6 |
|  | A_volume_fraction |  | 0 | 27.8 |
|  | C_volume_fraction |  | 0 | 22 |
|  | grain_size | μm | 0.14 | 84 |
|  | dislocation_density | m-2 | 1.00E+10 | 9.97E+15 |
|  | high_angle_grain_boundary_ratio | Scoring system | 2 | 5 |
|  | second_phase_distribution |  | 0 | 5 |
| Mechanical feature | yield_strength | Mpa | 280 | 2131 |
|  | tensile_strength |  | 400 | 2450 |

Table S2. Variable definitions, units, and numerical ranges for the aluminium-alloy dataset.

| Feature group | Content | Description | Min | Max |
| --- | --- | --- | --- | --- |
| Chemical feature | Al | wt.% | 70.22 | 93.96 |
|  | Zn |  | 0 | 27 |
|  | Mg |  | 0 | 4.57 |
|  | Cu |  | 0 | 6.54 |
|  | Zr |  | 0 | 0.26 |
|  | Nd |  | 0 | 0.26 |
|  | Sc |  | 0 | 0.72 |
|  | Fe |  | 0 | 0.3 |
|  | Si |  | 0 | 10.55 |
|  | Mn |  | 0 | 0.71 |
|  | Ti |  | 0 | 0.14 |
|  | Sr |  | 0 | 0.024 |
|  | V |  | 0 | 0.03 |
|  | Ce |  | 0 | 0.2 |
| Heat treatment feature | ST_tem1 | ℃ | 0 | 540 |
|  | ST_tem2 |  | 0 | 500 |
|  | AT_tem1 |  | 0 | 300 |
|  | AT_tem2 |  | 0 | 170 |
|  | AT_tem3 |  | 0 | 25 |
|  | AT_tem4 |  | 0 | 80 |
|  | ST_time1 | h | 0 | 16 |
|  | ST_time2 |  | 0 | 2 |
|  | AT_time1 |  | 0 | 132 |
|  | AT_time2 |  | 0 | 1440 |
|  | AT_time3 |  | 0 | 24 |
|  | AT_time4 |  | 0 | 34 |
|  | ST_cooling1 | 1.Water cooling, 2.Air cooling, 3.Oil cooling, 4.Others | 0 | 4 |
|  | ST_cooling2 |  | 0 | 2 |
|  | AT_cooling1 |  | 0 | 4 |
|  | AT_cooling2 |  | 0 | 2 |
|  | AT_cooling3 |  | 0 | 2 |
|  | AT_cooling4 |  | 0 | 2 |
| Mechanical feature | yield_strength | Mpa | 81.9 | 673.1 |
|  | tensile_strength |  | 199.7 | 739.7 |

Table S3. (a)Rule-based encoding scheme for second-phase distribution in the HSS dataset

| Score | Distribution characteristics | Representative reported descriptions* | Expected metallurgical implication |
| --- | --- | --- | --- |
| 5 | Uniformly dispersed distribution with fine particle size, consistent spacing, and no obvious local clustering or segregation | “uniform”, “homogeneous”, “finely dispersed”, “uniformly distributed precipitates/particles” | Strong strengthening contribution and favorable strength–toughness balance |
| 4 | Relatively uniform dispersed distribution, with slight local non-uniformity or moderate variation in particle size or spacing | “relatively uniform”, “mostly dispersed”, “fairly homogeneous”, “slightly non-uniform dispersion” | Good strengthening effect, slightly weaker than the ideal dispersed state |
| 3 | Mixed or bi-heterogeneous distribution, with coexisting dispersed and clustered regions | “heterogeneous distribution”, “mixed distribution”, “partly dispersed and partly aggregated”, “dual distribution” | Moderate and spatially variable strengthening effect |
| 2 | Clearly non-uniform distribution with local clustering, segregation, or preferential distribution along grain or phase boundaries | “non-uniform”, “clustered”, “segregated”, “boundary-decorated”, “agglomerated” | Often associated with unstable strengthening and possible toughness reduction |
| 1 | Severe localization at specific sites such as grain boundaries, phase boundaries, or other defect-rich regions, often forming coarse or continuous second phases | “localized at grain boundaries”, “continuous boundary phase”, “severe segregation”, “coarse boundary particles” | Typically detrimental to toughness and fatigue resistance; may promote crack initiation |
| 0 | No second phase reported, or distribution information unavailable, invalid, or too ambiguous for defensible scoring | “none”, blank entry, unspecified “carbide” or “precipitate” without distribution description, “not detected” | Non-informative state for this descriptor in the present dataset |

Table S3. (b) Rule-based encoding scheme for high-angle grain-boundary ratio in the HSS dataset.

| Score | Approximate reported range or qualitative level | Representative reported descriptions* | Expected metallurgical implication |
| --- | --- | --- | --- |
| 5 | High fraction of high-angle grain boundaries, typically corresponding to an upper-range interval in the reported source | “high HAGB fraction”, “predominantly high-angle boundaries”, “large proportion of HAGBs” | Generally associated with stronger grain-boundary strengthening potential and more effective interruption of slip transfer |
| 4 | Moderately high high-angle grain-boundary fraction | “relatively high HAGB fraction”, “substantial fraction of high-angle boundaries” | Favorable contribution to strength and microstructural stability, but weaker than the highest category |
| 3 | Intermediate high-angle grain-boundary fraction | “moderate HAGB fraction”, “mixed boundary character”, “intermediate proportion of high-angle boundaries” | Intermediate contribution to boundary-related strengthening |
| 2 | Low high-angle grain-boundary fraction, typically corresponding to a lower-range interval in the reported source | “low HAGB fraction”, “mostly low-angle boundaries”, “limited high-angle boundaries” | Relatively weak boundary-related strengthening contribution |
| Unassigned | Not scored when no defensible interval or qualitative boundary-character description was reported | vague or absent boundary-character description | Treated as unavailable rather than arbitrarily encoded |

Supplementary Note 2. Model-development settings

2.1. Candidate models and retained-feature budgets

To ensure fair comparisons across descriptor regimes and modelling strategies, matched retained-feature budgets of 10, 12, and 15 features were imposed for all candidate models in each prediction task. This controlled input dimensionality allowed performance differences to be attributed solely to descriptor content and modelling approach, rather than unequal feature counts.

Candidate regressors included random forest (RF), gradient boosting (GB), extreme gradient boosting (XGB), and support vector regression (SVR). A voting-based ensemble (VOTE) was constructed from tuned base learners but did not involve an independent hyperparameter search space. All model fitting, feature selection, and hyperparameter optimization were conducted strictly within the training folds of cross-validation splits to prevent information leakage.

Detailed feature-selection procedures, Bayesian optimization search spaces, and final hyperparameter settings are provided in Supplementary Tables S4–S6.

Table S4. Feature-selection settings and retained-feature budgets.

| Item | Setting used in this study | Description / purpose |
| --- | --- | --- |
| Feature selector | Custom SymmetricFeatureSelector | Training-pipeline-embedded selector used to enforce matched feature dimensionality across compared models |
| Selection principle | Composite ranking of linear and nonlinear relevance | Balances univariate target association and embedded model-based importance |
| Linear relevance component | f_regression F-statistic | Measures linear association between each feature and the target |
| Nonlinear relevance component | RandomForestRegressor.feature_importances_ | Captures nonlinear predictive contribution and interaction-related importance |
| Random forest size for scoring | rf_n_estimators = 300 | Number of trees used in the random forest for feature-importance estimation |
| Random state for feature selection | random_state = 42 | Fixed seed for reproducibility of random-forest-based scoring |
| Score normalization | Min-max normalization applied separately to F scores and RF scores | Places the two score components on a comparable scale before combination |
| Composite score | Si=αF~i+(1−α)R~iSi​=αF~i​+(1−α)R~i​ | Final ranking score for feature ii |
| Weighting coefficient | α=0.5α=0.5* | Gives equal weight to normalized linear and nonlinear relevance components |
| Non-finite score handling | NaN, +inf, and -inf replaced with 0 before normalization | Improves numerical robustness |
| Feature ranking direction | Descending order of composite score | Highest-ranked features retained |
| Retained-feature rule | Top kk ranked features retained | Ensures equal feature-count budget across compared models within a task |
| Supported k mode | Integer kk or k = "all" | If k = "all", all available features are preserved |
| Effective retained-feature count | min(k,p)min(k,p) when k≠all | Prevents requesting more features than the available input dimensionality pp |
| Retained-feature budgets evaluated | 10, 12, and 15 | Matched feature budgets used in benchmark comparisons |
| Output artifacts archived | Support mask, selected indices, raw scores, normalized scores, composite scores | Enables traceability and post hoc inspection |
| Fitting scope | Training fold only | Prevents information leakage during nested cross-validation and cascade construction |

Table S5. Hyperparameter search spaces for candidate models.

| Model | Hyperparameter | 10-feature setting | 12-feature setting | 15-feature setting | Notes |
| --- | --- | --- | --- | --- | --- |
| RF | n_estimators | 120–300 | fixed: 200 | 150–400 | Integer when optimized |
| RF | max_depth | 2–6 | 2–6 | 3–10 | Integer |
| RF | min_samples_split | 4–10 | 4–10 | 2–8 | Integer |
| RF | min_samples_leaf | 2–5 | 2–4 | 1–4 | Integer |
| RF | max_features | 2–10 | 3–7 | encoded by max_features_code | 10/12: integer range; 15: categorical mapping |
| RF | max_features_code | — | — | 0–3 | Mapped to "sqrt", "log2", 0.5, 0.7 |
| RF | random_state | fixed: 42 | fixed: 42 | fixed: 42 | Not optimized |
| RF | n_jobs | fixed: 1 | fixed: 1 | fixed: 1 | Not optimized |
| XGB | n_estimators | 40–140 | fixed: 80 | 50–180 | Integer when optimized |
| XGB | max_depth | 2–3 | fixed: 2 | 2–4 | Integer when optimized |
| XGB | learning_rate | 0.03–0.15 | 0.03–0.10 | 0.03–0.12 | Continuous |
| XGB | min_child_weight | 2–8 | 4–10 | 3–10 | Integer |
| XGB | subsample | 0.6–1.0 | 0.8–1.0 | 0.7–1.0 | Continuous |
| XGB | colsample_bytree | 0.5–1.0 | 0.6–1.0 | 0.7–1.0 | Continuous |
| XGB | reg_lambda | 1.0–12.0 | 3.0–15.0 | 1.0–10.0 | Continuous |
| XGB | random_state | fixed: 42 | fixed: 42 | fixed: 42 | Not optimized |
| XGB | n_jobs | fixed: 1 | fixed: 1 | fixed: 1 | Not optimized |
| XGB | verbosity | fixed: 0 | fixed: 0 | fixed: 0 | Not optimized |
| GB | n_estimators | 60–180 | 50–200 | 50–200 | Integer |
| GB | learning_rate | 0.03–0.12 | 0.03–0.12 | 0.03–0.12 | Continuous |
| GB | subsample | 0.7–1.0 | 0.7–1.0 | 0.7–1.0 | Continuous |
| GB | min_samples_split | 4–10 | 2–8 | 2–8 | Integer |
| GB | min_samples_leaf | 2–6 | 2–5 | 2–5 | Integer |
| GB | max_depth | 1–3 | 2–3 | 2–3 | Integer |
| GB | max_features | 2–10 | encoded by max_features_code | encoded by max_features_code | 10: integer range; 12/15: categorical mapping |
| GB | max_features_code | — | 0–3 | 0–3 | Mapped to "sqrt", "log2", 0.5, 0.7 |
| GB | random_state | fixed: 42 | fixed: 42 | fixed: 42 | Not optimized |
| SVR | C | 10−110−1–102102 | 0.5–100.0 | 0.5–100.0 | 10-feature: log-scaled; 12/15: linear continuous |
| SVR | gamma | 10−3.510−3.5–10−0.510−0.5 | 0.0001–0.1 | 0.0001–0.1 | 10-feature: log-scaled; 12/15: linear continuous |
| SVR | epsilon | 0.01–0.25 | 0.01–0.20 | 0.01–0.20 | Continuous |
| SVR | kernel | fixed: rbf | fixed: rbf | fixed: rbf | Not optimized |

Table S6. Final hyperparameter settings of representative anchor and top-performing configurations.

| Role | Setting | Final model | Final hyperparameter settings | Selected features | Inner-CV OOF R2 |
| --- | --- | --- | --- | --- | --- |
| Representative anchor | 10-feature, Direct-CP | GB | n_estimators=99; learning_rate=0.03; subsample=0.8740; min_samples_split=5; min_samples_leaf=6; max_depth=3; max_features=2; random_state=42 | Fe, C, Si, Mn, Cr, V, Nb, quenching_tem1, quenching_cooling1, tempering_tem1 | 0.8077 |
| Top-performing comparison | 10-feature, Direct-CPM | XGB | n_estimators=70; max_depth=3; learning_rate=0.0888; min_child_weight=2; subsample=0.8404; colsample_bytree=0.5; reg_lambda=1.0; random_state=42; n_jobs=1; verbosity=0 | C, Si, Mn, Cr, V, quenching_tem1, quenching_cooling1, M_volume_fraction, F_volume_fraction, grain_size | 0.8509 |
| Representative anchor | 12-feature, Direct-CP | GB | n_estimators=182; learning_rate=0.03; subsample=0.7; min_samples_split=2; min_samples_leaf=3; max_depth=2; max_features="sqrt"; random_state=42 | Fe, C, Si, Mn, Cr, V, Al, Nb, quenching_tem1, quenching_cooling1, tempering_tem1, annealing_tem2 | 0.8214 |
| Top-performing comparison | 12-feature, Cascade-CP, stage 1 (predicted_tensile_strength) | GB | n_estimators=50; learning_rate=0.12; subsample=1.0; min_samples_split=8; min_samples_leaf=2; max_depth=3; max_features="sqrt"; random_state=42 | Fe, C, Si, Mn, Cr, Ni, Mo, V, Nb, quenching_tem1, quenching_cooling1, annealing_tem2 | 0.9005 |
| Top-performing comparison | 12-feature, Cascade-CP, stage 2 | GB | n_estimators=179; learning_rate=0.0510; subsample=0.7924; min_samples_split=2; min_samples_leaf=5; max_depth=2; max_features="sqrt"; random_state=42 | Fe, C, Si, Mn, Cr, V, Al, Nb, quenching_tem1, quenching_cooling1, tempering_tem1, predicted_tensile_strength | 0.808 |
| Top-performing comparison | 12-feature, Direct-CPM | GB | n_estimators=105; learning_rate=0.12; subsample=1.0; min_samples_split=7; min_samples_leaf=2; max_depth=2; max_features="log2"; random_state=42 | C, Si, Mn, Cr, V, Nb, quenching_tem1, quenching_cooling1, M_volume_fraction, F_volume_fraction, grain_size, dislocation_density | 0.8428 |
| Top-performing comparison | 12-feature, Cascade-CPM, stage 1 (predicted_tensile_strength) | GB | n_estimators=192; learning_rate=0.1106; subsample=0.8157; min_samples_split=6; min_samples_leaf=4; max_depth=3; max_features=0.5; random_state=42 | Fe, C, Si, Mn, Cr, V, Nb, quenching_tem1, quenching_cooling1, M_volume_fraction, F_volume_fraction, dislocation_density | 0.9298 |
| Top-performing comparison | 12-feature, Cascade-CPM, stage 2 | GB | n_estimators=179; learning_rate=0.0814; subsample=0.8882; min_samples_split=2; min_samples_leaf=5; max_depth=3; max_features="sqrt"; random_state=42 | C, Si, Mn, Cr, V, quenching_tem1, quenching_cooling1, M_volume_fraction, F_volume_fraction, grain_size, dislocation_density, predicted_tensile_strength | 0.836 |

2.2. Symmetric feature selector

Feature selection was performed using a custom SymmetricFeatureSelector implemented in a scikit-learn-compatible style and embedded within the training-only modelling pipeline. The selector is termed symmetric because the same retained-feature budget was imposed across compared descriptor spaces and candidate models within a given prediction task. This design reduces the confounding effect of unequal input dimensionality, which is especially important in small, high-dimensional literature-derived datasets.

For each input feature, two complementary relevance measures were computed from the training data. First, the univariate F-statistic from f_regression was used to quantify linear association with the target variable. Second, a RandomForestRegressor was used to estimate nonlinear feature importance through feature_importances_, thereby capturing nonlinear predictive contribution and interaction-related effects. In the present implementation, the random forest used for feature scoring employed 300 trees (rf_n_estimators = 300) with random_state = 42.

Because the two scoring components are defined on different numerical scales, each score vector was independently normalized by min-max scaling. For a feature-level score vector x, the normalized score was defined as:

xi=xi-min⁡(x)maxx-min⁡(x)

and the final composite ranking score for feature i was computed as:

Si=αFi+(1-α)Ri

where Fi and Ri denote the normalized linear and nonlinear relevance scores, respectively, and α=0.5 assigns equal weight to the two components.

All feature scoring, ranking, and selection steps were performed within the training fold only at every stage of model development, including nested cross-validation and cascade construction, thereby preventing information leakage from validation or test data.

Supplementary Note 3. Repeated random-split evaluation and anchor selection

Repeated random-split evaluation was performed to assess whether conclusions from the fixed single train/test split remained reproducible under alternative data partitions. In each repeat, samples were randomly divided into training and test subsets using an 8:2 ratio, and all model-development steps—including feature selection, hyperparameter optimization, and cascade-stage training—were repeated using the same leakage-controlled workflow as in the main analysis.

This evaluation was designed as a robustness-oriented anchor analysis, rather than an exhaustive benchmark across all combinations of model type, descriptor regime, retained-feature budget, and prediction route. This choice was motivated by the limited sample size (n = 73 per dataset) and the combinatorially large search space. To minimize post hoc selection bias, anchor configurations were selected a priori based on inner-cross-validated R2 performance on the training set, not on held-out test performance.

For the HSS direct-prediction comparison, the 10-feature gradient boosting (GB) configuration was used as the anchor under the most stringent descriptor-limited setting. For HSS cascade-related comparisons and the aluminium-alloy analysis, the 12-feature GB configuration was selected as the anchor, as it exhibited strong and representative inner-CV performance across tasks. The selected anchor configurations are summarized in Supplementary Table S7.

Across all repeated splits, performance was summarized using the mean and standard deviation of test R2, RMSE, and MAE. These statistics were used in the main text to compare both average predictive performance and sensitivity to data partitioning.

Table S7. Anchor configurations used for repeated random-split evaluation in HSS system.

For the repeated random-split comparisons, two-sided t-based 95% confidence intervals were calculated for the within-seed paired metric differences across the 10 matched partitions as d±t0.975,9sd/10, where d and sd are the mean and sample standard deviation of the paired differences, respectively. Because the repeated partitions shared observations, these intervals quantify partition-induced uncertainty within the present datasets rather than uncertainty estimated from independent external samples. The corresponding results are shown in Table S8.

Table S7. The selected anchor configurations

| Budget | Route | Descriptor | Seed | OOF R2 | Test R2 |
| --- | --- | --- | --- | --- | --- |
| 10 | direct | CP | 11 | 0.765543 | 0.925172 |
| 10 | direct | CP | 22 | 0.836151 | 0.801275 |
| 10 | direct | CP | 33 | 0.798397 | 0.892187 |
| 10 | direct | CP | 44 | 0.780376 | 0.932675 |
| 10 | direct | CP | 55 | 0.802537 | 0.72968 |
| 10 | direct | CP | 66 | 0.860996 | 0.886955 |
| 10 | direct | CP | 77 | 0.844098 | 0.654748 |
| 10 | direct | CP | 88 | 0.792919 | 0.930162 |
| 10 | direct | CP | 99 | 0.775187 | 0.879568 |
| 10 | direct | CP | 111 | 0.805075 | 0.814438 |
| 10 | direct | CPM | 11 | 0.876794 | 0.892261 |
| 10 | direct | CPM | 22 | 0.840967 | 0.873171 |
| 10 | direct | CPM | 33 | 0.84128 | 0.871102 |
| 10 | direct | CPM | 44 | 0.829686 | 0.91284 |
| 10 | direct | CPM | 55 | 0.776455 | 0.767387 |
| 10 | direct | CPM | 66 | 0.788439 | 0.906436 |
| 10 | direct | CPM | 77 | 0.829317 | 0.705699 |
| 10 | direct | CPM | 88 | 0.826423 | 0.940094 |
| 10 | direct | CPM | 99 | 0.821183 | 0.868437 |
| 10 | direct | CPM | 111 | 0.816159 | 0.798559 |
| 12 | direct | CP | 42 | 0.812805 | 0.860821 |
| 12 | direct | CP | 43 | 0.847727 | 0.762546 |
| 12 | direct | CP | 44 | 0.842629 | 0.9717 |
| 12 | direct | CP | 45 | 0.753496 | 0.906438 |
| 12 | direct | CP | 46 | 0.832599 | 0.883394 |
| 12 | direct | CP | 47 | 0.841628 | 0.872383 |
| 12 | direct | CP | 48 | 0.788294 | 0.857097 |
| 12 | direct | CP | 49 | 0.819846 | 0.859674 |
| 12 | direct | CP | 50 | 0.86003 | 0.833433 |
| 12 | direct | CP | 51 | 0.898604 | 0.794328 |
| 12 | direct | CPM | 42 | 0.837021 | 0.857204 |
| 12 | direct | CPM | 43 | 0.871764 | 0.827616 |
| 12 | direct | CPM | 44 | 0.874603 | 0.900442 |
| 12 | direct | CPM | 45 | 0.779662 | 0.866579 |
| 12 | direct | CPM | 46 | 0.769417 | 0.848967 |
| 12 | direct | CPM | 47 | 0.881752 | 0.812787 |
| 12 | direct | CPM | 48 | 0.815545 | 0.891074 |
| 12 | direct | CPM | 49 | 0.832771 | 0.884234 |
| 12 | direct | CPM | 50 | 0.879372 | 0.861324 |
| 12 | direct | CPM | 51 | 0.908537 | 0.837821 |
| 12 | cascade | CP | 42 | 0.802224 | 0.839385 |
| 12 | cascade | CP | 43 | 0.843334 | 0.801526 |
| 12 | cascade | CP | 44 | 0.777302 | 0.978595 |
| 12 | cascade | CP | 45 | 0.707378 | 0.895846 |
| 12 | cascade | CP | 46 | 0.80305 | 0.859016 |
| 12 | cascade | CP | 47 | 0.774296 | 0.860058 |
| 12 | cascade | CP | 48 | 0.739738 | 0.803437 |
| 12 | cascade | CP | 49 | 0.762674 | 0.850129 |
| 12 | cascade | CP | 50 | 0.815963 | 0.823602 |
| 12 | cascade | CP | 51 | 0.857331 | 0.741505 |
| 12 | cascade | CPM | 42 | 0.813952 | 0.890144 |
| 12 | cascade | CPM | 43 | 0.84518 | 0.769073 |
| 12 | cascade | CPM | 44 | 0.829683 | 0.877926 |
| 12 | cascade | CPM | 45 | 0.764848 | 0.880767 |
| 12 | cascade | CPM | 46 | 0.755805 | 0.859358 |
| 12 | cascade | CPM | 47 | 0.865894 | 0.802285 |
| 12 | cascade | CPM | 48 | 0.770618 | 0.889666 |
| 12 | cascade | CPM | 49 | 0.817744 | 0.891785 |
| 12 | cascade | CPM | 50 | 0.826355 | 0.830009 |
| 12 | cascade | CPM | 51 | 0.887395 | 0.81277 |

Table S8. Repeated random-split performance and paired 95% confidence intervals for the principal strategy comparisons.

| Prediction task | Strategy comparison | Reference mean R² | Alternative mean R² | Mean paired ΔR² | Paired 95% CI |
| --- | --- | --- | --- | --- | --- |
| TS, 10 features | CP direct vs CPM direct | 0.889 | 0.902 | 0.013 | −0.005 to 0.031 |
| YS, 10 features | CP direct vs CPM direct | 0.845 | 0.854 | 0.009 | −0.016 to 0.034 |
| YS, 12 features | CP direct vs CP cascade | 0.861 | 0.845 | −0.015 | −0.071 to 0.041 |
| YS, 12 features | CPM direct vs CPM cascade | 0.858 | 0.850 | −0.008 | −0.027 to 0.011 |

Supplementary Note 4. Full benchmark results

This section provides the consolidated inner-cross-validated R2 benchmark results underlying all comparisons in the main text, reporting only the inner-cross-validated R2—the metric used for model selection during hyperparameter optimization. All other performance metrics (test R2, RMSE, MAE) are reported in the main text.

Table S9. Consolidated inner-cross-validated R2 benchmark results.

| System | Target | Descriptor regime | Route | Retained features | RF | XGB | GB | SVR | VOTE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HSS | TS | CP | Direct | 10 | 0.8604 | 0.8505 | 0.8849 | 0.0737 | 0.8686 |
| HSS | TS | CP | Direct | 12 | 0.8653 | 0.87 | 0.9005 | 0.6704 | 0.8625 |
| HSS | TS | CP | Direct | 15 | 0.92 | 0.9297 | 0.9332 | 0.6445 | 0.9135 |
| HSS | TS | CPM | Direct | 10 | 0.8799 | 0.8952 | 0.9203 | 0.1171 | 0.902 |
| HSS | TS | CPM | Direct | 12 | 0.8992 | 0.9227 | 0.9298 | 0.7455 | 0.9111 |
| HSS | TS | CPM | Direct | 15 | 0.9259 | 0.9351 | 0.9425 | 0.6232 | 0.923 |
| HSS | YS | CP | Direct | 10 | 0.7758 | 0.7884 | 0.8077 | 0.6432 | 0.7812 |
| HSS | YS | CP | Direct | 12 | 0.7917 | 0.7808 | 0.8214 | 0.6856 | 0.8014 |
| HSS | YS | CP | Direct | 15 | 0.8073 | 0.8142 | 0.845 | 0.7487 | 0.834 |
| HSS | YS | CPM | Direct | 10 | 0.8349 | 0.8509 | 0.8423 | 0.7787 | 0.8462 |
| HSS | YS | CPM | Direct | 12 | 0.8307 | 0.8314 | 0.8428 | 0.6514 | 0.8295 |
| HSS | YS | CPM | Direct | 15 | 0.8387 | 0.8485 | 0.8585 | 0.6581 | 0.8437 |
| HSS | YS | CP | Cascade | 10 | 0.768 | 0.746 | 0.797 | 0.1939 | 0.7723 |
| HSS | YS | CP | Cascade | 12 | 0.7793 | 0.7725 | 0.808 | 0.6951 | 0.7936 |
| HSS | YS | CP | Cascade | 15 | 0.7981 | 0.8097 | 0.8336 | 0.6629 | 0.821 |
| HSS | YS | CPM | Cascade | 10 | 0.8159 | 0.8034 | 0.8351 | 0.2028 | 0.8183 |
| HSS | YS | CPM | Cascade | 12 | 0.8333 | 0.8051 | 0.836 | 0.6684 | 0.8251 |
| HSS | YS | CPM | Cascade | 15 | 0.8408 | 0.8353 | 0.8679 | 0.6884 | 0.8499 |
| HSS | YS | CP | Idealized | 10 | 0.8234 | 0.8776 | 0.8587 | 0.7122 | 0.862 |
| HSS | YS | CP | Idealized | 12 | 0.8359 | 0.8393 | 0.8793 | 0.7008 | 0.8522 |
| HSS | YS | CP | Idealized | 15 | 0.8088 | 0.7954 | 0.8396 | 0.6453 | 0.816 |
| HSS | YS | CPM | Idealized | 10 | 0.8594 | 0.8652 | 0.8464 | 0.7938 | 0.8624 |
| HSS | YS | CPM | Idealized | 12 | 0.8543 | 0.8407 | 0.8652 | 0.6896 | 0.8455 |
| HSS | YS | CPM | Idealized | 15 | 0.8627 | 0.8642 | 0.8728 | 0.7486 | 0.8678 |
| Aluminium | TS | CP | Direct | 10 | 0.8381 | 0.7809 | 0.8106 | 0.4833 | 0.805 |
| Aluminium | TS | CP | Direct | 12 | 0.8543 | 0.7949 | 0.8619 | 0.771 | 0.8372 |
| Aluminium | TS | CP | Direct | 15 | 0.8551 | 0.8461 | 0.8964 | 0.7338 | 0.854 |
| Aluminium | YS | CP | Direct | 10 | 0.8572 | 0.9259 | 0.9035 | 0.756 | 0.8909 |
| Aluminium | YS | CP | Direct | 12 | 0.8671 | 0.8963 | 0.8944 | 0.7288 | 0.8726 |
| Aluminium | YS | CP | Direct | 15 | 0.8865 | 0.9174 | 0.9154 | 0.7189 | 0.8871 |
| Aluminium | YS | CP | Cascade | 10 | 0.8296 | 0.8908 | 0.8789 | 0.5054 | 0.8602 |
| Aluminium | YS | CP | Cascade | 12 | 0.8953 | 0.9095 | 0.9167 | 0.7723 | 0.8966 |
| Aluminium | YS | CP | Cascade | 15 | 0.8816 | 0.917 | 0.9281 | 0.7536 | 0.8987 |

Supplementary Note 5. Software environment and reproducibility statement

All modelling workflows were implemented in Python 3.14.5 using a unified pipeline-based framework for preprocessing, feature selection, hyperparameter optimization, model fitting, and performance evaluation. Thermodynamic estimation of phase fractions was performed using JMatPro (version 7.0) where applicable, and model interpretation was carried out using the SHAP package.