Supplementary Information (SI)

Synthesis of mesoporous SiO2 derived from coal fly ash for methylene blue adsorption

Chen Zhana, Jingwen Wuc, Zegang Fub, *,Jun Yanga,*

a School of Environmental and Municipal Engineering, Lanzhou Jiaotong University, Lanzhou 730070, China

b Key Laboratory of Chemical Engineering in South Xinjiang, College of Chemistry and Chemical Engineering, Tarim University, Alar 843300, PR China

c Key Laboratory of Industrial Ecology and Environmental Engineering, School of Environmental Science & Technology, Dalian University of Technology, Dalian 116024, China

* Corresponding authors.

E-mail address: zegangfu@taru.edu.cn (Z. Fu); yangjun@mail.lzjtu.cn (J. Yang)

Text S1 MB standard calibration curve

The absorbance of the standard methylene blue solutions was determined using a single-wavelength method. A full-wavelength scan was performed on a UV-Vis spectrophotometer over the range of 500-750 nm, revealing that the maximum absorption peak of methylene blue was located at 665 nm. Therefore, an analytical wavelength of 665 nm was employed in this study. A 1 g·L-1 methylene blue solution was prepared as the standard stock solution, and appropriate aliquots were diluted to obtain standard methylene blue solutions with concentrations of 1, 2, 3, 4, 5, 6, and 7 mg·L-1. The absorbance of each solution was measured at 665 nm, and the resulting data were fitted using the least-squares method. As shown in Figure S1, the fitted equation describes the relationship between the MB concentration (CMB) and absorbance (Abs), with a linear regression equation of Abs = 0.0214C + 0.1339 and a correlation coefficient of R2 = 0.9997, indicating excellent linearity.

Figure S1 The methylene blue solution standard curve