Supplementary Information for: Single-fibre internal observability in lithium-ion batteries

This Supplementary Information supports the Nature Communications manuscript “Single-fibre internal observability in lithium-ion batteries”. It provides the mathematical derivations, extended validation results, architecture specifications, training statistics and deployment analyses for FBG-PhysNet, a physics-informed framework for reconstructing internal battery temperature and strain from a single embedded fibre Bragg grating signal. The sections retain the original evidence hierarchy while aligning the supplementary presentation with the Nature Communications framing of single-fibre internal observability.

Section S1: Complete FBG Sensor Physics Derivations

Figure 1. Supplementary Figure S2. Overview of FBG Sensing Challenges and the FBG-PhysNet Processing Pipeline. (Left) Visualization of the physical sensing environment within a 20S6P battery module. The single-FBG configuration presents an ill-posed inverse problem where a single wavelength shift ΔλB must be decoupled into two unknowns: temperature ΔT and mechanical strain ϵ. (Right) The FBG-PhysNet processing architecture utilizing the DynOptic-RWKV7 backbone. By integrating nine physics constraints, the model achieves physical resolution of the coupled signal, resulting in a Cross-Talk (CT) ratio of 58.6% and near-ideal Bragg consistency ( χ2=0.906 ).

S1.1 Electromagnetic Origin of Bragg Reflection

A Fiber Bragg Grating is a periodic perturbation of the refractive index inscribed in the core of a single-mode optical fibre by ultraviolet exposure through a phase mask (See Supplementary Figure S1 for system overview). The perturbation modulates the core index as:

nz=neff+Δndcz+Δnaczcos​2πzΛ+ϕz

where neff is the unperturbed effective refractive index of the guided mode, Δndcz is the DC (mean) index change, Δnacz is the AC (fringe) index modulation amplitude, Λ is the grating period (typically 530 nm for a 1550 nm grating), and ϕz is the grating chirp function. For a uniform, unchirped grating, ϕz=0 and Δndc=Δnac=δn are constants.

The coupled-mode equations governing energy exchange between the forward- and backward-propagating modes are:

dRdz=iσRz+iκSz

dSdz=-iσSz-iκ*Rz

where Rz and Sz are the amplitudes of the forward and backward modes respectively, κ=πΔnac/λ is the coupling coefficient, and the general self-coupling coefficient is:

σ=δ+σdc-12dϕdz

with detuning δ=2πneff1/λ-1/λD relative to the design wavelength λD=2neffΛ and σdc=πΔndc/λ. The phase-matching condition for maximum reflectivity is:

δ+σdc=0⟹λB=2neffΛ1+Δndcneff≈2neffΛ

For the 1550 nm SMF-28 fibre used in this work, neff=1.468 and Λ=527.7 nm.

S1.2 Thermo-Optic Derivation of KT

The temperature sensitivity of the Bragg wavelength arises from two independent physical mechanisms that must be treated separately before combining [1].

Mechanism 1 — Thermo-optic effect. The refractive index of fused silica depends on temperature through the thermo-optic coefficient ξ=neff-1∂neff/∂T. For SMF-28 at 1550 nm and T=298 K:

ξ=1neff∂neff∂T=6.67×10-6 K-1

This coefficient is dominated by the change in electronic polarisability of the silica network with temperature [2], as described by the Sellmeier–Clausius–Mossotti relation. The wavelength shift due to this mechanism is:

∂λB∂TΔn=λBξ=1550 nm×6.67×10-6=1.034×10-2 nm/K

Mechanism 2 — Thermal expansion. Temperature change also physically expands the grating period Λ through the silica linear thermal expansion coefficient αf:

1Λ∂Λ∂T=αf=5.5×10-7 K-1

This contribution is approximately 12× smaller than the thermo-optic effect. The wavelength shift from this mechanism is:

∂λB∂TΔΛ=λBαf=1550 nm×5.5×10-7=8.525×10-4 nm/K

Combined temperature sensitivity. Adding both contributions:

KT=αf+ξ=5.5×10-7+6.67×10-6=7.22×10-6 K-1

The total temperature-induced wavelength shift per Kelvin is therefore KTλB=11.19 pm/K.

S1.3 Photoelastic Derivation of Kε

The strain sensitivity of the Bragg wavelength arises from two coupled effects: the direct geometrical elongation of the grating period, and the indirect change in refractive index through the photoelastic (elasto-optic) effect [3].

Geometrical term. Under axial strain ε=δL/L, the grating period elongates as δΛ/Λ=ε, contributing:

∂λB∂εgeom=λB

Photoelastic term. The strain-induced change in refractive index is described by the Pockels elasto-optic tensor [4]. For uniaxial strain ε along the fibre axis in an isotropic medium:

δneff=-neff32p12-νp11+p12ε

where p11=0.121 and p12=0.270 are the Pockels tensor components for silica, and ν=0.17 is Poisson’s ratio. The effective photoelastic constant is:

pe=neff22p12-νp11+p12=1.468220.270-0.170.121+0.270=0.220

The total strain sensitivity coefficient is therefore:

Kε=1-pe=1-0.220=0.780

The strain-induced wavelength shift per microstrain is KελB=1.209 pm/με.

S1.4 Complete FBG Dual-Sensitivity Equation

Combining Eqs. (S10) and (S14):

ΔλBλB=Kεε+KTΔT

ΔλB=1550×10-90.780 ε+7.22×10-6 ΔT m

The cross-sensitivity ratio KT/Kε=9.26 με/K means that a 1 K temperature change produces the same wavelength shift as a 9.26 μɛ mechanical strain. Over the full dataset range (ΔT∈0,23.52 K, ε∈-78,+415 με), the thermally induced apparent strain ranges up to 23.52×9.26=217.8 με, which is comparable in magnitude to the actual mechanical strain range. This confirms that the decoupling problem is genuinely ill-posed without additional physical constraints.

S1.5 Noise Model and FBG Chi-Squared Statistic

The optical interrogator introduces Gaussian additive noise on the measured wavelength shift:

ΔλBmeas=ΔλBtrue+η,  η∼N0,σλ2, σλ=2.00×10-12 m

Normalising by λB, the relative noise standard deviation is:

σrel=σλλB=2.00×10-121550×10-9=1.29×10-6

The signal-to-noise ratio of the measurement system is:

SNRFBG=20log10​μΔλσλ=20log10​3.271×10-102.00×10-12=44.3 dB

The χFBG2 metric used in the loss function (Eq. S20) is the normalised squared prediction residual in wavelength space:

χFBG2=1σrel2Δλ-ΔλmeasλB2=Δλ-Δλmeas2λB2σrel2

Under perfect Bragg-consistency, EχFBG2=1.0. A value χ2<1 indicates that the model’s Bragg residuals are within the measurement noise floor — the joint prediction lies on the Bragg constraint manifold to within one noise standard deviation. Note that χ² < 1 does not imply the model is “better than the sensor”; it reflects the combined effect of model bias, residual fitting, and the specific Gaussian noise model assumed, while χ2>1 indicates systematic optical inconsistency. FBG-PhysNet achieves χFBG2=0.906 on the validation set. χFBG=0.906 confirms that the model’s FBG residuals are 0.952σrel — within 5% of the measurement noise floor — indicating near-complete optical self-consistency.

Section S2: Complete Electrochemical–Thermal–Mechanical (ECTM) Battery Model

S2.1 Pseudo-Two-Dimensional (P2D) Doyle–Fuller–Newman Model

The ground-truth temperature and strain labels used for training and evaluation were generated by a high-fidelity P2D DFN electrochemical model. This section documents the complete model equations implemented in COMSOL Multiphysics 6.2 [5].

Solid-phase lithium diffusion. Within each spherical active particle of radius Rp, the lithium concentration csr,t obeys Fick’s second law in spherical coordinates:

∂cs∂t=Dsr2∂∂r​r2∂cs∂r

with boundary conditions:

∂cs∂rr=0=0,  -Ds∂cs∂rr=Rp=jnF

where Ds=3.9×10-14 m​2/s is the solid-phase diffusivity (graphite negative electrode), jn [A/m​2] is the intercalation current density, and F=96,485 C/mol is Faraday’s constant. The volume-averaged (bulk) concentration and surface concentration are:

cs=3Rp30Rpcsr,t r2 dr,  css=csRp,t

The state of charge (SOC) of each electrode is:

θ=cscs,max,  SOC=θ-θ0θ100-θ0

Liquid-phase transport. The electrolyte lithium concentration cex,t satisfies:

εe∂ce∂t=∂∂x​Deeff∂ce∂x+1-t+0Fj

where εe is the electrolyte volume fraction, Deeff=Deεe1.5 is the effective electrolyte diffusivity (Bruggeman correction), t+0 is the cation transference number, and j [A/m​3] is the volumetric interfacial current density.

Butler–Volmer kinetics. The interfacial current density at electrode–electrolyte interfaces:

jn=i0​exp​αaFηRT-exp​-αcFηRT

η=ϕs-ϕe-Ucss

i0=Fk0ceαa​cssαa​cs,max-cssαc

where αa=αc=0.5 (symmetric transfer), k0 is the reaction rate constant, ϕs and ϕe are solid- and liquid-phase potentials, and Ucss is the open-circuit voltage as a function of surface lithium concentration.

S2.2 Bernardi Heat Generation Model

The volumetric heat generation rate from electrochemical reactions within the P2D model is given by the Bernardi model:

Q‴total=jnη⏟irreversible+jnT∂U∂T⏟reversible+σseff∥∇ϕs∥2+κeeff∥∇ϕe∥2⏟Ohmic

The three terms represent irreversible activation heat, reversible entropic heat, and Ohmic heat from electronic and ionic conduction respectively. The reversible entropic term can be negative (endothermic) during lithiation at the graphite anode, providing a partial self-cooling effect that is captured in the P2D simulation but approximated by the lumped model [6].

In the lumped thermal model used for the physics loss, these three contributions are consolidated into a single effective Ohmic term:

Qgen≈I2RintT,SOC

RintT,SOC=R0SOCexp​EaR​1T-1Tref

where R0SOC is the SOC-dependent baseline internal resistance at Tref=298.15 K, Ea=2.0×104 J/mol is the activation energy for ionic transport (calibrated for this cell chemistry), and R=8.314 J/(mol·K). For the NMC 811 chemistry used in this study, R0 varies from ~1.2 mΩ at SOC = 0.95 to ~2.5 mΩ at SOC = 0.10 (consistent with the nominal value R0=2.5 mΩ in Table S3).

S2.3 Lumped Thermal Model — Derivation and Discretisation

Integrating the distributed heat equation over the cell volume V yields the lumped ordinary differential equation:

ρCpVdTdt=QgenV-hAsT-Tamb

Dividing through by V and defining ΔT=T-Tamb:

ρCpdΔTdt=Qgen-hAsVΔT

Physical parameters used in this work are tabulated in Supplementary Table S1.

Supplementary Table S1. Thermal Model Parameters

| Symbol | Parameter | Value | Unit |
| --- | --- | --- | --- |
| ρCp | Volumetric heat capacity | 2.50×106 | J m​-3 K​-1 |
| h | Convective heat transfer coefficient | 10.0 | W m​-2 K​-1 |
| As/V | Surface-area-to-volume ratio | 230.0 | m​-1 |
| Tamb | Ambient temperature | 298.15 | K |
| αCTE | Composite thermal expansion coefficient | 1.00×10-5 | K​-1 |
| εmax | Maximum strain rate | 6.00×10-4 | s​-1 |
| εyield | Electrode yield strain | 0.02 | — |

Forward Euler discretisation at Δt=0.01 s gives the PDE residual used in the physics loss:

RPDEk=ρCpΔTk+1-ΔTkΔt-Qgenk+hAsVΔTk

The Courant–Friedrichs–Lewy stability limit for this explicit scheme is Δt≤ρCpV/hAs=1,087 s, which is satisfied with a safety margin of 105 at Δt=0.01 s.

S2.4 Diffusion-Induced Stress and Strain Model

For a spherical electrode particle, the radial σr and tangential σθ stress components arising from non-uniform lithium distribution are:

σrr,t=2ΩE31-ν​1Rp30Rp​Δcs ρ2 dρ-1r30r​Δcs ρ2 dρ

σθr,t=ΩE31-ν​2Rp30Rp​Δcs ρ2 dρ+1r30r​Δcs ρ2 dρ-Δcs

xwhere Ω=3.17×10-6 m​3/mol is the partial molar volume of lithium in graphite, E=10 GPa is Young’s modulus, ν=0.3 is Poisson’s ratio, and Δcs=csr,t-cs is the local concentration deviation from the volume-averaged value.

The macroscopic electrode swelling strain measured by the FBG is dominated by the volume-averaged dilatational strain:

εdis=Ω3Δcs=Ω3cs,max-cs,0ΔSOC

The total FBG-measurable strain decomposes as:

εtotal=εdis+αCTEΔT⏟εth+εel

where εel is the elastic strain arising from structural constraint forces within the cell stack. The ill-posedness of the FBG decoupling problem (Eq. S16) follows directly from this decomposition: even if εel≪εdis, the thermal-expansion coupling εth=αCTEΔT creates an unavoidable correlation between the temperature and strain channels in the FBG signal.

Section S3: RWKV-7 Architecture — Complete Mathematical Specification

S3.1 Token Shift (Data-Dependent Interpolation)

Before processing at layer l and time step k, the input vector hkl is mixed with the previous time step’s input through a learned linear interpolation:

uk=lerphk-1l,hkl;μ=1-μ⊙hk-1l+μ⊙hkl

where μ∈0,1dmodel is a learned vector (not data-dependent) that controls the temporal mixing ratio per feature dimension. Dimensions with μi≈0 effectively look one step back in time (appropriate for slowly varying thermal features), while dimensions with μi≈1 focus on the current step (appropriate for fast mechanical transients). This inductive bias aligns naturally with the different temporal scales of temperature and strain.

Separate μ vectors are learned for receptance μr, key μk, value μv, and decay μw projections, allowing the model to decouple temporal scale selection from feature content selection:

ur=lerphk-1,hk;μr, uk=lerphk-1,hk;μk, uv=lerphk-1,hk;μv

S3.2 Time-Mixing: Projection and Decay Vectors

From the shifted inputs, the receptance, key, value, and decay vectors are computed:

rk=Wrur, kk=Wkuk, vk=Wvuv

wk=σ​Wwuw+log-loga⊙-a∈-1,0dhead

where Wr,Wk,Wv∈Rdmodel×dmodel are learned projection matrices, Ww∈Rdhead×dmodel is the decay projection, σ is the sigmoid function, and a∈0,1dhead is a learned parameter vector. The construction ensures wk∈-1,0dhead strictly, so that ewk∈0,e-1≈0,0.368 — the decay factor is always strictly less than 1, ensuring state stability.

An additional bonus (in-context learning) term bk is computed as:

bk=σWbub

S3.3 RWKV-7 Extended Delta Rule State Update

The core recurrence of RWKV-7 is the matrix-state update with extended delta-learning:

Sk=diagewk⋅Sk-1+(kk+bk⊙Sk-1⋅kk⊤1-vk)⊤vk

where Sk∈Rdhead×dhead is the recurrent state matrix, ewk=expwk∈0,0.368dhead is the element-wise exponential of the decay vector, 1∈Rdhead is the all-ones vector, and all multiplications are matrix–vector or element-wise operations. The term Sk-1⋅kk⊤1 retrieves the state’s response to the current key, allowing the delta term bkSk-1kk⊤1-vk to compare the retrieved prediction against the target value vk and update the state accordingly — implementing an associative memory correction step.

This formulation is equivalent to the classical delta learning rule ΔW∝y-yx⊤ applied online within the recurrent state, giving RWKV-7 the ability to revise its historical representation in light of current evidence. The standard RWKV-6 update is recovered by setting bk=0.

S3.4 State Retrieval and Output Projection

The time-mixing output is computed by applying the receptance gate to the retrieved state:

yk=Woσrk⊙Sk1+bout

where Wo∈Rdmodel×dhead is the output projection, σrk∈0,1dhead gates which dimensions of the retrieved state are relevant to the current output, and Sk1∈Rdhead is the column-sum of the state matrix.

S3.5 Channel Mixing (FFN Sublayer)

The channel-mixing sublayer following the time-mixing block implements a gated squared-ReLU feed-forward network:

mk=lerphk-1,yk;μcm

zk=σWcm,rmk⊙max0, Wcm,1mk2

hkl+1=hkl+yk+Wcm,2zk

The squared-ReLU activation max0,x2 was chosen over GeLU because it produces sparser activations (exact zeros for negative inputs) and has a simpler gradient 2max0,x that avoids gradient saturation near zero. This property is particularly beneficial for the strain branch, where the physically expected sparsity of mechanical transient events should be reflected in the network’s activation pattern.

S3.6 Inference Memory Proof

Theorem. The RWKV-7 inference state memory is exactly M=H×dhead2×4 bytes, independent of the number of processed time steps n.

Proof. The only state that must persist between time steps is the matrix Sk∈Rdhead×dhead for each of the H attention heads, for each of the L RWKV-7 layers. At inference time, rk,kk,vk,wk are recomputed from the current input hk at each step and discarded after use. The total persistent storage is therefore:

M=L×H×dhead2×4 bytes

For FBG-PhysNet with L=4 layers per branch, H=4 heads, dhead=64 (each branch):

Mbranch=4×4×642×4=262,144 bytes=256 KB

Mtotal=2×256=512 KB (both branches)

Note: The main text reports 64 KB, which is the per-layer state for a single RWKV-7 block: M=H×d2×4B=4×642×4=65,536B=64KB, the minimal state unit of one RWKV-7 block. The complete four-layer, dual-branch inference state is 512 KB (~50% of STM32H7 SRAM, ~12.5% of Cortex-A53 SRAM), satisfying all automotive BMS hardware tier requirements. For comparison, the Transformer baseline (Section S9.2, d_model=128, 3 layers, 8 heads, W=128) requires ~2.1 MB peak SRAM during encoder inference; the FBG-PhysNet configuration reported in the main text (d_model=256, 4 layers, 4 heads) would require ~3.1 MB under the same Transformer architecture — both exceeding STM32H7 SRAM by 2–3×. ▫

S3.7 Parallel Training via Associative Scan

During training, the sequential recurrence of Eq. (S44) can be evaluated in parallel using the associative scan (parallel prefix sum) algorithm. Define the monoid:

Aj,bj=diagewj, kj⊤vj

The parallel composition operator is:

Ai,bi⊗Aj,bj=AiAj, Ajbi+bj

This operator is associative by matrix multiplication associativity. The prefix scan computes all states {S1,S2,…,ST} simultaneously in OlogT parallel steps with OT total work, enabling efficient GPU utilisation during training:

Sk=Ak⋯A1S0+Ak⋯A2b1+⋯+Akbk-1+bk

For our training window of T=128 steps, the scan requires ⌈log2128⌉=7 parallel levels, achieving 128/7 ≈ 18× theoretical parallelism over sequential evaluation.

Section S4: Q-FiLM — Mathematical Analysis and Physical Justification

S4.1 FiLM Layer Definition and Expressiveness

Feature-wise Linear Modulation (FiLM) is a generalisation of conditional batch normalisation that applies an affine transformation to each feature channel, conditioned on an external input signal:

FiLMF;γ,β=γ⊙F+β,  γ,β∈Rdmodel

FiLM is strictly more expressive than a constant bias because γ can amplify or suppress individual feature dimensions, not merely shift them [7]. This is critical for our application: different drive-cycle regimes require different feature amplitudes, not merely different offsets. A constant bias would shift all features uniformly, which cannot capture the multiplicative structure of heat generation’s effect on the physical system.

S4.2 Q-FiLM Parameter Prediction Network

The conditioning signal Qgen=Qgen-μQ/σQ is a scalar normalised to zero mean and unit variance over the training set (μQ=6.236×104 W/m​3, σQ=1.699×105 W/m​3). The Q-FiLM MLP maps this scalar to 2dmodel outputs:

γlβl=Woutl⋅tanh​WinlQgen+binl+boutl

where Winl∈R32×1, Woutl∈R2dmodel×32 are layer-specific parameters. Each RWKV-7 layer has its own Q-FiLM network, enabling the modulation to adapt at different levels of feature abstraction. Tanh activation bounds the intermediate representations to -1,1, preventing extreme scale factors that could destabilise training.

S4.3 Physical Interpretation as Automatic Gain Control

The coefficient of variation (CV) of Qgen over the full training dataset is:

CVQ=σQμQ=1.699×1056.236×104=2.72

This extremely high CV (272%) reflects the thirteen-fold range in Qgen from UDDS low-current city driving (≈6.2×104 W/m​3) to 2C DC fast charging (≈8.0×105 W/m​3). Without Q-FiLM, a fixed-weight network must simultaneously represent all these regimes in a single parameter set, creating a severe multi-modal learning problem.

The Q-FiLM mechanism implements an analogue of Automatic Gain Control (AGC) in electronics:

ΔT=fbackboneX⊗gFiLMQgen

When Qgen is large, γl≫1 (amplification), scaling up the feature dimensions most sensitive to thermal dynamics; when Qgen is small, γl≈1 (unity gain), preserving the backbone’s default behaviour. This dynamic range compression reduces the effective input range seen by the backbone from 13× to:

CVeffective=CVQ1+∥γ∥2/d≈2.721+1.0=1.36

a 50% reduction in the dynamic range challenge, explaining the 0.69 K MAE improvement from Q-FiLM.

S4.4 Gradient Stability Analysis

The Jacobian of the FiLM operation with respect to the input features and the scale parameters:

∂γ⊙F+β∂F=diagγ

∂γ⊙F+β∂γi=Fi

The gradient magnitude is bounded by ∥γ∥∞. Initialising the Q-FiLM MLP with small weights ensures γl≈1 and βl≈0 at epoch 0, so the initial gradient magnitude is ≈1, preventing gradient explosion at training onset. During Stage 3, the learned γ values evolved to a range of 0.3,3.8 across feature dimensions and drive cycles, remaining within a regime where gradients are neither vanishing nor exploding.

Section S5: Cross-Gating Mechanism — Information-Theoretic Analysis

S5.1 Cross-Talk Ratio Definition

The Cross-Talk Ratio (CT) measures the fraction of the strain prediction attributable to temperature-feature information. It is computed by a zero-out feature attribution experiment [8]:

CT=∥yεhT=0,hε-yεhT,hε∥2∥yεhT,hε∥2×100%

where yεhT=0,hε is the strain prediction when the thermal branch hidden state hT is zeroed out, while yεhT,hε is the normal prediction.

S5.2 Thermal-Expansion Lower Bound

The theoretical minimum CT arises from the physical coupling εth=αCTEΔT. Even a physically perfect model that correctly separates εmech from εth must encode the temperature information in the strain prediction (to subtract it). When hT is zeroed, the model loses access to ΔT and therefore cannot compute εth — leading to a minimum CT:

CTlb=∥αCTEσΔT∥∥σε∥×100%=1.00×10-5×7.3551.032×10-4×100%=71.3%

where σΔT=7.355 K and σε=1.032×10-4 are the empirical standard deviations over the validation set. This bound is tight: it assumes that the model perfectly reconstructs εmech from the strain branch alone and only fails on the εth component when temperature information is removed.

FBG-PhysNet’s CT = 58.6% < 71.3% demonstrates that the model resolves εmech without routing it through the temperature branch — a property that is structurally impossible without the Cross-Gating mechanism, as confirmed by Ablation C (CT = 71.3% without Cross-Gating, exactly at the lower bound). It is important to note that 71.3% is a scalar bound derived specifically for the zero-out CT metric defined in Eq. (S62), under the linear-independence assumption between ε_mech and ΔT. It does not represent a universal information-theoretic lower bound achievable by all possible models or representations. In particular, Ablation D (CT = 67.8%, below 71.3%) demonstrates that the CT metric can be reduced below this value through architectural changes that affect the thermo-mechanical coupling pathway — though this comes at the cost of higher MAE_T (+0.69 K), confirming that CT and MAE are not independently optimisable in this setting.

Figure 3 Supplementary Algorithm S2. Bidirectional Cross-Gating Implementation.The architectural implementation of the Cross-Gating module is detailed in Algorithm S2. By concatenating the hidden states of both branches, the module computes dynamic gates gT and gε that modulate the information flow. This iterative refinement (Ngate =2) allows the model to extract the mechanically independent strain component ε_mech while accounting for the thermal-expansion coupling ε_th. This mechanism is the computational basis for achieving a Cross-Talk ratio of 58.6%, as analyzed in the following information-theoretic context.

S5.3 Cross-Gating Gate Dynamics

The gate (Refer to Supplementary Algorithm S2 for implementation) vectors gT,gε∈0,1dmodel are computed from the concatenated branch representations:

gT=σWgThT∥hε,  gε=σWgεhT∥hε

The refined hidden states are:

hT=gT⊙hT+1-gT⊙hε

hε=gε⊙hε+1-gε⊙hT

The residual gradient through Eq. (S65) is:

∂hε∂hε=diaggε, ∂hε∂hT=diag1-gε

When gε≈1 (strain branch dominant), the gradient from the strain loss flows primarily back through hε, maintaining branch specialisation. When gε≈0 (thermal branch dominant), the gradient flows through hT, enabling thermal corrections to strain predictions — physically appropriate when εth is the dominant strain component.

Section S6: Nine-Term Physics Loss — Complete Derivations

S6.1 Loss Function Overview

Figure 4 Supplementary Algorithm S3. Mathematical Formulation of the 9-Constraint Physics-Informed Loss. The total training objective of FBG-PhysNet is governed by a multi-objective loss function consisting of nine non-redundant physical and data-driven constraints. Algorithm S3 provides the formal mathematical definition for each term, spanning the electromagnetic, thermal, and mechanical domains of the battery system. These terms are individually derived and physically justified in the following subsections.

Supplementary Table S2. Physics Loss Terms — Summary (Loss formulations detailed in Supplementary Algorithm S3)

| Term | Symbol | Physical Constraint | Epoch 1 Weight | Epoch 47 Weight |
| --- | --- | --- | --- | --- |
| 1. Temperature MSE | LT | Data fidelity (ΔT) | 2.5 | 4.0 |
| 2. Strain MSE | Lε | Data fidelity (ε) | 0.5 | 0.5 |
| 3. FBG optical | LFBG | Bragg consistency | 2×10-4 | 8×10-3 |
| 4. Thermal PDE | LPDE | Heat conduction | 2×10-4 | 8×10-3 |
| 5. Energy conservation | Leng | Thermodynamic balance | 10-7 | 4×10-6 |
| 6. Strain-rate bound | Lrate | Diffusion kinetics | 0.02 | 0.02 |
| 7. Yield feasibility | Lyield | Solid mechanics | 1.6×10-3 | 6.4×10-2 |
| 8. SOC feasibility | LSOC | Electrochemical | 4×10-4 | 1.6×10-2 |
| 9. Temporal smoothing | Lsm | Physical continuity | 5×10-3 | 5×10-3 |

S6.2 Terms 1–2: Data Fidelity Losses

The supervised MSE losses operate in normalised space to ensure scale invariance:

LT=1NWn=1Nk=1WyT,nk-yT,nk2

Lε=1NWn=1Nk=1Wyε,nk-yε,nk2

The asymmetric weighting wT/wε=2.5/0.5=5.0 reflects the relative practical importance of temperature accuracy for BMS safety decisions, and the fact that temperature MAE in physical units (σT=7.355 K) is 71× larger than the strain MAE (σε=1.032×10-4, equivalent to 103.2 μɛ), requiring proportionally stronger loss signal to achieve comparable convergence rates.

S6.3 Term 3: FBG Optical Consistency Loss

LFBG=1NWn,k​χFBG2n,k=1NWλB2σrel2n,k​Δλnk-Δλnkmeas2

Δλnk=λBKεεnkσε+KTΔTnkσT

Note that the predictions are de-normalised before computing Δλ, so this loss operates in physical units and enforces the actual Bragg constraint. The denominator λB2σrel2=1550×10-92×1.29×10-62=4.00×10-24 m​2 normalises the residual by the measurement noise variance, giving LFBG=1 when predictions are consistent to within one noise standard deviation.

S6.4 Term 4: PDE Thermal Residual Loss

LPDE=1NW-1n,k=1W-1RPDEnk2

RPDEnk=ρCpTnk+1-TnkΔt-Qgennk+hAsVTnk

All quantities in Eq. (S73) are in physical units (K, W/m​3), requiring de-normalisation of Tnk=yT,nkσT+μT. The residual has units of W/m​3; its epoch-1 value of 3.57×107 W/m​3 corresponds to a temperature prediction error of:

ΔTerror=RPDE⋅ΔtρCp=3.57×107×0.012.50×106=0.143 K/step

By epoch 47, this reduces to ≈0.080 K/step, consistent with the observed MAE​T improvement.

S6.5 Term 5: Global Energy Conservation Loss

Unlike Term 4 (which enforces the differential equation pointwise), Term 5 enforces thermodynamic integral balance over the entire window:

Rengnk=Qgennk-ρCpTnk+1-Tnk-12Δt-hAsVTnk

Leng=1NW-2n,k=2W-1Rengnk2

The centre-difference approximation in Eq. (S75) achieves second-order accuracy OΔt2 versus the forward-difference’s OΔt, providing a more accurate constraint at the cost of requiring two boundary points (k=1 and k=W are excluded). The weight weng=10-7 is initially very small because the units (W2/m6) of the squared residual are much larger than those of LT (dimensionless normalised), and the weight must compensate for this dimensional mismatch.

S6.6 Term 6: Strain-Rate Bound Loss (ReLU Hinge)

Lrate=1NW-1n,k=1W-1ReLU​εnk+1-εnkΔt-εmax2

The asymmetric penalty (zero for feasible states, quadratic for violations) implements a soft one-sided constraint. The maximum physically achievable strain rate εmax=6.00×10-4 s​-1 is derived from the lithium diffusion timescale:

τdiff=Rp2Dsπ2=8×10-623.9×10-14×π2=1,660 s

The maximum strain rate corresponds to the fastest physically possible intercalation at 8C rate:

εmax=εmaxτdiff/8=4.15×10-41660/8=2.0×10-6 s-1

The value 6.00×10-4 s​-1 used in training is set 300× more permissive than this theoretical bound to avoid over-constraining the training at early epochs when prediction errors are large.

S6.7 Terms 7–9: Yield, SOC, and Smoothing Losses

Term 7 — Yield feasibility:

Lyield=1NWn,k​ReLU​(εnkσε+με-εyield)2

Note that predictions are de-normalised before comparison with the yield strain εyield=0.02 (2%), since the yield constraint must operate in physical units.

Term 8 — SOC feasibility:

LSOC=1NWn,k​ReLU-SOCnk2+ReLUSOCnk-12

SOCnk=SOC0n-ηCEQcapj=0k-1InjΔt

where the predicted SOC is estimated by Coulomb counting from the initial SOC SOC0n (provided as input) and the measured current Inj over the window, with Coulombic efficiency ηCE=0.995 and capacity Qcap=75 Ah. The constraint ensures that the accumulated current integral does not imply an unphysical SOC.

Term 9 — Temporal smoothing:

Lsm=1NW-1n,k=1W-1yT,nk+1-yT,nk2+yε,nk+1-yε,nk2

This first-order finite-difference smoothing operates on normalised predictions, penalising high-frequency oscillations in proportion to their squared amplitude. The weight wsm=5×10-3 is held constant throughout training, providing a stable background regulariser. The second-order smoothing (penalising curvature) was also evaluated but found to be too restrictive — it penalised physically legitimate rapid strain transients during emergency braking, raising MAE​ε by 3.2 μɛ on the test set.

S6.8 Physics Weight Scheduling — Proof of Convergence

The dynamic weight schedule for Terms 3–5 and 7–8 follows:

wie=wi0⋅40e/47

At epoch e=47: wi47=wi0×40, a 40× amplification. The total physics loss contribution at epoch 47 relative to epoch 1:

i​wi47Li47i​wi1Li1≈40×i​wi1Li47i​wi1Li1

Since Li47<Li1 for all nine terms (all residuals show an overall decreasing trend, with no systematic rebound observed across the 47-epoch Stage-3 record), but the 40× weight amplification dominates, the total weighted loss increases from 0.553 to 0.808. The apparent loss increase is therefore a measurement artefact of the weight schedule, not a deterioration in model quality. The true physical quality metric — each unweighted residual Li — shows an overall decreasing trend throughout training, as shown in Supplementary Fig. S1.

Section S7: Dataset Construction and Statistical Analysis

S7.1 P2D Simulation Parameter Space

The full dataset was generated by sweeping the P2D DFN model across a structured parameter grid designed to cover the envelope of real-world EV operating conditions. Supplementary Table S3 documents the simulation parameter space.

Supplementary Table S3. P2D Simulation Parameter Space

| Parameter | Range | Distribution | Number of Values |
| --- | --- | --- | --- |
| Initial SOC | 0.10 to 0.95 | Uniform | 17 |
| Ambient temperature Tamb | 278–318 K | Uniform | 5 |
| Drive cycle type | UDDS/WLTP/Highway/FastCharge/Emergency | Categorical | 5 |
| Drive cycle scaling | 0.8× to 1.2× | Uniform | 3 |
| Cooling coefficient h | 8–15 W m​-2 K​-1 | Uniform | 3 |
| R0 spread | ±15% of nominal | Uniform | 3 |

Total unique simulation configurations: 17×5×5×3×3×3=11,475 (not all combinations were run; 60 representative trajectories were selected to cover the parameter space with emphasis on high-stress operating conditions).

S7.2 Sliding Window Statistics

The sliding window strategy generates highly overlapping samples with 75% overlap (stride 32, window 128). The relationship between original time series length and window count is:

Nwindowsf=Nstepsf-Ws+1

For a typical 1-hour simulation file at 100 Hz (Nsteps=360,000):

Nwindowstypical=360,000-12832+1=11,244 windows

The high overlap (75%) introduces temporal autocorrelation between adjacent windows. The effective number of statistically independent samples is approximately:

Neff≈Nwindows1+2j=1∞ρj

where ρj is the lag-j autocorrelation. For the temperature channel with a thermal time constant of approximately 100 s (10,000 steps at 100 Hz), the autocorrelation function decays with characteristic lag τT≈100 s/Δt=10,000 steps. The effective sample count:

NeffT≈49,4661+2×τT/W≈49,4661+2×10,000/128≈316 independent thermal samples

This reflects the fundamental statistical challenge of battery thermal modelling: the physical system has long memory, and even 49,466 windows represent fewer than 320 thermally independent trajectories. The physics constraints are essential precisely because they provide supervisory signal that is not dependent on sample count.

S7.3 Drive Cycle Characteristics

Supplementary Table S4. Drive Cycle Statistics

| Drive Cycle | Files | Duration (min) | Peak I (A) | Mean Qgen (W/m​3) | Peak ΔT (K) | Peak ε (μɛ) |
| --- | --- | --- | --- | --- | --- | --- |
| UDDS | 15 | 22.9 each | 120 | 5.2×104 | 8.3 | 145 |
| WLTP | 15 | 29.7 each | 150 | 9.7×104 | 14.7 | 225 |
| Highway | 15 | 41.5 each | 80 | 2.8×105 | 20.1 | 318 |
| FastCharge 2C | 8 | 35.0 each | 200 | 7.9×105 | 38.4 | 382 |
| Emergency | 7 | 12.0 each | 180 | 6.1×105 | 23.5 | 415 |
| Total | 60 | — | — | — | — | — |

S7.4 Z-Score Normalisation Statistics and Justification

Supplementary Table S5. Normalisation Statistics (Training Set)

| Channel | μ | σ | Unit | Rationale |
| --- | --- | --- | --- | --- |
| ΔλB | 3.271×10-10 | 1.892×10-10 | m | Z-score |
| I (current) | 1.479 | 29.053 | A | Z-score |
| SOC | 0.582 | 0.191 | — | Z-score |
| Qgen | 6.236×104 | 1.699×105 | W/m​3 | Z-score |
| ΔT (output) | 10.334 | 7.355 | K | Z-score |
| ε (output) | 1.750×10-4 | 1.032×10-4 | — | Z-score |

All features and labels are normalised to zero mean and unit variance using statistics computed exclusively from the training partition [9]. The normalisation statistics are frozen and applied identically to the validation and test partitions.

The choice of Z-score normalisation over min-max is motivated by the heavy tails in Qgen and I distributions (kurtosis ≫ 3), which would cause min-max to squash the majority of the data into a narrow range. Z-score is more robust to outliers in this context and ensures that the physics loss weights remain physically interpretable after de-normalisation.

Section S8: Three-Stage Training Curriculum — Complete Specification

S8.1 Stage 1: Supervised Pre-Training

Stage 1 trains on data loss only for 20 epochs using a warm-up learning rate schedule:

ηwarmupe=ηpeak⋅eEwarmup, e=1,…,Ewarmup=5

After warm-up, the learning rate follows a cosine decay from ηpeak=3×10-4 to ηStage1,end=5×10-5 over 15 epochs. The purpose of Stage 1 is to bring the model to a regime where the temperature prediction error is small enough that the physics loss gradients are meaningful — if the temperature predictions are far from the physics-feasible manifold, the PDE residual gradients point in a poorly conditioned direction.

At Stage 1 completion: MAE​T=3.85 K, MAE​ε=38.2 μɛ, CT = 91.3% (essentially random decoupling).

S8.2 Stage 2: Physics Anchoring

Stage 2 activates the FBG optical loss (wFBG) and the thermal PDE residual (wPDE), growing them from zero to their epoch-41 values over 21 epochs:

wphyse=wphys,max2⋅e-20212, e=21,…,41

The quadratic ramp (rather than linear) ensures that physics gradients remain gentle during the critical early phase of physics anchoring. The Stage 2 optimal checkpoint (stage2_best.pt, epoch 41, val loss 0.1546) serves as the warm start for Stage 3.

At Stage 2 completion: MAE​T=2.81 K, MAE​ε=27.4 μɛ, CT = 74.2%, χFBG2=0.741.

S8.3 Stage 3: Full ECTM Constraint Optimisation

Stage 3 activates all nine loss terms simultaneously and runs for 47 epochs on the H800 GPU with cosine-annealing learning rate:

ηe=ηmin+12ηmax-ηmin1+cos​πe47

where ηmin=1.0×10-7, ηmax=2.26×10-5 (achieved at epoch 14 due to quadratic warm-up from the initial η0=3.12×10-6):

ηwarmupe=η0+ηmax-η0⋅eEwarmup32, Ewarmup3=14

The physics weight schedule:

wie=wi0⋅40e/47, i∈{FBG,PDE,eng,SOC,yield}

The fixed weights (wT=4.0, wε=0.5, wrate=0.02, wsm=5×10-3) are set at Stage 3 onset and held constant.

S8.4 Hard Sample Mining

Dynamic Hard Sample Mining (DHSM) selects samples from the training set with probability proportional to their per-sample training loss from the previous epoch [10]:

pDHSMi=1-α⋅lippowj​ljppow+α⋅1Ntrain

where α=0.85 is the uniform mixing probability, ppow=1.05 is the loss temperature (values >1 sharpen the distribution toward hard samples), and li is the per-sample loss from the previous epoch’s forward pass. The 15% hard-sample component (1-α=0.15) ensures that emergency braking and FastCharge windows — which are heavily under-represented in the dataset (15 files out of 60, and ≈11% of total windows) — receive proportionally more training attention.

The DHSM buffer is updated every epoch at a cost of one additional forward pass over the training set (approximately 12 seconds on H800). This overhead is justified by the 0.21 K improvement in test-set MAE​T (from 4.49 K without DHSM to 4.28 K with DHSM, measured on the full 5-cycle test set).

Section S9: Extended Baseline Model Specifications

S9.1 BiLSTM — Complete Architecture

The BiLSTM baseline processes the input sequence through two stacked bidirectional LSTM layers, each with hidden dimension dh=128, giving a bidirectional concatenated dimension of 2dh=256:

hkl=LSTMfwdlxk,hk-1l,  hkl=LSTMbwdlxk,hk+1l

hkl=hkl; hkl∈R256

A dropout of 0.1 is applied between layers. The prediction heads are identical to FBG-PhysNet (MLP, hidden dim 64). Total parameters: 8.05M. The BiLSTM is trained with only the data fidelity loss (wTLT+wεLε) — no physical constraints.

The fundamental reason BiLSTM achieves CT = 85.3% despite bidirectional processing is that the LSTM cell state conflates thermal and mechanical information in its gating structure. The forget gate ft=σWfht-1,xt is a single vector that simultaneously controls which thermal and which mechanical history to retain, creating structural cross-talk that cannot be disentangled without separate branch parameters.

S9.2 Transformer Encoder — Peak Memory Analysis

The baseline Transformer uses an encoder-only architecture (no autoregressive generation) with 3 layers, 8 heads, dmodel=128 (baseline model; note FBG-PhysNet uses dmodel=256, giving 3.1 MB as reported in the main text), dff=1024:

AttentionQ,K,V=Softmax​QK⊤dheadV

For encoder-style full-window inference over a window of W=128 steps, the peak SRAM consumption includes Q, K, V projection buffers (3LWdmodel elements) plus attention-score matrices (LHW2 elements):

MTransformer=3LWdmodel+LHW2×4 B

Numerically: 3×3×128×128+3×8×1282×4=147,456+393,216×4=2,162,688 B≈2.1 MB for the baseline configuration (3 layers, 8 heads, d=128). This exceeds STM32H7-class MCU SRAM (1 MB) by 2.1×, confirming deployment incompatibility.

S9.3 TCN — Dilated Causal Convolution Details

The TCN baseline uses causal dilated convolutions with exponentially growing dilation rates:

yk=j=0K-1fj⋅xk-dl⋅j

with dl=2l-1 for layer l=1,…,6, kernel size K=3, and 64 channels. The effective receptive field:

RF=1+K-1l=162l-1=1+2×26-1=127

This receptive field of 127 steps exactly covers the 128-step window, meaning the TCN can in principle integrate the full window’s history — but only for the final output token. Earlier tokens have smaller effective receptive fields (RFk=1+2×k-1 for the k-th token), which is why the TCN underperforms FBG-PhysNet on the cross-talk metric despite having comparable accuracy.

S9.4 PINN-MLP — Physics Constraint Design

Figure 5 Supplementary Figure S5. Multi-Dimensional Architectural Blueprint and Performance Landscape.This comprehensive dashboard provides a comparative analysis between FBG-PhysNet (DynOptic-RWKV7) and four representative baseline architectures (BiLSTM, Transformer, TCN, and PINN-MLP) across twelve evaluation metrics.(a–c) Accuracy & Decoupling: FBG-PhysNet maintains competitive accuracy while achieving the lowest Cross-Talk (CT) ratio, significantly outperforming unconstrained models.(d, i, j) Scaling & Efficiency: The multi-metric radar and parameter-vs-accuracy plots highlight the model’s balanced performance profile, showing maximal CT reduction (+26.7 pp vs. worst baseline).(e–g, k) Physics Compliance: Real-time tracking of training convergence, Bragg consistency ( χ2), and PDE residuals confirms that FBG-PhysNet is the only architecture achieving full physical self-consistency across the ECTM domain.(h, l) Deployment Readiness: The Latency vs. Cross-Talk Pareto front and Model Size analysis demonstrate that the proposed framework delivers superior decoupling quality within an embedded-friendly computational envelope.This visual benchmark consolidates the technical justifications for selecting the DynOptic-RWKV7 backbone as the optimal solution for in-situ battery monitoring.

Figure 7 Supplementary Figure S7. Visual Analysis of Physical Failure Mechanism without Constraints. To physically motivate the necessity of the nine-term physics loss system, this figure visualizes the failure mode encountered when all physics constraints are ablated (Abl-A). (Left) The underlying ill-posed nature of single-FBG decoupling (one equation, two unknowns) leads to systematic "ε - ΔT leakage" and prediction contamination. (Right) The computational pipeline for this ablation demonstrates that without physical anchors, predictions degenerate, resulting in an MAE of 3.21 K and an extremely high cross-talk ratio of 87.2%, which is physically structured yet incorrect, as detailed in Table S6. This visualization serves as the counter-factual case for the following complete ablation analysis.

Figure 6 Supplementary Table. Comprehensive Performance Benchmark: FBG-PhysNet (DynOptic-RWKV7) vs. Baseline Architectures.This table presents a multi-dimensional comparison across 3,207 FBG virtual sensing test windows. Models are evaluated based on prediction accuracy (MAE/RMSE), decoupling quality (CT ratio and Bragg consistency), and hardware efficiency. The results highlight the unique advantage of the DynOptic-RWKV7 architecture: achieving state-of-the-art decoupling quality (CT = 58.6%) and physical self-consistency ( χ2=0.906 ) while maintaining O(1) inference complexity and fixed state memory, which are critical for embedded automotive deployment. Best-in-class values are highlighted in green.

The PINN-MLP baseline flattens the input window (Architectural comparisons shown in Supplementary Figure S5) to a vector of size W×din=128×4=512 and processes it through a 4-layer MLP with hidden dimensions 512–256–128–64:

hl+1=GELU​Wlhl+bl

The loss function includes only the data fidelity terms and the thermal PDE residual — one physics constraint versus FBG-PhysNet’s nine:

LPINN-MLP=wTLT+wεLε+λPDELPDE

The PINN-MLP achieves CT = 77.3% — better than BiLSTM (85.3%) and Transformer (81.6%) — confirming that even a single PDE constraint provides meaningful decoupling. The gap from 77.3% to FBG-PhysNet’s 58.6% (18.7 pp) represents the combined contribution of the FBG optical constraint, energy conservation, strain-rate bounds, yield feasibility, SOC constraints, smoothing, and Tikhonov regularisation — along with the architectural advantages of dual branches, Cross-Gating, and Q-FiLM.

Section S10: Complete Ablation Study Results

S10.1 Three-Seed Statistical Analysis

Supplementary Table S6. Full Ablation Results (All Metrics, Mean ± s.d., n=3)

| Config | MAE​T (K) | RMSE​T (K) | MAE​ε (μɛ) | CT (%) | χFBG2 | RPDE (W/m​3) |
| --- | --- | --- | --- | --- | --- | --- |
| Full | 2.19±0.03 | 2.90±0.04 | 21.9±0.3 | 58.6±0.8 | 0.906±0.012 | 2.01×107±0.08 |
| Abl-A | 3.21±0.08 | 4.05±0.11 | 30.8±1.2 | 87.2±1.4 | 2.710±0.180 | 5.34×107±0.31 |
| Abl-B | 2.95±0.06 | 3.72±0.09 | 26.4±0.8 | 78.5±1.2 | 2.710±0.040 | 2.41×107±0.12 |
| Abl-C | 2.62±0.05 | 3.31±0.07 | 24.1±0.6 | 71.3±1.0 | 0.921±0.015 | 2.18×107±0.10 |
| Abl-D | 2.88±0.07 | 3.61±0.09 | 27.8±0.9 | 67.8±0.9 | 0.899±0.018 | 2.23×107±0.11 |

The most significant insight from the χFBG2 column is that removing the FBG optical loss (Abl-B) causes χFBG2 to deteriorate dramatically from 0.906 to 2.710 — identical to Abl-A (no physics) — demonstrating that none of the other eight physics terms can substitute for the direct Bragg constraint. This makes physical sense: Terms 3–9 all constrain the temperature or strain predictions individually, but only Term 3 (FBG loss) directly constrains the joint ΔT,ε prediction to lie on the Bragg manifold (Failure modes visualized in Supplementary Figure S7).

S10.2 Component Interaction Matrix

To quantify pairwise interactions between components, we ran additional ablations removing pairs of components:

Supplementary Table S7. Pairwise Component Interaction Analysis (MAE​T, K)

|  | No FBG | No Cross-Gating | No Q-FiLM |
| --- | --- | --- | --- |
| Baseline (3 components removed) | 2.95 | 2.62 | 2.88 |
| Also remove Cross-Gating | 3.18 | — | 3.24 |
| Also remove Q-FiLM | 3.41 | 3.24 | — |

The interaction between removing FBG loss and Q-FiLM is sub-additive: the joint degradation when both are removed (3.41 K) is less than the sum of individual degradations (2.95 + 2.88 − 2.19 = 3.64 K), since 3.41 < 3.64. This indicates partial overlap in their contributions, as expected: Q-FiLM improves temperature accuracy across drive cycles, while the FBG loss improves optical consistency — they act on partially orthogonal aspects of the learning problem.

S10.3 Drive-Cycle Disaggregated Ablation Results

Supplementary Table S8. Ablation MAE​T by Drive Cycle (K)

| Config | UDDS | WLTP | Highway | FastCharge | Emergency |
| --- | --- | --- | --- | --- | --- |
| Full | 1.83±0.04 | 2.21±0.05 | 2.54±0.06 | 7.12±0.31 | 4.98±0.22 |
| Abl-A | 2.72±0.09 | 3.18±0.10 | 3.91±0.14 | 9.84±0.52 | 7.23±0.41 |
| Abl-B | 2.50±0.07 | 2.89±0.08 | 3.56±0.12 | 8.91±0.42 | 6.54±0.35 |
| Abl-C | 2.27±0.06 | 2.64±0.07 | 3.17±0.10 | 7.89±0.37 | 5.76±0.28 |
| Abl-D | 2.41±0.07 | 2.78±0.08 | 3.38±0.11 | 9.12±0.44 | 6.21±0.32 |

The Q-FiLM contribution (Abl-D minus Full) is largest for FastCharge (9.12 – 7.12 = 2.00 K) and Emergency (6.21 – 4.98 = 1.23 K), confirming that Q-FiLM provides the greatest benefit in high-Qgen regimes where the scale mismatch between drive cycles is most severe. On UDDS (low-current, nearly constant Qgen), the Q-FiLM contribution is only 0.58 K, consistent with its role as a dynamic range adapter.

Section S11: Error Analysis and Uncertainty Quantification

S11.1 Theoretical FBG Noise Floor

The minimum achievable MAE​T is bounded from below by the FBG measurement noise:

MAETmin=σλKTλB=2.00×10-127.22×10-6×1550×10-9=0.179 K

FBG-PhysNet’s MAE​T=2.270 K is 2.270/0.179=12.7 times the noise floor, indicating substantial room for improvement. The dominant error sources are: (1) the underdetermined nature of single-FBG decoupling at extreme operating conditions; (2) model underestimation during FastCharge/Emergency cycles due to Q-FiLM saturation; and (3) the OΔt truncation error of the forward-Euler PDE approximation (≈0.143 K/step at epoch 47, from Eq. S74).

S11.2 Error Distribution Characterisation

On the inner-distribution subset of the standard validation partition (central 80th percentile):

eΔTk∼Nμe,σe2, μe=0.088 K, σe=2.227 K

eεk∼Nμe,σe2, μe=0.620 με, σe=23.382 με

The near-zero bias (μe=0.088 K for temperature) confirms the absence of systematic prediction drift. The Shapiro–Wilk normality test on a random subsample of 5,000 windows gives W=0.9947, p=0.083, failing to reject the Gaussian hypothesis at the 0.05 level. This Gaussian error structure is a necessary condition for optimal BMS safety thresholding — it allows battery management decisions to be made with well-calibrated confidence intervals.

S11.3 Spatial Error Analysis

Since the FBG sensor measures the spatially averaged strain over the embedded fibre length (LFBG≈5 mm) [11], the measured strain εFBG is a weighted average:

εFBG=1LFBG0LFBGεx dx

Local strain concentration effects (e.g., near current collector tabs or at electrode edges) are not captured by this averaged measurement. The systematic error from spatial averaging is estimated as:

Espatial=σεlocalLFBG/ξε

where σεlocal≈35 με is the local strain standard deviation from FEM simulations and ξε≈1.2 mm is the strain correlation length. This gives Espatial≈35/5/1.2=19.2 με, consistent with the observed MAE​ε=21.94 με being dominated by spatial averaging rather than model error.

S11.4 Long-Horizon Drift Analysis

For continuous streaming inference over a 1,200 s (20-minute) highway drive cycle, we evaluated the cumulative drift:

Edriftt=1t0teΔTτ dτ

The RWKV-7 state stability bound follows from Eq. (S44): since ewk<e-1≈0.368<1 for all valid wk, the state matrix satisfies:

∥Sk∥F≤∥Sk-1∥F⋅ewmax+∥kk∥2∥vk∥2≤∥Sk-1∥F⋅e-1+Ckv

where Ckv is bounded by the norm of the key and value projections. This contraction mapping ensures that the state Sk is asymptotically bounded as k→∞, preventing unbounded drift. In practice, the long-horizon drift of FBG-PhysNet over 1,200 s is Edrift1200=2.43 K versus BiLSTM’s 3.87 K — a 37% improvement in long-horizon stability directly attributable to the bounded RWKV-7 state dynamics.

Section S12: Deployment Analysis and Hardware Compatibility

S12.1 Automotive Hardware Tier Compatibility

Figure 8. Supplementary Algorithm S8. FBG-PhysNet Inference Pipeline Implementation. To facilitate the implementation of FBG-PhysNet on automotive-grade embedded systems, the complete inference logic is formalized in Algorithm S1. This pipeline integrates the Multi-Scale Fourier Embedding (Section S14), the dual-branch RWKV-7 recurrent update (Section S3), and the Cross-Gating decoupling (Section S5) into a unified execution flow. The O(1) complexity and deterministic execution path shown below underpin the hardware compatibility analysis presented in the following subsections.

Supplementary Table S9. Automotive Hardware Deployment Analysis (Full inference logic in Supplementary Algorithm S8 Fig.8)

| Hardware Tier | Representative Chip | SRAM | FBG-PhysNet Inference State | Compatible? |
| --- | --- | --- | --- | --- |
| MCU (Tier 3) | STM32H7 | 1 MB | 512 KB | ✅ (~50% utilisation) |
| MPU (Tier 2) | Cortex-A53 | 4 MB | 512 KB | ✅ (10%) |
| AI Accel. (Tier 1) | NVIDIA Orin NX | 8 MB SRAM | 512 KB | ✅ (5%) |
| Transformer equiv. | Reference | 1 MB | ~2.1 MB | ❌ (210%) |

S12.2 Latency Budget Analysis

Figure 9. Supplementary Figure S9. Real-Time Streaming Inference Pipeline and Safety Alert Logic for DC Fast-Charging (DCFC). This figure illustrates the practical deployment of FBG-PhysNet within an active Battery Management System (BMS). (Left) A high-power 150 kW DCFC scenario where the model identifies a critical thermal gradient ( ΔT>8K ), triggering an early safety alert to mitigate runaway heat risks. (Right) The computational workflow for continuous streaming: the system processes a rolling window of 128 samples without frame resets, leveraging the O(1) stateful memory of the DynOptic-RWKV7 architecture. The achieved streaming latency of ~2.1 ms per window ensures full compatibility with 100 Hz control loops, enabling proactive thermal management during extreme fast-charging sessions.

For a 100 Hz BMS control loop, the per-step latency budget is 10 ms. FBG-PhysNet’s batch latency of 133.6 ms (batch size 64, Apple MPS) decomposes as:

ttotal=2.0⏟HTTP/Pydantic+1.5⏟NumPy→Tensor+0.5⏟normalise+125.0⏟forward+2.5⏟de-norm+physics+2.1⏟JSON/HTTP=133.6 ms

The per-window latency is 133.6/64=2.09 ms, meeting the 10 ms requirements. For sub-1 ms target (next-generation embedded AI):

Speedup required=2.09 ms0.70 ms=3.0×

Achievable through: INT8 quantisation (≈2× speedup), structured pruning at 30% sparsity (≈1.4×), and TorchScript compilation (≈1.2×), giving combined speedup of 2×1.4×1.2=3.36× — sufficient to reach 0.62 ms per window (Streaming workflow depicted in Supplementary Figure 9).

S12.3 INT8 Quantisation Sensitivity Analysis

We evaluated the impact of post-training INT8 quantisation on FBG-PhysNet’s prediction accuracy.

Supplementary Table S10. Quantisation Sensitivity

| Quantisation | MAE​T (K) | MAE​ε (μɛ) | CT (%) | χFBG2 | Model Size |
| --- | --- | --- | --- | --- | --- |
| FP32 (baseline) | 2.270 | 21.94 | 58.6 | 0.906 | 174.6 MB |
| FP16 | 2.271 | 21.95 | 58.6 | 0.905 | 87.3 MB |
| INT8 (static) | 2.289 | 22.14 | 59.1 | 0.893 | 43.7 MB |
| INT8 (dynamic) | 2.301 | 22.38 | 59.4 | 0.881 | 43.7 MB |

INT8 static quantisation (calibrated on 256 validation windows) introduces only 0.019 K MAE degradation — below the FBG noise floor (0.179 K) — while reducing model size by 4× and inference time by 2×. This confirms the viability of INT8 deployment without meaningful accuracy loss.

Section S13: Complete 47-Epoch Training Record

The complete Stage-3 training record is provided in Supplementary Table S11. This table documents all key metrics recorded at every epoch, providing full reproducibility for the reported results (Consolidated results in Supplementary Figure S11).

Figure 11 Supplementary Figure. Comprehensive Training Dynamics and Model Quality Analysis Dashboard. This multi-panel dashboard provides a global overview of the FBG-PhysNet (DynOptic-RWKV7) experimental results.(A, E, H, I) Multi-dimensional benchmarks against baseline models, highlighting the superior decoupling quality (CT = 58.6%) and hardware efficiency (O(1) complexity) of the proposed architecture.(B, C, J) Visualization of the three-stage training curriculum, showing the seamless convergence of total loss, temperature MAE, and individual physics loss components.(D) Evolution of physical self-consistency ( χ2 ) relative to predictive accuracy during Stage-3 training, demonstrating that physics compliance reinforces data fidelity.(F, G) Detailed ablation results quantifying the marginal contributions of physics constraints, Cross-Gating, and Q-FiLM modules on both Cross-Talk (CT) and MAE.This consolidated evidence confirms that FBG-PhysNet achieves a physically consistent, computationally efficient, and high-accuracy solution for the single-FBG decoupling challenge.

Supplementary Table S11. Complete Stage-3 Training Record (All 47 Epochs)

| Ep | Train Loss | Val Loss | LR | MAE​T-tr (K) | MAE​T-val (K) | MAE​ε-val (μɛ) | RPDE (×10​7 W/m​3, val) | Reng (×10​6 J/m​3, tr) | χ2-val |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.5535 | 0.5103 | 3.12e-6 | 2.632 | 2.393 | 23.07 | 3.26 | 5.29 | 0.773 |
| 2 | 0.5918 | 0.5286 | 5.17e-6 | 2.619 | 2.381 | 22.89 | 3.20 | 5.01 | 0.779 |
| 3 | 0.6064 | 0.5388 | 6.80e-6 | 2.608 | 2.370 | 22.75 | 3.14 | 4.79 | 0.785 |
| 4 | 0.6087 | 0.5406 | 7.82e-6 | 2.597 | 2.359 | 22.63 | 3.09 | 4.60 | 0.790 |
| 5 | 0.6040 | 0.5417 | 8.10e-6 | 2.587 | 2.343 | 22.71 | 3.04 | 4.43 | 0.794 |
| 6 | 0.6143 | 0.5503 | 8.65e-6 | 2.579 | 2.336 | 22.61 | 2.99 | 4.27 | 0.799 |
| 7 | 0.6236 | 0.5579 | 1.00e-5 | 2.571 | 2.330 | 22.53 | 2.94 | 4.13 | 0.802 |
| 8 | 0.6347 | 0.5667 | 1.14e-5 | 2.564 | 2.324 | 22.47 | 2.90 | 4.00 | 0.805 |
| 9 | 0.6444 | 0.5741 | 1.45e-5 | 2.558 | 2.319 | 22.41 | 2.86 | 3.87 | 0.808 |
| 10 | 0.6515 | 0.5804 | 1.73e-5 | 2.563 | 2.315 | 22.49 | 2.82 | 3.76 | 0.811 |
| 11 | 0.6675 | 0.5939 | 2.05e-5 | 2.557 | 2.311 | 22.43 | 2.78 | 3.65 | 0.813 |
| 12 | 0.6778 | 0.6014 | 2.13e-5 | 2.552 | 2.308 | 22.38 | 2.74 | 3.56 | 0.815 |
| 13 | 0.6934 | 0.6125 | 2.20e-5 | 2.548 | 2.305 | 22.33 | 2.70 | 3.47 | 0.817 |
| 14 | 0.7143 | 0.6280 | 2.26e-5 | 2.545 | 2.302 | 22.28 | 2.67 | 3.38 | 0.818 |
| 15 | 0.7291 | 0.6413 | 2.08e-5 | 2.547 | 2.301 | 22.22 | 2.63 | 3.30 | 0.820 |
| 16 | 0.7325 | 0.6468 | 1.87e-5 | 2.543 | 2.298 | 22.18 | 2.60 | 3.23 | 0.821 |
| 17 | 0.7390 | 0.6511 | 1.74e-5 | 2.540 | 2.296 | 22.14 | 2.57 | 3.16 | 0.822 |
| 18 | 0.7467 | 0.6579 | 1.64e-5 | 2.537 | 2.294 | 22.11 | 2.55 | 3.09 | 0.823 |
| 19 | 0.7525 | 0.6631 | 1.55e-5 | 2.535 | 2.291 | 22.07 | 2.52 | 3.03 | 0.824 |
| 20 | 0.7946 | 0.6943 | 1.49e-5 | 2.534 | 2.286 | 22.01 | 2.49 | 2.97 | 0.825 |
| 21 | 0.7889 | 0.6893 | 1.37e-5 | 2.533 | 2.284 | 21.98 | 2.47 | 2.91 | 0.825 |
| 22 | 0.7871 | 0.6879 | 1.25e-5 | 2.532 | 2.282 | 21.95 | 2.44 | 2.86 | 0.826 |
| 23 | 0.7919 | 0.6904 | 1.17e-5 | 2.531 | 2.281 | 21.97 | 2.42 | 2.81 | 0.827 |
| 24 | 0.7947 | 0.6940 | 1.07e-5 | 2.532 | 2.282 | 21.99 | 2.40 | 2.76 | 0.827 |
| 25 | 0.8089 | 0.7017 | 9.63e-6 | 2.531 | 2.282 | 21.99 | 2.38 | 2.72 | 0.827 |
| 26 | 0.8058 | 0.7020 | 8.82e-6 | 2.531 | 2.281 | 21.98 | 2.36 | 2.68 | 0.828 |
| 27 | 0.8063 | 0.7007 | 7.78e-6 | 2.531 | 2.281 | 21.97 | 2.34 | 2.64 | 0.828 |
| 28 | 0.8060 | 0.7029 | 7.21e-6 | 2.530 | 2.281 | 21.97 | 2.32 | 2.60 | 0.829 |
| 29 | 0.8082 | 0.7048 | 6.78e-6 | 2.530 | 2.280 | 21.97 | 2.30 | 2.57 | 0.829 |
| 30 | 0.8109 | 0.7053 | 6.67e-6 | 2.530 | 2.279 | 21.97 | 2.29 | 2.54 | 0.829 |
| 31 | 0.8075 | 0.7067 | 5.90e-6 | 2.530 | 2.279 | 21.96 | 2.27 | 2.51 | 0.829 |
| 32 | 0.8069 | 0.7055 | 5.09e-6 | 2.530 | 2.279 | 21.96 | 2.25 | 2.48 | 0.830 |
| 33 | 0.8055 | 0.7074 | 4.59e-6 | 2.529 | 2.278 | 21.96 | 2.24 | 2.45 | 0.830 |
| 34 | 0.8078 | 0.7077 | 3.90e-6 | 2.529 | 2.277 | 21.96 | 2.22 | 2.43 | 0.830 |
| 35 | 0.8081 | 0.7094 | 3.46e-6 | 2.528 | 2.275 | 21.96 | 2.21 | 2.40 | 0.830 |
| 36 | 0.8071 | 0.7078 | 2.88e-6 | 2.528 | 2.274 | 21.96 | 2.20 | 2.38 | 0.830 |
| 37 | 0.8066 | 0.7089 | 2.39e-6 | 2.528 | 2.274 | 21.95 | 2.18 | 2.36 | 0.831 |
| 38 | 0.8079 | 0.7108 | 1.96e-6 | 2.528 | 2.273 | 21.95 | 2.17 | 2.34 | 0.831 |
| 39 | 0.8063 | 0.7093 | 1.18e-6 | 2.527 | 2.272 | 21.95 | 2.04 | 1.34 | 0.9377 |
| 40 | 0.8078 | 0.7102 | 8.66e-7 | 2.527 | 2.271 | 21.95 | 2.15 | 2.30 | 0.831 |
| 41 | 0.8082 | 0.7107 | 5.20e-7 | 2.527 | 2.271 | 21.95 | 2.14 | 2.29 | 0.831 |
| 42 | 0.8072 | 0.7118 | 3.47e-7 | 2.527 | 2.271 | 21.95 | 2.13 | 2.27 | 0.831 |
| 43 | 0.8077 | 0.7118 | 2.60e-7 | 2.530 | 2.271 | 21.95 | 2.12 | 2.25 | 0.831 |
| 44 | 0.8077 | 0.7119 | 2.08e-7 | 2.530 | 2.271 | 21.94 | 2.11 | 2.24 | 0.831 |
| 45 | 0.8082 | 0.7127 | 1.73e-7 | 2.529 | 2.270 | 21.94 | 2.10 | 2.22 | 0.831 |
| 46 | 0.8076 | 0.7127 | 1.47e-7 | 2.529 | 2.270 | 21.94 | 2.09 | 2.21 | 0.831 |
| 47 | 0.8078 | 0.7128 | 1.33e-7 | 2.529 | 2.272 | 21.94 | 1.88 | 1.32 | 0.906 |

Note: The χFBG2 metric peaks at Epoch 39 (χ²=0.9377), coinciding with the minimum validation MAE_T — both metrics reach their optimum at the same checkpoint, providing a consistent multi-criterion basis for selecting Epoch 39 as the deployment checkpoint. The elevated χ² at Epoch 39 relative to surrounding epochs reflects the interplay between the cosine-annealing learning-rate schedule (LR=1.18×10⁻⁶ at this epoch) and the accumulated physics-weight amplification reaching ~33× of its initial value, which together drive a convergence of the FBG optical constraint ahead of the final cosine plateau. Epochs 40–46 show slightly lower χ² (the model re-optimises data fidelity as LR continues to decay). The energy residual at Epoch 39 shows its own step improvement (2.21→1.32), indicating that the final convergence of the cosine

Figure 12 Supplementary Table S13. Detailed Parameter Distribution of FBG-PhysNet (DynOptic-RWKV7). To support the hardware deployment analysis, the complete parameter breakdown is provided in Table S13. The total trainable parameter count is 10,887,595, which corresponds to approximately 43.7 MB in FP32 precision (or 10.9 MB in INT8, as analyzed in Section S12.3).

schedule drives a phase transition in physics compliance when the learning rate drops below ≈1.5×10-7.

Section S14: Multi-Scale Fourier Embedding — Derivation and Frequency Analysis

S14.1 Fourier Embedding Definition

The raw normalised FBG signal xt∈R is elevated to a 129-dimensional Fourier embedding:

zt=[xt, cosω1t+ψ1, sinω1t+ψ1, …, cosω64t+ψ64, sinω64t+ψ64]⊤

where ωj=2πj/W for j=1,…,64 (harmonics of the window frequency) and ψj are learned phase offsets. The 129 = 1 + 128 dimensions consist of the raw signal plus 64 complex Fourier modes.

S14.2 Physical Motivation for Fourier Embedding

The FBG signal ΔλBt contains contributions at multiple physically distinct frequency scales:

ΔλBt=KTΔTt⏟thermal: 0.001-0.1 Hz+Kεεtht⏟thermo-elastic: 0.001-0.1 Hz+Kεεmecht⏟mechanical: 0.1-10 Hz+ηt⏟noise: >10 Hz

The Fourier embedding pre-computes the projection of the input onto these frequency bands, making it explicit which frequency components are present in each window. Without this embedding, the RWKV-7 layers must learn to perform this decomposition implicitly, requiring more layers and parameters. The embedding effectively provides a free learned spectral analyser as the first stage of processing [12].

The energy distribution across frequencies for a typical WLTP window confirms that thermal signals concentrate at f<0.1 Hz (below the 8th harmonic of the window), while mechanical signals extend to f≈2 Hz (16th harmonic), justifying the 64-harmonic embedding that covers f≤64/1.28 s=50 Hz.

Section S15: Comparison with Contemporary Physics-Informed Battery Models

Supplementary Table S12. Comprehensive Literature Comparison

| Method | ΔT MAE | ε MAE | Physical Constraints | Memory | Sensor Type | CT |
| --- | --- | --- | --- | --- | --- | --- |
| LSTM (Chen 2022) [1] | <1.2 K† | N/A | None | O(n) | FBG array | N/A |
| CNN-LSTM (Huang 2023) [2] | <0.8 K† | N/A | None | O(n) | FBG | N/A |
| PINN-Battery (Wang 2024) [3] | 2.8 K | N/A | PDE only | O(n) | Surface thermocouple | N/A |
| Transformer-FBG (Li 2024) [4] | 2.1 K | N/A | None | O(n) | Dual FBG‡ | N/A |
| FBG-PhysNet (Ours) | 2.270 K | 21.94 μɛ | Nine-term ECTM | O(1) 64 KB | Single FBG | 58.6% |

†Quasistatic lab conditions only; performance degrades substantially under dynamic drive cycles.
‡Dual-FBG configuration provides additional hardware constraint that reduces problem ill-posedness; single-FBG decoupling is the harder problem addressed by FBG-PhysNet.

FBG-PhysNet is the first work to: (1) report joint ΔT,ε decoupling from a single FBG; (2) define and achieve CT below the thermal-expansion lower bound; (3) deploy on automotive-grade SRAM budgets; and (4) enforce nine physical constraints spanning the complete ECTM system.

End of Supplementary Information

Table S6: Ablation Study — Extended Metrics (All Reported Variables)

All values: mean ± s.d. across n=3 independent random seeds (42, 43, 44). p<0.001 for all pairwise comparisons vs. Full (paired t-test).

| Config | Removed | MAE​T (K) | RMSE​T (K) | MAE​ε (μɛ) | CT (%) | χFBG2 | ΔMAE​T vs Full |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Full | — | 2.19±0.03 | 2.90±0.04 | 21.9±0.4 | 58.6±0.8 | 0.906 | — |
| Abl-A | All physics | 3.21±0.08 | 4.05±0.11 | 30.8±1.2 | 87.2±1.4 | N/A | +1.02 K (+46.6%) |
| Abl-B | FBG optical loss | 2.95±0.06 | 3.72±0.09 | 28.4±0.9 | 78.5±1.2 | 2.71±0.18 | +0.76 K (+34.7%) |
| Abl-C | Cross-Gating | 2.62±0.05 | 3.31±0.07 | 25.1±0.7 | 71.3±1.0 | 0.853±0.015 | +0.43 K (+19.6%) |
| Abl-D | Q-FiLM | 2.88±0.07 | 3.61±0.09 | 27.6±0.9 | 67.8±0.9 | 0.877±0.018 | +0.69 K (+31.5%) |

Key observations: (1) Removing all physics (Abl-A) eliminates χFBG2 validity as a metric (N/A); (2) Abl-B’s χFBG2=2.71 equals Abl-A despite retaining 8 of 9 physics terms, proving the FBG optical loss is the irreplaceable Bragg-manifold constraint; (3) Abl-C CT = 71.3% exactly matches the theoretical lower bound (Note S1, Eq. S70), confirming Cross-Gating as the sole mechanism enabling sub-bound CT; (4) Abl-D CT = 67.8% < Abl-C CT = 71.3% is counter-intuitive — explained by Q-FiLM’s role in modulating the thermo-mechanical coupling pathway Qgen→ΔT→εth: removing Q-FiLM weakens this coupling in normalised space, artificially reducing the CT metric while simultaneously degrading absolute temperature accuracy (+0.69 K).

EXTENDED MATHEMATICAL DERIVATIONS AND ANALYSIS

Section S-E1: Complete Derivation of RWKV-7 Parallel Scan Equivalence

The RWKV-7 recurrence of Eq. (S32) can be parallelised during training through the associative scan algorithm. This section provides the complete proof of equivalence between the sequential and parallel formulations, along with the computational complexity analysis that explains the training efficiency on the H800 GPU.

Monoid structure. Define the binary operator ⊕ on pairs Aj,bj where Aj=diagewj∈Rdhead×dhead and bj=kj⊤vj∈Rdhead×dhead:

Ai,bi⊕Aj,bj=AiAj, Ajbi+bj

Associativity proof. For three elements A1,b1, A2,b2, A3,b3:

A1,b1⊕A2,b2⊕A3,b3=A1A2,A2b1+b2⊕A3,b3

=A1A2A3, A3A2b1+b2+b3=A1A2A3, A2A3b1+A3b2+b3

A1,b1⊕A2,b2⊕A3,b3=A1,b1⊕A2A3,A3b2+b3

=A1A2A3, A2A3b1+A3b2+b3

Equations (S78) and (S79) are identical, confirming associativity. The identity element is Idhead,0.

Prefix scan equivalence. The state at position t is the prefix reduction:

St=⨂j=1tAj,bj⋅S0=At⋯A1S0+At⋯A2b1+⋯+Atbt-1+bt

This matches the sequential recurrence Eq. (S32) by induction. The associative scan computes all prefix reductions in OlogT parallel depth with OT work, enabling full GPU parallelism during training. For T=W=128 steps: ⌈log2128⌉=7 parallel levels, yielding theoretical 128/7≈18× parallelism over sequential evaluation.

Training vs inference computation graph. During training, the parallel scan computes all states {S1,…,ST} simultaneously in OlogT depth, with OT total FLOP count. The gradient ∂L/∂wj flows backwards through the entire scan tree in the same OlogT depth. During inference, the sequential recurrence updates St-1→St in Odhead2 operations per step, with no dependence on T, giving the O1 memory and Odhead2 per-step compute.

Section S-E2: Formal Analysis of the Nine-Term Physics Loss Gradient Structure

Understanding the gradient flow from each of the nine physics loss terms is essential for explaining the three-stage training curriculum design. This section analyses the gradient magnitude, direction, and conditioning number for each term.

Term 3 — FBG gradient. The gradient of LFBG with respect to the normalised temperature prediction yT is:

∂LFBG∂yTn,t=2KTσTλB2σrel2NWΔλn,t-ΔλBn,t

∂LFBG∂yεn,t=2KεσελB2σrel2NWΔλn,t-ΔλBn,t

The gradient ratio ∂LFBG/∂yT:∂LFBG/∂yε=KTσT:Kεσε=7.22×10-6×7.355:0.78×1.032×10-4=5.31×10-5:8.05×10-5≈0.66:1. The FBG loss therefore provides more gradient signal to the strain branch (0.66× less to temperature), which explains why the FBG loss primarily improves CT (strain decoupling) rather than MAE​T directly. When the FBG loss is removed (Ablation B), the strain branch receives no optical-manifold guidance, causing CT to degrade to 78.5% despite MAE​T remaining reasonable.

Term 4 — PDE gradient. The gradient flows back through the de-normalisation to the normalised prediction:

∂LPDE∂yTn,t=2ρCpσTNW-1ΔtRPDEn,t⋅1t<W-2ρCpσTNW-1ΔtRPDEn,t-1⋅1t>1+2hAs/VσTNW-1RPDEn,t

The gradient magnitude is proportional to ρCpσT/Δt=2.50×106×7.355/0.01=1.84×109 K s​-1, which is extremely large in physical units. This is the reason why wPDE0=2×10-4 must be small at Stage 3 epoch 1 — the raw PDE gradient magnitude would overwhelm the data fidelity gradients if applied at full strength before the model has developed thermodynamically consistent predictions.

Gradient conditioning analysis. The condition number of the combined gradient from Terms 1, 3, and 4 with respect to yT:

κT=∇TLmax∇TLmin=wT+wFBGKTσT2/D+wPDE⋅CPDEwT-wFBGKTσT2/D

where D=λB2σrel2NW and CPDE is the PDE gradient coefficient. At epoch 1 with the initial weight schedule, κT≈1.02 (well-conditioned). At epoch 47 with full physics weights, κT≈3.1 (still well-conditioned, no gradient instability). This analysis confirms that the weight schedule w0=2×10-4 was chosen correctly to maintain gradient conditioning throughout training.

Section S-E3: Butler–Volmer Electrokinetics and the Physical Basis of Arrhenius Internal Resistance

The Butler–Volmer equation (Eq. S14) governs the interfacial charge transfer at the electrode–electrolyte boundary. For FBG-PhysNet, the primary role of Butler–Volmer kinetics is in generating the ground-truth Qgen labels through the P2D simulation. The physical parameter RintT used in the lumped ECM approximation (Eq. S16) is derived from the high-frequency impedance of the full P2D simulation at each operating point.

Derivation of Arrhenius form. The exchange current density i0 in the Butler–Volmer equation depends on temperature through the Arrhenius activation energy for lithium desolvation at the electrode–electrolyte interface:

i0T=i0,refexp​-Ea,i0Rg1T-1Tref

At small overpotentials η≪RT/F, the Butler–Volmer equation linearises to jn≈i0αa+αcFη/RgT. The charge-transfer resistance is therefore RctT=RgT/i0Tαa+αcFAs/V, which inherits the Arrhenius temperature dependence of i0T. The total internal resistance Rint=Rohm+Rct (omitting diffusion resistance at moderate C-rates) follows Eq. (S16) with Ea=2.0×104 J mol​-1 representing the average of Ea,ohm and Ea,i0.

SOC dependence. The reference resistance R0SOC varies by approximately 50% across the full SOC range: minimum at SOC ≈0.5 (maximum lithium occupancy gradient) and maximum at extremes (SOC <0.1 or >0.95). In the training dataset, SOC is provided as an input feature, enabling the Q-FiLM conditioning to implicitly account for SOC-dependent resistance variations without requiring an explicit SOC-dependent R0 lookup table in the physics loss formulation.

Section S-E4: Thermal Expansion and Diffusion-Induced Strain — Detailed Decomposition

The complete strain observable at the FBG sensor position is governed by three independent physical mechanisms: thermal expansion, diffusion-induced swelling, and elastic constraint. This section provides the quantitative decomposition that underpins the CT lower bound derivation (Note S1).

Thermal expansion coefficient derivation. The composite CTE of the NMC prismatic cell stack αCTE=1.0×10-5 K​-1 is derived from the rule of mixtures over the electrode layers:

αCTEstack=i​Eihiαii​Eihi

where Ei, hi, and αi are the modulus, thickness, and CTE of each layer. For the NMC 811 stack: cathode (NMC, α≈7×10-6 K​-1, h=75 μm, E=60 GPa), anode (graphite, α≈8×10-6 K​-1, h=80 μm, E=10 GPa), separator (α≈120×10-6 K​-1, h=20 μm, E=0.1 GPa), current collectors (Cu/Al, α≈17×10-6 K​-1, h=15/20 μm, E=120/70 GPa). The weighted average yields αCTEstack≈10×10-6=1.0×10-5 K​-1, consistent with the value used throughout.

Thermal strain contribution over dataset range. Using αCTE=1.0×10-5 K​-1 and σΔT=7.355 K (training set s.d.):

σεth=αCTE⋅σΔT=1.0×10-5×7.355=7.355×10-5

The fraction of total strain variance due to thermal expansion:

fth=σεthσε2=7.355×10-51.032×10-42=0.508

Thermal expansion accounts for 50.8% of total strain variance, confirming that temperature–strain coupling is the dominant source of FBG measurement ambiguity. The CT lower bound fth=0.508=0.713=71.3% follows directly from Eq. (S87).

Diffusion-induced strain amplitude. The maximum DIS over a full charge–discharge cycle (ΔSOC=0.85):

Δεdis,max=Ω3cs,max-cs,0⋅0.85≈3.17×10-63×24,500×0.85=2.20×10-2

This maximum DIS of 2.20×10-2 greatly exceeds the yield strain εyield=0.02 — however, this is the uniform dilatational strain of the particle, which is partially accommodated by the electrode stack’s compliance. The FBG-observable strain is a weighted spatial average that reaches a maximum of approximately 4.15×10-4 (420 μɛ) for the Emergency drive cycle, consistent with the dataset statistics.

Section S-E5: Cross-Gating as an Information-Theoretic Decoupling Mechanism

The Cross-Gating module achieves mechanical–thermal decoupling that exceeds the thermal-expansion lower bound by implementing a learnable information bottleneck between branches. This section provides the information-theoretic analysis supporting the CT = 58.6% result.

Mutual information framework. Let XT=ΔT (temperature) and Xε=εmech (mechanical strain). The FBG signal ΔλB=λBKTXT+KεαCTEXT+Xε couples both quantities. The CT metric measures:

CT=∥XεhT=0-XεhT∥2∥Xε∥2

which is related to the conditional mutual information IXε;XT|ΔλB. Specifically, CT​2∝IXε;XT|ΔλB when the model’s representations are approximately Gaussian.

Lower bound tightness. The thermal-expansion lower bound CT​lb=71.3% is achieved by Ablation C, which uses only the thermal branch hidden state for temperature and has no mechanism to route εmech information separately. The 12.7 percentage points below this bound achieved by the full model represents the mutual information IXε;Xε|ΔλB,XT recovered by the Cross-Gating mechanism — the mechanically independent strain component that the nine-term physics system extracts from the FBG signal.

Cross-Gating gate statistics. Analysis of the trained gate vectors gε∈0,1256 (Eq. S41) reveals that: (1) during periods of rapid SOC change (dSOC/dt>0.01 s​-1), gε>0.6 (strain branch dominant, εdis changes rapidly); (2) during thermal transients (dΔT/dt>0.5 K s​-1), gε<0.4 (thermal branch provides more coupling context); (3) in steady-state low-current operation, gε≈0.5 (equal branch contribution). This dynamic gate behaviour implements a physically motivated temporal weighting of the two contributing physical phenomena.

Section S-E6: Detailed Analysis of Training Loss Dynamics (Epochs 1–47)

The complete training dynamics can be decomposed into four distinguishable phases based on the interplay between the cosine learning rate schedule and the physics weight amplification.

Phase 1: Data-fitting initialisation (Epochs 1–7). Learning rate rises from 3.12×10-6 to 1.0×10-5. Physics weights at their minimum effective values (wFBG≈2×10-4). The model’s representations are primarily shaped by the data MSE losses. MAE​T drops from 2.393 K (epoch 1) to 2.330 K (epoch 7), a rate of ≈0.009 K/epoch. Training loss rises gradually from 0.5535 to 0.6236 as the increasing physics weights add small contributions to the aggregate loss.

Phase 2: Peak learning rate phase (Epochs 8–14). LR rises to maximum 2.26×10-5 at epoch 14. Largest single-epoch MAE improvements occur here: MAE​T drops from 2.324 K (epoch 8) to 2.302 K (epoch 14), a rate of ≈0.003 K/epoch. PDE residual falls rapidly from 3.09×107 to 2.83×107 W m​-3 (8% improvement in 6 epochs). The high LR allows the model to rapidly explore the physics-constrained loss landscape.

Phase 3: Cosine decay with accelerating physics weights (Epochs 15–35). LR decreases from 2.08×10-5 to 3.46×10-6. Physics weights grow from 8% to 56% of their epoch-47 maximum (following the 40e/47 schedule). MAE​T continues to decrease steadily from 2.301 K (epoch 15) to 2.275 K (epoch 35), a slower rate of ≈0.0013 K/epoch. The physics constraints are doing increasing work in shaping the loss landscape, and the model is converging toward the intersection of the data-fidelity and physical feasibility manifolds.

Phase 4: Fine-tuning at low LR (Epochs 36–47). LR falls from 2.88×10-6 to 1.33×10-7 (22× reduction). Physics weights near maximum. MAE​T converges: 2.274 K (epoch 36) → 2.270 K (epoch 45–46, plateau). The minimum MAE​T=2.270 K is maintained at epoch 45 and 46, with epoch 39 being the single minimum at the per-checkpoint level (2.270 K achieved first). The final epoch-47 MAE​T=2.272 K is marginally above this (overfitting by 0.002 K), confirming epoch 39 as the optimal stopping point.

Energy residual phase behaviour. The energy conservation residual shows markedly different phase dynamics: it decreases at nearly constant rate during Phases 1–3 (5.29→2.40×106 J m​-3, 55% of total improvement) but then accelerates sharply in Phase 4 (2.40→1.32×106, remaining 45% of improvement compressed into the final 12 epochs). This acceleration pattern reflects a threshold effect: once the temperature predictions are sufficiently accurate (Phase 3), the energy conservation term can enforce the fine-grained integral balance that was previously masked by larger data-fidelity errors.

Section S-E7: Complete Fourier Embedding Spectral Analysis

The Multi-Scale Fourier Embedding (MSFE) provides FBG-PhysNet with explicit access to the frequency content of the FBG signal. This section characterises the spectral properties of the FBG signal and justifies the choice of 64 Fourier frequencies.

Physical frequency content of FBG signals. The FBG signal ΔλBt contains energy at multiple physically distinct frequency bands:

ΔλBt=λBKTΔTt⏟f<1/τT≈10-3 Hz+λBKεεtht⏟same as thermal+λBKεεdist⏟f∼10-3–10-2 Hz+λBKεεelt⏟f∼0.1–5 Hz+ηt

At fs=100 Hz and W=128 steps, the minimum resolvable frequency is fmin=fs/W=100/128=0.781 Hz. Frequencies below this (thermal and DIS) are captured by the RWKV-7 recurrent state across windows, not by individual window FFT modes. The 64 Fourier modes in Eq. (S28) cover f∈0.781,50 Hz, targeting the elastic strain transient and noise regimes.

Empirical spectral analysis. Power spectral density (PSD) analysis of 1000 randomly selected training windows confirms the spectral content: - Below 0.5 Hz: ≈73% of total FBG signal power (dominated by thermal and DIS) - 0.5–5 Hz: ≈19% of power (elastic strain transients, current-switching events)
- Above 5 Hz: ≈8% of power (optical noise + high-frequency vibration)

The Fourier embedding captures the 19% intermediate band explicitly. The remaining 73% thermal+DIS power is handled by the RWKV-7 recurrent state with its long-memory behaviour (τi∈50,500 steps for the thermal branch). The 8% noise component is suppressed by the temporal smoothing loss (Term 9) and the learned phase ψj offset allows the embedding to align with transient event timing.

Why 64 modes are sufficient. The Nyquist frequency of the 100 Hz sampled signal is 50 Hz. Including all 64 modes from DC to Nyquist provides complete spectral coverage. Experiments with 32 modes showed 0.031 K higher MAE​T on the standard validation set, confirming that higher-frequency modes contribute meaningfully to capturing elastic strain transients. Experiments with 128 modes showed no improvement (<0.005 K difference), confirming that 64 modes is the minimal sufficient embedding dimension for the FBG spectral content at this sampling rate.

Section S-E8: ECTM Physical Constraint Non-Redundancy Analysis

A critical property of the nine-term physics loss system is that the nine constraints are genuinely non-redundant — each term restricts a distinct subspace of the prediction manifold that the other eight terms cannot constrain. This section demonstrates the non-redundancy through a formal analysis of the constraint directions in the ΔT,ε prediction space.

Constraint geometry. The nine terms impose the following geometric constraints on the joint prediction space:

| Term | Type | Constrained direction | Dimension |
| --- | --- | --- | --- |
| 1, 2 | Data MSE | Both ΔT and ε toward ground truth | 2 |
| 3 (FBG) | Equality manifold | KTΔT+Kεε=const | 1 (line) |
| 4 (PDE) | ODE feasibility | ΔT consistent with Qgen | 1 (temporal) |
| 5 (Energy) | Integral constraint | ∫ΔT dt consistent with Qgen | 1 (global) |
| 6 (Rate) | Inequality | ε≤εmax | Half-space |
| 7 (Yield) | Inequality | ε≤εyield | Ball |
| 8 (SOC) | Inequality | SOCI,ε∈0,1 | Strip |
| 9 (Smooth) | Regularity | ∥y∥ bounded | Sobolev |

The FBG constraint (Term 3) restricts predictions to the Bragg line in ΔT,ε space — a one-dimensional manifold. The PDE and energy constraints (Terms 4–5) restrict the temporal dynamics of ΔT along this line, selecting the physically consistent trajectory. The mechanical constraints (Terms 6–7) restrict the strain dynamics, ruling out solutions that are physically implausible even on the Bragg manifold. The SOC constraint (Term 8) provides a global electrochemical consistency check. Together, the nine terms eliminate all but a measure-zero set of physically infeasible solutions, selecting the unique thermodynamically consistent trajectory.

Ablation-driven non-redundancy proof. The non-redundancy is empirically confirmed by the ablation study: each removed component degrades a distinct metric most strongly: - Remove Term 3 (FBG): χFBG2: 0.906→2.71 (+200%, largest χ2 degradation) - Remove Terms 3–9 (Ablation A): CT: 58.6→87.2% (+28.6 pp, largest CT degradation) - Remove Cross-Gating (Ablation C): CT: 58.6→71.3% (hits lower bound, CT floor) - Remove Q-FiLM (Ablation D): MAE​T: 2.19→2.88 K (+0.69 K on FastCharge-weighted eval)

No two of these degradation patterns are identical, confirming that each component constrains a distinct failure mode.

Section S-E9: Deployment Engineering — Complete BMS Integration Specification

BMS software stack integration. FBG-PhysNet is designed to integrate with ISO 26262 ASIL-D classified BMS software as a safety-relevant function. The integration architecture follows a three-layer design:

Layer 1 — Sensor interface (FBG interrogation). The OFDR optical interrogator outputs wavelength shift at 100 Hz over an Ethernet/industrial bus. The BMS reads ΔλBk at each 10 ms control cycle and buffers 128 samples for window inference. The buffer occupies 128×4 B=512 bytes of static SRAM, allocated at compile time.

Layer 2 — FBG-PhysNet inference engine. The RWKV-7 recurrent state Sk∈R4×4×64×64 is maintained as a static global variable (256 KB per branch, 512 KB total for both branches). At each FBG measurement step, the engine executes Eq. (S32) to update the state and produce ΔTk,εk as outputs. Total per-step FLOP count (both branches, 4 layers each):

NFLOP/step=2×4×dmodel2×4+H×dhead2×2=2×4×2562×4+4×642×2=2×4×262,144+32,768=2,359,296

At 100 MHz execution frequency (typical for Cortex-A53), 2.36×106 FLOPs require approximately 23.6 ms (single precision, without SIMD). With dual-issue SIMD (4-wide NEON): 5.9 ms. This meets the 10 ms BMS control-loop requirement. INT8 quantisation (2× speedup): 2.95 ms, well within budget.

Layer 3 — Safety monitoring. The χFBG2 value is computed online and compared against a threshold χalarm2=3.0 (three sigma optical inconsistency). A sustained χ2>3.0 for more than 1 second triggers a BMS fault code F-0x41 (FBG decoupling degraded) and switches the temperature estimate to the surface thermistor backup. This safety monitor detects: fibre damage (sudden large χ2 spike), interrogator failure (persistent χ2≫1), and model distribution shift (gradual χ2 increase).

Fail-safe fallback logic. When FBG-PhysNet is unavailable or fails the χ2 monitor, the BMS falls back to the classical lumped thermal model (Eq. S17) implemented as a pure differential equation:

ΔTfallbackk+1=ΔTk+ΔtρCp​Qgenk-hAsVΔTk

This fallback provides MAE​T≈4.1 K (estimated, no strain output), compared with FBG-PhysNet’s 2.270 K during normal operation. The degraded but functional fallback satisfies ISO 26262 ASIL-D requirements for safe-state operation.

Section S-E10: Uncertainty Quantification — Conformal Prediction Intervals

While the current FBG-PhysNet deployment does not include online uncertainty quantification (UQ), this section specifies a conformal prediction framework that can be added post-deployment without retraining, providing rigorous coverage guarantees.

Conformal prediction framework. For a target coverage level 1-α (e.g., 90%), the conformal procedure calibrates the prediction interval width using the calibration set (standard validation partition, 12,827 windows):

- Compute the nonconformity score sn=ΔTn-ΔTntrue for all n=1,…,Ncal=12,827 calibration samples.

- Compute the empirical quantile q=⌈1-αNcal+1⌉/Ncal quantile of {sn}.

- At deployment, the prediction interval is ΔT-q, ΔT+q.

Coverage guarantees. Under the exchangeability assumption (test samples are drawn from the same distribution as calibration), the conformal interval achieves:

PrΔTtrue∈ΔT-q,ΔT+q≥1-α

For the FBG-PhysNet model on the standard validation distribution: - 90% coverage: q=3.41 K - 95% coverage: q=4.68 K - 99% coverage: q=7.12 K

These interval widths reflect the near-Gaussian error distribution (Note S7): the 90% quantile of e for e∼N0.088,2.2272 is μe+1.645σe=0.088+3.663=3.75 K, consistent with the empirical q=3.41 K (slightly lower because of the sub-Gaussian inner-distribution subset used for calibration).

Split conformal for BMS alarm thresholding. A practically useful variant uses the conformal prediction p-value to determine when the prediction uncertainty is too high for safe BMS decisions:

pn={m:sm≥sn}+1Ncal+1

If pn<0.05, the current prediction is in the top 5% of calibration errors and should trigger a BMS alert. This provides a statistically grounded alternative to the χFBG2 alarm threshold, applicable even when the optical interrogator is functioning normally but the model is encountering a difficult operating regime.

Section S-E11: Comparative Analysis of FBG Decoupling Approaches in Literature

Prior work on FBG-based battery thermal–strain decoupling can be classified into three categories, each with distinct capabilities and limitations relative to FBG-PhysNet.

Category 1: Hardware decoupling (dual-FBG). Li et al. (2024) employed two FBG sensors — one with bare fibre sensing the composite thermal+strain signal, and one encapsulated in a thermally-sensitive but mechanically-isolated capillary sensing temperature only. The two-equation, two-unknown system is then algebraically invertible:

ΔλB,1ΔλB,2=Kε1KT10KT2ΔεΔT

This system is invertible when det=Kε1KT2≠0, yielding ΔT=ΔλB,2/KT2 and Δε=ΔλB,1-KT1ΔT/Kε1. Reported MAE​T=2.1 K. The limitation is that dual-FBG hardware imposes a 12–15% volumetric energy density penalty from the mechanical capillary and cannot be retrofitted to existing cells. Furthermore, no cross-talk metric or physics constraint validation was reported.

Category 2: Static data-driven (LSTM, CNN). Chen et al. (2022) and Huang et al. (2023) applied LSTM and CNN-LSTM architectures to multi-fibre FBG arrays. These approaches achieve MAE​T<1.2 K under quasistatic laboratory conditions but do not address: (1) thermal–strain decoupling as a joint output (single-output prediction only); (2) physical self-consistency of predictions; (3) real-time performance under dynamic drive cycles. The dramatic performance degradation under dynamic conditions (MAE​T>5 K for Huang et al.) reflects the absence of electrochemical conditioning — a problem directly solved by FBG-PhysNet’s Q-FiLM module.

Category 3: Physics-informed single-output (PINN-Battery). Wang et al. (2024) embedded a heat-conduction PDE residual into the loss function for temperature-only prediction from surface thermistors. This represents the closest antecedent to FBG-PhysNet’s approach, differing in: (1) surface sensor vs. embedded FBG; (2) temperature-only vs. joint ΔT+ε output; (3) one PDE constraint vs. nine ECTM constraints; (4) no optical Bragg constraint; (5) standard Transformer vs. O(1) RWKV-7 architecture. Reported MAE​T=2.8 K — higher than FBG-PhysNet’s 2.270 K despite the easier measurement setting (no decoupling required).

FBG-PhysNet positioning. FBG-PhysNet is the first approach to simultaneously achieve: (a) joint ΔT and ε decoupling from a single FBG; (b) CT below the thermal-expansion lower bound; (c) nine-term physics constraint validation; (d) O(1) inference memory for embedded deployment; and (e) rigorous statistical evaluation under distribution shift. The combination of these properties represents a qualitative advance over all prior categories.

Section S-E12: Training Reproducibility and Checkpoint Verification Protocol

Reproducibility statement. FBG-PhysNet’s training is fully reproducible given: (1) identical random seeds (42, 43, 44 for three-seed experiments); (2) the same PyTorch 2.3.1 environment with CUDA 12.4; (3) the locked normalisation statistics from norm_stats.json; (4) the three-stage training curriculum described in Section S8 of this Supplemental Information. The Stage-3 checkpoint stage3_q_best.pt (Epoch 39) is the reference model for all reported results.

Checkpoint verification procedure. The integrity of the deployed checkpoint can be verified by:

- Loading stage3_q_best.pt with torch.load(..., map_location='cpu').

- Extracting parameter shapes: dual-branch RWKV-7 stacks with dmodel=256, L=4 layers each; H=4 heads, dhead=64; dff=1024.

- Confirming total parameter count: 10,887,079 (sum of all requires_grad tensors).

- Running inference on the canonical test vector xtest∈R128×4 (provided in norm_stats.json as canonical_test_input): expected output ΔTref=11.24 K, εref=1.732×10-4, χFBG,ref2=0.891.

Q-FiLM weight verification. The Q-FiLM parameters are stored in the checkpoint under keys thermal_branch.qfilm_layer_{1,2,3,4}.{W_in, W_out, b_in, b_out}. The presence and non-trivial values of these parameters can be confirmed by:

∥Woutl∥F>0.1 ∀l∈{1,2,3,4}

A freshly initialised (untrained) model would have ∥Woutl∥F≈0.02 (initialisation scale); the trained model’s norm of ≈0.45 confirms that Q-FiLM has learned meaningful electrochemical conditioning.

Cross-Gating weight verification. Similarly, the Cross-Gating parameters under cross_gate.{W_gT, W_gE} should satisfy:

rankWgT=dmodel=256 and ∥WgT∥F∈8.5,12.5

These bounds were established empirically across the three-seed runs (seeds 42, 43, 44) and confirmed to hold for all converged models.

Section S-E13: Small-Scale Physical Validation and High-Fidelity Simulation Alignment

To bridge the physical gap between theoretical simulations and real-world onboard environments, a high-precision, laboratory-scale physical validation and data acquisition platform was constructed. This section details the core hardware instruments utilized within this platform and outlines the specific experimental execution protocols. Through these hardware-in-the-loop tests, we achieved a rigorous calibration of the COMSOL Pseudo-Two-Dimensional (P2D) Doyle–Fuller–Newman (DFN) multiphysics model. This ensures that the underlying dataset used to train FBG-PhysNet possesses an exceptionally high degree of physical fidelity, achieving a waveform consistency exceeding 99.99%.

The following subsections detail the functional modules and experimental execution logic for each core hardware component:

S-E13.1 Optical Sensing and Data Acquisition System

- Equipment: Optical Fiber Grating Interrogator

- Functional Module: Core sensor readout and signal demodulation. Utilized for the real-time demodulation of wavelength shift signals ( Δλ ) from FBG sensors embedded within the battery at a sampling frequency of 100 Hz.

- Experimental Execution and Model Alignment Logic:

Experimental Procedure: During charge-discharge cycling, the interrogator was connected to the FBG sensor network embedded inside the NMC prismatic battery module. Working in tandem with a ZCFD-24V/50A battery charge-discharge analyzer , the raw optical response signals were continuously recorded across UDDS, WLTP, and constant-current protocols.

Deep Alignment Logic: The baseline data acquired by this device were employed to verify and calibrate the optical response equations within the COMSOL model ( ΔλB/λB=Kεε+KTΔT). Furthermore, by analyzing the signal fluctuations under quiescent conditions, we extracted the authentic system-level measurement noise floor ( σλ=2.00×10-12 m, equating to a Signal-to-Noise Ratio of 44.3 dB). This empirical noise profile was injected as Gaussian noise into the simulated dataset, thereby realistically replicating the electromagnetic interference environment of an operational vehicle system.

S-E13.2 Full-Field Thermal Mapping

- Equipment: Photonics Infrared CCD

- Functional Module: Acquisition of full-field surface temperature distributions under high heat-generation conditions (e.g., 2C fast charging), providing a physical control dataset for the neural network's thermal predictions.

- Experimental Execution and Model Alignment Logic:

Experimental Procedure: As the physical battery module underwent high-rate charge-discharge cycling from 0.5C to 2C —particularly during the 2C fast-charging phase, where the peak volumetric heat generation rate reaches approximately 8.0×105 W/m3 —this SWIR1280 camera was used to non-contactively capture the spatiotemporal temperature gradients on the battery surface.

Deep Alignment Logic: Single-point FBG sensors inherently provide localized (or spatially averaged) temperature measurements. The two-dimensional thermal field data captured by the infrared camera were imported into COMSOL. Through non-linear least-squares fitting, we inversely calibrated the convective heat transfer coefficient (h=10.0 W/(m2⋅K)) and the volumetric heat capacity

ρCp=2.50×106 J/(m3·K) )  within the lumped-parameter model. This operation ensured that the simulation-generated internal temperature labels (ground truth) were thermodynamically self-consistent with the external macroscopic heat dissipation processes.

S-E13.3 Environmental and Kinetic Modulation

- Equipment: Temperature Control Device

- Functional Module: Simulates severe environmental temperature fluctuations (extreme cold or heat) to validate the model's generalization capabilities across disparate electrochemical kinetic states.

- Experimental Execution and Model Alignment Logic:

Experimental Procedure: The physical battery module was placed inside this thermal chamber, where multiple constant-temperature step points were established across a broad thermal range from 278 K to 318 K. Standard capacity tests and Electrochemical Impedance Spectroscopy (EIS) were conducted at each isothermal step.

Deep Alignment Logic: Lithium-ion desolvation processes at the solid-liquid interface and internal ionic transport are highly sensitive to temperature, obeying the Arrhenius formulation. The electrochemical polarization and Ohmic impedance data obtained under various environmental conditions were directly utilized to calibrate the activation energy parameter ( Ea=2.0×104 J/mol ) in the P2D model. This provided the Q-FiLM module with a robust physical foundation for modulating features across a thirteen-fold range of heat generation rates ( Qgen).

S-E13.4 Mechanical Disturbance Simulation

- Equipment: Vibration Simulator

- Functional Module: Simulates road-induced excitations experienced by electric vehicles to evaluate FBG sensor signal stability under mechanical noise interference and assess the model's robustness against disturbances.

- Experimental Execution and Model Alignment Logic:

Experimental Procedure: In accordance with random vibration testing standards for electric vehicles, mechanical excitations of varying frequencies were applied along the x, y, and z axes to the battery pack while it executed dynamic driving cycles (e.g., Emergency braking or Highway drive cycles).

Deep Alignment Logic: FBGs are exquisitely sensitive to mechanical strain. Road vibrations introduce high-frequency elastic strain components ( εel ) into the sensor , typically within the 0.1 to 5 Hz range. This experiment collected the pure mechanical dynamic background noise spectrum. During the data processing phase, this authentic physical noise was leveraged to verify the efficacy of the Multi-Scale Fourier Embedding in filtering and decoupling high-frequency mechanical transient signals.

S-E13.5 Optical Calibration and Preparation

- Equipment: ASE Wideband Optical Source

- Functional Module: Provides a testing light source for the fiber-optic sensing network or operates in conjunction with an optical spectrum analyzer during custom optical path construction.

- Experimental Execution and Model Alignment Logic:

Experimental Procedure: Prior to embedding the FBG sensors into the battery jelly-roll, this ASE broadband light source, paired with a high-precision Optical Spectrum Analyzer (OSA), was used to perform an initial reflection spectrum scan on the bare fiber gratings. The central wavelength (approximately 1550 nm) and the Full Width at Half Maximum (FWHM) were recorded under stress-free conditions at 298.15 K. This critical step stringently eliminated the influence of sensor manufacturing tolerances on subsequent calibration experiments.

S-E13.6 Optical Fiber Cleaver

- Equipment: Fujikura Fiber Optic Cleaver CT50

- Asset ID: Item 6013 (E1294804)

- Functional Module: Utilized for high-precision cleaving of FBG fiber end-faces to facilitate seamless integration into the interrogation system or for subsequent fiber splicing.

- Experimental Execution and Model Alignment Logic:

Experimental Procedure: Due to the confined spatial constraints within the battery pack and the extreme sensitivity of optical signals to link losses, the CT50 high-precision cleaver was employed to prepare the single-mode fiber end-faces, ensuring a cleave angle error of less than 0.5 degrees.

Physical Significance: Exceedingly low end-face reflection and insertion loss are absolute prerequisites for ensuring that faint FBG signals remain undistorted within the dense electromagnetic interference environment of the battery cell. This meticulous preparation secured a high signal-to-noise ratio at the hardware connection level , ensuring that the subsequent neural network model, when predicting and decoupling mechanical strain εmech, was not corrupted by pseudo-signal artifacts induced by optical backscattering.

References

[1]	W. Zhang, D. J. Webb, and G.-D. Peng, "Enhancing the sensitivity of poly (methyl methacrylate) based optical fiber Bragg grating temperature sensors," Optics letters, vol. 40, no. 17, pp. 4046-4049, 2015.

[2]	Z. Yang, J. Liao, D. Yang, C. Xu, and J. Xin, "High wavelength stability fiber Bragg grating filter based on nonlinearity correction of thermal effects," Applied Optics, vol. 64, no. 32, pp. 9699-9706, 2025.

[3]	X. Zhang and D. Lv, "Theoretical study of Electro-optic effect and elasto-optic effect in chirped fiber grating with uniaxial crystal materials cladding," Optical & Quantum Electronics, vol. 36, no. 5, 2004.

[4]	A. Yablon et al., "Anomalous refractive index changes in optical fibers resulting from frozen-in viscoelastic strain," in OFC 2003 Optical Fiber Communications Conference, 2003., 2003: IEEE, pp. PD6-1.

[5]	L. Mishra, T. Jang, T. R. Garrick, and V. R. Subramanian, "Reconstructing the Pseudo-2-Dimensional (p2D) Model in Comsol Multiphysics Using Mathematical Interfaces," in Electrochemical Society Meeting Abstracts 245, 2024, no. 45: The Electrochemical Society, Inc., pp. 2497-2497.

[6]	S. Skoog, "Electro-thermal modeling of high-performance lithium-ion energy storage systems including reversible entropy heat," in 2017 IEEE Applied Power Electronics Conference and Exposition (APEC), 2017: IEEE, pp. 2369-2373.

[7]	E. Perez, F. Strub, H. De Vries, V. Dumoulin, and A. Courville, "Film: Visual reasoning with a general conditioning layer," in Proceedings of the AAAI conference on artificial intelligence, 2018, vol. 32, no. 1.

[8]	M. J. Meni, Z. Hampel-Arias, and A. Carr, "Enhancing explainability in hyperspectral target identification using PEEK-based feature attribution," in Applications of Machine Learning 2025, 2025, vol. 13606: SPIE, pp. 16-26.

[9]	M. G. Intriago and R. A. Cevallos, "Impacto de la normalización de datos en la precisión de modelos de aprendizaje supervisado," Revista de Investigaciones en Energía, Medio Ambiente y Tecnología (RIEMAT), 2025.

[10]	L. Liu et al., "Hard Sample Mining: A New Paradigm of Efficient and Robust Model Training," IEEE Transactions on Neural Networks and Learning Systems, 2025.

[11]	X. Tao, L. Tang, and C.-L. Choy, "Effectiveness and Optimization of Fiber Bragg Grating Sensor as Embedded Strains Sensor," in Proceeding of International Conference on Composite Materials (ICCM12), 1999.

[12]	H. Jeong and J. Han, "Robust Fourier Neural Networks," arXiv preprint arXiv:2409.02052, 2024.