Supporting Information

Plant-Derived Hydrolates as Functional Components in Nanostructured Topical Systems: A Comparative Study of Hydrolate-Based Nanogel and Emulgel Platforms

Figure S1. Macroscopic appearance of the hydrolate-loaded nanogel formulations prepared with increasing proportions of HDAo in the aqueous phase. From left to right: NG-6, containing 25% HDAo; NG-7, containing 50% HDAo; NG-8, containing 75% HDAo; and NG-9, containing 100% HDAo. All formulations showed a homogeneous visual appearance, supporting the compatibility of HDAo incorporation into the Pluronic F127/Carbopol 974P nanogel matrix.

Figure S2. Macroscopic demonstration of the thermoresponsive behavior of Ao-NG. The formulation remained in the sol state at low temperature, showing fluidity and flow under the evaluated condition. After temperature increase, Ao-NG transitioned to the gel state, maintaining its position after vial inversion. This sol--gel transition supports the thermoresponsive character of the Pluronic F127/Carbopol 974P nanogel matrix containing HDAo.

Figure S3. Macroscopic appearance of the hydrolate-loaded emulgel formulations prepared with increasing proportions of HDPb in the aqueous phase. From left to right:  EG-15, EG-16, EG-17, EG-18, and EG-19, corresponding respectively to 10%, 20%, 30%, 40%, and 50% HDPb in the aqueous phase. The formulations showed visually homogeneous emulgel characteristics without evident macroscopic phase separation, supporting the compatibility of HDPb incorporation into the Pluronic F127/Carbopol 974P/babassu oil polymer–lipid matrix.

Figure S4. FTIR spectra of the nanogel systems. The spectrum on the left corresponds to NG, representing the reference nanogel matrix, whereas the spectrum on the right corresponds to Ao-NG, representing the Anacardium occidentale hydrolate-loaded nanogel. The comparison indicates that hydrolate incorporation modified the spectral profile of the polymeric matrix, particularly in the O--H stretching region and in the C--O--C band associated with Pluronic F127.

Figure S5. FTIR spectra of the emulgel-related systems. From top to bottom, the spectra correspond to babassu oil, EG, and Pb-EG. The babassu oil spectrum shows characteristic bands associated with aliphatic C--H stretching and ester carbonyl groups, while EG preserves the main absorption bands of the polymer--lipid matrix. After HDPb incorporation, Pb-EG shows changes mainly in the O--H stretching region and in bands associated with polar functional groups, indicating the contribution of hydrolate-derived constituents and non-covalent interactions within the emulgel matrix.

Figure S6. DSC thermograms of the nanogel systems. The upper curve corresponds to NG, representing the reference nanogel matrix, whereas the lower curve corresponds to Ao-NG, representing the Anacardium occidentale hydrolate-loaded nanogel. NG showed a main endothermic event at approximately 57 °C, while Ao-NG showed a shifted thermal event at approximately 54 °C with reduced intensity, suggesting hydrolate-induced modulation of the polymeric matrix organization. Additional thermal events observed in NG at higher temperatures indicate subsequent matrix reorganization or degradation processes.

Figure S7. DSC thermograms of the emulgel systems. The upper curve corresponds to EG, representing the reference emulgel matrix, whereas the lower curve corresponds to Pb-EG, representing the Pectis brevipedunculata hydrolate-loaded emulgel. Both systems showed a main thermal event in the lower temperature region, while Pb-EG exhibited a smoother thermal profile and lower heat-flow variation over the evaluated range, suggesting that hydrolate incorporation contributed to greater matrix homogeneity and modified the thermal organization of the polymer–lipid system.