Supplementary Information

Experimental and Thermodynamic Investigation of Ash Chemistry and Combustion Conditions Governing Biogenic Silica Production from Agricultural Biomass Residues

Clement Owusu Prempeh 1,2*, Hossein Beidaghy Dizaji2, Ingo Hartmann1, Steffi Formann3 and Michael Nelles1,4

1Department of Thermochemical Conversion, DBFZ Deutsches Biomasseforschungszentrum Gemeinnützige GmbH, Torgauer Straße 116, 04347 Leipzig, Germany; Ingo.Hartmann@dbfz.de (I.H.); Michael.Nelles@dbfz.de (M.N.)

2 ORCID: 0000-0002-1255-9480;

3 Department of Geosciences and Geography, Faculty of Natural Sciences III, Martin Luther University Halle-Wittenberg, Von-Seckendorff-Platz 3-4, 06120 Halle (Saale), Germany; steffi.formann@geo.uni-halle.de (S.F.)

4Department of Agriculture and Environmental Science, University of Rostock, Justus-von-Liebig-Weg 6, 18059 Rostock, Germany

*Correspondence: Clement.OwusuPrempeh@dbfz.de; Tel.: +49-(0)341-2434-523

Table S1 Analysis of variance (ANOVA) for the quadratic model describing the effect of combustion temperature and holding time on the specific surface area (SBET) of silica derived from cornhusk.

| Source | Sum of Squares | df | Mean Square | F-value | p-value | Remark |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 32763.76 | 5 | 6552.75 | 22.92 | 0.0048 | Significant |
| Temperature (T) | 12349.95 | 1 | 12349.95 | 43.19 | 0.0028 | Significant |
| Residence Time (RT) | 239.51 | 1 | 239.51 | 0.84 | 0.4119 | Not significant |
| T × RT | 3497.73 | 1 | 3497.73 | 12.23 | 0.0250 | Significant |
| T² | 3187.65 | 1 | 3187.65 | 11.15 | 0.0289 | Significant |
| RT² | 3.88 | 1 | 3.88 | 0.0136 | 0.9129 | Not significant |
| Residual | 1143.83 | 4 | 285.96 | – | – | – |
| Cor Total | 33907.59 | 9 | – | – | – | – |

Model statistics: R² = 0.9663; Adjusted R² = 0.9241; Adequate Precision = 15.7543; C.V. = 19.11%.

Table S2 Analysis of variance (ANOVA) for the quadratic model describing the effect of combustion temperature and holding time on the pore volume (PV) of silica derived from cornhusk.

| Source | Sum of Squares | df | Mean Square | F-value | p-value | Remark |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 0.2705 | 5 | 0.0541 | 6.90 | 0.0424 | Significant |
| Temperature (T) | 0.0342 | 1 | 0.0342 | 4.36 | 0.1051 | Not significant |
| Holding Time (RT) | 0.0013 | 1 | 0.0013 | 0.16 | 0.7096 | Not significant |
| T × RT | 0.0700 | 1 | 0.0700 | 8.92 | 0.0404 | Significant |
| T² | 0.0788 | 1 | 0.0788 | 10.05 | 0.0338 | Significant |
| RT² | 0.0030 | 1 | 0.0030 | 0.3823 | 0.5698 | Not significant |
| Residual | 0.0314 | 4 | 0.0078 | – | – | – |
| Cor Total | 0.3019 | 9 | – | – | – | – |

Model statistics: R² = 0.8961; Adjusted R² = 0.7661; Adequate Precision = 8.5497; C.V. = 38.08%.