## Slide 1
Increasing combustion severity reduces surface area (SBET) and pore volume (PV)
K, Na, Ca, and Mg promote alkali–silicate melt formation and silica network depolymerization
Citric acid removes AAEMs, suppresses slagging, and enriches SiO₂
Optimal conditions:
550–650 °C, ~2 h
FEEDSTOCK CHEMISTRY + PROCESS OPTIMIZATION → HIGH-PURITY POROUS BIOGENIC SILICA
AGRICULTURAL BIOMASS RESIDUES
Thermodynamic modeling reveals biomass-specific melt evolution with reduced slagging
THERMOCHEMICAL CONVERSION
Controlled combustion at 400–700 °C
1-4 h
CITRIC ACID PRETREATMENT
Citric acid
(50 °C, 2 h)
Solid-to-liquid ratio: 1:10 (w/v)
(Cassava, Yam, Coconut,
Corncob, Cornhusk)
High silica purity, porosity
MULTIVARIATE MODELING & THERMODYNAMIC ANALYSIS
PCA
Leached ash
FactSage
Contour plot
PCA Score Plot
KEY FINDINGS
Optimal silica production