Assembly of Foldameric Copolymers into Ordered Nanostructures and Crystalline Networks

Hyeonmin Jeong1, Thi Vo1*

1 Chemical and Biomolecular Engineering, Johns Hopkins University, Baltimore, MD 21218

* Corresponding Author: tvo12@jhu.edu

Contents

Appendix A: Coarse-Grained Simulation Model for Foldameric Block Copolymer Assembly

Appendix B: Shape-Particle Simulation Model for Large-Scale Porous Network Formation

Appendix C: Characterization and Analysis

Appendix D: Melting Curves of Coarse-Grained Patchy Polygon

Appendix A: Coarse-Grained Simulation Model for Foldameric Block Copolymer Assembly

A.1 Model Design and Motivation

The coarse-grained (CG) model is designed to capture the essential physics of a linear block copolymer architecture consisting of alternating foldameric (B) and flexible (Ax) domains, following the Ax-[B-Ax]n motif described in the main text. The key physical requirement of this design is that the rigid, helical foldameric blocks act as steric spacers to prevent the hydrophobic flexible blocks from globally collapsing into an amorphous SNP-like globule, thereby directing chain folding into porous polygonal nanostructures. To encode these features, the model distinguishes between two chemically distinct block types. The foldameric block (B) is represented by rigid monomers capable of forming a stable α-helix, whose length scales linearly with the number of monomers (Lh∼Nh), consistent with a rigid-rod behavior. The flexible block (Ax) is represented by monomers whose size scales as Rf∼Nf1/3 upon hydrophobic collapse, mimicking the classical behavior of collapsed chains in a poor solvent. The interplay between Lh and Rf — specifically the condition Rf<Lh, or equivalently Nf<Nh3 — defines the boundary between well-folded polygonal nanostructures and misfolded morphologies, as established in the main text. Molecular dynamics simulations are performed using HOOMD-Blue v4.9.1

A.2 Particle Types and Interactions

The polymer chain is represented by monomers of two functional classes corresponding to the foldameric (B) and flexible (Ax) block types. Helix monomers, representing the foldameric block, are treated as part of rigid bodies to enforce the structural rigidity intrinsic to the folded helical domain; directional patch interactions between these monomers encode the specific geometry of helix–helix stacking, the key interaction driving the formation of straight, rigid edges in the folded nanostructure. Flexible monomers, representing the flexible block, interact isotropically and are designed to collapse upon activation of hydrophobic-like attraction, forming the compact vertex regions of the folded polygonal chain; the size of the collapsed flexible domain sets the vertex patch size used in the coarse-grained polygon model described in the main text. Additionally, long-range repulsive interactions between helix monomers prevent parallel edge alignment, promoting the formation of open, porous polygonal nanostructures rather than close-packed, globular morphologies, consistent with the design rationale outlined in the main text.

A.3 Interaction Potentials

Lennard-Jones (LJ) Potential

Steric interactions between all monomer pairs are described by the Lennard-Jones (LJ) potential,

ULJ(r)=4ϵσr12-σr6#A.1

where r is the center-to-center distance, ϵ is the interaction strength, and σ is the effective monomer diameter. For purely repulsive pairs, the cutoff is set at the WCA limit rcut=21/6σ with ϵrep=1.0. Selective attractive LJ interactions are activated between specific pairs during the simulation protocol to drive either helical–flexible block interfacial repulsion (ϵhelix-flex=10.0) or flexible–flexible monomer hydrophobic collapse, where the flexible monomer attraction strength is initially set to ϵflex,att=1.5 to complete the collapse of flexible blocks into the vertices and is subsequently increased to ϵflex,att=8.0 during the network formation stage.

Anisotropic Patchy LJ Potential

Directional helix–helix stacking interactions are modeled using an anisotropic patchy Lennard-Jones (PatchyLJ) potential, wherein the standard LJ potential is modulated by an orientation-dependent envelope function. The full pair potential between particles i and j takes the form,

Upatch(rij,qi,qj)=m=1Npatch,in=1Npatch,jf(θm,i, α, ω) f(θn,j, α, ω) ULJ(rij)#A.2

where ULJ(rij) is the isotropic Lennard-Jones pair potential with the attraction strength of patch ϵpatch and f is the normalized sigmoid envelope function defined as

f(θ, α, ω)=1e-ω(cos⁡θ-cos⁡α)-1-fminfmax-fmin#A.3

with normalization bounds

fmax=1e-ω(1-cos⁡α)-1,fmin=1e-ω(-1-cos⁡α)-1#A.4

Here, θm,i is the angle between the m-th patch director of particle i (rotated into the lab frame by its orientation quaternion qi) and the interparticle unit vector rij. The parameter α is the patch half-opening angle and ω controls the steepness of the patch boundary. In the limit f→1 (θ≪α, i.e., well within the patch), the potential reduces to the bare LJ interaction; when θ>α, the envelope decays rapidly to zero, suppressing interaction outside the patch cone. In the present model, each helix patch monomer carries a single director aligned along the helix axis, with α=30° and ω=30, such that two helix monomers interact attractively only when both directors are mutually pointed toward each other along the helix propagation axis, enforcing the end-to-end stacking geometry. The attractive strength is ϵpatch=17.5, activated during the folding stage.

Yukawa Potential

Long-range repulsive interactions between helix monomers are modeled using the Yukawa potential2,

UY(r)=ϵlaterale-κrr#A.5

where ϵ is the interaction strength, κ is the inverse screening length, and r is the center-to-center distance. Here ϵlateral=0.5 and κ=0 (unscreened), with a cutoff of 8.0σ. This long-range repulsion between helix monomers prevents parallel alignment of adjacent helical edges, which is the physical mechanism by which the model suppresses globular collapse and instead promotes the formation of open, porous polygonal geometries — analogous to the role of the steric repulsion between rigid foldameric edges described in the main text.

FENE-WCA Bond Potential

Covalent connectivity along the chain backbone is described by the finitely extensible nonlinear elastic (FENE) bond potential combined with a WCA repulsive term,

UFENE(r)=-12kr02ln⁡1-rr02+UWCA(r)#A.6

where k=30.0 is the spring constant and r0 is the maximum extensibility. The FENE potential connects both helix and flexible monomers along the chain contour, providing the bonded connectivity that constitutes the Ax-[B-Ax]n polymer sequence. The maximum extensibility r0 is logarithmically ramped from 5.0σ down to 1.0σ (helical block) and 2.0σ (flexible block), allowing the chain to gradually adopt its equilibrium bonded geometry without steric overlaps during initialization.

Gravitational Deposition Potential

To model substrate-directed deposition of the folded polygonal nanostructures, an external-field term was introduced in the form of a weak constant body force together with an attractive planar wall potential. The gravity-like driving force was implemented using a constant force acting along the negative x-direction, such that the flexible segments experience a force Fg=(-3gfactor,0,0), where gfactor=0.01. This external bias promotes gradual settling of the folded structures toward the substrate while avoiding abrupt distortion of the pre-formed polygonal conformations.

The substrate was represented by a planar Lennard-Jones wall positioned near the lower x-boundary of the simulation box. All backbone and patch particles experienced short-range steric repulsion from the wall with ϵwall,plane=1.0, while attractive wall interactions were additionally assigned to the flexible monomers with ϵwall,att=3.0 in the initial setup and increased to 6.0 during the gravity-assisted deposition stage. The combination of weak directional forcing and selective wall attraction enables quasi-two-dimensional deposition of folded nanostructures onto the surface, providing an initialized configuration suitable for subsequent lateral compression and network ordering.

A.4 Simulation Protocol

The simulation proceeds through sequential stages designed to first form the folded helical structure, then deposit the folded nanostructures onto a substrate, and subsequently drive inter-chain network assembly under lateral confinement. The chain backbone is first compacted during a FENE ramp stage, wherein the maximum extensibility r0 is reduced logarithmically over 750 steps × 200 MD timesteps to establish the equilibrium bonded geometry without steric overlaps. The system is then equilibrated for 3×105 steps at constant temperature, allowing residual stress from the ramp to relax.

A subsequent temperature-cycling stage applies a cyclic schedule with kBT oscillating between kBTlow=1.3 and kBThigh=1.7, with hold and ramp times of 2×105 steps each, to assist the helix monomers in sampling favorable orientational configurations prior to structure formation. During this stage, directional PatchyLJ attraction between helix patch monomers is activated with ϵpatch=17.5, while temporary long-range repulsive Yukawa interactions are introduced between helix-associated and flexer-associated species to suppress premature collapse and promote formation of well-defined polygonal conformations. The system is evolved for 1×106 steps under this cycling protocol, allowing helix-helix stacking contacts to develop and trigger chain cyclization into closed polygonal nanostructures.

Following folding, a gravity-assisted deposition stage is applied to transfer the folded structures toward the planar substrate. In this step, the constant external force Fg=(-3gfactor,0,0) with gfactor=0.01 is applied to flexible monomers, and the attractive wall interaction acting on the flexible block is strengthened to ϵwall,att=6.0, and the system is evolved for 1.5×106 steps to allow gradual surface deposition and relaxation of the folded polygons into a surface-associated configuration.

After deposition, the system is subjected to a quasi-static compression stage to increase lateral packing and promote crystalline network ordering. The box dimensions in the y and z directions are reduced using a BoxResize protocol, while the x-dimension is retained to preserve the substrate-normal direction established during deposition. Specifically, the target area is defined from Afinal=Vtotal/ϕtarget with ϕtarget=0.25, and the corresponding lateral box lengths are set to Ly=Lz=Afinal. The box is then compressed over 3×105 steps using a linear ramp, allowing the deposited polygons to reorganize into a more compact porous arrangement without abrupt mechanical disruption. In the final assembly stage, flexible block-mediated isotropic attractions are maintained, and the system is evolved for up to 1×109 steps to drive inter-chain association between pre-formed vertices and produce an extended porous crystalline network. All simulations are performed in the NVT ensemble using the Nosé--Hoover MTTK thermostat with thermostat relaxation time τ=1.0 and timestep Δt=5×10-4, and configurations are saved every 2×104 timesteps in GSD format.

Appendix B: Shape-Particle Simulation Model for Large-Scale Porous Network Formation

B.1 Model Design and Motivation

The shape-particle model represents each folded nanostructure as a single rigid polygonal particle equipped with localized interaction sites. The polygonal “core” captures the overall cross-sectional shape and size of the folded chain, while two classes of patches are attached: vertex patches located near the polygon vertices and edge patches positioned along the polygon edges. The polygonal area of each core is used to set the moment of inertia, ensuring that the rotational dynamics are consistent with the particle’s geometric size.

This construction coarse-grains away all internal monomeric detail and treats each folded object as a rigid polygon decorated with isotropic interaction sites. The goal is to efficiently probe how such shape-particles assemble into extended networks at larger length scales, focusing on how vertex-mediated attraction and edge-mediated exclusion encode connectivity and porosity in the resulting structures.

An initial configuration is prepared by placing a single shape particle at the origin and replicating it on a regular two-dimensional lattice within a square simulation domain. The system thickness in the out-of-plane direction is taken to be negligible, so that the dynamics are effectively two-dimensional. A replication factor of nrep×nrep (with nrep=28) produces nrep2 identical polygons, and the total polygonal area is Vtot=nrep2vpoly. A target area fraction ϕtarget=0.4 defines the final packing density of the assembly.

B.2 Interaction Potentials

Vertex–vertex Lennard–Jones attraction

Vertex–vertex attraction between vertex patches is modeled by an isotropic Lennard–Jones pair potential acting only on the centers of the vertex patches. The interaction between two vertex patches at separation r is given by

Uvert(r)=4 ϵvertσvertr12σvertr6#B.1

where ϵvert=15 is the well depth in reduced units and σvert sets the characteristic length scale associated with the vertex patch diameter. The potential is truncated and shifted at a finite cutoff rc,vert (of order a few σvert) so that attractive vertex–vertex contacts form when two vertex patches approach within a distance comparable to σvert.

Edge–edge Yukawa repulsion

Edge–edge repulsion between edge patches is described by an isotropic Yukawa potential. The interaction between two edge patches at separation r takes the form

Uedge(r)=ϵedgee-κrr#B.2
with ϵedge=60 and κ=0 (unscreened limit). This repulsive interaction is applied only between edge patches and is truncated at a cutoff rc,edge≈4 σedge, where σedge is the effective diameter of the edge patch. The resulting long-ranged, purely repulsive edge–edge interaction penalizes close approach of edge patches and suppresses tightly edge-aligned aggregates.

B.3 Simulation Protocol

Initially, only steric repulsion acts and the system is equilibrated at low density, after which the box area is reduced quasi-statically until the polygons occupy a fraction ϕtarget of the box, yielding a dense, unbonded packing. Short-ranged isotropic Lennard-Jones attractions between vertex patches are then activated to promote vertex–vertex binding, while isotropic Yukawa-type repulsions between edge patches penalize edge–edge approach, biasing connectivity toward open, vertex-connected networks. A subsequent temperature-cycling protocol between low and high reduced temperatures repeatedly breaks and reforms patch-mediated contacts, allowing the system to explore network-scale rearrangements; over many cycles, this drives the formation of mechanically stable polygonal networks whose connectivity and porosity can be analyzed at a larger emergent length scale than in the underlying monomer-level model.

Appendix C: Characterization and Analysis

C.1 Length of Folded Helical Block

The end-to-end distance of each helical block was quantified as the magnitude of the displacement vector between its first and last backbone monomers. For a helical block comprising monomers with indices i=istart,…,iend and positions ri=(xi,yi,zi), the end-to-end distance Lh is defined as

Lh=∣riend-ristart∣=xiendxistart2+yiendyistart2+ziendzistart2#C.1

When multiple helical blocks are present in a configuration, the block-averaged end-to-end length is computed as

⟨Lh⟩=1Nblockk=1NblockLhk#C.2

where Lhk denotes the end-to-end distance of the k-th helical block and Nblock is the total number of helical blocks in the system.

C.2 Radius of Gyration of Flexible Block

The conformational size of each flexible block was characterized by its radius of gyration Rg, defined with respect to the block’s center of mass. For a flexible block comprising Nf monomers with positions ri=(xi,yi,zi), the instantaneous center-of-mass position rcm is first computed as

rcm=1Nfi=1Nfri#C.3

The radius of gyration of that block is then given by

Rg=1Nfi=1Nf∣ri-rcm∣21/2#C.4

which measures the root-mean-square distance of the flexible monomers from their center of mass. When multiple flexible blocks are present, the block-averaged radius of gyration is obtained by averaging Rg over all flexible blocks and over sampled configurations.

C.3 Vertex-to-Vertex Distance (Polygon Edge Length)

The distance between two vertices was defined as the magnitude of the displacement vector between the centers of mass of the corresponding flexible blocks, dkl=∣rcml-rcmk∣, where rcmk denotes the center-of-mass position of the k-th flexible (vertex) block.

C.4 Polygon Area

The polygonal area was calculated from the center-of-mass positions of the flexible vertex blocks projected onto the substrate plane. Assuming that the folded polygon lies approximately parallel to the substrate, the in-plane coordinates of the k-th vertex were taken as xcmkycmk, where rcmk is the center-of-mass position of the corresponding flexible block. The area of the n-sided polygon was then obtained using the shoelace formula,

Apoly=12k=1nxcmkycmk1-xcmk1ycmk#C.5

with xcmn1ycmn1≡xcm1ycm1.

C.5 Polygon Internal Angle

The internal angle at each polygon vertex was computed directly from the centers of mass of three consecutive flexible blocks in three dimensions. For the k-th vertex, the centers of mass of the preceding, current, and following vertices were denoted by rcmk1, rcmk, and rcmk1, respectively, where rcmk=(xcmk,ycmk,zcmk). The two edge vectors incident on vertex k were defined as

uk=rcmk1-rcmk,vk=rcmk1-rcmk#C.6

The internal angle θk at vertex k was then obtained from the standard three-dimensional dot-product relation,

θk=arccos⁡uk⋅vk∣uk∣∣vk∣#C.7

which corresponds to the angle between the two 3D edge vectors defined by the three vertex centers. The resulting set θk characterizes the internal polygon angles encoded by the flexible vertex blocks of the folded nanostructure.

Appendix D: Melting Curves of Coarse-Grained Patchy Polygon

Figure D1. Melting Curve of CG Patchy Polygons. Fraction of aggregate particles counts how many CG particles are connected into a network, normalized by the total particle counts. kT represents the system temperature. As kT increase, the crystal falls apart and the number of particles in a cluster decreases. We define the melting kT as the 50% mark of each curve.

References

- J. A. Anderson, J. Glaser and S. C. Glotzer, Comput. Mater. Sci., 2020, 173, 109363.

- H. Yukawa, Proc. Phys.-Math. Soc. Jpn. 3rd Ser., 1935, 17, 48–57.