Eco-Friendly Antimicrobial Food Packaging Films Based on PVA/Starch/Glycerol Blended with Frankincense Ethanolic Extract

(Supplementary information)

Table S-1: Quantities of starch, and PVA used in the preparation of PVA/starch blends

|  | PVA | Starch |
| --- | --- | --- |
| 1 | 100% | - |
| 2 | - | 100% |
| 3 | 70% | 30% |
| 4 | 50% | 50% |
| 5 | 30% | 70% |

Table S-2: Composition of biodegradable films (Quantities of starch, PVA, Plant extract and glycerol used in the preparation of formulated film).

| Sr. No. | (PVA/ Starch) (70%:30%) | Glycerol | Plant extract (Frankincense) |
| --- | --- | --- | --- |
| AR-01 | 50.0 g | 5.0 g | ___ |
| AR-02 | 50.0 g | 5.0 g | 0.1 g |
| AR-03 | 50.0 g | 5.0 g | 0.2 g |
| AR-04 | 50.0 g | 5.0 g | 0.3 g |
| AR-05 | 50.0 g | 5.0 g | 0.4 g |
| AR-06 | 50.0 g | 5.0 g | 0.5 g |

Figure S-1: EDX spectra of sample AR-01 film

Table S-3:  Elemental composition of AR-01 film

| Element | Weight % |
| --- | --- |
| Pt | 0.0 |
| C | 48.8 |
| O | 51.2 |

Figure S-2: EDX spectra of sample AR-02 film

Table S-4:  Elemental composition of AR-02 film

| Element | Weight % |
| --- | --- |
| C | 48.8 |
| O | 51.2 |

Figure S-3: EDX spectra of sample AR-04 film

Table S-5:  Elemental composition of AR-04 film

| Element | Weight % |
| --- | --- |
| C | 43.4 |
| O | 56.6 |

Figure S-4: EDX spectra of sample AR-05 film

Table S-6:  Elemental composition of AR-05 film

| Element | Weight % |
| --- | --- |
| N | 4.5 |
| C | 44.1 |
| O | 51.4 |

Figure S-5: EDX spectra of sample AR-06 film

| Element | Weight % |
| --- | --- |
| C | 41.7 |
| O | 58.3 |

Table S-7:  Elemental composition of AR-06 film

Figure S-6: DSC/DTA spectra (coupled with TGA) of AR-01 film

Figure S-7: DSC/DTA spectra (coupled with TGA) of AR-02 film

Figure S-8: DSC/DTA spectra (coupled with TGA) of AR-03 film.

Figure S-9: DSC/DTA spectra (coupled with TGA) of AR-04 film

Figure S-10: DSC/DTA spectra (coupled with TGA) of AR-05 film

Figure S-11: DSC/DTA spectra (coupled with TGA) of AR-06 film

| Sample | before | after | % |
| --- | --- | --- | --- |
| AR-01 | 0.1018 | 0.5545 | 81.64 |
| AR-02 | 0.1283 | 0.6445 | 80.09 |
| AR-03 | 0.1757 | 0.5540 | 68.29 |
| AR-04 | 0.1746 | 0.5355 | 67.39 |
| AR-05 | 0.0985 | 0.2918 | 66.24 |
| AR-06 | 0.1791 | 0.4206 | 57.42 |

# Table S-8:  Water absorption capacity test of Starch/PVA Films Before and After immersion

Table S-9: Tensile strength/elongation test of formulated films (AR-01 to AR-06)

| Sample | Tensile Strength | Elongation |
| --- | --- | --- |
|  | [MPa] | % |
| AR-01 | 2.752 | 6.241 |
| AR-02 | 2.852 | 7.356 |
| AR-04 | 3.025 | 8.325 |
| AR-05 | 3.45 | 9.574 |
| AR-06 | 3.941 | 10.235 |

Table S-10:  Soil Degradation of Starch/PVA Films Before and After Soil Burial

| Sample | Before | After |
| --- | --- | --- |
| AR-01 | 0.2804 | 0.2130 |
| AR-02 | 0.2187 | 0.1627 |
| AR-03 | 0.2074 | 0.1483 |
| AR-04 | 0.1812 | 0.1137 |
| AR-05 | 0.1768 | 0.1097 |
| AR-06 | 0.1709 | 0.1056 |

Figure S-12. A setup for the testing the formulated film by soil burial test.