Supplementary Information

Type II porous ionic liquid based on metal-organic cage that enables L-tryptophan identification

Zhuxiu Zhang1, Baolin Yang1, Bingjie Zhang1, Mifen Cui1, Jihai Tang*1,2, Xu Qiao*1,2

1State Key Laboratory of Materials-Oriented Chemical Engineering,

College of Chemical Engineering, Nanjing Tech University, No. 30 Puzhunan Road,

Nanjing 211816, China.

2Jiangsu National Synergetic Innovation Centre for Advanced Materials (SICAM),

No. 5 Xinmofan Road, Nanjing 210009, China.

E-mail: jhtang@njtech.edu.cn, qct@njtech.edu.cn

Table of contents:

Supplementary Fig. 1 TGA curves of HD/THTP_Cl and THTP_Cl.	1

Supplementary Fig. 2 Stress versus shear rate plots of HD/THTP_Cl measured at room temperature under rotation mode.	1

Supplementary Fig. 3 Viscosity versus shear rate plots of HD/THTP_Cl measured at room temperature under rotation mode.	2

Supplementary Fig. 4 The number of occupying methane molecules in the HD as a function of time during the production run at 25℃ and 65 bar.	2

Supplementary Fig. 5 L-Phe extraction isotherms of HD/THTP_Cl and THTP_Cl.	3

Supplementary Fig. 6 L-Tyr extraction isotherms of HD/THTP_Cl and THTP_Cl.	3

Supplementary Fig. 7 The simulation box of L-Phe simulation system. Snapshot of empty HD without L-Phe molecule in its cavity.	4

Supplementary Fig. 8 The simulation box of L-Tyr simulation system. Snapshot of empty HD without L-Tyr molecule in its cavity.	4

Supplementary Fig. 9 RMSD for L-Trp simulation system.	5

Supplementary Fig. 10 RMSD for L-Phe simulation system.	5

Supplementary Fig. 11 RMSD for L-Tyr simulation system.	6

Supplementary Fig. 12 Color-filled RDG isosurfaces depicting noncovalent interaction regions of the encapsulated-L-Trp and HD cage.	6

Supplementary Fig. 13 Color-filled RDG isosurfaces depicting noncovalent interaction regions of the absorption of L-Trp by the periphery of HD cages.	7

Supplementary Fig. 14 The van der Walls interactions between the encapsulated-L-Trp and HD cage by the RDG method.	7

Supplementary Fig. 15 The van der Walls interactions between the encapsulated-L-Trp and HD cage by the RDG method.	8

Supplementary Fig. 16 The C-H…π interaction between CH2 group and the benzene ring of ligand.	8

Supplementary Fig. 17 The N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.	9

Supplementary Fig. 18 The weak N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.	9

Supplementary Fig. 19 The weak N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.	9

Supplementary Fig. 20 The weak N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.	10

Supplementary Fig. 21 Calibration curve for the determination of L-Trp.	10

Supplementary Fig. 22 Calibration curve for the determination of L-Phe.	11

Supplementary Fig. 23 Calibration curve for the determination of L-Tyr.	11

Supplementary Fig. 24 1H NMR of the white precipitate (D2O, 400 MHz, 298 K).	12

Supplementary Table 1 RMSD values obtained from the MD simulations.	13

# Supplementary Fig. 1 TGA curves of HD/THTP_Cl and THTP_Cl.

# Supplementary Fig. 2 Stress versus shear rate plots of HD/THTP_Cl measured at room temperature under rotation mode.

# Supplementary Fig. 3 Viscosity versus shear rate plots of HD/THTP_Cl measured at room temperature under rotation mode.

# Supplementary Fig. 4 The number of occupying methane molecules in the HD as a function of time during the production run at 25℃ and 65 bar.

# Supplementary Fig. 5 L-Phe extraction isotherms of HD/THTP_Cl and THTP_Cl.

# Supplementary Fig. 6 L-Tyr extraction isotherms of HD/THTP_Cl and THTP_Cl.

# Supplementary Fig. 7 The simulation box of L-Phe simulation system. Snapshot of empty HD without L-Phe molecule in its cavity.

# Supplementary Fig. 8 The simulation box of L-Tyr simulation system. Snapshot of empty HD without L-Tyr molecule in its cavity.

# Supplementary Fig. 9 RMSD for L-Trp simulation system.

# Supplementary Fig. 10 RMSD for L-Phe simulation system.

# Supplementary Fig. 11 RMSD for L-Tyr simulation system.

# Supplementary Fig. 12 Color-filled RDG isosurfaces depicting noncovalent interaction regions of the encapsulated-L-Trp and HD cage. The blue, green, and red clouds represent hydrogen bonding, van der Waals interactions, and steric hindrance, respectively.

# Supplementary Fig. 13 Color-filled RDG isosurfaces depicting noncovalent interaction regions of the absorption of L-Trp by the periphery of HD cages. The blue, green, and red clouds represent hydrogen bonding, van der Waals interactions, and steric hindrance, respectively.

# Supplementary Fig. 14 The van der Walls interactions between the encapsulated-L-Trp and HD cage by the RDG method.

# Supplementary Fig. 15 The van der Walls interactions between the encapsulated-L-Trp and HD cage by the RDG method.

# Supplementary Fig. 16 The C-H…π interaction between CH2 group and the benzene ring of ligand. Geometric parameters are measured according to the Brandl-Weiss system for defining C-H…π interaction: (1) the distance between the donor carbon and the ring centroid of the aromatic system (dC–X ≤ 4.5 Å), (2) the angle formed by the donor carbon, hydrogen and ring centroid (∠C–H–X ≥ 120°), (3) the distance of the vertical projection of the donor H-atom onto the acceptor π system from the geometric center of the aromatic system (dHp–X = 1–1.2 Å).

# Supplementary Fig. 17 The N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.

# Supplementary Fig. 18 The weak N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.

# Supplementary Fig. 19 The weak N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.

# Supplementary Fig. 20 The weak N-H…O hydrogen bond between between the nitrogen atom in the indole ring and oxygen atom in the polyoxovanadate.

# Supplementary Fig. 21 Calibration curve for the determination of L-Trp.

# Supplementary Fig. 22 Calibration curve for the determination of L-Phe.

# Supplementary Fig. 23 Calibration curve for the determination of L-Tyr.

# Supplementary Fig. 24 1H NMR of the white precipitate (D2O, 400 MHz, 298 K).

# Supplementary Table 1 RMSD values obtained from the MD simulations.

| System | RMSD (nm) |
| --- | --- |
| L-Trp simulation system | 3.38 ± 0.043 |
| L-Phe simulation system | 4.66 ± 0.035 |
| L-Tyr simulation system | 4.43 ± 0.050 |