Cerium oxide modified biochar as an adsorbent for efficient phosphorus recovery

Lang Wanga, Zhiyi Sunb, Haitao Shab*, Hui Wanga*

aSchool of Resources and Environmental Engineering, Jiangsu University of Technology, Changzhou 213001, China

bResearch Center of Secondary Resources and Environment, School of Chemical Engineering and Materials, Changzhou Institute of Technology, Changzhou 213032, China

*Corresponding author.

E-mail address: 101232727@czu.cn, 1316608390@qq.com

Table of contents

Table S1. BET surface area, pore volumes and pore of adsorbentsS3

Figure S1. Effect of time on the adsorption of P by the BC and Ce-BC. S3

Figure S2. Effect of initial concentration on the adsorption of P by the BC and Ce-BC.S4

Figure S3. Effect of dosage on the adsorption of P by the BC (a) and Ce-BC (b).S5

Table S2. Isotherm model parameters for P adsorption via the BC and Ce-BCS6

Figure S4. Isotherm models for P adsorption by Ce-BC S7

Figure S5. Kinetic models for P by the BCS8

Figure S6. Kinetic models for P by the Ce-BC S9

Table S3. Kinetic parameters for P removal by the BC and Ce-BC S10

Figure S7. Fractional distribution of P species in solution at various pH valuesS10

Figure S8. Zeta potential of BC and Ce-BC S11

Figure S9. Effect of pH on the adsorption of P by the BC and Ce-BCS12

Figure S10. Cyclic adsorption-regeneration study of P by Ce-BCS13

Table S1 BET surface area, pore volumes and pore of BC and Ce-BC.

| Samples | Surface area (m2/g) | Pore volume (mL/g) | Average pore diameter (nm) |
| --- | --- | --- | --- |
| BC | 2.67 | 0.0131 | 8.12 |
| Ce-BC | 3.08 | 0.0239 | 12.33 |

Figure S1. Effect of time on the adsorption of P by the BC and Ce-BC.

Figure S2. Effect of initial concentration on the adsorption of P by the BC and Ce-BC.

Figure S3. Effect of dosage on the adsorption of P by the BC (a) and Ce-BC (b).

Table S2 Isotherm model parameters for P adsorption via the BC and Ce-BC

| Adsorbents | Isotherm parameters |  | Temperature(K) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 298 | 303 | 308 |
| BC | Langmuir | qm(mg/g) | 23.3925 | 23.6056 | 24.7281 |
|  |  | KL(L/mg) | 0.0266 | 0.0301 | 0.03965 |
|  |  | R2 | 0.8524 | 0.8679 | 0.8938 |
|  | Freundlich | KF | 1.4943 | 1.7354 | 2.2312 |
|  |  | n | 1.8271 | 1.8686 | 2.0627 |
|  |  | R2 | 0.8064 | 0.8211 | 0.7928 |
|  | D-R | qm(mg/g) | 15.6251 | 15.7631 | 18.2445 |
|  |  | E (kJ mol-1) | 13.4152 | 18.3241 | 21.2543 |
|  |  | R2 | 0.8834 | 0.9314 | 0.9413 |
| Ce-BC | Langmuir | qm(mg/g) | 24.6651 | 25.6356 | 26.2214 |
|  |  | KL(L/mg) | 0.0822 | 0.0934 | 0.1009 |
|  |  | R2 | 0.7321 | 0.7695 | 0.7908 |
|  | Freundlich | KF | 3.2061 | 3.5121 | 4.3391 |
|  |  | n | 2.2714 | 2.3533 | 2.6354 |
|  |  | R2 | 0.6054 | 0.6314 | 0.6924 |
|  | D-R | qm(mg/g) | 19.3154 | 19.4091 | 19.8395 |
|  |  | E (kJ mol-1) | 25.1453 | 27.3321 | 29.3175 |
|  |  | R2 | 0.8564 | 0.8851 | 0.9009 |

Figure S4. Isotherm models for P adsorption by Ce-BC under different temperatures at the optimal adsorption condition (a) Langmuir isotherm model; (b) Freundlich isotherm model; (c) D-R isotherm model.

Figure S5. Pseudo-first and pseudo-second kinetic models for P (a); the external diffusion kinetic model for P (b); Intraparticle diffusion kinetic model for P (c) by the BC.

Figure S6. Pseudo-first and pseudo-second kinetic models for P (a); the external diffusion kinetic model for P (b); Intraparticle diffusion kinetic model for P (c) by the Ce-BC.

Table S3 Kinetic parameters for P removal by the BC and Ce-BC

| Kinetic models | Parameters | Adsorbents |  |
| --- | --- | --- | --- |
|  |  | BC | Ce-BC |
| Pseudo-first-order | k1 | 0.2618 | 0.5334 |
|  | qe | 9.8214 | 10.6636 |
|  | R2 | 0.9941 | 0.9950 |
| Pseudo-second-order | k2 | 0.01675 | 0.0461 |
|  | qe | 13.2426 | 12.7215 |
|  | R2 | 0.9861 | 0.9968 |
| External diffusion | kext | 0.1603 | 0.2965 |
|  | R2 | 0.9875 | 0.9685 |
| Intraparticle diffusion | kp,1 | 3.4771 | 4.5614 |
|  | R2 | 0.9353 | 0.9783 |
|  | kp,2 | 0.3146 | 0.0621 |
|  | R2 | 1 | 1 |

Figure. S7 Thermodynamic fit for P adsorption by BC (a) and Ce-BC (b).

Table S4 Thermodynamic parameters of adsorption for P onto the adsorbents at various temperatures.

| Adsorbents | C0 (mg/L) | ∆H0 (kJ/mol) | ∆S0 (kJ/mol∙K) | ∆G0 (kJ/mol) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 303 (K) | 313 (K) | 323 (K) |
| BC | 5 | 20.78 | 0.0644 | -0.1573 | -0.3247 | -0.7512 |
| Ce-BC | 5 | 28.55 | 0.1831 | -0.2258 | -0.8385 | -1.9656 |

Figure S8. Fractional distribution of P species in solution at various pH values

Figure S9. Zeta potential of BC and Ce-BC

Figure S10 Effect of pH on the adsorption of P by the BC and Ce-BC

Figure S11. Cyclic adsorption-regeneration study of P by Ce-BC