Table 3. Synthesis of functionalized aromatic heterocyclesa

aReaction conditions C: 6 (0.2 mmol), 1 (0.6 mmol), BiVO4-180 (5 mol%), DMSO/H2O (2.04 mL, v/v = 50/1) with the irradiation of blue LED (3 W) under air at room temperature for 3 h. Isolated yields were given. bReaction conditions D: 8 (0.2 mmol), 9 (0.4 mmol), BiVO4-180 (5 mol%), MeCN (2 mL) with the irradiation of blue LED (10 W) under air at room temperature for 24-72 h. Isolated yields were given. cReaction for 72 h at 55 oC. dReaction conditions D: 8 (0.2 mmol), 11 or NH4SCN (0.4 mmol), BiVO4 (5 mol%), MeCN (2 mL) with the irradiation of blue LED (10 W) under air at room temperature for 5-24 h. Isolated yields were given.