## Supplementary Information

### Table S1: Primer sequences used for qRT-PCR analysis

| Gene | Forward primer (5' → 3') | Reverse primer (5' → 3') | Amplicon size (bp) |
| --- | --- | --- | --- |
| Bax | GGC TGG ACA CTG GAC TTC CT | GGT GAG GAG GCC TGC CCA TA | 98 |
| Bcl-2 | GGT GGG GTC ATG TGT GTG G | CGG TTC AGG TAC TCA GTC ATC C | 89 |
| Caspase-3 | GGA GCA AGT CAG TGG CTC CA | GGA TGC AAT ATG GGA GCA GTC A | 105 |
| Caspase-9 | GAG TTC AGG AGG ACG GCC TG | GCA TGG CAC TCA CGT CAG GA | 112 |
| p53 | GAG GTT GGC TCT GAC TGT ACC | TCC GTC CCA AGA TCG CAC TC | 85 |
| GAPDH | GGA GCG AGA TCC CTC CAA AAT | GGC TGT TGT CAT ACT TCT CAT GG | 120 |

### Table S2: Complete ranking of all 25 complexes based on interaction energy (from most stable to least stable) (mean ± SD, n=3)

| Rank | Complex | E_int (kJ/mol) | Drug | Nanocage | Recommendation |
| --- | --- | --- | --- | --- | --- |
| 1 | NU-NC-Fe | -63.2 ± 1.7 | Nitrouracil | NC-Fe | ★★★★★ (Excellent) |
| 2 | FU-NC-Fe | -59.8 ± 1.6 | Fluorouracil | NC-Fe | ★★★★★ (Excellent) |
| 3 | NU-NC-Cu | -59.4 ± 1.6 | Nitrouracil | NC-Cu | ★★★★★ (Excellent) |
| 4 | NU-NC-Zn | -56.7 ± 1.5 | Nitrouracil | NC-Zn | ★★★★☆ (Good) |
| 5 | FU-NC-Cu | -56.2 ± 1.5 | Fluorouracil | NC-Cu | ★★★★☆ (Good) |
| 6 | TU-NC-Fe | -55.6 ± 1.5 | Thiouracil | NC-Fe | ★★★★☆ (Good) |
| 7 | NU-NC-O | -52.1 ± 1.5 | Nitrouracil | NC-O | ★★★★☆ (Good) |
| 8 | TU-NC-Cu | -52.3 ± 1.4 | Thiouracil | NC-Cu | ★★★★☆ (Good) |
| 9 | FU-NC-Zn | -53.4 ± 1.3 | Fluorouracil | NC-Zn | ★★★★☆ (Good) |
| 10 | U-NC-Fe | -53.4 ± 1.4 | Uracil | NC-Fe | ★★★☆☆ (Moderate) |
| 11 | U-NC-Cu | -50.1 ± 1.4 | Uracil | NC-Cu | ★★★☆☆ (Moderate) |
| 12 | TU-NC-Zn | -49.2 ± 1.3 | Thiouracil | NC-Zn | ★★★☆☆ (Moderate) |
| 13 | FU-NC-O | -48.7 ± 1.4 | Fluorouracil | NC-O | ★★★☆☆ (Moderate) |
| 14 | U-NC-Zn | -47.8 ± 1.3 | Uracil | NC-Zn | ★★★☆☆ (Moderate) |
| 15 | PU-NC-Fe | -49.8 ± 1.3 | Propyluracil | NC-Fe | ★★★☆☆ (Moderate) |
| 16 | TU-NC-O | -45.2 ± 1.3 | Thiouracil | NC-O | ★★★☆☆ (Moderate) |
| 17 | NU-NC | -45.6 ± 1.4 | Nitrouracil | NC | ★★★☆☆ (Moderate) |
| 18 | PU-NC-Cu | -46.5 ± 1.3 | Propyluracil | NC-Cu | ★★★☆☆ (Moderate) |
| 19 | PU-NC-Zn | -44.3 ± 1.2 | Propyluracil | NC-Zn | ★★☆☆☆ (Weak) |
| 20 | U-NC-O | -43.5 ± 1.3 | Uracil | NC-O | ★★☆☆☆ (Weak) |
| 21 | FU-NC | -42.3 ± 1.2 | Fluorouracil | NC | ★★☆☆☆ (Weak) |
| 22 | TU-NC | -40.1 ± 1.2 | Thiouracil | NC | ★★☆☆☆ (Weak) |
| 23 | U-NC | -38.2 ± 1.2 | Uracil | NC | ★★☆☆☆ (Weak) |
| 24 | PU-NC-O | -39.8 ± 1.2 | Propyluracil | NC-O | ★★☆☆☆ (Weak) |
| 25 | PU-NC | -34.5 ± 1.1 | Propyluracil | NC | ★☆☆☆☆ (Very weak) |

### Table S3: Complete pH data - Adsorption percentage (R%) at pH = 5 for all 25 complexes (mean ± SD, n=3)

| Drug | NC | NC-O | NC-Cu | NC-Fe | NC-Zn |
| --- | --- | --- | --- | --- | --- |
| Uracil (U) | 20.1 ± 1.2 | 23.5 ± 1.1 | 28.2 ± 1.4 | 31.5 ± 1.3 | 25.8 ± 1.2 |
| Fluorouracil (FU) | 29.2 ± 1.5 | 33.8 ± 1.4 | 39.5 ± 1.6 | 41.9 ± 1.5 | 36.2 ± 1.4 |
| Thiouracil (TU) | 24.5 ± 1.3 | 28.1 ± 1.2 | 33.2 ± 1.5 | 35.6 ± 1.4 | 30.4 ± 1.3 |
| Propyluracil (PU) | 15.2 ± 1.0 | 18.5 ± 1.1 | 22.8 ± 1.2 | 25.1 ± 1.2 | 20.3 ± 1.1 |
| Nitrouracil (NU) | 36.3 ± 1.6 | 40.2 ± 1.5 | 45.5 ± 1.7 | 48.3 ± 1.6 | 42.1 ± 1.5 |

*Conditions: contact time = 30 min, initial concentration = 20 ppm, adsorbent mass = 0.08 g, V = 10 mL, T = 25°C*

### Table S4: Complete pH data - Adsorption percentage (R%) at pH = 9 for all 25 complexes (mean ± SD, n=3)

| Drug | NC | NC-O | NC-Cu | NC-Fe | NC-Zn |
| --- | --- | --- | --- | --- | --- |
| Uracil (U) | 35.4 ± 1.3 | 39.8 ± 1.2 | 44.2 ± 1.4 | 47.8 ± 1.3 | 42.5 ± 1.3 |
| Fluorouracil (FU) | 45.2 ± 1.5 | 49.5 ± 1.4 | 54.8 ± 1.6 | 57.2 ± 1.5 | 52.1 ± 1.4 |
| Thiouracil (TU) | 40.1 ± 1.4 | 44.3 ± 1.3 | 49.0 ± 1.5 | 51.5 ± 1.4 | 46.8 ± 1.4 |
| Propyluracil (PU) | 28.5 ± 1.2 | 32.2 ± 1.2 | 37.1 ± 1.3 | 40.3 ± 1.3 | 34.8 ± 1.2 |
| Nitrouracil (NU) | 52.2 ± 1.6 | 56.5 ± 1.5 | 61.0 ± 1.7 | 64.5 ± 1.6 | 58.9 ± 1.5 |

*Conditions: contact time = 30 min, initial concentration = 20 ppm, adsorbent mass = 0.08 g, V = 10 mL, T = 25°C*

### Table S5: Complete time data - Adsorption percentage (R%) at 15 minutes for all 25 complexes (mean ± SD, n=3, pH = 7)

| Drug | NC | NC-O | NC-Cu | NC-Fe | NC-Zn |
| --- | --- | --- | --- | --- | --- |
| Uracil (U) | 38.2 ± 1.3 | 42.5 ± 1.2 | 48.1 ± 1.4 | 51.4 ± 1.3 | 45.8 ± 1.3 |
| Fluorouracil (FU) | 44.3 ± 1.5 | 49.2 ± 1.4 | 54.5 ± 1.6 | 58.2 ± 1.5 | 52.1 ± 1.4 |
| Thiouracil (TU) | 41.2 ± 1.4 | 45.8 ± 1.3 | 50.8 ± 1.5 | 54.2 ± 1.4 | 48.5 ± 1.4 |
| Propyluracil (PU) | 31.3 ± 1.2 | 35.5 ± 1.2 | 40.2 ± 1.3 | 43.8 ± 1.3 | 38.1 ± 1.2 |
| Nitrouracil (NU) | 50.5 ± 1.6 | 55.2 ± 1.5 | 60.8 ± 1.7 | 64.1 ± 1.6 | 57.8 ± 1.5 |

*Conditions: initial concentration = 20 ppm, adsorbent mass = 0.08 g, V = 10 mL, T = 25°C*

### Table S6: Complete time data - Adsorption percentage (R%) at 45 minutes for all 25 complexes (mean ± SD, n=3, pH = 7)

| Drug | NC | NC-O | NC-Cu | NC-Fe | NC-Zn |
| --- | --- | --- | --- | --- | --- |
| Uracil (U) | 49.5 ± 1.3 | 53.8 ± 1.2 | 59.4 ± 1.4 | 62.8 ± 1.3 | 57.1 ± 1.3 |
| Fluorouracil (FU) | 57.8 ± 1.5 | 63.5 ± 1.4 | 69.8 ± 1.6 | 73.2 ± 1.5 | 65.5 ± 1.4 |
| Thiouracil (TU) | 53.8 ± 1.4 | 58.5 ± 1.3 | 64.5 ± 1.5 | 67.8 ± 1.4 | 60.6 ± 1.4 |
| Propyluracil (PU) | 42.6 ± 1.2 | 47.5 ± 1.2 | 53.1 ± 1.3 | 56.4 ± 1.3 | 49.9 ± 1.2 |
| Nitrouracil (NU) | 63.5 ± 1.6 | 68.9 ± 1.5 | 74.5 ± 1.7 | 76.8 ± 1.6 | 70.3 ± 1.5 |

*Conditions: initial concentration = 20 ppm, adsorbent mass = 0.08 g, V = 10 mL, T = 25°C*

### Table S7: Complete concentration data - Adsorption percentage (R%) for all five drugs on NC-Fe at 5-100 ppm (mean ± SD, n=3)

| Conc. (ppm) | Uracil (U) | Fluorouracil (FU) | Thiouracil (TU) | Propyluracil (PU) | Nitrouracil (NU) |
| --- | --- | --- | --- | --- | --- |
| 5 | 65.2 ± 1.4 | 72.5 ± 1.5 | 68.8 ± 1.4 | 58.2 ± 1.3 | 78.5 ± 1.6 |
| 10 | 60.1 ± 1.4 | 68.5 ± 1.5 | 64.2 ± 1.4 | 52.5 ± 1.3 | 74.2 ± 1.6 |
| 20 | 61.4 ± 1.3 | 71.8 ± 1.5 | 66.5 ± 1.4 | 55.1 ± 1.3 | 75.5 ± 1.6 |
| 50 | 55.2 ± 1.4 | 64.8 ± 1.5 | 60.5 ± 1.4 | 48.2 ± 1.3 | 68.5 ± 1.6 |
| 100 | 48.2 ± 1.4 | 57.5 ± 1.5 | 53.2 ± 1.4 | 42.5 ± 1.3 | 62.5 ± 1.6 |

*Conditions: pH = 7, contact time = 30 min, adsorbent mass = 0.08 g, V = 10 mL, T = 25°C*

### Table S8: Complete concentration data - Adsorption capacity (q_e, mg/g) for all five drugs on NC-Fe at 5-100 ppm (mean ± SD, n=3)

| Conc. (ppm) | Uracil (U) | Fluorouracil (FU) | Thiouracil (TU) | Propyluracil (PU) | Nitrouracil (NU) |
| --- | --- | --- | --- | --- | --- |
| 5 | 0.41 ± 0.02 | 0.45 ± 0.02 | 0.43 ± 0.02 | 0.36 ± 0.02 | 0.49 ± 0.02 |
| 10 | 0.75 ± 0.03 | 0.86 ± 0.03 | 0.80 ± 0.03 | 0.66 ± 0.03 | 0.93 ± 0.03 |
| 20 | 1.54 ± 0.05 | 1.80 ± 0.05 | 1.66 ± 0.05 | 1.38 ± 0.05 | 1.89 ± 0.05 |
| 50 | 3.45 ± 0.08 | 4.05 ± 0.09 | 3.78 ± 0.08 | 3.01 ± 0.07 | 4.28 ± 0.09 |
| 100 | 6.03 ± 0.12 | 7.19 ± 0.14 | 6.65 ± 0.13 | 5.31 ± 0.11 | 7.81 ± 0.15 |

*Conditions: pH = 7, contact time = 30 min, adsorbent mass = 0.08 g, V = 10 mL, T = 25°C*

### Table S9: Complete dosage data - Adsorption percentage (R%) for all five drugs on NC-Fe at 0.02-0.10 g (mean ± SD, n=3)

| Dosage (g) | Uracil (U) | Fluorouracil (FU) | Thiouracil (TU) | Propyluracil (PU) | Nitrouracil (NU) |
| --- | --- | --- | --- | --- | --- |
| 0.02 | 42.5 ± 1.3 | 55.2 ± 1.5 | 48.8 ± 1.4 | 35.5 ± 1.2 | 62.2 ± 1.6 |
| 0.04 | 52.5 ± 1.3 | 64.2 ± 1.5 | 58.5 ± 1.4 | 45.2 ± 1.2 | 70.5 ± 1.6 |
| 0.06 | 58.2 ± 1.3 | 68.8 ± 1.5 | 63.5 ± 1.4 | 50.5 ± 1.2 | 73.5 ± 1.6 |
| 0.08 | 61.4 ± 1.3 | 71.8 ± 1.5 | 66.5 ± 1.4 | 55.1 ± 1.3 | 75.5 ± 1.6 |
| 0.10 | 67.5 ± 1.3 | 76.5 ± 1.5 | 72.2 ± 1.4 | 60.5 ± 1.3 | 79.8 ± 1.6 |

*Conditions: pH = 7, contact time = 30 min, initial concentration = 20 ppm, V = 10 mL, T = 25°C*

### Table S10: Complete dosage data - Adsorption capacity (q_e, mg/g) for all five drugs on NC-Fe at 0.02-0.10 g (mean ± SD, n=3)

| Dosage (g) | Uracil (U) | Fluorouracil (FU) | Thiouracil (TU) | Propyluracil (PU) | Nitrouracil (NU) |
| --- | --- | --- | --- | --- | --- |
| 0.02 | 4.25 ± 0.08 | 5.52 ± 0.10 | 4.88 ± 0.09 | 3.55 ± 0.07 | 6.22 ± 0.11 |
| 0.04 | 2.63 ± 0.05 | 3.21 ± 0.06 | 2.93 ± 0.05 | 2.26 ± 0.04 | 3.53 ± 0.07 |
| 0.06 | 1.94 ± 0.04 | 2.29 ± 0.05 | 2.12 ± 0.04 | 1.68 ± 0.03 | 2.45 ± 0.05 |
| 0.08 | 1.54 ± 0.05 | 1.80 ± 0.05 | 1.66 ± 0.05 | 1.38 ± 0.05 | 1.89 ± 0.05 |
| 0.10 | 1.35 ± 0.04 | 1.53 ± 0.04 | 1.44 ± 0.04 | 1.21 ± 0.03 | 1.60 ± 0.04 |

*Conditions: pH = 7, contact time = 30 min, initial concentration = 20 ppm, V = 10 mL, T = 25°C*

### Table S11: Empty NC-Fe cell viability (%) on MCF-7 and HFF cells at various concentrations and time points (mean ± SD, n=3)

| Concentration (µM) | MCF-7 (24 h) | MCF-7 (48 h) | MCF-7 (72 h) | HFF (24 h) | HFF (48 h) | HFF (72 h) |
| --- | --- | --- | --- | --- | --- | --- |
| 0 (control) | 100.0 ± 2.1 | 100.0 ± 2.3 | 100.0 ± 2.5 | 100.0 ± 2.0 | 100.0 ± 2.2 | 100.0 ± 2.4 |
| 1 | 98.5 ± 2.0 | 97.8 ± 2.2 | 96.9 ± 2.4 | 99.1 ± 1.9 | 98.5 ± 2.1 | 97.9 ± 2.3 |
| 5 | 97.2 ± 1.9 | 96.5 ± 2.1 | 95.8 ± 2.3 | 98.2 ± 1.8 | 97.6 ± 2.0 | 96.8 ± 2.2 |
| 10 | 96.1 ± 1.8 | 95.2 ± 2.0 | 94.3 ± 2.2 | 97.5 ± 1.8 | 96.8 ± 2.0 | 95.9 ± 2.2 |
| 25 | 94.8 ± 1.7 | 93.9 ± 1.9 | 92.8 ± 2.1 | 96.4 ± 1.7 | 95.5 ± 1.9 | 94.6 ± 2.1 |
| 50 | 93.2 ± 1.6 | 92.1 ± 1.8 | 91.0 ± 2.0 | 95.1 ± 1.6 | 94.2 ± 1.8 | 93.1 ± 2.0 |
| 100 | 91.5 ± 1.5 | 90.2 ± 1.7 | 89.1 ± 1.9 | 93.8 ± 1.5 | 92.5 ± 1.7 | 91.4 ± 1.9 |
| 200 | 89.8 ± 1.5 | 88.5 ± 1.6 | 87.2 ± 1.8 | 92.1 ± 1.5 | 90.8 ± 1.6 | 89.5 ± 1.8 |

No significant difference compared to control (P > 0.05 for all concentrations and time points)

### Table S12: Complete IC₅₀ values (µM) for all treatments on MCF-7 and HFF cells after 48 hours (mean ± SD, n=3)

| Treatment | IC₅₀ on MCF-7 (µM) | IC₅₀ on HFF (µM) | Selectivity Index (SI) |
| --- | --- | --- | --- |
| Free FU | 44.8 ± 2.1 | 112.5 ± 4.5 | 2.5 |
| Free NU | 35.2 ± 1.8 | 98.6 ± 3.8 | 2.8 |
| FU-NC-Fe | 18.5 ± 1.2 | 88.2 ± 3.2 | 4.8 |
| NU-NC-Fe | 12.5 ± 1.0 | 70.5 ± 2.8 | 5.6 |
| Empty NC-Fe | > 200 | > 200 | N/A |

### Table S13: Complete flow cytometry apoptosis data for MCF-7 cells after 48 hours of treatment (mean ± SD, n=3)

| Treatment | Viable (%) | Early Apoptotic (%) | Late Apoptotic (%) | Necrotic (%) | Total Apoptosis (%) |
| --- | --- | --- | --- | --- | --- |
| Control (untreated) | 95.2 ± 2.5 | 2.5 ± 0.5 | 1.2 ± 0.3 | 1.1 ± 0.3 | 3.7 ± 0.6 |
| Free FU | 68.5 ± 3.0 | 17.8 ± 1.8 | 10.7 ± 1.2 | 3.0 ± 0.5 | 28.5 ± 2.1 |
| Free NU | 61.2 ± 3.2 | 22.5 ± 2.0 | 12.7 ± 1.4 | 3.6 ± 0.6 | 35.2 ± 2.3 |
| FU-NC-Fe | 44.2 ± 3.0 | 34.5 ± 2.2 | 17.8 ± 1.6 | 3.5 ± 0.5 | 52.3 ± 2.5 |
| NU-NC-Fe | 34.5 ± 3.5 | 38.2 ± 2.4 | 24.6 ± 1.8 | 2.7 ± 0.4 | 62.8 ± 2.8 |

### Table S14: Complete qRT-PCR data - Fold change in gene expression for all treatments (mean ± SD, n=3)

| Treatment | Bax | Bcl-2 | Bax/Bcl-2 ratio | Caspase-3 | Caspase-9 | p53 |
| --- | --- | --- | --- | --- | --- | --- |
| Control | 1.0 ± 0.1 | 1.0 ± 0.1 | 1.0 | 1.0 ± 0.1 | 1.0 ± 0.1 | 1.0 ± 0.1 |
| Free FU | 2.5 ± 0.2 | 0.78 ± 0.07 | 3.2 | 3.2 ± 0.3 | 2.8 ± 0.2 | 3.5 ± 0.3 |
| Free NU | 3.2 ± 0.3 | 0.85 ± 0.08 | 3.8 | 4.1 ± 0.4 | 3.5 ± 0.3 | 4.2 ± 0.4 |
| FU-NC-Fe | 5.5 ± 0.4 | 0.71 ± 0.06 | 7.8 | 7.5 ± 0.6 | 6.8 ± 0.5 | 7.2 ± 0.6 |
| NU-NC-Fe | 7.2 ± 0.5 | 0.76 ± 0.07 | 9.5 | 9.2 ± 0.7 | 8.5 ± 0.6 | 8.5 ± 0.7 |

*Bax/Bcl-2 ratio SD calculated via error propagation; all values P < 0.01 vs. control; P < 0.05 nanocarrier vs. free drug*