Supplementary Information.

Transhydrogenation of Pentane with 1-Hexyne, 1,5-Hexadiene and 2,4-Hexadiene over a Pt/Al2O3 Catalyst

Mustapha D. Garbaa* and S. David Jacksonb

a Department of Pure and Industrial chemistry, Bayero University Kano, Nigeria

b School of Chemistry, University of Glasgow, Glasgow G12 8QQ, Scotland, UK.

Corresponding author

Email: mustcapture@yahoo.com

The yield of each product formed, assuming no interaction between the species, was calculated from the individual run and summed as the theoretical yield:

Palone + Halone= P+H Theory

This was then compared to the mixed feed runs termed as transhydrogenation yield, which was used to understand the effect of the transhydrogenation occurring during reaction.

Figure S1: XRD diffraction pattern of the Pt/Al2O3 catalyst

Table S1: Products yield of the trans-hydrogenation over 1HY sytem at 773 K

|  | P | H | Transhyd | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 37 |  | 71 | 37 |
| 1-Hexyne(1HY) |  | 71 | 85 | 71 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.67 | 0.23 | 0.23 | 1.9 |
| Pentene | 4.01 |  | 0.36 | 4.01 |
| Trans-2-Pentene | 5.27 | 8.03 | 3.15 | 13.3 |
| Cis-2-pentene | 2.64 |  | 0.18 | 2.64 |
| 4-methylpentene | 0.52 |  |  | 0.52 |
| hexane |  | 0.31 | 0.3 | 0.31 |
| 1-Hexene |  | 1.18 | 2.79 | 1.18 |
| 2-Hexene |  | 0.61 | 0.36 | 0.61 |
| 3-Hexene |  | 0.6 | 2.25 | 0.6 |
| Methyl-2-pentene |  | 10.31 | 3.3 | 10.31 |
| 3-Methylpentyne |  | 27.53 | 30.98 | 27.53 |
| 3-Methyl-1-hexene |  |  | 8.68 | 0 |
| Benzene |  |  | 0.9 | 0 |
| 3-Methylhexane |  | 2.5 | 1.44 | 2.5 |
| 2-Methyl-1,3-pentadiene |  | 0.46 | 5.98 | 0.46 |
| Methylcyclohexane | 17.03 | 14.62 | 9.32 | 31.65 |

Table S2: Products yield of the trans-hydrogenation over 1HY system at 673K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 34 |  | 56 | 34 |
| 1-Hexyne(1HY) |  | 74 | 77 | 74 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.18 | 1.22 | 2.21 | 2.4 |
| Pentene | 2.59 | 0.33 |  | 2.92 |
| Trans-2-Pentene | 1.92 | 0.2 |  | 2.12 |
| Cis-2-pentene | 1.93 | 2.87 |  | 3.8 |
| 4-Methylpentene |  | 5.38 |  | 5.38 |
| Hexane |  | 0.98 |  | 0.98 |
| 1-Hexene |  | 3.67 | 3.06 | 3.67 |
| 2-Hexene |  | 1.58 | 1.11 | 1.58 |
| 3-Hexene |  | 4.83 | 4.02 | 4.83 |
| Methyl-2-pentene |  | 7.77 | 10.99 | 7.77 |
| 3-Methylpentyne |  | 1.97 | 13.54 | 1.97 |
| 3-Methyl-1-hexene |  | 9.52 | 1.11 | 9.52 |
| Benzene |  | 6.95 |  | 6.95 |
| 3-Methylhexane |  | 3.21 |  | 3.21 |
| 2-Methyl-1,3-pentadiene |  | 13.25 | 16.99 | 13.25 |
| Methylcyclohexane | 17.03 | 3.06 | 9.44 | 20.09 |

Table S3: Products yield of the trans-hydrogenation over 1HY system at 623K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 35 |  | 41 | 35 |
| 1Hexyne(1HY) |  | 64 | 55 | 64 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.27 | 13.93 | 0.86 | 15.2 |
| Pentene | 0.16 |  |  | 0.16 |
| Trans-2-Pentene | 3.45 |  |  | 3.45 |
| Cis-2-pentene | 1.56 |  |  | 1.56 |
| Hexane |  | 0.17 |  | 0.17 |
| 1-Hexene |  | 0.74 | 3.06 | 0.74 |
| 2-Hexene |  | 0.39 | 1.84 | 0.39 |
| 3-Hexene |  | 0.67 | 1.38 | 0.67 |
| Methyl-2-pentene |  | 6.61 | 11.52 | 6.61 |
| 3-Methylpentyne |  | 18.41 | 14.54 | 18.41 |
| 3-methyl-1-hexene |  | 2.39 |  | 2.39 |
| Benzene |  |  |  | 0 |
| 3-Methylhexane |  | 0.71 |  | 0.71 |
| 2-Methyl-1,3-pentadiene |  | 8.95 | 12.55 | 8.95 |
| Methylcyclohexane | 14.83 | 2.82 | 10.65 | 17.65 |

Table S4: Products yield of the trans-hydrogenation over 1HY system at 573K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 25 |  | 37 | 25 |
| 1-Hexyne(1HY) |  | 47 | 51 | 47 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.51 |  | 0.22 | 1.51 |
| Pentene | 0.11 |  | 0.31 | 0.11 |
| Trans-2-Pentene | 0.69 |  | 0.2 | 0.69 |
| Cis-2-pentene | 0.23 |  |  | 0.23 |
| Hexane |  |  | 0.33 | 0 |
| 1-Hexene |  | 1.29 | 3.64 | 1.29 |
| 2-Hexene |  | 0.39 | 1.91 | 0.39 |
| 3-Hexene |  | 0.5 | 4.29 | 0.5 |
| Methyl-2-pentene |  |  | 1.04 | 0 |
| 3-Methylpentyne |  | 12.67 | 13.99 | 12.67 |
| 3-Methyl-1-hexene |  |  | 8.09 | 0 |
| Benzene |  |  |  | 0 |
| 3-Methylhexane |  | 0.71 | 1.30 | 0.71 |
| 2-Methyl-1,3-pentadiene |  | 0.47 | 19.7 | 0.47 |
| Methylcyclohexane | 14.83 | 4.85 | 12.51 | 9.68 |

Table S5: Products yield of the trans-hydrogenation over 1HY system at 523K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 25 |  | 26 | 25 |
| 1-Hexyne(1HY) |  | 37 | 29 | 37 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.08 |  | 2.01 | 1.08 |
| Pentene | 0.01 |  |  | 0.01 |
| Trans-2-Pentene | 2.04 |  |  | 2.04 |
| Cis-2-pentene | 0.01 |  |  | 0.01 |
| Hexane |  | 0.11 |  | 0.11 |
| 1-Hexene |  | 0.52 | 0.15 | 0.52 |
| 2-Hexene |  | 0.13 |  | 0.13 |
| 3-Hexene |  | 1.28 |  | 1.28 |
| Methyl-2-pentene |  | 0.61 | 4.21 | 0.61 |
| 3-Methylpentyne |  |  |  | 0 |
| 3-Methyl-1-hexene |  | 1.84 | 1.71 | 1.84 |
| Benzene |  |  |  | 0 |
| 3-Methylhexane |  | 0.38 |  | 0.38 |
| 2-Methyl-1,3-pentadiene |  | 1.64 | 0.59 | 1.64 |
| Methylcyclohexane | 12.21 | 11.59 | 11.99 | 23.8 |

Table S6: Products yield of the trans-hydrogenation over 1,5HD system at 773K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 37 |  | 59 | 37 |
| 1,5-Hexadiene(1,5HD) |  | 64 | 69 | 64 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.67 |  | 2.51 | 1.67 |
| Pentene | 4.01 |  | 0.01 | 4.01 |
| Trans-2-Pentene | 5.27 |  | 2.02 | 5.27 |
| Cis-2-pentene | 2.64 | 0.07 | 2.08 | 2.71 |
| 2-Methyl-2-butene | 0.52 | 0.16 | 0.01 | 0.68 |
| 4-Methylpentene | 1.67 | 0.02 |  | 1.69 |
| Hexane |  |  | 1.95 | 0 |
| 1-Hexene |  | 0.27 | 1.05 | 0.27 |
| 2-Hexene |  | 0.09 |  | 0.09 |
| 3-Hexene |  | 2.89 | 7.8 | 2.89 |
| Methyl-2-pentene |  | 3.64 | 3.8 | 3.64 |
| 3-Methyl-1-hexene |  | 5.8 | 5.24 | 5.8 |
| Benzene |  | 0.84 | 0.26 | 0.84 |
| 3-Methylhexane |  | 1.86 | 1.31 | 1.86 |
| 2-Methyl-1,3-pentadiene |  | 3.9 | 2.23 | 3.9 |
| 2-Methyl-1-1hexene |  | 0.45 |  | 0.45 |
| Methylcyclohexane | 17.03 | 12.75 | 19.75 | 29.78 |

Table S7: Products yield of the trans-hydrogenation over 1,5HD system at 673K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 34 |  | 54 | 34 |
| 1,5-hexadiene (1,5HD) |  | 56 | 65 | 56 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.18 |  | 1.03 | 1.18 |
| Pentene | 2.59 |  |  | 2.59 |
| Trans-2-Pentene | 1.92 |  |  | 1.92 |
| Cis-2-pentene | 1.93 | 0.05 |  | 1.98 |
| 2-Methyl-2-butene | 1.18 | 0.12 | 0.01 | 1.30 |
| Hexane |  | 1.18 | 3.1 | 1.18 |
| 1-Hexene |  | 1.77 | 2.31 | 1.77 |
| 2-Hexene |  | 1.27 | 1.13 | 1.27 |
| 3-Hexene |  | 5.16 | 6.35 | 5.16 |
| Methyl-2-pentene |  | 2.51 | 1.59 | 2.51 |
| 3-Methyl-1-hexene |  | 4.76 | 4.61 | 4.76 |
| Benzene |  | 0.43 |  | 0.43 |
| 3-Methylhexane |  | 2.12 | 3.45 | 2.12 |
| 2-Methyl-1,3-pentadiene |  | 6.57 | 4.71 | 6.57 |
| 2-Methyl-1-1hexene |  | 2.56 |  | 2.56 |
| Methylcyclohexane | 17.03 | 14.76 | 15.61 | 32.64 |

Table S8: Products yield of the trans-hydrogenation over 1,5HD system at 623K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 35 |  | 46 | 35 |
| 1,5-hexadiene (1,5HD) |  | 29 | 57 | 29 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.27 |  | 1.03 | 1.27 |
| Pentene | 0.16 |  |  | 0.16 |
| Trans-2-Pentene | 3.45 |  |  | 3.45 |
| Cis-2-pentene | 1.56 |  |  | 1.56 |
| 2-Methyl-2-butene |  | 0.13 | 0.04 | 0.13 |
| Hexane |  | 0.43 | 0.1 | 0.43 |
| 1-Hexene |  | 1.74 | 2.65 | 1.74 |
| 2-Hexene |  | 0.79 | 0.25 | 0.79 |
| 3-Hexene |  | 3.36 | 6.36 | 3.36 |
| Methyl-2-pentene |  | 1.41 | 1.11 | 1.41 |
| 3-Methyl-1-hexene |  | 3.08 | 4.62 | 3.08 |
| Benzene |  |  | 0.23 | 0 |
| 3-Methylhexane |  | 0.98 | 2.91 | 0.98 |
| 2-Methyl-1,3-pentadiene |  | 3.19 | 3.57 | 3.19 |
| 2-Methyl-1-1hexene |  | 0.54 | 2.67 | 0.54 |
| Methylcyclohexane | 14.83 | 4.51 | 17.21 | 19.34 |

Table S9: Products yield of the trans-hydrogenation over 1,5HD system at 573K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 25 |  | 47 | 25 |
| 1,5-hexadiene (1,5HD) |  | 30 | 44 | 30 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 0.89 |  | 1.03 |  |
| Pentene | 1.51 |  | 2.01 | 1.51 |
| Trans-2-Pentene | 0.11 |  |  | 0.11 |
| Cis-2-pentene | 0.69 |  |  | 0.69 |
| 2-Methyl-2-butene | 0.23 |  |  | 0.23 |
| Hexane |  | 0.22 |  | 0.22 |
| 1-Hexene |  | 0.98 | 1.1 | 0.98 |
| 2-Hexene |  | 1.39 |  | 1.39 |
| 3-Hexene |  | 2.51 | 5.3 | 2.51 |
| Methyl-2-pentene |  | 0.53 | 0.2 | 0.53 |
| 3-Methyl-1-hexene |  | 3.85 | 4.68 | 3.85 |
| Benzene |  | 1.38 | 2.65 | 1.38 |
| 3-Methylhexane |  | 3.72 | 3.62 | 3.72 |
| 2-Methyl-1,3-pentadiene |  | 1.54 | 2.76 | 1.54 |
| 2-Methyl-1-1hexene | 14.83 | 4.96 | 14.1 | 19.79 |

Table S10: Products yield of the trans-hydrogenation over 1,5HD system at 523K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 24 |  | 22 | 24 |
| 1,5-hexadiene (1,5HD) |  | 31 | 46 | 31 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.08 |  | 2.01 | 1.08 |
| Pentene | 0.01 |  |  | 0.01 |
| Trans-2-Pentene | 2.04 |  |  | 2.04 |
| Cis-2-pentene | 0.01 |  |  | 0.01 |
| 2-methyl-2-butene |  | 0.11 |  | 0.11 |
| Hexane |  | 1.52 | 2.15 | 1.52 |
| 1-Hexene |  | 1.13 |  | 1.13 |
| 2-Hexene |  | 3.28 | 3.79 | 3.28 |
| 3-Hexene |  | 0.61 | 0.21 | 0.61 |
| Methyl-2-pentene |  | 2.84 | 2.71 | 2.84 |
| 3-Methyl-1-hexene |  | 1.38 | 2.84 | 1.38 |
| Benzene |  | 1.64 | 1.59 | 1.64 |
| 3-Methylhexane |  | 2.65 | 3.46 | 2.65 |
| 2-Methyl-1,3-pentadiene | 12.21 | 6.59 | 11.99 | 18.80 |

Table S11: Products yield of the trans-hydrogenation over 2,4HD system at 773 K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 37 |  | 46 | 37 |
| 2,4-Hexadiene (2,4HD) |  | 63 | 63 | 63 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.67 |  | 20.7 | 1.67 |
| Pentene | 4.01 |  | 1.49 | 4.01 |
| Trans-2-Pentene | 5.27 |  | 0.44 | 5.27 |
| Cis-2-pentene | 2.64 |  |  | 2.64 |
| 2-Methyl-2-butene | 0.52 |  |  | 0.52 |
| 4-Methylpentene | 1.67 |  |  | 1.67 |
| hexane |  | 5.94 | 3.78 | 5.94 |
| Methyl-2-pentene |  | 14.26 | 4.04 | 14.26 |
| Benzene |  |  | 5.21 | 0 |
| 3-Methylhexane |  | 5.76 |  | 5.76 |
| 2-Methyl-1,3-pentadiene |  | 6.19 | 7.21 | 6.19 |
| Methylcyclohexane | 17.03 | 18.57 | 13.03 | 35.60 |

Table S12: Products yield of the trans-hydrogenation over 2,4HD system at 673 K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 34 |  | 36 | 34 |
| 2,4-Hexadiene (2,4HD) |  | 58 | 64 | 58 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.18 |  | 4.76 | 1.18 |
| Pentene | 2.59 |  |  | 2.59 |
| Trans-2-Pentene | 1.92 |  |  | 1.92 |
| Cis-2-pentene | 1.93 |  | 0.43 | 1.93 |
| 2-methyl-2-butene | 1.18 |  |  | 1.18 |
| Hexane |  |  | 2.91 |  |
| 3-Hexene |  | 2.88 |  | 2.88 |
| Methyl-2-pentene |  | 10.93 | 4.05 | 10.93 |
| 3-Methylhexane |  | 4.31 | 5.69 | 4.31 |
| 2-Methyl-1,3-pentadiene |  | 4.03 | 9.05 | 4.03 |
| Methylcyclohexane | 17.03 | 16.02 | 12.40 | 33.05 |

Table S13: Products yield of the trans-hydrogenation over 2,4HD system at 623K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 35 |  | 36 | 56 |
| 2,4-Hexadiene (2,4HD) |  | 49 | 44 | 52 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.27 |  | 4.25 | 1.27 |
| Pentene | 0.16 |  |  | 0.16 |
| Trans-2-Pentene | 3.45 |  |  | 3.45 |
| Cis-2-pentene | 1.56 |  |  | 1.56 |
| 2-methyl-2-butene |  | 3.68 |  | 3.68 |
| Hexane |  | 2.33 |  | 2.33 |
| 3-Hexene |  | 7.89 | 4.81 | 7.89 |
| Methyl-2-pentene |  |  | 3.51 |  |
| 3-Methylhexane |  | 2.13 | 8.18 | 2.13 |
| 2-Methyl-1,3-pentadiene |  | 4.94 |  | 4.94 |
| Methylcyclohexane | 14.83 | 19.11 | 8.94 | 33.94 |

Table S14: Products yield of the trans-hydrogenation over 2,4HD system at 573K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 25 |  | 28 | 25 |
| 2,4-Hexadiene (2,4HD) |  | 42 | 49 | 42 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.51 |  | 8.97 | 1.51 |
| Pentene | 0.11 |  |  | 0.11 |
| Trans-2-Pentene | 0.69 |  |  | 0.69 |
| Cis-2-pentene | 0.23 |  |  | 0.23 |
| Hexane |  | 10.93 | 3.3 | 10.93 |
| Methyl-2-pentene |  | 4.28 | 5.18 | 4.28 |
| 3-Methylhexane |  |  | 1.14 | 0 |
| 2-Methyl-1,3-pentadiene |  |  | 10.93 | 0 |
| 2-Methyl-1-1hexene |  | 3.21 |  | 3.21 |
| Methylcyclohexane | 14.83 | 14.55 | 7.61 | 29.38 |

Table S15: Products yield of the trans-hydrogenation over 2,4HD system at 523K

|  | P | H | P+H | P+H Theory |
| --- | --- | --- | --- | --- |
|  | Conversion (%) |  |  |  |
| Pentane(P) | 24 |  | 27 | 24 |
| 2,4-Hexadiene (2,4HD) |  | 32 | 36 | 32 |
|  | Yield (%) |  |  |  |
| Iso-pentane | 1.08 | 0.66 |  | 1.74 |
| Pentene | 0.01 |  |  | 1.08 |
| Trans-2-Pentene | 2.04 |  |  | 0.01 |
| Cis-2-pentene | 0.01 |  |  | 2.04 |
| Hexane |  | 1.03 | 3.4 | 1.03 |
| 1-Hexene |  | 0.41 |  | 0.41 |
| 2-Hexene |  | 0.4 |  | 0.4 |
| 3-Hexene |  | 1.85 |  | 1.85 |
| Methyl-2-pentene |  | 4.06 | 5.98 | 4.06 |
| 3-Methylhexane |  | 1.92 | 1.76 | 1.92 |
| 2-Methyl-1,3-pentadiene |  | 0.97 | 11.98 | 0.97 |
| Methylcyclohexane | 12.21 | 12.52 | 8 | 7.73 |

Table S16: Products yield during the hydrogenation of 1HY over the Pt/Al2O3 at 623K

|  | 1HY | P+H | P+H Theory |
| --- | --- | --- | --- |
| 1-Hexyne(1HY) | Conversion (%) |  |  |
|  | 76 | 55 | 64 |
|  | Yield (%) |  |  |
| Iso-pentane | 6.73 | 0.86 | 15.2 |
| Pentene |  |  | 0.16 |
| Trans-2-Pentene |  |  | 3.45 |
| Cis-2-pentene |  |  | 1.56 |
| Hexane | 1.37 |  | 0.17 |
| 1-Hexene | 16.86 | 3.06 | 0.74 |
| 2-Hexene | 3.12 | 1.84 | 0.39 |
| 3-Hexene | 2.41 | 1.38 | 0.67 |
| Methyl-2-pentene | 3.63 | 11.52 | 6.61 |
| 3-Methylpentyne | 4.46 | 14.54 | 18.41 |
| 3-Methyl-1-hexene | 0.6 |  | 2.39 |
| Benzene |  |  | 0 |
| 3-Methylhexane |  |  | 0.71 |
| 2-Methyl-1,3-pentadiene | 3.24 | 12.55 | 8.95 |
| Methylcyclohexane | 8.69 | 10.65 | 17.65 |