Table 1: Precursor quantities and experimental conditions for the co-precipitation synthesis of Zn1-xNixFe2O4 nanoparticles.

| Parameter | Chemical/Value | Quantity |
| --- | --- | --- |
| Precursors | ZnSO4H2O | Zn1-xNixFe2O4 0.00 ≤ x ≤ 0.04 |
|  | NiCl2.4H2O |  |
|  | Fe2 (SO4).7H2O |  |
| Solvent | Deionized (DI) Water | 100 mL |
| Capping Agent | Polyvinyl Alcohol (PVA) | 1.0 g |
| Precipitating Agent | Ammonia (NH3) | 2 M Solution |
| Process | Potential Hydrogen (pH) | 11 |
|  | Reaction Temperature | 60 °C |
|  | Magnetic stirrer | 1000 RPM for 4 hours |
| Post-Processing | Drying Conditions | 100 °C for 5 hours |
|  | Calcination Conditions | 900 °C for 5 hours |

Table 2: Structural parameters, including crystallite size (D), lattice constant (a), and microstrain (ε), derived from the XRD analysis of the synthesized Zn1-xNixFe2O4 nanoparticles.

| Sample | 2θ (°) | d-spacing (Ǻ) | FWHM (°) | Crystallite size (D) [nm] | Lattice constant [Ǻ] | Strain [No unit] |
| --- | --- | --- | --- | --- | --- | --- |
| 0.00 | 35.05 | 2.5583 | 0.2349 | 35.1 | 8.485 | 0.0032 |
| 0.01 | 35.13 | 2.5527 | 0.1762 | 46.8 | 8.466 | 0.0024 |
| 0.02 | 35.19 | 2.548 | 0.2349 | 35.1 | 8.451 | 0.0032 |
| 0.03 | 34.89 | 2.5696 | 0.4173 | 19.7 | 8.522 | 0.0058 |
| 0.04 | 35.14 | 2.5515 | 0.2349 | 35.1 | 8.462 | 0.0032 |

Table 3: Tetrahedral (Kt) and Octahedral (Ko) Force Constants of Zn1-xNixFe2O4 nanoparticles

| Sample (x) | ν1​ (cm-1) | ν2​ (cm-1) | Tetrahedral Force Constant, Kt​ (×105 dyne/cm) | Octahedral Force Constant, Ko​ (×105 dyne/cm) |
| --- | --- | --- | --- | --- |
| 0.00 | 547 | 460 | 2.19 | 1.55 |
| 0.01 | 549 | 453 | 2.21 | 1.5 |
| 0.02 | 548 | 457 | 2.2 | 1.53 |
| 0.03 | 550 | 457 | 2.22 | 1.53 |
| 0.04 | 550 | 451 | 2.22 | 1.49 |

Table 4: Cyclic Voltammetry (CV) parameters and calculated specific capacitance of                      Zn1-xNixFe2O4 nanoparticles at a scan rate of 10 mV/s

| Sample (x) | Peak Potential, Ep​ (mV) | Peak Current, Ip​ (μA) | Peak Range, ΔV (mV) | Integrated Charge, Q (μC) | Specific Charge, Qs​ (mC/g) | Specific Capacitance, Csp​ (mF/g) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.00 | 123.3 | 1.548 | 234 | 3.246 | 1.082 | 4.62 |
| 0.01 | -146.9 | -0.273 | 212.9 | 1.245 | 0.415 | 1.95 |
| 0.02 | -257.3 | -0.808 | 186.5 | 3.622 | 1.207 | 6.47 |
| 0.03 | -196 | -0.858 | 200.9 | 3.76 | 1.253 | 6.24 |
| 0.04 | -338.6 | -0.402 | 177 | 1.666 | 0.555 | 3.14 |

Table 5: Electrochemical Impedance Spectroscopy (EIS) parameters derived from Nyquist plot circle fitting for Zn1-xNixFe2O4 nanoparticles

| Sample (x) | Grain Resistance, Rg​ (Ω) | Grain Boundary Resistance, Rgb​ (Ω) | Total Resistance, Rt​ (Ω) | Depression Angle, θ (°) | Relaxation Parameter (n) |
| --- | --- | --- | --- | --- | --- |
| 0.00 | 1099.9 | 8583.4 | 9683.3 | 44.73 | 0.503 |
| 0.01 | 973.8 | 10493 | 11466.8 | 40.99 | 0.545 |
| 0.02 | 995.9 | 10250 | 11245.9 | 39.59 | 0.56 |
| 0.03 | 904.9 | 11119 | 12023.9 | 36.75 | 0.592 |
| 0.04 | 1086.3 | 9043.9 | 10130.2 | 43.68 | 0.515 |

Table 6: Dynamic Light Scattering (DLS) parameters of Zn1-xNixFe2O4 nanoparticles dispersed in an aqueous medium

| Sample (x) | Z-average Hydrodynamic Diameter, dcumulant​ (nm) | Contin Average Diameter (nm) | Polydispersity Index (PDI) | Diffusion Constant, D(×10−9 cm2/s) |
| --- | --- | --- | --- | --- |
| 0.00 | 3009.9 | 7596.3 | 0.927 | 1.634 |
| 0.01 | 3182.6 | 8370.7 | 1.018 | 1.546 |
| 0.02 | 3006.4 | 7416.7 | 0.907 | 1.636 |
| 0.03 | 4539.9 | 13100.2 | 1.27 | 1.084 |
| 0.04 | 4211.3 | 12491.6 | 1.121 | 1.168 |

Table 7. Magnetic parameters, including saturation magnetization (Ms), remanence magnetization (Mr), coercivity (Hc), calculated net magnetic moment (µB), effective anisotropy constant (K), and remanence ratio (R), for the annealed Zn1-xNixFe2O4 nanoparticles.

| Sample (x) | Ms (emu/g) | Mr (emu/g) | Hc (Oe) | μB (Bohr magneton) | K (erg/g) | R (No unit) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.00 | 26.158×10−3 | 1.3838×10−3 | 19.03 | 1.13×10−3 | 0.249 | 0.0529 |
| 0.01 | 19.975×10−3 | 934.21×10−6 | 201.56 | 8.62×10−4 | 2.013 | 0.0468 |
| 0.02 | 0.23306 | 774.67×10−6 | 8.0641 | 1.00×10−2 | 0.94 | 0.0033 |
| 0.03 | 23.087×10−3 | 725.09×10−6 | 150 | 9.96×10−4 | 1.732 | 0.0314 |
| 0.04 | 0.11786 | 544.20×10−6 | 26.774 | 5.08×10−3 | 1.578 | 0.0046 |