Supplementary information

High-performance and hysteresis-free perovskite transistors with anion engineering

Huihui Zhu1, 7, Ao Liu1, 7, Kyu In Shim2, Haksoon Jung1, Taoyu Zou1, Youjin Reo1, Hyunjun Kim1, Jeong Woo Han2, Yimu Chen3, Hye Yong Chu4, Jun Hyung Lim4, Hyung-Jun Kim4, Sai Bai5, 6*, Yong-Young Noh1*

1Department of Chemical Engineering, Pohang University of Science and Technology, 77 Cheongam-Ro, Nam-Gu, Pohang 37673, Republic of Korea

2Department of Chemical Engineering and School of Interdisciplinary Bioscience and Bioengineering,  Pohang University of Science and Technology, 77 Cheongam-Ro, Nam-Gu, Pohang 37673, Republic of Korea

3Ministry of Industry and Information Technology Key Lab of Micro-Nano Optoelectronic Information System, Harbin Institute of Technology, Shenzhen, 518055, China

4R&D Center, Samsung Display Inc., Yongin 17113, Republic of Korea

5Institute of Fundamental and Frontier Sciences, University of Electronic Science and Technology of China, Chengdu, 611731, China

6Department of Physics, Chemistry and Biology (IFM), Linköping University, Linköping SE-58183, Sweden

7These authors contributed equally to this work.

*Corresponding to authors: Y. Y. Noh (yynoh@postech.ac.kr) and S. B (sai.bai@liu.se)

Methods

Chemicals. N,N-dimethylformamide (DMF, anhydrous, 99.8%, Sigma-Aldrich), dimethyl sulfoxide (DMSO, anhydrous, ≥99.9%, Sigma-Aldrich), methylammonium iodide (MAI, ≥99.5%, Xi’an Polymer Light Technology Corp), tin(II) iodide (SnI2, anhydrous, beads, 99.99% trace metals basis, Sigma-Aldrich), lead(II) iodide (PbI2, 99.9985% metals basis, Alfa Aesar), tin(II) fluoride (SnF2, 99%, Sigma-Aldrich), lead(II) bromide (PbBr2, 99.99% trace metals basis, Sigma-Aldrich), lead(II) chloride (PbCl2, >99.99%, Xi’an Polymer Light Technology Corp), tin(II) chloride (SnCl2, 99.99% trace metals basis, Sigma-Aldrich) and chlorobenze (anhydrous, 99.8%, Sigma-Aldrich) were used as received without further purification.

Precursor and device preparation. The precursor solutions were prepared by mixing MAX and SnX2 (X = I, Cl, Br) in DMF/DMSO binary solvents at a volume ratio of 4/1. The ratio of different composition is expressed as MASn(I1-yXy)3, X = Cl or Br, and y=0~0.08. The precursor concentration was around 0.15 M. For example, to prepare the MASnI3 precursor, 102 mg of MAI, 216 mg of SnI2, 17 mg of PbI2, and 8.4 mg of SnF2 were dissolved in 4 mL of mixed solvent (3.2 mL of DMF and 0.8 mL of DMSO). The others were made similarly. Same amounts of SnF2 (8 mol% with respect to the Sn source) and lead substitution (6 mol%) were added in each precursor as anti-oxidation and stabilizer additives. Each precursor was stir-heated at 60 oC for 2h before use. Dielectric layers were the reliable 40-nm HfO2 on Si substrates with capacitance of 270 nF cm-2 grown by the mature atomic layer deposition (ALD) in National Institute for Nanomaterials Techanology, Pohang. For the perovskite film deposition, the HfO2/Si substrates (1.5×1.5 cm2) were first treated with UV ozone for 30 mins, then the precursor solutions were dropped on the substrates and spin-coated at the speed of 4000 rpm for 25 s with 60 uL of chlorobenzene dripping after ~10 s from the beginning. Afterwards, the films were annealed at 70 oC for 10 mins. All precursor solutions and films were prepared in an N2-filled glove box (O2 and H2O levels: 1–2 ppm). Then thermal evaporation and a shadow mask were used for the Au source/drain electrode deposition. The channel width and length of the TFTs are 1000 and 150 um, respectively. For the complementary inverter integration, we used design-patterned indium tin oxide (ITO, 10 Ω/□) glass by photolithography as the bottom gate, ALD HfO2 as the dielectric layer, solution-processed self-patterned1 triple-halide perovskite as the p-channel and IGZO as the n-channel, and evaporated gold through a bespoke shadow mask as electrodes.

Film and device characterizations. The film XRD patterns were recorded using a Rigaku D/MAX 2600 V with Cu K(= 1.5406 Å) radiation. SEM images were obtained using a field-emission scanning electron microscope (Hitachi S4800). AFM height profile data were collected using an atomic force microscopy (Nanosurf Nanite AFM). XPS characterizations were conducted using a VersaProbe Scanning Microprobe under vacuum (10−8 Torr). The Hall measurements were performed using the van der Pauw method, using a 0.51T magnet and a bespoke sample holder in an N2-filled glove box at room temperature. The electrical signal during the Hall measurement was obtained using a Keithley 4200-SCS and probe station (MST-4000A, MS TECH, Korea). Transistor transfer characteristics were measured using a semiconductor parameter analyser (Keithley 4200-SCS) in an N2-filled glove box at room temperature in continuous mode. The saturation TFT mobility was calculated as2:

μsat=2LWCi∂IDS∂VGS2,

where L, W, and Ci are the channel length and width and dielectric areal capacitance, respectively.

DFT calculations. All density functional theory (DFT) calculations were performed using the Vienna ab Initio Simulation Package (VASP)3. The Perdew-Burke-Ernzerhof (PBE) functional of the generalized gradient approximation (GGA) was used for the exchange-correlation energies4, 5. Bulk MASnI3 tetragonal crystal structure was initially optimized to have the parameters of a = 6.230 Å, b = 6.230 Å, and c = 6.232 Å. Based on this, (5 × 3 × 1) MASnI3 slab structures were constructed with 6 layer thickness and ~15 Å vacuum spacing in the direction normal to the surface. Br-doped slab model, MASn(I/Br)3, was also created with same parameters. The energy cutoff for the plane-wave basis set was set to be 600 eV, and Monkhorst-Pack 1 × 1 × 1 k-point meshes were used6. Moreover, the DFT-D3 method was employed to introduce the van der Waals interaction7. For the structural optimization, the bottom three layers were fixed, but rest of atoms were relaxed using a conjugate-gradient algorithm until the difference in the total force was < 0.03 eV/Å, and spin-polarization was taken into considerations8. VESTA package was used for structural visualization9. For the calculation of binding affinity towards I vacancy site, two slab models of pure MASnI3 and Br-doped MASn(I/Br)3 were employed. For each slab model, I vacancy site was created on the surface, and different halides (X = I-, Br-, Cl-) were placed at the I vacancy site. Affinity towards I vacancy site depending on different halides was calculated using below equations,

Eaffinity=Ehalide passivated -EIvac-n*12Ehalogeng,

where Eaffinity is the adsorption energy of halide to the I vacancy site on the surface, Ehalide passivated  is the total energy of halide passivated at the I vacancy site on the surface, n is the number of halides being passivated, Eaniong is the total energy of halogen gas. For MASn(I/Br)3 model, above equation was also applied using total energy of passivated at the I vacancy site of MASn(I/Br)3 slab instead of MASnI3 slab. In order to simulate the randomness of Br passivation, Br was doped at random locations within the slab layers at Br to I ratio of 0.05.

Supplementary Fig. 1. The optimizations of halide composition for MASnX3 based perovskite TFTs. Br4, Cl2, Cl4, Cl8, Br1Cl7, and Br3Cl5 denote the devices based on channel films processed from precursors of MASn(I0.96Br0.04)3, MASn(I0.98Cl0.02)3, MASn(I0.96Cl0.04)3, MASn(I0.92Cl0.08)3, MASn(I0.92Br0.01Cl0.07)3, and MASn(I0.92Br0.03Cl0.05)3, respectively.

Supplementary Fig. 2. Output characteristics of the (a) I-pristine, (b) I/Br, (c) I/Cl and (d) I/Br/Cl perovskite TFTs. I-pristine, I/Br, I/Cl, and I/Br/Cl denote the devices based on channel films processed from precursors of MASnI3, MASn(I0.98Br0.02)3, MASn(I0.94Cl0.06)3 and MASn(I0.92Br0.02Cl0.06)3, respectively.

Supplementary Fig. 3. |IDS|1/2 of the perovskite TFTs with the I-pristine, I/Br, I/Cl and I/Br/Cl channel films, respectively.

Supplementary Fig. 4. Dual-sweep mobilities of the perovskite TFTs with the I-pristine, I/Br, I/Cl and I/Br/Cl channel films, respectively. The maximum values were extraced from reverse and forward sweeps for per device, respectively.

Supplementary Fig. 5. XRD peak shift of the perovskite TFTs with the I-pristine, I/Br, I/Cl and I/Br/Cl channel films, respectively.

Supplementary Fig. 6. Subthreshold swing (SS) statistics from ten individual TFTs with the I, I/Br, I/Cl and I/Br/Cl channel films, respectively. The mean values are labelled.

Supplementary Fig. 7. DFT slab models of (a) basic MASnI3, (b) MASnI3 with an iodine vacancy (VI). Illustrations of VI passivation by (c) Br or (d) Cl anions in MASnI3, and (e) illustrations of VI passivation by a Br anion in MASn(I/Br)3 case.

Supplementary Fig. 8. Transfer characteristics of (a) I-pristine and (b) I/Br/Cl TFTs under cycling test (VDS=-12 V).

Supplementary Fig. 9. Transfer characteristics of (a) I-pristine and (b) I/Br/Cl TFTs under bias (VGS=VDS=-12 V).

Supplementary Fig. 10. Transfer characteristics and mobility statistics of 50 individual I/Br/Cl TFTs. The average mobility extracted from reverse scans is 19±1.2 cm2 V−1 s−1.

Supplementary Fig. 11. The butterfly voltage transfer curves plot of the integrated perovskite/IGZO complementary inverter. The black-dash curve was plotted in mirror. The noise margin can be estimated by nesting the largest possible rectangular area inside the butterfly plot, following the maximum equal criterion method10.

Supplementary Table 1. Performance parameters of Pb-and Sn-based perovskite transistors.

|  | Perovskite Channel | Interlayer/ Processing* | Operation Temp. | Mobility (cm2 V−1 s−1) |  | On/off ratio | Year |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | h | e |  |  |  |  |
| 3D Pb-based perovskites | MAPbI3 | / | 78 K | 2.1 × 10−2 | 7.2 × 10−2 | ~105 | 2015 |  | 11 |
|  |  | / | 180 K | / | 1 × 10−2 | ~104 | 2015 |  | 12 |
|  |  | PEIE | 300 K | / | 0.5 | ~104 | 2017 |  | 13 |
|  |  | Microplate | 200 K | / | 0.3 | ~105 | 2016 |  | 14 |
|  |  | Microplate, Gra modified | 77 K | / | ~4 | ~105 | 2017 |  | 15 |
|  |  | Surface cleaning | RT | 1.8 | 3.0 | ~105 | 2020 |  | 16 |
|  | MAPbI3−xClx | TTFB-SAM | RT | 1.3 | 1.0 | ~103 | 2015 |  | 17 |
|  |  | Protein treated | RT | 0.11 | / | ~104 | 2017 |  | 18 |
|  | Csx(MA0.17FA0.83)1−xPb(Br0.17I0.83)3 | DTS | RT | 2.1 | 2.5 | ~104 | 2017 |  | 19 |
|  | RbCsFAMAPbI3 | Sol. treated | RT | / | 1.2 | ~104 | 2020 |  | 20 |
|  | MAPbX3, X = Cl, Br, I | Single crystal | RT | 4.7 | 1.5 | ~105 | 2018 |  | 21 |
| 2D Sn-based perovskites | (PEA)2SnI4 | / | RT | 0.6 | / | 104 | 1999 |  | 22 |
|  | (PEA)2SnI4 | Melt processed | RT | 2.6 | / | ~106 | 2002 |  | 23 |
|  | (PEA)2SnI4 | MoOx, NH3I-SAM | RT | 12 | / | ~106 | 2016 | 24 |  |
|  | (PEA)2SnI4 | Semi-CNTs hybrid | RT | 1.5 | / | ~105 | 2019 |  | 25 |
|  | (PEA)2SnI4 | Precursor- film-FET optimization | RT | 3.5 | / | ~106 | 2020 |  | 26 |
|  | (PEA)2SnI4 | Binary sol. | RT | 3.8 | / | ~106 | 2020 |  | 27 |
|  | (PEA)2SnI4 | Urea | RT | 4.2 | / | ~105 | 2021 |  | 28 |
|  | (m-FPEA)2SnI4 m=2, 3, 4 | / | RT | 0.2~0.6 | / | ~105 | 2001 |  | 29 |
|  | (4Tm)2SnI4 | / | RT | 2.32 | / | ~106 | 2019 |  | 30 |
|  | (TT)2SnI4 | / | RT | 9.35 | / | ~106 | 2021 |  | 31 |
| 2D/3D Sn-based perovskite | (FA/PEA)SnIx | / | RT | 0.21 | / | ~104 | 2021 |  | 32 |
| 3D Sn-based perovskites | MASn(I)3 | / | RT | 1.3 | / | 106 | This work |  |  |
|  | MASn(I/Br/Cl)3 | Halide engineering | RT | 19.6 | / | 3×107 |  |  |  |

Note: The perovskite FETs based on mature dielectrics with uncontested capacitance, e.g. SiO2, Cytop, PMMA, were summarized here.33 *Thin-film channel layers were solution-processed unless otherwise noted. Research on perovskite-based FETs is still at a relatively early stage,34, 35 and device test and mobility calculation vary in a wide range from lab to lab.36-40 It is suggested: i) drain current should be very distinguishable from gate leakage current; ii) capacitance of dielectric layer should be verified; iii) contact resistance between channel layer and source-drain electrodes should be small enough for precise mobility extraction; iv) if dual-sweep hysteresis exists, detailed mobility extraction should be provided; v) device reproducibility should be reasonable.

References

(1)	Park, W.-T.; Noh, Y.-Y., A Self-Aligned High Resolution Patterning Process for Large Area Printed Electronics. J. Mater. Chem. C 5, 6467-6470 (2017).

(2)	Wang, Z.; Nayak, P. K.; Caraveo-Frescas, J. A.; Alshareef, H. N., Recent Developments in P-Type Oxide Semiconductor Materials and Devices. Adv. Mater. 28, 3831-3892 (2016).

(3)	Kresse, G.; Furthmüller, J., Efficient Iterative Schemes for Ab Initio Total-Energy Calculations Using a Plane-Wave Basis Set. Phys. Rev. B 54, 11169-11186 (1996).

(4)	Grimme, S., Semiempirical Gga-Type Density Functional Constructed with a Long-Range Dispersion Correction. J. Comput. Chem. 27, 1787-1799 (2006).

(5)	Sholl, D.; Steckel, J. A., Density Functional Theory: A Practical Introduction. John Wiley & Sons: 2011.

(6)	Monkhorst, H. J.; Pack, J. D. J. P. r. B., Special Points for Brillouin-Zone Integrations. 13, 5188 (1976).

(7)	Grimme, S.; Antony, J.; Ehrlich, S.; Krieg, H., A Consistent and Accurate Ab Initio Parametrization of Density Functional Dispersion Correction (Dft-D) for the 94 Elements H-Pu. J. Chem. Phys. 132, 154104 (2010).

(8)	Press, W. H.; Flannery, B. P.; Teukolsky, S. A.; Vetterling, W. T. J. C.; New York, C. U. P., , 839, Numerical Recipes: The Art of Scientific Computing. (1986).

(9)	Momma, K.; Izumi, F., Vesta 3 for Three-Dimensional Visualization of Crystal, Volumetric and Morphology Data. J. Appl. Crystallogr. 44, 1272-1276 (2011).

(10)	Hauser, J. R., Noise Margin Criteria for Digital Logic-Circuits. Ieee. T. Educ. 36, 363-368 (1993).

(11)	Chin, X. Y.; Cortecchia, D.; Yin, J.; Bruno, A.; Soci, C., Lead Iodide Perovskite Light-Emitting Field-Effect Transistor. Nat. Commun. 6, 7383 (2015).

(12)	Labram, J. G.; Fabini, D. H.; Perry, E. E.; Lehner, A. J.; Wang, H.; Glaudell, A. M.; Wu, G.; Evans, H.; Buck, D.; Cotta, R.; Echegoyen, L.; Wudl, F.; Seshadri, R.; Chabinyc, M. L., Temperature-Dependent Polarization in Field-Effect Transport and Photovoltaic Measurements of Methylammonium Lead Iodide. J. Phys. Chem. Lett. 6, 3565-3571 (2015).

(13)	Senanayak, S. P.; Yang, B.; Thomas, T. H.; Giesbrecht, N.; Huang, W.; Gann, E.; Nair, B.; Goedel, K.; Guha, S.; Moya, X., Understanding Charge Transport in Lead Iodide Perovskite Thin-Film Field-Effect Transistors. Sci. Adv. 3, e1601935 (2017).

(14)	Li, D.; Wang, G.; Cheng, H.-C.; Chen, C.-Y.; Wu, H.; Liu, Y.; Huang, Y.; Duan, X., Size-Dependent Phase Transition in Methylammonium Lead Iodide Perovskite Microplate Crystals. Nat. Commun. 7, 11330 (2016).

(15)	Li, D.; Cheng, H.-C.; Wang, Y.; Zhao, Z.; Wang, G.; Wu, H.; He, Q.; Huang, Y.; Duan, X., The Effect of Thermal Annealing on Charge Transport in Organolead Halide Perovskite Microplate Field-Effect Transistors. Adv. Mater. 29, 1601959 (2017).

(16)	She, X. J.; Chen, C.; Divitini, G.; Zhao, B. D.; Li, Y.; Wang, J. Z.; Orri, J. F.; Cui, L. S.; Xu, W. D.; Peng, J.; Wang, S.; Sadhanala, A.; Sirringhaus, H., A Solvent-Based Surface Cleaning and Passivation Technique for Suppressing Ionic Defects in High-Mobility Perovskite Field-Effect Transistors. Nat. Electron. 3, 694-703 (2020).

(17)	Mei, Y.; Zhang, C.; Vardeny, Z.; Jurchescu, O., Electrostatic Gating of Hybrid Halide Perovskite Field-Effect Transistors: Balanced Ambipolar Transport at Room-Temperature. MRS Commun. 5, 297-301 (2015).

(18)	Ward, J. W.; Smith, H. L.; Zeidell, A.; Diemer, P. J.; Baker, S. R.; Lee, H.; Payne, M. M.; Anthony, J. E.; Guthold, M.; Jurchescu, O. D., Solution-Processed Organic and Halide Perovskite Transistors on Hydrophobic Surfaces. ACS Appl. Mater. Interfaces 9, 18120-18126 (2017).

(19)	Yusoff, A. R. b. M.; Kim, H. P.; Li, X.; Kim, J.; Jang, J.; Nazeeruddin, M. K., Ambipolar Triple Cation Perovskite Field Effect Transistors and Inverters. Adv. Mater. 29, 1602940 (2017).

(20)	Senanayak, S. P.; Abdi-Jalebi, M.; Kamboj, V. S.; Carey, R.; Shivanna, R.; Tian, T.; Schweicher, G.; Wang, J.; Giesbrecht, N.; Di Nuzzo, D.; Beere, H. E.; Docampo, P.; Ritchie, D. A.; Fairen-Jimenez, D.; Friend, R. H.; Sirringhaus, H., A General Approach for Hysteresis-Free, Operationally Stable Metal Halide Perovskite Field-Effect Transistors. Sci. Adv. 6, eaaz4948 (2020).

(21)	Yu, W.; Li, F.; Yu, L.; Niazi, M. R.; Zou, Y.; Corzo, D.; Basu, A.; Ma, C.; Dey, S.; Tietze, M. L., Single Crystal Hybrid Perovskite Field-Effect Transistors. Nat. Commun. 9, 5354 (2018).

(22)	Kagan, C.; Mitzi, D.; Dimitrakopoulos, C., Organic-Inorganic Hybrid Materials as Semiconducting Channels in Thin-Film Field-Effect Transistors. Science 286, 945-947 (1999).

(23)	Mitzi, D. B.; Dimitrakopoulos, C. D.; Rosner, J.; Medeiros, D. R.; Xu, Z.; Noyan, C., Hybrid Field‐Effect Transistor Based on a Low‐Temperature Melt‐Processed Channel Layer. Adv. Mater. 14, 1772-1776 (2002).

(24)	Matsushima, T.; Hwang, S.; Sandanayaka, A. S.; Qin, C.; Terakawa, S.; Fujihara, T.; Yahiro, M.; Adachi, C., Solution‐Processed Organic–Inorganic Perovskite Field‐Effect Transistors with High Hole Mobilities. Adv. Mater. 28, 10275-10281 (2016).

(25)	Zhu, H.; Liu, A.; Luque, H. L.; Sun, H.; Ji, D.; Noh, Y.-Y., Perovskite and Conjugated Polymer Wrapped Semiconducting Carbon Nanotube Hybrid Films for High-Performance Transistors and Phototransistors. ACS Nano 13, 3971-3981 (2019).

(26)	Zhu, H.; Liu, A.; Shim, K. I.; Hong, J.; Han, J. W.; Noh, Y.-Y., High-Performance and Reliable Lead-Free Layered-Perovskite Transistors. Adv. Mater. 32, 2002717 (2020).

(27)	Zhu, H.; Liu, A.; Kim, H.; Hong, J.; Go, J.-Y.; Noh, Y.-Y., High-Performance Layered Perovskite Transistors and Phototransistors by Binary Solvent Engineering. Chem. Mater. 33, 1174-1181 (2021).

(28)	Zhu, H.; Liu, A.; Zou, T.; Jung, H.; Heo, S.; Noh, Y. Y., A Lewis Base and Boundary Passivation Bifunctional Additive for High Performance Lead-Free Layered-Perovskite Transistors and Phototransistors. Mater. Today Energy 21, 100722 (2021).

(29)	Mitzi, D. B.; Dimitrakopoulos, C. D.; Kosbar, L. L., Structurally Tailored Organic−Inorganic Perovskites:  Optical Properties and Solution-Processed Channel Materials for Thin-Film Transistors. Chem. Mater. 13, 3728-3740 (2001).

(30)	Gao, Y.; Wei, Z.; Yoo, P.; Shi, E.; Zeller, M.; Zhu, C.; Liao, P.; Dou, L. J. J. o. t. A. C. S., Highly Stable Lead-Free Perovskite Field-Effect Transistors Incorporating Linear Π-Conjugated Organic Ligands. J. Am. Chem. Soc. 141, 15577-15585 (2019).

(31)	Liang, A.; Gao, Y.; Asadpour, R.; Wei, Z.; Finkenauer, B. P.; Jin, L.; Yang, J.; Wang, K.; Chen, K.; Liao, P.; Zhu, C.; Huang, L.; Boudouris, B. W.; Alam, M. A.; Dou, L., Ligand-Driven Grain Engineering of High Mobility Two-Dimensional Perovskite Thin-Film Transistors. J. Am. Chem. Soc. 143, 15215-15223 (2021).

(32)	Shao, S.; Talsma, W.; Pitaro, M.; Dong, J.; Kahmann, S.; Rommens, A. J.; Portale, G.; Loi, M. A., Field‐Effect Transistors Based on Formamidinium Tin Triiodide Perovskite. Adv. Funct. Mater. 31, 2008478 (2021).

(33)	Yang, T.; Wu, Q.; Dai, F.; Huang, K.; Xu, H.; Liu, C.; Chen, C.; Hu, S.; Liang, X.; Liu, X.; Noh, Y.-Y.; Liu, C., Understanding, Optimizing, and Utilizing Nonideal Transistors Based on Organic or Organic Hybrid Semiconductors. Adv. Funct. Mater. 30, 1903889 (2020).

(34)	Shining a Light on Perovskite Devices. Nat. Electron. 3, 657-657 (2020).

(35)	Zhu, H.; Liu, A.; Noh, Y.-Y., Perovskite Transistors Clean up Their Act. Nat. Electron. 3, 662-663 (2020).

(36)	Paulus, F.; Tyznik, C.; Jurchescu, O. D.; Vaynzof, Y., Switched-On: Progress, Challenges, and Opportunities in Metal Halide Perovskite Transistors. Adv. Funct. Mater. 31, 2101029 (2021).

(37)	Zhu, H.; Shin, E.-S.; Liu, A.; Ji, D.; Xu, Y.; Noh, Y.-Y., Printable Semiconductors for Backplane Tfts of Flexible Oled Displays. Adv. Funct. Mater. 30, 1904588 (2020).

(38)	Zhu, H.; Liu, A.; Noh, Y.-Y., Recent Progress on Metal Halide Perovskite Field-Effect Transistors. Journal of Information Display, 1-12 (2021).

(39)	Liu, X.; Yu, D.; Song, X.; Zeng, H., Metal Halide Perovskites: Synthesis, Ion Migration, and Application in Field‐Effect Transistors. Small 14, 1801460 (2018).

(40)	Lin, Y.-H.; Pattanasattayavong, P.; Anthopoulos, T. D., Metal-Halide Perovskite Transistors for Printed Electronics: Challenges and Opportunities. Adv. Mater. 29, 1702838 (2017).