Supplementary Information

Supplementary Information 1. Details of the model used

The model describes a system of particles represented by the vector radius , the momentum , and the interaction potential corresponding to  the following Hamiltonian:

.								(S1)

It is opportune to represent the interaction potential by a pair of the Gauss potentials:, where and define the magnitude, while andthe radii of attraction and repulsion, respectively. The minimisation condition corresponding to an equilibrium reads as follows: , . In numerical experiments, the particles are initially placed at random on a rectangle with the side lengths of  and . For the case of shear deformation, it is convenient to employ periodic boundary conditions on the horizontal axis. Accordingly, a particle leaving the interval  is returned to it at the opposite end and the vectors  connect particles located within the interval  or the images of escaped particles at the opposite side of the system. On the vertical axis the system is limited by plates at andwith reflecting boundary conditions:  and . The stronger the inequalitiesand , the more rigid and sharp are the walls in relation to other forces and lengths relevant to the system. Since the parameters ,, , and form arrays covering all possible combinations, it can be said without loss of generality that the Hamiltonian given by Eq. (S1) describes systems with any number of components, including one- and two-component systems, which are of interest in this paper. What is required is just to specify the parameters , ,, etc.

The simplicity of the equations of motion,

, 									(S2)

is deceptive. Summation at every time step over all possible neighbours, including very distant ones and the fictitious image particles stemming from the periodic boundary conditions, is required. In addition, in the case of contact with a thermal bath the boundary conditions need to be replaced with more realistic ones. If the temperature of the thermal bath at a given boundary (or within the system) is non-zero, an array of random -correlated Langevin forces need to be included. These are to satisfy the fluctuation-dissipation theorem in the form of , where ,  is the Boltzmann constant,  is a dissipation constant, and is the discrete time step. Interacting particles exchange momentum, and hence a dissipation channel acting to equilibrate the relative velocities of particles that happen to be within the distance close to the equilibrium one needs to be introduced. This is done by including an additive force on the i-th particle, with yet another dissipation constant. As a result, the equations of motion assume the following form:

(S3)

They can be integrated by using Verlet’s method, which conserves the energy of the system at each time step, provided no energy is supplied externally through mechanical work or temperature variation.

Supplementary Information 2. Calculation of the force

Here we calculate a measurable quantity: the external force acting on the system. First, we calculate the work produced by the forces acting on each particle of the system or the corresponding power. Summation over all particles yields the total power  expended by a pair of external forces to maintain the motion of the boundary plates with a constant velocity,   This yields the total force,. Calculating spatially distributed power enables one to evaluate the degree of localisation of excitations and hence the fraction of the regions in which the fragments of the lattice move practically as a whole. As at a particular site the energy is absorbed and released at different points in time, it is useful to characterise these sites by the absolute value of the power,.

For that, we start with plotting a histogram for the probability of finding a given value of . As expected, the function has a pronounced maximum at low values of  associated with small perturbations of the system almost everywhere within the ordered domains. The regions of large strain contribute to the total powermost significantly, but the partial contribution of an individual region is not very significant. As a result, the distributionhas an extended ‘tail’ at large .

For both the locations of the maxima and the asymptotes to be well-resolved at the same a nonlinear function is plotted in Fig. S1(a). It can roughly be divided in two regions – left and right of a vertical dashed line that marks a certain characteristic value. The fraction of points where holds, i.e., those points where intensive processes occur, evolves with time. The results of this procedure for a particular realisation of the deformation process are shown exemplary in Fig. S1(b). One can recognise pronounced bursts of activity, which can be associated with the periods of emergence and development of rebuilt structures localised at the edges of domains seen in Supplementary Movie_01.avi. The same periods can also be identified in the time dependence of the total presented in Fig. S1(c). To facilitate the comparison, some of the bursts are marked with dash-dotted lines.

Figure S1. Square root of the histogram (a) and the time dependence of the fraction of the points for which the inequality  holds (b). Note the bursts in the magnitude of this fraction corresponding to the peaks in the time dependence of the total force Fextt=Pt/V, which is presented in (c).

The functionrepresents the time dependence of the force required to slide a solid on a surface. From this dependence the yield force, or yield stress, can be identified. In our computer experiments, this dependence resembled that for the resistance force for sliding a solid on a surface with random roughness in the stick-slip regime. This is not surprising, as in our case at any given moment at least two layers of the material separated by a rough interface are engaged in a relative frictional motion. In Fig. S2, the occurrence of an upper and a lower yield point can be identified. In metallic materials possessing such a property, propagating localised deformation bands (Lüders bands) occur under tensile loading. A natural question to be asked is why such stick-slip- or Lüders-like effects are not observed or are very weak in real experiments on shear flow of solids. In our opinion, the reason is that shear flow experiments are commonly done on macroscopic objects. In the thermodynamic limit, ‘self-averaging’ over the individual bursts of the force, which occur in different areas of a macroscopic sample, would suppress pronounced jerky flow.

Figure S2. The results of averaging of the force over ten realisations of the computer experiments for four different values of the parameter C11 representing the stiffness of the interaction potential.

Since one cannot replicate this ‘self-averaging’ procedure in numerical modelling, it can be replaced with averaging over multiple realisations of the mesoscopic system we are dealing with. Physically, this should correspond to adding up the contributions of different areas of the real body. Fig. S2 displays the results of such averaging over ten realisations for four systems with different values of the stiffness parameter C11. The thin lines in the graphs on the left ((a), (c), (e), and (g)) show the time dependence of the force (or the shear, which is equivalent to the force for V = const), whilst the heavy lines represent the results of averaging. The diagrams on the right ((b), (d), (f), and (h)) show the corresponding histograms for the probability of finding an instantaneous value of the force accumulated in all realisations over the entire period of observation.

It should be mentioned that the position of the maximum of a histogram, i.e., the most probable magnitude of the force, is practically stiffness-independent, while due to the tail of a distribution the average force is shifted to larger values when the stiffness is increased. As this shift owes to relatively seldom, but large, maxima of the force, one can conclude that the measured force is governed by sharp discontinuous stick-slip events, which are more pronounced in stiff systems.

Figure S3. Results of computations of the time-averaged force as a function of the stiffness of the system (normalised with respect to a certain value C11*, which was fixed in all numerical experiments). The dash-dotted horizontal line corresponds to a background common to all systems considered.

It can be shown that the common background stems from the viscous contribution to the resistance to plastic flow, which in the model considered is present for all systems – whether stiff or soft (‘fluid’) systems alike. To exclude it, we conducted similar numerical experiments on soft systems, which were otherwise similar to those with a much lower dissipation constant of  and. A continual drop of the background level, which is to be subtracted from the force readings when determining the plastic yield limit, is determined for a fixed value of , was observed.

In principle, the integral force can be determined both for a large system or, alternatively, through averaging over a large number of realisations. However, analysis of the time dependence of the force, even when averaged over a relatively small number of realisations, shows that it becomes rather flat. For a prolonged steady state, the results of averaging over the histograms in Fig. S2 and the time average converge. This is in keeping with the ‘ergodic hypothesis’ which states that for a sufficiently large system the average over time and that over the realisations coincide. We used this observation to determine the average force for a representative large number of cases and to establish its dependence on the key parameter,  , which governs the stiffness of the system. The calculated values of the force, which were shown to be in accord with the expected values, are compiled in Fig. S3.  The horizontal dash-dotted line corresponding to the background, which is to be subtracted from the data in the case of

Annotations to the videos

Supplementary Movie_01.avi

Typical motion of a solid under shear deformation. The colour code is the same as in Fig. 3. It is seen that initially the solid deforms elastically, the particles’ motion smoothly following the displacement of the boundary plates. The corresponding force vs. displacement curve is smooth. When a critical shear is reached, the bonds between neighbouring particles start breaking. However, locally the lattice domains into which the solid gets fragmented move as a whole, switching to a different crystallographic plane only at the contacts between the domains.  The profile of the translation velocity averaged over the horizontal axis varies and exhibits different combinations of steps at different points in time. A well-pronounced correlation between the development of cracks and bursts of the power and the total force, as well as waves of localised excitations, is seen on the spatiotemporal velocity diagram.

Supplementary Movie_02.avi

The dynamic process leading to the ruptures of a layer of a stiff material sandwiched between two layers of a more compliant material. The particles of the stiff material and the compliant one are marked by filled and open circles, respectively. The same colour code as in Supplementary Movie_01.avi is used.  It is seen how the motion of the compliant sub-system in gradually transmitted to the stiff inner layer, engaging it in motion. The diagrams on the right show the distributions of the absolute values of the force and the velocity, averaged along the horizontal axis. It should be noted that the deformation of the inner layer leads to smoothening of the characteristic features of the distributions of the force and the velocity.