# Supplementary Information

# Chemically and Microstructurally Modulated High-Temperature Release of CsI in Nd-doped UO2 Nanoceramics

Daniil Shirokiy1*, Karin Popa2*, Marco Cologna2, Felix Brandt1, Jean-Yves Colle2, Damien Prieur3,4, Olaf Walter2, Walter Bonani2, Anna Isabel Martinez Ferri2, Ondřej Beneš2, Martina Klinkenberg1,
Răzvan Buda2, Dirk Bosbach1 and Gabriel L. Murphy1*

1Institute of Fusion Energy and Nuclear Waste Management (IFN-2), Forschungszentrum Jülich GmbH, 52428 Jülich, Germany

2European Commission, Joint Research Centre (JRC), 76344 Karlsruhe, Germany

3Rossendorf Beamline (BM20), European Synchrotron Radiation Facility, Avenue des Martyrs 71, 38043 Grenoble, France

4Institute of Resource Ecology, Helmholtz-Zentrum Dresden-Rossendorf, Bautzner Landstraße 400, 01328 Dresden, Germany

* Corresponding authors: Daniil Shirokiy (d.shirokiy@fz-juelich.de), Karin Popa (karin.popa@ec.europa.eu), Gabriel L. Murphy (g.murphy@fz-juelich.de)

# Supplementary Information Note 1 – The KEMS spectra of all gaseous fractions

Supplementary Figure 1 displays KEMS signal for each of the gaseous fractions measured.

Supplementary Figure 1 – KEMS signal from all the measured gaseous fractions for a) Nd 0%, b) Nd 15% and c) Nd 30% samples.

# Supplementary Information Note 2 – Nd-doped UO2 nanoparticles

Supplementary shows the nanoparticles of Nd-doped UO2 produced from thermal decomposition.

Supplementary Figure 2 – Nanoparticles obtained by hydrothermal decomposition of a) Nd-free uranyl nitrate, b) a mixture of uranyl nitrate (85 mol %) and Nd nitrate (15 mol %), and c) a mixture of uranyl nitrate (70 mol %) and Nd nitrate (30 mol %).

# Supplementary Information Note 3 – Lattice parameter linear fit

A linear fit was performed using the Origin software tool with the y = a + b × x function. Values of a and b, together with their uncertainties, as well as the R2 values are presented in the Supplementary Table 1.

Supplementary Table 1 – The linear fit values for the lattice parameter as a function of temperature and Nd doping

| Sample | a | b | R2 |
| --- | --- | --- | --- |
| As a function of temperature |  |  |  |
| Nd 0% | 5.4548(13) | 6.28(19) × 10-5 | 0.99430 |
| Nd 15% | 5.44090(110) | 7.03(17) × 10-5 | 0.99652 |
| Nd 30% | 5.43718(141) | 6.71(22) × 10-5 | 0.99384 |
| As a function of Nd-doping |  |  |  |
| – | 5.4567(39) | -5.6(2.0) × 10-4 | 0.77531 |

# Supplementary Information Note 4 – Overlaid electron dispersive X-ray spectroscopy images

Supplementary Figure 3 presents the overview of the pellet cross section surface and overlaid EDX maps on Cs and I.

Supplementary Figure 3 – The overview of the pellet cross section surface together with the overlaid EDX I and Cs maps in two distinct locations (indicated by the white arrow marks) for samples a,b,c) Nd 0%, d,e,f) for sample Nd 15%, g,h,i) for sample Nd 30%, that highlight the differences between Cs and I distribution, indicating the occurrence of CsI speciation when Nd is introduced.