Supporting Information for

Electrical Performance of Cement Nanofiller Composites for Low-Grade Thermoelectric Energy Harvesting

Thakur Ramjiram Singh1, Subhasis Pradhan1*, Shiv Singh2*, Dheerendra Singh3

1Department of Civil Engineering, Birla Institute of Technology & Science Pilani, Pilani Campus, Rajasthan - 333 031, India.

2Council of Scientific and Industrial Research - Advanced Materials and Processes Research Institute, Bhopal, Madhya Pradesh - 462026, India

3Department of Electrical Engineering, Birla Institute of Technology and Science Pilani, Pilani Campus, Rajasthan- 333 031, India

Corresponding authors:

Subhasis Pradhan1*,  Subhasis.pradhan@pilani.bits-pilani.ac.in

Shiv Singh2*, sshiv.ampri@csir.res.in

The file includes:

Supplementary Tables S1-S4

Supplementary Figures S1-S9

Supplementary References

Supplementary Tables

Table S1. Physical properties, chemical compositions and mineral compositions of Ordinary Portland cement (P.O.42.5).

| Physical properties Value |  | Chemical compositions (%) |  | Mineral compositions of clinker (%) |  |
| --- | --- | --- | --- | --- | --- |
| Specific gravity | 3.14 | SiO2 | 12.94 | C3S | 59.26 |
| Fineness (m2/kg) | 240 | CaO | 68.78 | C3A | 8.02 |
| Normal consistency (%) | 33 | Al2O3 | 2.52 | C4AF | 14.27 |
| Initial setting time (min) | 85 | Fe2O3 | 5.99 | C2S | 17.14 |
| Finally setting time (min) | 240 | MgO | 3.71 | Others | 1.31 |
| Loss on ignition (%) | 1.80 | SO3 | 3.29 |  |  |
| Colour | grey | Others | 2.77 |  |  |

Table S2.  Physical and Chemical Properties of Super-grade Graphene

| Sr. No. | Physical property | value | Sr. No. | Physical property | value |
| --- | --- | --- | --- | --- | --- |
| 1. | Average thickness | 1.6nm | 11. | Average particle size | 70nm |
| 2. | Average dimension | 15nm | 12. | Lump grain size | 500μ-5nm |
| 3. | Graphitized carbon | 93% | 13. | Zeta potential | 19.1mv |
| 4. | Oxygen | 7% | 14. | Physical form | fluffy |
| 5. | Electrical conductivity | 5 S/cm | 15. | Layer number | 20% monolayer 20% bilayer 60% Tri-layer |
| 6. | Colour | black |  |  |  |
| 7. | No. of layers | 3 |  |  |  |
| 8. | Pore size | 50nm |  |  |  |
| 9. | Bulk density | 0.06g/ml |  |  |  |
| 10. | SSA | >700m2/g |  |  |  |

Table S3.  Physical and chemical properties of MWCNT

| Sr. No. | Physical property | value |
| --- | --- | --- |
| 1. | Average diameter | 20nm |
| 2. | Average length | 15μ |
| 3. | Colour | black |
| 4. | Bulk density | 0.16g/ml |
| 5. | SSA | 220m2/g |
| 6. | Physical form | Black powder |

Table S4.  BET Surface and pore characteristics of Candle soot and CNP

| Surface area & porosity analysis | Soot | CNP |
| --- | --- | --- |
| Average pore size summary | Average Pore Radius = 27 nm | Average pore Radius = 15 nm |
| BJH adsorption summary | Surface Area = 50.625 m²/g Pore Volume = 1.030 cc/g Pore Radius Dv(r) = 1.708 nm | Surface Area = 90.963 m²/g Pore Volume = 1.000 cc/g Pore Radius Dv(r) =15.009 nm |
| BJH desorption summary | Surface Area = 57.487 m²/g Pore Volume = 1.025 cc/g Pore Radius Dv(r) = 1.702 nm | Surface Area = 114.727 m²/g Pore Volume = 1.011 cc/g Pore Radius Dv(r) =16.080 nm |
| BET summary | Slope= 44.028 1/g Intercept = 2.936e-01 1/g Correlation coefficient, r = 0.999825 C constant=150.940 Surface Area = 78.573 m²/g | Slope = 26.251 1/g Intercept = 5.307e-02 1/g Correlation coefficient, r = 0.999830 C constant= 495.630 Surface Area =132.392 m²/g |
| Total Pore Volume summary | Total pore volume = 1.047e+00 cc/g for pores smaller than 170.2 nm (Radius) at P/Po = 0.99434 | Total pore volume = 1.025e+00 cc/g for pores smaller than 140.0 nm (Radius) at P/Po = 0.99311 |

Supplementary Figures

Figure S1. Filler concentration vs. Percolation threshold

Figure S2. Filler concentration vs. Electrical conductivity zones

Figure S3. Cement-conductive filler interaction

Figure S4. Four-point probe measurement

Figure S5. Semiconductor Parameter Analyser-4 Probe instrument

Figure S6. CNP (a-b) Incremental pore volume and area change, and (c-d) Cumulative Pore volume and area before and after treatment

Figure S7: Electron image, EDS, elemental mapping of cement-SGG(a-c), cement-CNP (d-f) and cement-MWCNT (g-i).

Figure S8: XRD of (a) CSGG, (b) CMWCNT, (c) CCNP, (d) SGG, (e) MWCNT, (f) CNP, and (g) Cement control mix.

Figure S9: Raman Spectrum of (a) CSGG, (b) CMWCNT, (c) CCNP, (d) SGG, (e) MWCNT, (f) CNP, and (g) Cement control mix.