Overcoming Efficiency and Thermal Quenching in Cr3+-Activated NIR Phosphors via Donor-Level Engineering​

Junyu Chen, Zixuan Gao, Miaocui Lu, Shufei Qin, Wangchuan Zou, Lige Qiao, Zuizhi Lu*, Yuzhen Zhang*.

Key Laboratory of Chemistry and Engineering of Forest Products, State Ethnic Affairs Commission, Guangxi Key Laboratory of Chemistry and Engineering of Forest Products, Guangxi Collaborative Innovation Center for Chemistry and Engineering of Forest Products, School of Chemistry and Chemical Engineering, Guangxi Minzu University, Nanning 530006, Guangxi, China.

Corresponding Author

*Email: luzuizhi@foxmail.com

Table S1 The various excited-state ZPL energies in the Tanabe-Sugano energy level diagram

| Spectra |  | Wavelength (nm) | wave number (cm-1) |
| --- | --- | --- | --- |
| PLE | 4A2→4T1 | 260 | 2 387 068 |
|  | 4A2→4T2 | 450 | 954 477 |
|  | 4A2→2E | 635 | 15 748 |
| PL | 4T2→4A2 | 792 | 1 305 717 |
| Zero phonon line | E(2Eg) ZPL | 635 | 15 748 |
|  | E(4T2g) ZPL | 668 | 14 970 |
| Stokes | S |  | 2686 |

Table S2 The calculated results of crystal field parameters

| Dq (cm-1) | B (cm-1) | Dq/B | C (cm-1) | C/B |
| --- | --- | --- | --- | --- |
| 1497 | 656.6 | 2.28 | 3766 | 5.74 |

Fig. S1. and S2. The O1s and C1s in XPS spectrum of CGGGO: 1.0 % Cr3+ phosphor.

Fig. S3. Density of States Diagram of CGGGO Cr3+

Fig. S4.Calculated indirect band gap of CGGGO.

Fig. s5. PL of CGGGO: x Cr3+ (x = 0.5-5.0 %) phosphors at 450nm

Fig. s5. PL and PLE of CGGGO: 1%Cr3+ phosphors at 450nm

Fig. s6. Gaussian fitting curves of emission spectrum of CGGGO: 1.0 % Cr3+ at 450nm.

Fig. s7. Rietveld refinement of CGGGO: 1.0 % Cr3+ 1% Tb3+

Fig. s8. PL of CGGGO: 1 Cr3+ x% Tb3+ (x = 0.5-5.0 %) phosphors at 450nm

Fig. s9. PL and PLE of CGGGO: 1%Cr3+ 1% Tb3+ phosphors at 450nm

Fig. s10. The TRES of CGGGO: 1%Cr3+ 1% Tb3+ phosphors