Supporting Information

Prismatic rod-like structure CoP for efficient hydrogen evolution reaction

Fan Yanga, Pengyu Zhan b, Zhanqing Liu a, Linlin Sun a, Yangyang Xub*

a College of Chemistry and Materials Science, Weinan Normal University, Chaoyang Street, Shaanxi 714099, China

b Research Institute of Textile and Clothing Industries, Zhongyuan University of Technology, Zhengzhou, Henan Province 450007, China

*Corresponding Author: xi314209@126.com

Figure S1 (a-c) SEM images and (d) EDS spectrum of CoP/NF.

| Element | Line Type | Weight % | Atomic % |
| --- | --- | --- | --- |
| C | K series | 6.97 | 22.64 |
| O | K series | 5.18 | 12.71 |
| P | K series | 10.81 | 13.63 |
| Co | K series | 77.04 | 51.02 |
| Total |  | 100.00 | 100.00 |

Table S1. EDS quantitative results acquired from elemental mapping analysis. wt% and at% denote weight percentage and atomic percentage, respectively.

Figure S2 Full spectrum of CoP/NF.

Figure S3 The cyclic voltammetry curves of (a) Co-MOF/NF, (b) Co3O4/NF, and (c) CoP/NF in the non-Faradaic potential range.