Table 2. Surface roughness values and two-way ANOVA for the tested materials.

| Material | Aging condition | Ra, µm mean ± SD | 95% CI | Median | IQR | Min–max |
| --- | --- | --- | --- | --- | --- | --- |
| THA | Baselinea | 0.06 ± 0.02 | 0.05–0.07 | 0.06 | 0.03 | 0.02–0.10 |
| THA | Thermocyclingb | 0.09 ± 0.02 | 0.08–0.10 | 0.09 | 0.03 | 0.05–0.13 |
| THA | Thermocycling + coffeec | 0.11 ± 0.03 | 0.095–0.125 | 0.11 | 0.04 | 0.05–0.17 |
| SRB | Baselinea | 0.08 ± 0.02 | 0.07–0.09 | 0.08 | 0.03 | 0.04–0.12 |
| SRB | Thermocyclingb | 0.12 ± 0.03 | 0.105–0.135 | 0.12 | 0.04 | 0.06–0.18 |
| SR B | Thermocycling + coffeec | 0.15 ± 0.03 | 0.135–0.165 | 0.15 | 0.04 | 0.09–0.21 |
| VTC | Baselinea | 0.10 ± 0.03 | 0.085–0.115 | 0.10 | 0.04 | 0.04–0.16 |
| VTC | Thermocyclingb | 0.15 ± 0.04 | 0.13–0.17 | 0.15 | 0.05 | 0.07–0.23 |
| VTC | Thermocycling + coffeec | 0.18 ± 0.04 | 0.16–0.20 | 0.18 | 0.05 | 0.10–0.26 |

Superscript letters indicate Tukey-adjusted main-effect comparisons only, not cell-wise material × aging comparison.

Different uppercase superscript letters indicated significant differences among materials within the same aging condition. Different lowercase superscript letters indicated significant differences among aging conditions within the same material.