Table 2. Surface roughness values and two-way ANOVA for the tested materials.
	Material
	Aging condition
	Ra, µm mean ± SD
	95% CI
	Median
	IQR
	Min–max

	THA
	Baselinea
	0.06 ± 0.02
	0.05–0.07
	0.06
	0.03
	0.02–0.10

	THA
	Thermocyclingb
	0.09 ± 0.02
	0.08–0.10
	0.09
	0.03
	0.05–0.13

	THA
	Thermocycling + coffeec
	0.11 ± 0.03
	0.095–0.125
	0.11
	0.04
	0.05–0.17

	SRB
	Baselinea
	0.08 ± 0.02
	0.07–0.09
	0.08
	0.03
	0.04–0.12

	SRB
	Thermocyclingb
	0.12 ± 0.03
	0.105–0.135
	0.12
	0.04
	0.06–0.18

	SR B 
	Thermocycling + coffeec
	0.15 ± 0.03
	0.135–0.165
	0.15
	0.04
	0.09–0.21

	VTC
	Baselinea
	0.10 ± 0.03
	0.085–0.115
	0.10
	0.04
	0.04–0.16

	VTC
	Thermocyclingb
	0.15 ± 0.04
	0.13–0.17
	0.15
	0.05
	0.07–0.23

	VTC
	Thermocycling + coffeec
	0.18 ± 0.04
	0.16–0.20
	0.18
	0.05
	0.10–0.26


Superscript letters indicate Tukey-adjusted main-effect comparisons only, not cell-wise material × aging comparison.
Different uppercase superscript letters indicated significant differences among materials within the same aging condition. Different lowercase superscript letters indicated significant differences among aging conditions within the same material.





