Table 1. Materials used in the study.
	Material Name
	Manufacturer
	Composition
	Post-curing protocol

	VarseoSmile TriniQ (VT)
	BEGO GmbH & Co KG, Bremen, Germany
	Ceramic-filled methacrylate based hybrid resin consisting of (meth)acrylates, ceramic fillers, initiators, additives, and pigments
	Otoflash, 2 × 2000 flashes

	SprintRay Ceramic Crown Resin (SR)
	SprintRay Inc., Los Angeles, CA, USA
	Ceramic-filled methacrylate based resin, oligomers, acrylic monomers, photoinitiators and >50 wt% inorganic filler. 
	ProCure 2, Ceramic Crown profile

	Tera Harz C&B TC-80DP (TH)
	Graphy Inc., Seoul, Republic of Korea
	Urethane acrylate/polyurethane-based photopolymer
	Tera Harz Cure, 30 min, 95% nitrogen








