Supplementary Information

Synthesis of 2-methylacrylamide/high-molecular-weight cellulose for removing anionic dyes from water by irradiation with gamma rays

Shuaifeng Zhang a, b, Jun Gu b, c, Baochao Fan b, c, Li Li a, b, d*, Bin Li b, c, d *

a School of Materials Science & Engineering, Jiangsu University, Zhenjiang, China

b Institute of Veterinary Medicine, Jiangsu Academy of Agricultural Sciences, Key Laboratory of Veterinary Biological Engineering and Technology Ministry of Agriculture; Jiangsu Key Laboratory for Food Quality and Safety-State Key Laboratory Cultivation Base of Ministry of Science and Technology, Nanjing 210014, China

c School of Food and Biological Engineering, Jiangsu University, Zhenjiang, China

d Jiangsu Coinnovation Center for Prevention and Control of Important Animal Infectious Diseases and Zoonoses, Yangzhou University, Yangzhou, Jiangsu 225000, China

*Corresponding Author:

Professor Li Li.

E-mail: muzishuiqudou@163.com. (L. Li)

Address: 50 Zhongling Stree, Nanjing 210014, China

Professor Bin Li.

E-mail: libinana@126.com (B. Li)

Fox: +86-25-8439 0082

Address: 50 Zhongling Street, Nanjing 210014, China

Supplementary Table 1. Parameters of the deconvoluted X-ray diffraction (XRD) patterns of the irradiated high-molecular-weight (HMW)-cellulose.

| Irradiated HMW-cellulose |  | Fit crystalline peaks |  |  |  | Fit amorphous peak | CrI |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Peak 1 | Peak 2 | Peak 3 | Peak 4 |  |  |
| 0 kGy | Center degree | 14.6˚ | 16.1˚ | 23.5˚ | 34.3˚ | 21.3˚ | 83.3% |
|  | Area | 116.47 | 43.91 | 1887.69 | 40.36 | 418.72 |  |
| 10 kGy | Center degree | 14.5˚ | 15.9˚ | 23.5˚ | 34.2˚ | 20.8˚ | 74.6% |
|  | Area | 81.42 | 17.24 | 1759.91 | 31.76 | 642.49 |  |
| 20 kGy | Center degree | 14.8˚ | 15.9˚ | 22.9˚ | 34.3˚ | 22.0˚ | 64.0% |
|  | Area | 32.58 | 78.36 | 979.04 | 16.69 | 621.30 |  |
| 30 kGy | Center degree | - | - | 23.5˚ | - | 21.4˚ | 58.8% |
|  | Area | - | - | 1745.35 | - | 1221.45 |  |
| 40 kGy | Center degree | - | - | 23.3˚ | - | 22.1˚ | 53.1% |
|  | Area | - | - | 1502.78 | - | 1329.36 |  |
| 50 kGy | Center degree | - | - | 23.1˚ | - | 21.8˚ | 42.5% |
|  | Area | - | - | 919.61 | - | 1244.58 |  |

Supplementary Table 2. Parameters of the deconvoluted high-resolution C1s core-level spectra of the cellulose based samples

|  | C-C/C-H | C-O | C=O |
| --- | --- | --- | --- |
| 40-kGy-irradiated HMW-cellulose | 284.8 eV 82.2 % | 286.4 eV 17.8 % |  |
| AC 1/5 | 285.0 eV 77.8 % | 286.3 eV 12.5 % | 287.1 eV 9.7 % |

Supplementary Table 3. Elemental analysis parameters and surface degree of substitution (SDS) vales of the cellulose based samples.

| Samples | C% | O% | N% | SDS |
| --- | --- | --- | --- | --- |
| 40-kGy-irradiated HMW-cellulose | 60.2 | 39.8 | 0.0 | 0.00 |
| AC 1/50 | 59.8 | 39.4 | 0.8 | 0.047 |
| AC 1/25 | 59.6 | 39.2 | 1.2 | 0.072 |
| AC 1/10 | 58.2 | 40.1 | 1.7 | 0.104 |
| AC 1/5 | 58.3 | 39.7 | 2.0 | 0.123 |