Supplementary Materials

Carboxylated magnetic polymer microspheres with tunable poly(acrylic acid) shells for charge-selective adsorption of cationic dyes

Linlin Du, Shangfang Zhao, Bing Niu*, Sisi Ma*

College of Textile Engineering, Henan University of Engineering, Zhengzhou 451191, China

Fig. S1 Dynamic light scattering size distributions of magnetic particles (MPs) and carboxylated magnetic polymer microspheres prepared with different polymer-shell contents: (a) MPs, (b) CMPs-1, (c) CMPs-2, (d) CMPs-3, (e) CMPs-4, and (f) CMPs-5.

Fig. S2 Zeta potential of CMPs-4 as a function of solution pH.

Fig. S3 Kinetic fitting for adsorption of methylene blue (MB) and methyl violet (MV) onto CMPs: (a) pseudo-first-order kinetic model and (b) intraparticle diffusion model.

Fig. S4 Isotherm fitting for adsorption of MB and MV onto CMPs: (a) Freundlich model and (b) Temkin model.

Fig. S5 SEM images of CMPs (a) before and (b) after five adsorption-desorption cycles.

Table S1. Comparison of the adsorption capacities of CMPs with those of reported biosorbents.

| Adsorbents | Dye types | Qmax (mg·g-1) | References |
| --- | --- | --- | --- |
| Magnetic chitosan-Fe3O4/activated carbon composite | MB | 11.02 | [1] |
| gum/Fe3O4 nano-bioadsorbent | MB | 85.7 | [2] |
| Fe3O4/Polypyrrole/Phytic Acid Magnetic Nanocomposite | MB | 153.84 | [3] |
| EDTA modified Fe3O4/sawdust carbon nanocomposites | MB | 227.3 | [4] |
| CMPs | MB | 322.58 | Present study |
| gum xanthan/Fe3O4 based nanocomposite hydrogel | MV | 642 | [5] |
| gum/Fe3O4 nano-bioadsorbent | MV | 113 | [2] |
| Clay/starch/Fe3O4 nanocomposite | MV | 29.67 | [6] |
| montmorillonite/graphene oxide/CoFe2O4 nanocomposite | MV | 97.26 | [7] |
| CMPs | MV | 653.59 | Present study |

References

[1] Tsauria Q D, Gareso P L, Abdullah B, et al. Magnetic chitosan-Fe3O4/activated carbon composite for efficient simultaneous removal of methylene blue and congo red from water[J]. Advanced Powder Technology, 2026, 37(7): 105315.

- Kumar A, Sur D, Algethami N, et al. Synthesis and characterization of gum/Fe3O4 nano-bioadsorbent for removing methylene blue and methyl violet in batch and continuous systems[J]. Journal of Sol-Gel Science and Technology, 2025, 116(2): 1188-1204.

- Mohanty N, Behera S, Patra B N. Fabrication of Fe3O4/polypyrrole/phytic acid magnetic nanocomposite for preferential adsorption of cationic dye: Adsorption properties, kinetics, and mechanism[J]. Industrial and Engineering Chemistry Research, 2025, 64 (4), 2274-2282.

- Kataria N, Garg V K. Application of EDTA modified Fe3O4/sawdust carbon nanocomposites to ameliorate methylene blue and brilliant green dye laden water[J]. Environmental research, 2019, 172: 43-54.

- Mittal H, Kumar V, Saruchi, et al. Adsorption of methyl violet from aqueous solution using gum xanthan/Fe3O4 based nanocomposite hydrogel[J]. International Journal of Biological Macromolecules, 2016, 89: 1-11.

- Ansari Mojarad A, Tamjidi S, Esmaeili H. Clay/starch/Fe3O4 nanocomposite as an efficient adsorbent for the removal of methyl violet dye from aqueous media[J]. International Journal of Environmental Analytical Chemistry, 2022, 102(19): 8159-8180.

- Foroutan R, Mohammadi R, Mousa Khanloo F, et al. Performance of montmorillonite/graphene oxide/CoFe2O4 as a magnetic and recyclable nanocomposite for cleaning methyl violet dye-laden wastewater[J]. Advanced Powder Technology, 2020, 31(9): 3993-4004.