Electronic Supplementary Material on

Journal of Inorganic and Organometallic Polymers and Materials

Modification of magnetic graphene oxide by an earth-friendly deep eutectic solvent to preconcentrate ultratrace amounts Pb(II) in oil seeds

Melika Hejazi Khah and Parastoo Jamshidi*

School of Chemistry, College of Science, University of Tehran, P.O. Box 14155–6455,Tehran, Iran

Corresponding author:

Parastoo Jamshidi*

E-mail: parastoo.jamshidi@ut.ac.ir

Tel: +98 21 61112481

Fax: +98 21 66405141

Author:

Melika Hejazi Khah

E-mail: Melika.hejazi.kh@ut.ac.ir

School of Chemistry, College of Science, University of Tehran, P.O. Box 14155–6455,Tehran, Iran

Characterization

Plot of identified phases of mGO is shown in Fig. S1. Magnetite Fe3O4 and carbon structure match with JCPDS cards No. 01-075-0449 and JCPDS cards No. 01-079-1715, respectively. No peaks of impurities are detected.

Fig. S1 XRD pattern of mGO

Analytical figure of merits

A series of Pb(II) ranging from (5.0 × 10-6 g L-1 to 23 × 10-5 g L-1 was preconcentrated under the optimum condition to find the calibration plot. UreaLiCl-mGO (1.0 × 10-2  g) was added to aqueous solutions of Pb(II) (50 mL) at the pH of 5 ± 0.5. Afterwards the samples were shaken for 15 minutes and then an external magnet removed UreaLiCl-mGO. The elution step was done by HNO3 (0.5 mL, 2 mol L-1) during 4 minutes in an ultrasonic bath. The eluent was separated and Pb(II) was determined by FAAS. The plot was linear from 5.0 × 10-6 to 23 × 10-5 g L−1 for Pb(II) (Fig. S2) The calibration equation is A = 0.001C + 0.0158 with a correlation coefﬁcient of 0.99. In this equation, A is the atomic absorbance of Pb(II) and C is its concentration in the sample solution (μg L−1).

Fig. S2 The calibration plot for Pb(II) preconcentrated by UreaLiCl-mGO

LOD is 99 × 10-8 g L-1 and is expressed as 3Sb/m (Sb is blank standard deviation and m is slope of the calibration plot). LOQ is 33 × 10-7 g L-1 and is defined as 3.33 LOD. The precision of the method based on relative standard deviation (RSD%) was determined by performing five experiments from solutions containing Pb(II) (50 mL, 5.0 × 10-5 g L-1). It was found 1.3%. PF (the ratio between volumes of analyte and volume of eluent) is 100.

Adsorption isotherm

Adsorption isotherm studies the nature of analyte adsorption onto adsorbent, basing on the amounts of analyte adsorbed per unit mass of adsorbent. According to Fig. S3a, by increasing the initial concentration of Pb(II), adsorption capacity (qe) of UreaLiCl-mGO increased. qe is achieved according to following equation.

Eq. S1

C0 is initial concentration of analyte, Ce is equilibrium concentration of analyte, V is volume of analyte and W is amount of adsorbent. Four different models including Langmuir, Freundlich, Temkin and Dubinin-Radushkevich were applied to investigate the system.

The Langmuir model is valid for analyte adsorption onto solid adsorbents in aqueous samples. According to this model, the analyte is distributed between the solid and liquid phase homogeneously. The adsorbent has identical and homogenous sites with equivalent energy so one layer of analyte covers the outer surface of the adsorbent. Moreover, by increasing distance, the strength of intermolecular attractive forces falls off rapidly. Langmuir equation is written as following:

(Eq. S2)

In this equation, q0 and KL are monolayer coverage capacity and Langmuir isotherm constant, respectively. Fig. S3b shows the Langmuir plot.

Freundlich model shows reversible multilayer adsorption. According to this model, the adsorbent has heterogeneous surfaces and the ﬁnishing sites has less energy than other active sites. Equation S3 shows the Freundlich equation in linear form.

(Eq. S3)

Kf and n are Freundlich isotherm constant and intensity of adsorption, respectively. Freundlich model is plotted in Fig. S3c.

Temkin model is more valid for hydrogen adsorption onto platinum electrodes in acidic samples. However, by considering some assumptions, it is applicable for heavy metals adsorption using biosorbent. These assumptions are related to complexity of liquid systems such as random organization of adsorbed molecules on packed structure of sorbent without identical orientation, micelles formation from adsorbed molecules and environment factors. According to this model, the heat of sorption follows a linear function versus temperature. Temkin equation is reported in equation S4:

(Eq. S4)

AT and B are Temkin isotherm equilibrium binding constant and the heat of sorption, respectively. The Temkin plot is demonstrated in Fig. S3d.

Dubinin–Radushkevich model depends on temperature and explains the estimation of apparent free energy and the characteristics of adsorption. Equation S5 shows the Dubinin–Radushkevich equation:

(Eq. S5)

K, qm and Ɛ are the Dubinin–Radushkevich isotherm constant related to the adsorption energy, theoretical isotherm saturation capacity and the Polanyi potential calculated, respectively. Dubinin–Radushkevich graph is plotted in Fig. S3e.

Among the four mentioned models, Freundlich is fitted with adsorption of Pb(II) onto UreaLiCl-mGO. Isotherm parameters are summarized in Table S1.

Fig. S3 a Effect of initial concentration of Pb(II) on adsorption capacity of UreaLiCl-mGO, b the Langmuir model, c the Freundlich model, d the Temkin model and e the Dubinin - Radushkevich model for the adsorption of Pb(II) on to UreaLiCl-mGO

Table S1 Adsorption isotherms for Pb(II) adsorption onto UreaLiCl-mGO

| Model | Parameters | Value | R2 |
| --- | --- | --- | --- |
| Langmuir | q0 (mg g-1) KL (L mg-1) | 67.56 0.95 | 0.91 |
| Freundlich | nF (mg-1) KF ( mg1-1n L1n g-1) | 3.04 27.94 | 0.99 |
| Temkin | AT (L mg-1) BT (J mol-1) | 5.60 143.64 | 0.94 |
| Dubinin-Radushkevich | K (mol2 kJ-2) qM (mg g-1) | 1×10-7 62.80 | 0.68 |

Adsorption kinetic

Adsorption kinetic model describes the relationship between amounts of ions bound with sorbent and time. Pseudo-First order and Pseudo-Second-Order models are common models, which are valid for adsorption of Pb(II) onto UreaLiCl-mGO.

Pseudo-First-Order Model – a Lagergren’s rate equation - is one of the most common models for adsorption of heavy metals onto solid adsorbents. This Model describes the adsorption in solid–liquid systems based on the sorption capacity of solids and assumes that one ion is adsorbed onto one unoccupied adsorption site. The linear form of pseudo-first-order equation is written in equation S6:

(Eq. S6)

qt (mg g−1) and k1 (min−1) are the amount of adsorbed Pb(II) onto UreaLiCl-mGO at several times and the pseudo-first order kinetic, respectively. Pseudo-First-Order model is plotted in Fig. S4a.

Pseudo-Second-Order Model shows the chemisorption of analyte onto surface of solid adsorbent, because of sharing or transferring electron(s) between the analyte and the adsorbent. Equation S7 provides the linear equation of this model.

(Eq. S7)

Where qt (mg g−1) and k2 (g mg−1 min−1) are the amount of adsorbed analyte onto the surface of solid adsorbent at various times and the rate constant of the Pseudo-Second Order kinetic, respectively. Fig. S4b shows the plots of Pseudo second order kinetic models.

According to Table S2, the pseudo-first order model satisfies the kinetic model.

Fig. 4 a Pseudo first order kinetic and b Pseudo second order kinetic for the adsorption of Pb(II) onto UreaLiCl-mGO

Table S2 Comparison of pseudo first- and pseudo second-order kinetic parameters for Pb(II) adsorption onto UreaLiCl-mGO

| Model | Parameters | Values | R2 |
| --- | --- | --- | --- |
| Pseudo first order | k1 (min-1) qe (mg g-1) | 0.02 8.5 | 0.99 |
| Pseudo second order | k2 (g mg-1 min-1) qe (mg g-1) | 0.04 196 | 0.97 |

Adsorption thermodynamic

The thermodynamic experiments were calculated to study the influence of temperature on the adsorption process. By increasing temperature from 0 °C to 90 °C, adsorption capacity of UreaLiCl-mGO increased (Fig. S5a).

The ΔH◦ and ΔS◦ values obtained from the slope and intercept of Van’t Hoff plots of LnKC versus 1T, respectively (Fig. S5b). Equation S8 and S9 are applicable to calculate the parameters.

(Eq. S8)

(Eq. S9)

Free energy (ΔG◦), enthalpy (ΔH◦) and entropy (ΔS◦) are summarized in Table S3. The positive value of ΔH showed endothermic adsorption of Pb(II) onto UreaLiCl-mGO. ΔS is positive, due to randomness affinity of adsorbents toward Pb(II) and agitation of water molecules during the process. Negative values of ΔG are related to spontaneous adsorption and physisorption nature of the system. In addition, ΔG value between 0 and -20 KJ mol−1 provided a physisorption process; otherwise, -80 to -400 KJ mol−1 indicated chemisorption process.

Fig. 5 a Temperature effect on the adsorption of Pb(II) on to UreaLiCl-mGO and b Thermodynamic parameters, enthalpy and entropy for the adsorption of Pb(II) onto UreaLiCl-mGO.

Table S3 Thermodynamic parameters for the Pb(II) adsorption onto UreaLiCl-mGO

| T (K) | qe | lnKC | ΔH◦ (J mol−1) | ΔS◦ (J K−1 mol−1) | ΔG◦ (J mol−1) |
| --- | --- | --- | --- | --- | --- |
| 273 | 13 | -0.72 | 22 × 103 | 83 × 103 | -1.6 × 103 |
| 283 | 41 | 0.65 |  |  | -1.4 × 103 |
| 298 | 63 | 1.2 |  |  | -2.9 × 103 |
| 333 | 85 | 1.8 |  |  | -4.3 × 103 |
| 363 | 123 | 3.1 |  |  | -7.1 × 103 |