Organic-Inorganic Hyphenated Beads Supporting Co-adsorption of Congo Red and Crystal Violet dyes: Studies on Composition Flip-Flop and Crosslinking Effects

Arundhati Chakraborty1, Sonai Dutta1, Reetika Sarkar1, Debasis Brahma1, Anirban Mukherjee2, Amit Sen3, Prasenjit Ghosh3, Rabindra Mukhopadhyay3, Suman Acharya4, Debdipta Basu4, Arjun Maity5 and Abhijit Bandyopadhyay1,5,*

1Department of Polymer Science & Technology, University of Calcutta 92, A.P.C. Road Kolkata - 700009, India

2Department of Microbiology, Gurudas College, University of Calcutta, 1/1, Suren Sarkar Road, Jewish Graveyard, Phool-Bagan, Narkeldanga, Kolkata, 700054 India

3Hari Shankar Singhania Elastomer and Tyre Research Institute, Hebbal Industrial Estate, Mysuru, India

4Indian Rubber Materials Research Institute, East Centre, Rubber Park, PO- Dhulagarh, P.S-Sankrail, Howrah, West Bengal 711302, India

5College of Science, Engineering and Technology (CSET), University of South Africa, Florida Park, Roodepoort, 1709, South Africa

*Corresponding Author: Abhijit Bandyopadhyay, E-mail: abpoly@caluniv.ac.in

Supporting Information:

Figure 1: UV plot of supernatant after CR and CV dyes removal from their binary mixture by AC-1 beads at pH=7

Figure 2: UV plot of supernatant after CR and CV dyes removal from their binary mixture by AC-1 beads at pH=1

Figure 3: UV plot of supernatant after CR and CV dyes removal from their binary mixture by AC-20 beads at pH=1

Table ST1: Correlation coefficients and comparison of experimental and calculated qe values of for CR and CV dye:

| Kinetics model | Pseudo first order | Pseudo-second order | Second order | Intraparticle Diffusion | qe(experimental) (mg/g) | qe(calculated) (mg/g) |
| --- | --- | --- | --- | --- | --- | --- |
| R2 (CR dye) | 0.889 | 0.997 | 0.862 | 0.970 | 1.926 | 1.954 |
| R2 (CV dye) | 0.957 | 0.996 | 0.808 | 0.951 | 1.868 | 1.865 |

Figure 4: Linear kinetic models (a) pseudo first order, (b) second order, (c) pseudo second order and (d) intraparticle diffusion models for CR dye

Figure 5: Linear kinetic models (a) pseudo first order, (b) second order, (c) pseudo second order and (d) intraparticle diffusion models for CV dye

Figure 6: EDX diffractograms of AC-20 beads (i) before and (ii) after adsorption of CR and CV from their binary mixture