Supporting information

Construction and Properties of Ag-I Polymeric clusters attach with Nitrogen Heterocyclic Transition Metal moiety

Min Liua, Yu Xina, Yong Heng Xinga*, Feng Ying Baia*, Zhan Shib

aCollege of Chemistry and Chemical Engineering, Liaoning Normal University, Huanghe Road 850#, Dalian 116029, P. R. China

bState Key Laboratory of Inorganic Synthesis and Preparative Chemistry, College of Chemistry, Jilin University, Changchun 130012, P.R. China

Supplementary Index

Materials and methods	2

X-ray crystallographic determination	2

Preparations of 1 and 2	3

Standard curves of PNP solution	7

IR spectra	8

UV-vis spectra	9

PXRD pattern	10

TG curves	11

# Materials and methods

All starting materials were of reagent grade quality and were obtained from commercial sources without further purification.  The powder X-ray diffraction patterns (PXRD) of 1 and 2 were obtained on Advance-D8 equipped with Cu-Kα radiation, and the range was 5° <2θ <60°, with a step size of 0.02° (2θ) and a count time of 2 s per step at room temperature.  All IR measurements were obtained using a Bruker AXS TENSOR-27 FT-IR spectrometer with pressed KBr pellets in the range of 400–4000 cm-1 at room temperature.  UV-vis-NIR spectra were recorded on a JASCO V-570 UV/vis/NIR microspectrophotometer (200-2500 nm).  Liquid UV-visible absorption spectroscopy was performed on SPECORD 250/PLUS.  The maximum absorption wavelength of the PNP solution was measured on spectrophotometer UV-1000.  Thermogravimetric analysis (TG) was performed on a PerkinElmer Diamond TG/DTA under N2 atmosphere from 30 °C to 800 °C with a heating rate of 10 °C/min.

# X-ray crystallographic determination

Single crystals of 1 and 2 were mounted on glass fibers for X-ray measurement.  Reflection data was collected at room temperature on a Bruker AXS SMART APEX II CCD diffractometer with graphite monochromatized Mo-Kα radiation (λ = 0.71073 Å).  All the measured independent reflections (I > 2σ (I)) were used in the structural analyses, and semi-empirical absorption corrections were applied using the SADABS program[1].  All calculations were performed in OLEX2 platform[2,3]. The crystal was kept at 296 K during data collection.  SQUEEZE the diffraction peaks of the disordered guest molecules of 1 and 2 using PLATON software.  The results show that there are 138 electrons in each structural unit of 2.  According to the calculation result of SQUEEZE, three DMF molecules and two H2O molecules was directly added to the final molecular formula of the compound 2, and it was verified by elemental analysis and thermogravimetric analysis.  The crystal was measured using a single axis diffractometer, we made various attempt to grow crystals of better quality without success.  The crystal showed poor diffraction data with reflections of moderate intensity as showed the Rint.  So, the compound 2 has an A level alert that is diffrn measured fraction theta full value low 0.761. The crystallographic data for compounds 1 and 2 were listed in Table S1.  The major bond lengths of the compounds were listed in Table S2.1 and Table S2.2.

# Preparations of 1 and 2

Preparation of AgI2- solution: Weigh AgNO3 (0.339 g, 0.002 mol) and KI (0.664 g, 0.004 mol) in 50mL beaker, respectively put 10 mL DMF to dissolve them completely, and add the AgNO3 solution dropwise to the KI solution, and the resulting precipitate just completely dissolved.

The synthesis methods of 1 and 2 are similar, and 1 was mainly introduced.  Dissolve Co(NO3)2·6H2O (0.0146 g, 0.05 mmol) in 2 mL DMF solution, add 5 mL AgI2- solution to it, stir for 10 min, and then add 1,10′-phenanthroline ( 0.0198 g, 0.1 mmol) of 2 mL DMF solution, adjusted to pH=6 with HI and DMF solution, stirred for about 30 min, an orange transparent solution was obtained, which was volatilized at room temperature for ten days to obtain orange massive crystals.

{[Co(1,10′-phen)3]2‧[Ag8I12]} (1) Yield: 0.1218g; 68% (calculated based on Co (II)).  Elemental analysis C72H48N12I12Ag8Co measured value (%): C, 24.36; H, 1.31; N, 4, 70; theoretical value (%): C, 24.12; H, 1.35; N, 4.69.  Infrared spectrum (KBr, cm-1): 3446, 3137, 1673, 1520, 1421, 1149, 1095, 726.

{[Co(2,2′-bipy)3]‧[Ag10I11]‧(OH)‧3DMF‧2H2O} (2) Yield: 0.089g; 59% (calculated based on Co (II)).  Elemental analysis C30H25N6OI11Ag10Co measured value (%): C, 14.35; H, 1.08; N, 3.81; theoretical value (%): C, 14.31; H, 1.11; N, 3.85. Infrared spectrum (KBr, cm-1): 3426, 3129, 1663, 1601, 1412, 1167, 1089, 760.

Table S1  Crystallographic data for 1 and 2*

| Compounds | 1 | 2 |
| --- | --- | --- |
| Formula | C72H48N12I12Ag8Co | C30H25N6OI11Ag10Co |
| M (g·mol-1) | 3584.84 | 3019.09 |
| Crystal system | Monoclinic | Monoclinic |
| Space group | P21/c | C2/c |
| a (Å) | 29.2509(11) | 12.402(8) |
| b (Å) | 17.6371(6) | 32.754(19) |
| c (Å) | 24.6865(9) | 14.532(9) |
| α (°) | 90 | 90 |
| β (°) | 111.9820(10) | 106.895(11) |
| γ (°) | 90 | 90 |
| V (Å3) | 11809.9(7) | 5648(6) |
| Z | 4 | 4 |
| Dc (g·cm-3) | 2.016 | 3.550 |
| F(000) | 6520.0 | 5340.0 |
| Μ(Mo Kα) (mm-1) | 4.740 | 9.713 |
| 2θ (°) | 1.502-56.558 | 3.65-49.986 |
| Reflections collected | 75291 | 10537 |
| Independent reflections(I>2σ(I)) | 28864 | 3794 |
| Parameters | 955 | 242 |
| ∆(ρ)(e Å-3) | 1.96 and -1.70 | 0.77 and -0.90 |
| Goodness of fit | 0.867 | 0.936 |
| Ra | 0.0446(0.0847)b | 0.0758(0.1621)b |
| wR2a | 0.1100(0.1208)b | 0.1666(0.2180)b |

*aR=∑│FO-FC│/∑│FO, wR2={∑[w(FO2-FC2)2]/∑[w(FO2)2]}1/2; [FO>4σ(FO)].  bBased on all data.

Table S2.1  Major bond lengths for 1 (Å)*

| 1 |  |  |  |
| --- | --- | --- | --- |
| Co(1)-N(1) | 2.138(4) | Co(1)-N(4) | 2.146(4) |
| Co(1)-N(2) | 2.129(4) | Co(1)-N(5) | 2.122(4) |
| Co(1)-N(3) | 2.123(4) | Co(1)-N(6) | 2.155(4) |
| Co(2)-N(7) | 2.153(4) | Co(2)-N(10) | 2.114(4) |
| Co(2)-N(8) | 2.124(4) | Co(2)-N(11) | 2.125(4) |
| Co(2)-N(9) | 2.148(4) | Co(2)-N(12) | 2.125(4) |
| I(3)-Ag(4) | 2.8954(8) | I(3)-Ag(2) | 3.2524(7) |
| I(3)-Ag(1) | 2.9046(8) | I(9)-Ag(8) | 2.8490(7) |
| I(3)-Ag(3) | 2.9860(8) | I(9)-Ag(7) | 2.292(7) |
| I(11)-Ag(6) | 2.8368(7) | I(11)-Ag(7) | 2.8802(7) |
| I(11)-Ag(8) | 3.0781(8) | I(5)-Ag(6) | 2.8990(7) |
| I(5)-Ag(4) | 2.8277(7) | I(5)-Ag(3) | 2.9920(7) |
| I(4)-Ag(4) | 2.8597(7) | I(4)-Ag(5) | 2.9243(7) |
| I(4)-Ag(2) | 2.9418(9) | I(6)-Ag(6) | 2.9991(8) |
| I(6)-Ag(4) | 2.8912(7) | I(6)-Ag(7) | 3.0389(8) |
| I(6)-Ag(5) | 2.9181(7) | I(8)-Ag(5) | 2.8122(7) |
| I(8)-Ag(1) | 2.7099(7) | I(2)-Ag(1) | 2.8446(8) |
| I(2)-Ag(2) | 2.8048(8) | I(10)-Ag(6) | 2.8007(7) |
| I(10)-Ag(8) | 2.8643(8) | I(7)-Ag(7) | 2.8237(8) |
| I(7)-Ag(5) | 2.7883(8) | I(1)-Ag(3) | 2.8389(8) |
| I(12)-Ag(8) | 2.8598(8) | I(12)-Ag(3)#1 | 2.7922(8) |

*Symmetry codes: 1: #1 x, 1.5-y, 0.5+z

Table S2.2  Major bond lengths for 2 (Å)*

| 2 |  |  |  |
| --- | --- | --- | --- |
| Co(1)-N(1) | 1.914(9) | I(4)- Ag(6) | 2.981(4) |
| Co(1)-N(2) | 1.976(11) | I(5)-Ag(6) | 2.783(5) |
| Co(1)-N(3) | 1.912(8) | I(1)-Ag(2) | 2.736(3) |
| I(4)-Ag(5) | 3.057(4) | I(4)-Ag(2) | 2.784(4) |
| I(5)-Ag(5) | 3.024(5) | I(3)-Ag(3) | 2.740(5) |
| I(5)-Ag(5)#1 | 2.886(5) | I(2)-Ag(3) | 2.996(6) |
| I(6)-Ag(5)#1 | 2.794(5) | I(1)-Ag(1) | 2.783(5) |
| I(6)-Ag(5) | 2.907(5) | I(6)-Ag(4) | 2.922(6) |
| I(3)-Ag(5) | 2.934(5) | I(2)-Ag(4) | 2.838(6) |
| I(2)-Ag(5) | 3.212(6) |  |  |
| I(3)-Ag(2) | 2.776(5) |  |  |
| I(4)-Ag(3) | 2.847(5) |  |  |
| I(5)-Ag(3) | 2.911(5) |  |  |
| I(6)-Ag(3) | 2.927(5) |  |  |
| I(2)-Ag(1)#2 | 2.761(6) |  |  |
| I(2)-Ag(1) | 2.461(6) |  |  |

*Symmetry codes: 2: #1 1-x, y, 0.5-z; #2 2-x, y, 0.5-z

# Standard curves of PNP solution

Figure S1  Standard curves of PNP solution

IR spectra:

Figure S 2  IR spectrum: (a) 1, 10′-phen; (b) 2, 2ʹ-bipy; (c) 1; (d) 2

Table S3  IR spectra (cm-1) of 1, 10′-phen, 2, 2ʹ-bipy, 1 and 2

|  | 1, 10′-phen | 2, 2ʹ-bipy | 1 | 2 |
| --- | --- | --- | --- | --- |
| νAr-H | 3064 | 3057 | 3137 | 3129 |
| νC=N | 1654 | 1665 | 1673 | 1663 |
| νC=C | 1510, 1432 | 1593, 1456 | 1520, 1421 | 1601, 1412 |
| νC-C | 1149 | 1087 | 1149 | 1167 |
| νC-N | 1087 | 1050 | 1095 | 1089 |
| δAr-H | 761 | 761 | 726 | 760 |

UV-vis spectra

Fig. S3.  UV spectrum: (a) 1, 10′-phen; (b) 2, 2ʹ-bipy; (c) 1; (d) 2

Table S4  UV spectrum (nm) of 1, 10′-phen, 2, 2ʹ-bipy, 1 and 2

|  | LLCT |  | LMCT | MMCT |
| --- | --- | --- | --- | --- |
|  | π-π* | n-π* |  |  |
| 1, 10′-phen | 256 | 325 |  |  |
| 2, 2ʹ-bipy | 264 | 316 |  |  |
| 1 | 220 | 261 | 376 |  |
| 2 | 218 | 321 | 411 |  |

PXRD pattern

Figure S4  The PXRD spectrum: (a) 1 ;(b) 2

Figure S5  The crystallinity rate: (a) 1; (b) 2

TG curves

Figure S6  Thermal analysis: (a) 1（b） 2

Table S5  TG analysis of 1 and 2

| Compound |  | The first stage of weightlessness | The second stage of weightlessness | The third stage of weightlessness | Residue |
| --- | --- | --- | --- | --- | --- |
| 1 | Temperature (°C) | 30-560 | 560-800 |  | Ag2O CoO |
|  | Weightlessness designation | Six 1, 10′-phen | Skeleton collapse |  |  |
|  | Actual weightlessness (%) | 29.6 | 8.6 |  |  |
|  | Theoretical weight loss rate (%) | 30.1 |  |  |  |
| 2 | Temperature (°C) | 30-150 | 150-530 | 530-800 | Ag2O CoO |
|  | Weightlessness designation | Two H2O, and one OH- | Three DMF, and three 2, 2ʹ-bipy | Skeleton collapse |  |
|  | Actual weightlessness (%) | 1.7 | 16.9 | 6.0 |  |
|  | Theoretical weight loss rate (%) | 1.6 | 16.0 |  |  |

Table S6  the coordination environment of metal Ag of 1 and 2*

| 1 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Center metal | Coordination environment | Ligand | Center metal | Coordination environment | Ligand |
| Ag1 | Three coordination | I2 I3 I8 | Ag5 | Four coordination | I4 I6 I7 I8 |
| Ag2 | Three coordination | I1 I2 I4 | Ag6 | Four coordination | I5 I6 I10 I11 |
| Ag3 | Four coordination | I1 I3 I5 I12 | Ag7 | Four coordination | I6 I7 I9 I11 |
| Ag4 | Four coordination | I3 I4 I5 I6 | Ag8 | Four coordination | I9 I10 I11 I12 |
| 2 |  |  |  |  |  |
| Center metal | Coordination environment | Ligand | Center metal | Coordination environment | Ligand |
| Ag1 | Four coordination | I1 I1#1 I2 I2#1 | Ag4 | Two coordination | I4 I6 |
| Ag2 | Three coordination | I2 I3 I4 | Ag5 | Seven coordination | I1 I1#1 I2 I3 I5 I6 I6#1 |
| Ag3 | Three coordination | I4 I5 I5#1 | Ag6 | Five coordination | I1 I2 I3 I5 I6 |

*Symmetry codes: 2: #1 1-x, y, 0.5-z

References

[1]. SMART and SAINT (software packages); Siemens Analytical X-ray Instruments, Inc.: Madison, WI, 1996.

[2]. O.V. Dolomanov，L.J. Bourhis，R.J. Gildea，J. Howard，H. Puschmann, Journal of Applied Crystallography, 2009, 42, 339-341.

[3]. G.M. Sheldrick, Acta Crystallographica, 2015, 71, 3-8.