Table 1. The anisotropic hyperelastic material models and their classifications.

| Material model | Strain energy density function | Classification |
| --- | --- | --- |
| Fung model [17] | W=c2eQ-1 Q=b1Eθθ2+b2EZZ2+b3ERR2+2b4EθθEZZ+2b5EZZERR+2b6ERREθθ | Polynomial implementation of the Green-Lagrange tensor approach |
| Choi-Vito model [18] | W=b0expb1E112+expb2E222+exp2b3E11E22-3 | Exponential implementation of the Green-Lagrange tensor approach |
| Holzapfel (2000) [19] | W=c12c2expc2I4-12-1 | Exponential implementation of the strain invariant approach |
| Holzapfel (2005) [20] | W=c12c2expc21-κI1-32+κI4-12-1 | Exponential implementation of the strain invariant approach |
| Four-fiber family model [21, 22] | W=c2I1-3+i=14c1i4c2iexpc2iI4i-12-1 | Combination of polynomial and exponential implementation of the strain invariant approach |
| Polynomial anisotropy [23] | W=i=13aiI1-3i+j=13bjI2-3j+k=26ckI4-1k+m=26emI6-1m | Polynomial implementation of the strain invariant approach |

Table 2. Materials parameters (c, b1, b2, b3, b4, b5, b6 and R2) of average material parameters based on Fung hyperelastic model for the LV, RV and STW subjected to biaxial testing,

|  | c | b1 | b2 | b3 | b4 | b5 | b6 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LV | 5.60±1.68 | 2.70±0.44 | 1.81±0.46 | 1.07±0.20 | 0.56±0.20 | 0.34±0.12 | 0.56±0.21 | 0.75±0.08 |
| STW | 7.32±2.25 | 3.17±0.66 | 1.83±0.23 | 1.12±0.29 | 0.42±0.17 | 0.26±0.16 | 0.67±0.16 | 0.75±0.06 |
| RV | 2.95±1.33 | 2.31±0.64 | 4.24±0.78 | 0.53±0.42 | 0.73±0.12 | 0.49±0.04 | 0.35±0.10 | 0.82±0.08 |

Table 3. Materials parameters (c, b1, b2, b3 and R2) of average material parameters based on Choi-Vito hyperelastic model for the LV, RV and STW subjected to biaxial testing,

|  | c | b1 | b2 | b3 | R2 |
| --- | --- | --- | --- | --- | --- |
| LV | 3.17±0.72 | 5.96±0.03 | 3.97±0.28 | 1.95±0.28 | 0.81±0.09 |
| STW | 4.40±1.01 | 5.95±0.04 | 3.93±0.31 | 1.86±0.28 | 0.86±0.09 |
| RV | 3.84±1.21 | 6.38±1.10 | 4.04±0.04 | 2.43±0.49 | 0.85±0.09 |

Table 4. Materials parameters (a1, a2, a3, b1, b2, b3 , c2, c3, c5, c6, φ and R2) of average material parameters of LV, RV and STW based on Polynomial (Anisotropic) hyperelastic model for the subjected to biaxial testing.

|  | a1 | a2 | a3 | b1 | b2 | b3 | c2 | c3 | c4 | c5 | c6 | φ | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LV | 4.49±1.13 | 1.61±0.56 | 0.27±0.11 | 13.38±2.43 | 13.38±2.43 | 13.38±2.43 | -0.62±0.79 | 0.33±0.12 | 0.11±0.05 | 0.04±0.02 | 0.02±0.02 | 0.18±0.17 | 0.96±0.01 |
| STW | 5.46±1.49 | 1.93±0.60 | 0.31±0.12 | 11.39±2.15 | 11.39±2.15 | 11.39±2.15 | 0.02±0.91 | 0.37±0.10 | 0.12±0.04 | 0.04±0.02 | 0.01±0.01 | 0.18±0.12 | 0.96±0.02 |
| RV | 4.31±1.74 | 3.14±0.82 | 0.87±0.25 | 15.19±3.66 | 15.19±3.66 | 15.19±3.66 | -3.06±1.02 | 0.38±0.34 | 0.27±0.10 | 0.15±0.05 | 0.09±0.03 | 0.12±0.31 | 0.89±0.09 |

Table 5. Materials parameters (μ, k1, k2, φ, and R2) of average material parameters of LV, STW and RV based on Holzapfel (2000) hyperelastic model for the subjected to biaxial testing.

|  | μ | k1 | k2 | φ | R2 |
| --- | --- | --- | --- | --- | --- |
| LV | 9.34±3.59 | 1.54±0.36 | 1.16±0.08 | 0.69±0.77 | 0.93±0.02 |
| STW | 14.17±3.46 | 1.76±0.31 | 1.22±0.11 | -2.18±9.06 | 0.92±0.01 |
| RV | 4.36±3.44 | 2.42±0.63 | 1.35±0.11 | 1.47±0.84 | 0.78±0.11 |

Table 6. Materials parameters (μ, k1, k2, φ, ρ, and R2) of average material parameters of LV, STW and RV based on Holzapfel (2005) hyperelastic model for the subjected to biaxial testing.

|  | μ | k1 | k2 | φ | ρ | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| LV | 4.90±1.30 | 1.07±0.10 | 0.91±0.05 | 0.63±1.09 | 0.52±0.11 | 0.93±0.02 |
| STW | 7.26±1.35 | 1.43±0.26 | 0.97±0.03 | 0.28±0.53 | 0.60±0.18 | 0.93±0.01 |
| RV | 2.81±2.15 | 2.02±0.48 | 1.07±0.08 | 1.40±0.71 | 0.67±0.15 | 0.79±0.10 |

Table 7. Materials parameters (c, c11, c21, , c21, c12, c22, c134, c234, φ0, and R2) of 14 specimens Left Ventricle (LV) fitting on Four-Fiber Family hyperelastic model for the subjected to biaxial testing, including the average materials parameters.

|  | c | c11 | c21 | c12 | c22 | c134 | c234 | φ0 | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| LV | 9.64±3.33 | 2.09±1.54 | 1.49±1.17 | 1.98±0.80 | 1.57±0.81 | 0.71±0.12 | 1.40±0.23 | 0.98±0.35 | 0.93±0.02 |
| STW | 14.56±3.04 | 1.29±1.41 | 3.13±2.40 | 3.78±1.74 | 1.36±0.35 | 0.52±0.17 | 1.82±0.33 | 0.75±0.25 | 0.92±0.02 |
| RV | 4.19±3.63 | 7.86±2.81 | 1.12±0.14 | 0.58±0.52 | 5.86±6.66 | 0.23±0.31 | 8.10±8.78 | 0.58±0.80 | 0.82±0.09 |