Supporting Information for:

Ambient polyol-enabled self-densification of wood into transparent, high-strength and biodegradable bioplastics

Hongqing He 1,2, Houjuan Qi 1,2*, Runze Hu 1,2, Dawei Zhao3*,

Haipeng Yu 1,2*, Zhanhua Huang 1,2*

1 State Key Laboratory of Woody Oil Resources Utilization, Northeast Forestry University, Harbin, 150040, China

2 Key Laboratory of Bio-based Material Science and Technology, Ministry of Education, College of Material Science and Engineering, Northeast Forestry University, Harbin, 150040, China

3 Key Laboratory on Resources Chemicals and Materials of Ministry of Education, Shenyang University of Chemical Technology, Shenyang 110142, China

* Corresponding to: 15006383472@163.com; daweizhao@syuct.edu.cn; yuhaipeng20000@nefu.edu.cn; huangzh1975@163.com or nefuhzh@nefu.edu.cn

This Word file includes:

- Supplementary Methods                   (Pages 2-5)

- Supplementary Figures (Figs.S1 to S 27)      (Pages 6-18)

- Supplementary Tables (Tables.S1 to S8)      (Pages 19-28)

- Supplementary videos (video 1 to 4)         (Page 29)

All-atom molecular dynamics simulations

Cellulose and glycerol molecular models were built in Materials Studio. The molecular structures were optimized using Gaussian 16 with the B3LYP-D3 functional and 6-31G(d) basis set. Water was described using the TIP3P model, and bonded and non-bonded parameters for the remaining molecules were obtained using AuToFF. All-atom molecular dynamics simulations were performed in GROMACS 2021.5 with the Amber03 force field. For the W-bioplastic system, 40 cellulose monomers were randomly inserted into a 6 nm × 6 nm × 6 nm cubic box, which was then filled with 4,734 water molecules. For the G-bioplastic system, 40 cellulose monomers, 10 glycerol molecules and 4,677 water molecules were inserted into an identical simulation box. Each system was energy minimized by the steepest descent method, followed by 100 ps NVT and 100 ps NPT pre-equilibration. A 50 ns NPT simulation was then conducted to relax the structure. The equilibrated systems were stretched in the XY direction at a rate of 0.05 nm ns−1 for 20 ns, followed by 3 ns NPT re-equilibration. Pressure was maintained at 1.0 bar using a Parrinello-Rahman barostat, and temperature was controlled at 298 K using a velocity-rescale thermostat with a coupling constant of 0.1 ps. Non-bonded interactions were calculated with a cutoff distance of 1.2 nm, and long-range electrostatics were treated using particle-mesh Ewald summation. All hydrogen bonds were constrained with the LINCS algorithm. The time step was 2 fs, the neighbour list was updated every 10 steps, and periodic boundary conditions were applied in all directions. PyMOL 3.0.3 (http://www.pymol.org/pymol) was used for visualization.

Coarse-grained molecular dynamics simulations

Two coarse-grained molecular dynamics (CGMD) systems were constructed to compare the mechanical behaviour of biomass-derived materials prepared under different conditions. The W-bioplastic system consisted of cellulose (65.05 wt.%), hemicellulose (33.21 wt.%) and lignin (0.75 wt.%), whereas the G-bioplastic system contained cellulose (59.51 wt.%), hemicellulose (28.66 wt.%), lignin (0.53 wt.%) and glycerol (11.30 wt.%). Initial configurations were built in Materials Studio by constructing amorphous cellulose, hemicellulose, lignin and glycerol structures and packing them into cubic simulation boxes with a density of 1.4 g cm-3. CGMD simulations were performed in the Mesocite module using the Martini force field, which has been used to describe organic and polymeric materials at the mesoscale. Before mechanical deformation, each system was energy minimized with the conjugate-gradient algorithm until the maximum force on any bead was below 0.001 kcal/(mol·Å), and then equilibrated under isothermal-isobaric (NPT) conditions at 298 K and 1 atm for 1 ns. Temperature and pressure were controlled with a Nose-Hoover thermostat and a Parrinello-Rahman barostat, respectively.

Uniaxial tensile simulations were performed under NPT conditions at 298 K and 1 atm. A constant strain rate of 1 × 108 s-1 was applied along the x-axis of the simulation box, while the two transverse dimensions were allowed to relax freely. Stress-strain curves were obtained from the virial stress tensor. Tensile strength (σmax) from the maximum stress.

Life cycle assessment

Life cycle assessment (LCA) was performed to quantify the environmental impact of producing 1.0 kg of G-bioplastic. Calculations were carried out in SimaPro 9.3 (PRé Sustainability, the Netherlands) using the TRACI 2.2 V1.00/US 2008 impact assessment model. Background inventory data were mainly obtained from the Ecoinvent 3.0 database. The functional unit was 1.0 kg of G-bioplastic. The assessed categories were ozone depletion (kg CFC-11 eq), global warming potential (kg CO2 eq), smog formation (kg O3 eq), acidification (kg SO2 eq), carcinogenic toxicity (CTUh), non-carcinogenic toxicity (CTUh), respiratory effects (kg PM2.5 eq), ecotoxicity (CTUe), freshwater eutrophication (kg P eq) and marine eutrophication (kg N eq). Water flows were integrated according to operation type. Because sodium chlorite inventory data were unavailable in the database, sodium hypochlorite was used as a proxy inventory based on molecular-weight similarity. Process water was mainly used to rinse residual chemicals and was modelled as recyclable; the energy consumption associated with water recycling was excluded from the system boundary.

Characterization

Fourier-transform infrared spectroscopy (Nicolet iS0) was used to analyse chemical changes over 400-4000 cm-1. Chemical composition, including alpha-cellulose, hemicellulose and acid-insoluble lignin, was determined according to ASTM D1104, TAPPI T 429 and TAPPI T 222, respectively. Microstructure was observed by scanning electron microscopy (FEI Quanta 200). Raman spectra were collected using a LabRAM HR Evolution spectrometer with 532 nm excitation over 50-4000 cm-1. Optical anisotropy was examined using a polarized optical microscope (CaiKon XPF-550C). X-ray diffraction was performed on an X’Pert 3 Powder diffractometer over 2θ = 5-50° at 5° min-1. Nanofibre spacing was estimated from small-angle X-ray scattering data by plotting I(q)q2 against q to identify qpeak and calculate d = 2π/qpeak. Density was calculated from sample mass and volume. Total transmittance and haze were measured using a UV-vis spectrophotometer (TU-1950) and a haze meter (Lambda 950). Tensile tests were performed using a universal testing machine (UTM2203) at 2.0 mm min-1. Folding endurance was measured with a YN-MIT 135 folding endurance tester. The coefficient of thermal expansion was measured using a TMA Q400 analyser from 30 to 200 °C. Accelerated UV ageing was performed using a UVLED constant-temperature curing machine (ULHX200-200-DR) for 1 h at 50 °C and 50 W m-2, after which macroscopic morphology and colour changes were recorded.

Supplementary Fig. 1. Effect of water saturation on ambient self-densification of delignified wood. a, Water-saturated state. b, Dehydrated state.

Supplementary Fig. 2. FTIR spectra of the four bioplastics.

Supplementary Fig. 3. Relative cellulose, hemicellulose and lignin contents in natural wood, delignified wood and G-bioplastic.

Supplementary Fig. 4. Cross-sectional SEM images of the four bioplastics. a-d, W-bioplastic, M-bioplastic, E-bioplastic and G-bioplastic, respectively.

Supplementary Fig. 5. Surface SEM images, corresponding photographs (insets) and magnified views of the four bioplastics prepared with alcohol-bridged hydrogen-bond networks. a-d, W-bioplastic, M-bioplastic, E-bioplastic and G-bioplastic, respectively.

Supplementary Fig. 6. Raman spectra of the four bioplastic.

Supplementary Fig. 7. Polarized optical microscopy images of the four bioplastics. a-d, W-bioplastic, M-bioplastic, E-bioplastic and G-bioplastic, respectively.

Supplementary Fig. 8. XRD patterns of the four bioplastics.

Supplementary Fig. 9. Crystallinity comparison of the four bioplastics.

Supplementary Fig.10. Photographs of the four bioplastics showing a, transparency and b, haze.

Supplementary Fig. 11. Total transmittance comparison of the four bioplastics.

Supplementary Fig. 12 Atomic models of a, a glycerol molecule and b, a single cellulose chain. Carbon atoms in cellulose are shown in grey, carbon atoms in glycerol in cyan, oxygen atoms in red and hydrogen atoms in white.

Supplementary Fig. 13. Representative all-atom molecular dynamics snapshots. a, Initial and final snapshots of the W-bioplastic system during unbiased molecular dynamics. b, Time-series snapshots of the W-bioplastic system during steered molecular dynamics. c, Initial and final snapshots of the G-bioplastic system during unbiased molecular dynamics. d, Time-series snapshots of the G-bioplastic system during steered molecular dynamics. Carbon atoms in cellulose are shown in grey, carbon atoms in glycerol in cyan, oxygen atoms in red, hydrogen atoms in white and water molecules as red sticks.

Supplementary Fig. 14. Time evolution of the number of hydrogen bonds.

Supplementary Fig. 15. Number of cellulose atom pairs within hydrogen bonding distance (<0.35 nm).

Supplementary Fig. 16. Tensile strength of bioplastics prepared with different glycerol contents (0, 1, 2.5 and 5 wt.%).

Supplementary Fig. 17. SEM images and magnified views of longitudinal tensile fracture surfaces for the four lignocellulosic bioplastics. a-d, W-bioplastic, M-bioplastic, E-bioplastic and G-bioplastic, respectively.

Supplementary Fig. 18. Folding demonstration for a, A4 paper and b, G-bioplastic.

Supplementary Fig. 19. Folding endurance comparison of W-bioplastic, M-bioplastic and paper-based materials.

Supplementary Fig. 20. Tensile strength comparison of G-bioplastic and E-bioplastic before and after folding (F-G-bioplastic and F-E-bioplastic).

Supplementary Fig. 21. Coarse-grained molecular dynamics model of the W-bioplastic wood cell wall.

Supplementary Fig. 22. Simulated microfibril movement in W-bioplastic, showing straightening, sliding and bending.

Supplementary Fig. 23. Normalized average end-to-end length (L/L0) of hemicellulose, lignin and cellulose as a function of cell-wall strain for a, G-bioplastic and b, W-bioplastic.

Supplementary Fig. 24. Photographs of G-bioplastic after 7 days of immersion in water, HCl solution (pH 1), NaOH solution (pH 13) and seven organic solvents.

Supplementary Fig. 25. Tensile strength comparison of recycled G-bioplastic (R-G-bioplastic) and A4 paper.

Supplementary Fig. 26. Material and energy flow diagram for production of 1.0 kg of G-bioplastic.

Supplementary Fig. 27. Degradation process of G-bioplastic and five reference plastics (PLA, PVC, PET, PE and PS) in natural soil in Harbin, China.

Supplementary Table 1. Comparison of tensile strength, environmental sustainability, treatment time, cost, and bulk process of G-bioplastic with lignocellulosic bioplastic (L-bioplastic), Paper plastic, cellulose fiber film (CF-film), polymeric material (P-material), and transparent wood film (TW-film) (all values are normalized by the maximum value of each indicator).

| Properties | G-bioplastic | L-bioplastic | Paper plastic | CF-film | P-film | TW-film | BM plastics |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Tensile strength (MPa) | 516 | 128 | 126 | 258 | 98.2 | 350 | 110 |
| Environmental sustainability | High | High | Middle | Low | Middle | Middle | High |
| Treatment time | 5h | 10 h | 28h | 72 h | 75 h | 8 h | 42h |
| Cost | Low | High | Middle | High | High | Middle | Middle |
| Bulk process | Yes | Yes | Yes | Yes | Yes | Yes | Yes |
| Refs. | This work | (9) | (15) | (30) | (31) | (32) | (14) |

Supplementary Table 2. The specific strength (σ), and specific Young’s modulus (E) of G-bioplastic and Self-densified TWF, Densified wood, and Isotropic cellulose nanopaper.

| Material | Density (g cm-3) | Strength σ |  | Young’s modulus E |  | Refs. |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | σ (MPa) | Specific σ (MPa/g cm-3) | E (GPa) | Specific E (GPa/g cm-3) |  |
| W-bioplastic | 0.79 | 306.0 | 387.3 | 16.2 | 20.5 | This work |
| M-bioplastic | 0.85 | 348.1 | 409.5 | 22.4 | 26.4 | This work |
| E-bioplastic | 0.89 | 463.1 | 520.3 | 27.6 | 31.0 | This work |
| G-bioplastic | 1.1 | 516.6 | 475.4 | 30.8 | 28.0 | This work |
| Self-densified TWF1 | 0.81 | 228.4 | 281.7 | 25.3 | 31.3 | (23) |
| Self-densified TWF2 | 1.32 | 449.1 | 340 | 51.1 | 38.2 | (24) |
| Self-densified TWF3 | 1.05 | 530.9 | 505.6 | 26.8 | 25.5 | (36) |
| Densified wood 1 | 1.3 | 548 | 422.2 | 47.1 | 36.2 | (37) |
| Densified wood 2 | 1.2 | 351.8 | 290 | 32.9 | 27.4 | (38) |
| Densified wood 3 | 1.35 | 430 | 318.5 | 39 | 28.9 | (39) |
| Densified wood 4 | 1.24 | 173.6 | 140 | 17.3 | 14 | (40) |
| Isotropic cellulose nanopaper1 | 1.08 | 214 | 198.1 | 13.2 | 12.2 | (41) |
| Isotropic cellulose nanopaper2 | 0.72 | 123 | 170.8 | 12 | 16.7 | (42) |
| Isotropic chitin nanopaper | 1.27 | 134.4 | 105.8 | 1.7 | 1.3 | (43) |

Supplementary Table 3. Comparative Analysis of the Mechanical Performance of Lignocellulosic Bioplastics, paper, films, and transparent wood films (TWF).

| Material category | Material | Tensile stress (MPa) | Toughness (MJ m-3) | Refs. |
| --- | --- | --- | --- | --- |
| Paper | PAA fibers paper | 195 | 2.3 | (44) |
|  | Paper impregnated by CMC | 140 | 8.5 | (45) |
|  | Paper impregnated by RC solution | 39 | 2.8 | (46) |
|  | TEMPO microfiber paper | 89 | 1.0 | (47) |
|  | TEMPO microfiber paper | 105 | 1.9 | (48) |
| Film | Hot pressing wood film | 150 | 2.4 | (49) |
|  | RC Macrofibers film | 122 | 8.8 | (50) |
|  | Hot-pressing CNF film | 230 | 9.9 | (51) |
|  | TEMPO-CNF film | 287 | 11.7 | (52) |
| TWF | Delignified/PMMA | 76.36 | 0.87 | (32) |
|  | Clear wood/epoxy | 43.39 | 6.1 | (40) |
|  | Acetylated/ delignified/ PMMA | 78.9 | 1 | (53) |
|  | Delignified/epoxy | 45.38 | 1.2 | (54) |
|  | Delignified/PMMA | 23.38 | 0.59 | (55) |
|  | Clear wood/PVA | 143 | 3.03 | (56) |
|  | TWF | 350 | 7.38 | (57) |
| Bioplastic | W-bioplastic | 306.03 | 10.82 | This work |
|  | M-bioplastic | 348.05 | 12.28 | This work |
|  | E-bioplastic | 463.10 | 24.05 | This work |
|  | G-bioplastic | 516.61 | 28.37 | This work |

Supplementary Table 4. Folding endurance of G-bioplastic compared with that of paper substrates and polymeric films under a standardized tension of 9.81 N.

| Material | Folding times (×10*3) | Ref. |
| --- | --- | --- |
| Kraft paper | 0.50 | (12) |
| All-celluloulose film | 3.34 | (12) |
| CMC/fiber hybrid film | 3.342 | (13) |
| Money paper | 3.38 | (12) |
| Tracing paper | 5.613 | (13) |
| CM-ASAM paper | 6.45 | (12) |
| CM-Kraft paper | 9.22 | (12) |
| CNF/PET film | 10.97 | (58) |
| G-bioplastic | 15.067 | This work |

Supplementary Table 5. LCA inventory for 1.0 kg G-bioplastic production.

| Inputs/Outputs | Quantity | Unit | Corresponding LCI | Database |
| --- | --- | --- | --- | --- |
| Step 1: Delignification |  |  |  |  |
| Input |  |  |  |  |
| Balsa wood | 1.334 | kg | Wood, unspecified, standing/kg | Ecoinvent 3 |
| NaClO2 | 0.222 | kg | Sodium hypochlorite, without water, in 15% solution state {RoW}¦ market for sodium hypochlorite, without water, in 15% solution state ¦ Cut-off, U | Ecoinvent 3 |
| CH3COOH | 0.0333 | L | Acetic acid, without water, in 98% solution state {GLO}¦ market for acetic acid, without water, in 98% solution state ¦ Cut-off, U | Ecoinvent 3 |
| Water | 66.667 | L | Water, decarbonised {CN}¦ market for water, decarbonised ¦ Cut-off, U | Ecoinvent 3 |
| Energy | 0.00091 | kWh | Electricity, at grid {CN} ¦ Electricity, at grid, CN, 2018 | Ecoinvent 3 |
| Output |  |  |  |  |
| Delignified wood | 6.6 | kg | Intermediate products |  |
| Wastewater | 60 | L | Wastewater, average {RoW}¦ market for wastewater, average ¦ Cut-off, U | Ecoinvent 3 |
| Step 2: Hemicellulose removal |  |  |  |  |
| Input |  |  |  |  |
| Delignified wood | 6.6 | kg | Intermediate products |  |
| NaOH | 0.111 | kg | Sodium hydroxide, without water, in 50% solution state {GLO}¦ chlor-alkali electrolysis, diaphragm cell ¦ Cut-off, U | Ecoinvent 3 |
| Water | 66.667 | L | Water, decarbonised {CN}¦ market for water, decarbonised ¦ Cut-off, U | Ecoinvent 3 |
| Output |  |  |  |  |
| Alkali treatment wood | 0.867 | kg | Intermediate products |  |
| Wastewater | 60 | L | Wastewater, average {RoW}¦ market for wastewater, average ¦ Cut-off, U | Ecoinvent 3 |
| Step 3: Soaking in Glycerol and drying at room temperature |  |  |  |  |
| Input |  |  |  |  |
| Alkali treatment wood | 0.867 | kg | Intermediate products |  |
| Glycerol | 0.111 | L | Glycerine {GLO}¦ stearic acid production ¦ Cut-off, U | Ecoinvent 3 |
| Water | 33.334 | L | Water, decarbonised {CN}¦ market for water, decarbonised ¦ Cut-off, U | Recycled |
| Output |  |  |  |  |
| G-bioplastic | 1.0 | kg | Cellulose fibre {RoW}¦ market for cellulose fibre ¦ Cut-off, U | Avoided products |

Supplementary Table 6. LCA inventory and environmental impact values for 1.0 kg plastic.

| Impact category | Unit | PLA | PVC | PET | PE | PS |
| --- | --- | --- | --- | --- | --- | --- |
| Amount |  | 1.0 | 1.0 | 1.0 | 1.0 | 1.0 |
| Corresponding LCI | kg | Polylactide (PLA) biopolymer resin, at plant {RNA} ¦ Polylactide (PLA) biopolymer resin, at plant | Polyvinyl chloride (PVC) resin, at plant {RNA} ¦ Polyvinyl chloride (PVC) virgin resin, at plant | Polyethylene terephthalate, granulate, amorphous {RoW}¦ polyethylene terephthalate, granulate, amorphous, recycled to generic market for amorphous PET granulate ¦ Cut-off, U | Polyethylene, low density, granulate {GLO}¦ market for polyethylene, low density, granulate ¦ Cut-off, U | Polystyrene, general purpose {GLO}¦ market for polystyrene, general purpose ¦ Cut-off, U |
| Ozone depletion | kg CFC-11 eq | 4.01E-09 | 2.09E-06 | 1.86E-08 | 9.66E-08 | 2.50E-09 |
| Global warming | kg CO2 eq | -2.29E-01 | 1.90E+00 | 1.65E+00 | 3.16E+00 | 3.60E+00 |
| Smog | kg O3 eq | 1.90E-01 | 1.03E-01 | 1.00E-01 | 1.55E-01 | 1.47E-01 |
| Acidification | kg SO2 eq | 7.01E-03 | 3.60E-03 | 6.37E-03 | 1.14E-02 | 1.17E-02 |
| Carcinogenics | CTUh | 6.77E-09 | 9.91E-09 | 5.78E-07 | 7.97E-07 | 1.17E-07 |
| Non carcinogenics | CTUh | 5.38E-07 | 7.71E-07 | 1.03E-06 | 7.38E-07 | 1.09E-07 |
| Respiratory effects | kg PM2.5 eq | 1.57E-04 | 1.63E-04 | 1.95E-03 | 2.10E-03 | 9.00E-04 |
| Ecotoxicity | CTUe | 1.47E+01 | 1.66E+01 | 6.56E+01 | 4.88E+01 | 9.42E+00 |
| Freshwater eutrophication | kg P eq | 2.11E-05 | 9.42E-07 | 5.81E-04 | 4.49E-04 | 4.48E-05 |
| Marine eutrophication | kg N eq | 1.64E-03 | 8.52E-04 | 1.00E-03 | 1.29E-03 | 1.24E-03 |

Supplementary Table 7. LCA characterization data results for producing 1.0 kg G-bioplastic.

| Impact category | Ozone depletion | Global warming | Smog | Acidification | Carcinogenics | Non carcinogenics | Respiratory effects | Ecotoxicity | Freshwater eutrophication | Marine eutrophication |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Unit | kg CFC-11 eq | kg CO2 eq | kg O3 eq | kg SO2 eq | CTUh | CTUh | kg PM2.5 eq | CTUe | kg P eq | kg N eq |
| Total | 9.223E-08 | 0.59769253 | 0.02307303 | 0.00210273 | -6.787E-09 | 3.3377E-07 | 0.00071123 | 7.2772273 | 0.00042477 | 0.000378024 |
| Acetic acid | 2.156E-09 | 0.10719191 | 0.00511691 | 0.00044713 | 2.1788E-08 | 2.6991E-08 | 8.6614E-05 | 1.3417444 | 1.891E-05 | 4.30504E-05 |
| Glycerine | 6.356E-10 | 0.050433123 | 0.0029925 | 0.00021747 | 1.8461E-08 | 2.0422E-08 | 5.2676E-05 | 1.4574222 | 1.082E-05 | 2.67104E-05 |
| Sodium hydroxide | 8.625E-08 | 0.1626443 | 0.00981084 | 0.00075552 | 4.3846E-08 | 5.8437E-08 | 0.00021129 | 3.1908762 | 4.3071E-05 | 8.93717E-05 |
| Sodium hypochlorite | 6.454E-09 | 0.55883755 | 0.03353227 | 0.00257245 | 1.5244E-07 | 1.9762E-07 | 0.00068258 | 11.016833 | 0.00013493 | 0.000303229 |
| Water | 9.133E-11 | 0.018148173 | 0.00140819 | 8.6493E-05 | 2.7342E-08 | 1.7041E-08 | 1.4832E-05 | 0.45367647 | 1.1516E-05 | 2.76643E-05 |
| Electricity | 1.393E-13 | 0.000724807 | 4.8454E-05 | 5.8071E-06 | 4.4017E-13 | 2.6252E-11 | 2.7946E-07 | 0.0003104 | 5.8636E-12 | 3.81357E-07 |
| Cellulose fibre | -3.707E-09 | -0.33441984 | -0.0318537 | -0.0021188 | -3.001E-07 | -1.764E-07 | -0.0003714 | -11.950028 | -8.419E-05 | -0.00029286 |
| Wastewater | 3.529E-10 | 0.034132502 | 0.00201755 | 0.00013665 | 2.9458E-08 | 1.8963E-07 | 3.4401E-05 | 1.7663923 | 0.00028971 | 0.000180477 |

Supplementary Table 8. Percentage contribution of material and energy during the production of 1.0 kg G-bioplastic.

| Impact category | Acetic acid | Glycerine | NaOH | NaClO | Water | Electricity | Cellulose fibre | Wastewater |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OD | 2.16E+00 | 6.38E-01 | 8.66E+01 | 6.48E+00 | 9.17E-02 | 1.40E-04 | -3.72E+00 | 3.54E-01 |
| GWP | 8.46E+00 | 3.98E+00 | 1.28E+01 | 4.41E+01 | 1.43E+00 | 5.72E-02 | -2.64E+01 | 2.69E+00 |
| PS | 5.90E+00 | 3.45E+00 | 1.13E+01 | 3.86E+01 | 1.62E+00 | 5.58E-02 | -3.67E+01 | 2.32E+00 |
| AC | 7.05E+00 | 3.43E+00 | 1.19E+01 | 4.06E+01 | 1.36E+00 | 9.16E-02 | -3.34E+01 | 2.16E+00 |
| HHC | 3.67E+00 | 3.11E+00 | 7.39E+00 | 2.57E+01 | 4.61E+00 | 7.42E-05 | -5.06E+01 | 4.96E+00 |
| HHNC | 3.93E+00 | 2.97E+00 | 8.51E+00 | 2.88E+01 | 2.48E+00 | 3.82E-03 | -2.57E+01 | 2.76E+01 |
| RE | 5.96E+00 | 3.62E+00 | 1.45E+01 | 4.69E+01 | 1.02E+00 | 1.92E-02 | -2.55E+01 | 2.37E+00 |
| EC | 4.30E+00 | 4.67E+00 | 1.02E+01 | 3.53E+01 | 1.46E+00 | 9.96E-04 | -3.83E+01 | 5.67E+00 |
| FEU | 3.19E+00 | 1.82E+00 | 7.26E+00 | 2.27E+01 | 1.94E+00 | 9.89E-07 | -1.42E+01 | 4.88E+01 |
| MEU | 4.47E+00 | 2.77E+00 | 9.27E+00 | 3.15E+01 | 2.87E+00 | 3.96E-02 | -3.04E+01 | 1.87E+01 |

4. Supplementary Videos

In a 6 nm × 6 nm × 6 nm cubic box: W-bioplastic system: 40 cellulose units + 4,734 TIP3P water molecules; G-bioplastic system: 40 cellulose monomers + 10 glycerol molecules + 4,677 water molecules. Both systems underwent 50 ns of NPT equilibration (Supplementary Video 1: the W-bioplastic system; Supplementary Video 2: the G-bioplastic system), 20 ns of stretching (Supplementary Video 3: the W-bioplastic system; Supplementary Video 4: the G-bioplastic system), and 3 ns of NPT re-equilibration.