Table 1 Comparison of Key Properties between Phase Change Composites and Sintered Hollow Bricks

| Comparison Dimension | Fatty Acid-based Composite Phase Change Material | Sintered Hollow Brick |
| --- | --- | --- |
| Functional Positioning | Latent heat storage and temperature regulation within the temperature zone | Structural enclosure matrix |
| Temperature Regulation Mechanism | Solid-liquid phase change latent heat, enabling time redistribution of heat absorption, storage, and release | Sensible heat storage and thermal resistance |
| Dynamic Thermal Response | Peak reduction, peak delay, and significant temperature fluctuation convergence | Primarily reduces heat flux; limited dynamic peak-shaving capability |
| Phase Change Temperature Zone | Customizable via eutectic ratio design | No phase change platform; temperature zone not customizable |
| Heat Transfer Capability | Intrinsically low; can be enhanced by thermally conductive fillers | Affected by porosity and moisture content; overall medium-low thermal conductivity |
| Leakage Risk | Requires shape-stabilized encapsulation and interface control to suppress leakage | No leakage issues |
| Mechanics & Construction | Needs integration with substrate; limited standalone load-bearing capacity | High compressive strength; mature construction system |
| Durability & Safety | Requires verification of thermal cycling stability and fireproofing design | Fire-resistant and weather-resistant; stable long-term service |
| Engineering Integration | Suitable for interlayers and functional layers embedded in walls or panels | Suitable for main masonry and infill wall materials |

Table 2 Physical parameters of various materials of the model house

| Material | Thermal Conductivity (W/(m·K)) | Density (kg/m³) | Specific Heat at Constant Pressure (J/(kg·K)) | Specific Heat Ratio | Phase Change Temperature (°C) | Phase Change Latent Heat (kJ/kg) |
| --- | --- | --- | --- | --- | --- | --- |
| Ordinary concrete wall | 1.28 | 2352 | 970 | 1 | / | / |
| Phase change concrete wall (before phase change) | 1.18 | 2100 | 2260 | 1.1 | 30 | 100 |
| Phase change concrete wall (after phase change) | 1 | 2100 | 4500 | 1 | 30 | 100 |
| Air (software embedded) | 0.023 | 1.29 | 1005 | 1.4 | / | / |